Supplementary information

Influence of 3D architecture and surface roughness of SiOC anodes on bioelectrochemical system performance: A comparative study of freeze-cast, 3D-printed, and tape-cast materials with uniform composition

Table S1: X-ray micro-computed tomography scanning parameters and specifications

| Scanning parameter | Specification |
| --- | --- |
| Radiographic field of vision / mm | 30 × 50 |
| Detector pixel size / μm | 30 |
| Acquisition time / min | 130 |
| Exposure time / s | 1 |
| Energy of X-ray / kV | 70 |
| Number of projections per revolution | 3200 |
| The angular step / ° | 0.4 |

Figure S1: Reconstructed spatial representation of anode materials.

Figure S2 A) Water and n-heptane adsorption, and B) chemical stability of anode materials

Figure S3 Chronoamperometric measurements of the bioelectrocatalytic activity of a Geobacter spp. biofilm on SiOC-based working electrodes on triplicates.

Table S2: Chemical composition of the solid fraction (all chemicals excluding the solvent p-xylene).

| Chemical | Mass fraction / wt.% |
| --- | --- |
| Poly (methyl silsesquioxane) | 20 |
| Poly (methyl phenyl silsesquioxane) | 20 |
| Graphite | 29.2 |
| Carbon black | 5 |
| Molybdenum disilicide | 8 |
| Azodicarbonamide | 17 |
| Imidazole | 0.8 |