Table. S1 Electrolytic bath and experimental conditions of Sn electrodeposition.

| Parameter | Value |
| --- | --- |
| Bath chemical composition | 4.6 g SnCl2∙2H2O, 30 g K4P2O7, 0.8 g glycine, 0.8 g potassium sodium tartrate per 100 ml pure water. |
| Cathode | Ni Scaffold |
| Anode | Pure Sn (99.8%) |
| Current density, mA/cm2 | 75 mA/cm2 |
| Electrodes area | Anode: 0.56 cm2 , Cathode: 3 cm2 |
| Temperature, Cº | 25 |
| Stirring speed (rpm) | 250 |

Table. S2 Electrolytic bath and experimental conditions of carbon electrodeposition

| Parameter | Value |
| --- | --- |
| Bath chemical composition | pure ethanol (99.8% Honeywell) |
| Cathode | Sn plated Ni Scaffold |
| Anode | Graphite |
| Voltage | 100 V |
| Temperature, Cº | 25 |
| Time, min | 180 |

Table. S3 EDS analysis of electrodeposited Sn layer (Pulsed electrodeposition, 15% duty cycle, 2 min electrodeposition with effective time, ton/off = 3/17 sec.

| Element | Weight % |  | Atomic % | Net Int. | Error % |
| --- | --- | --- | --- | --- | --- |
| SnL | 81.25 | 68.19 |  | 54.6 | 6.49 |
| NiK | 18.75 | 31.8 |  | 9.28 | 18.34 |

Table. S4 EDS analysis of C/Sn/Ni nanocomposite

| Element | Weight % | Atomic % | Net Int. | Error % |
| --- | --- | --- | --- | --- |
| C K | 9.82 | 34.54 | 5.2 | 19.28 |
| O K | 7.39 | 19.51 | 8.78 | 17.74 |
| SnL | 37.51 | 13.35 | 58.78 | 7.24 |
| NiK | 45.29 | 32.59 | 51.51 | 6.1 |

Table. S5 Electrochemical parameters for Sn layers compared with Ni scaffold obtained from linear polarization tests.

| Specimen |  | Corrosion rate (mm/year) | Ecorr(V) | J corr (A/cm2) | Βc (V/dec) | Βa (V/dec) |
| --- | --- | --- | --- | --- | --- | --- |
| Ni | Ni foam | 0.035 | 0.085 | 3.2615E-6 | 0.272 | 0.175 |
| Sn/Ni | Direct 3 min | 0.7003 | -0.241 | 5.191E-5 | 0.239 | 0.217 |
|  | Pulse, 50% duty cycle, ton/off : 3/3, 3 min | 0.579 | -0.27 | 4.292E-5 | 0.203 | 0.218 |
|  | Pulse, 15% duty cycle, ton/off: 3/17, 2 min | 0.222 | -0.294 | 2.09E-5 | 0.175 | 0.127 |
|  | Pulse, 15% duty cycle, ton/off: 3/17, 3 min | 0.155 | -0.139 | 1.28E-5 | 0.162 | 0.179 |
|  | Pulse, 15% duty cycle, ton/off: 2/11.333, 3 min | 0.113 | -0.145 | 2.86E-6 | 0.139 | 0.184 |
|  | Pulse, 15% duty cycle, ton/off: 1/5.667, 2 min | 0.073 | -0.083 | 6.066E-6 | 0.151 | 0.189 |
|  | Pulse, 15% duty cycle, ton/off: 0.1/0.567, 2 min | 0.017 | -0.113 | 0.00018 | 0.175 | 0.230 |
| C/Sn/Ni | Sn layer: Pulse, 15% duty cycle ton/off: 3/17, 2 min | 0.2703 | -0.269 | 2.24E-5 | 0.202 | 0.105 |
|  | Sn layer: Pulse, 15% duty cycle, ton/off: 3/17, 3 min | 0.2011 | -0.296 | 1.499E-5 | 0.193 | 0.143 |

Table. S6 Parameters obtained by fitting EIS experimental spectra recorded in 1M LiPF6 solution.

| Samples |  | Rp(Ω) | Rs(Ω) | CPE.Y0(F) | CPE.N |
| --- | --- | --- | --- | --- | --- |
| Ni | Ni without any deposition | 12677 | 69 | 1.2 E-4 | 0.885 |
| Sn/Ni | Direct, 3 min | 127 | 60 | 2.4E-4 | 0.505 |
| Sn/Ni | Pulse, 50% duty cycle, ton/off : 3/3, 3 min | 182 | 58.5 | 7.3E-4 | 0.382 |
| Sn/Ni | Pulse, 15% duty cycle, ton/off : 3/17, 2 min | 168 | 61.6 | 4.3E-4 | 0.572 |
| Sn/Ni | Pulse, 15% duty cycle, ton/off : 3/17, 3 min | 703 | 77.5 | 1E-3 | 0.687 |
| Sn/Ni | Pulse, 15% duty cycle, ton/off : 2/11.333, 3 min | 654 | 83.7 | 4.5E-4 | 0.669 |
| Sn/Ni | Pulse, 15% duty cycle, ton/off : 1/5.667, 2 min | 1300 | 65.3 | 3.5E-4 | 0.606 |
| Sn/Ni | Pulse, 15% duty cycle, ton/off : 0.1/0.567, 2 min | 9510 | -217 | 1.67E-4 | 0.402 |
| C/Sn/Ni | Sn layer: Pulse, 15% duty cycle, ton/off : 3/17, 2 min | 94 | 57 | 2.2E-4 | 0.574 |
| C/Sn/Ni | Sn layer: Pulse, 15% duty cycle, ton/off : 3/17 sec, 3 min | 415.88 | 94.7 | 9.34E-5 | 0.643 |

Fig. S1 EDS analysis of electrodeposited Sn on Ni foam substrate (Pulsed electrodeposition, 15% duty cycle, 2 min electrodeposition effective time, t on/off = 3/17 sec.

Fig. S2 EDS analysis of electrodeposited C/ Sn layers on Ni foam substrate.