Wetting of the microporous layer at the cathode of an anion exchange membrane water electrolyzer

*†Raziyeh Akbari1, †Marta Mastrosimone1, Mohsin Muhyuddin1, Tommaso Caielli1, Piercarlo Mustarelli1, **Carlo Santoro1, Carlo Antonini1

1 Department of Materials Science, University of Milano-Bicocca U5, Via Roberto Cozzi 55, 20125, Milano (Italy)

Corresponding authors

* Raziyeh Akbari: e-mail: raziyeh.akbari@unimib.it

** Carlo Santoro: e-mail: carlo.santoro@unimib.it

† Contributed equally.

Table SI 1. Summary of impacting distances, drop velocities, and Weber numbers for water and 1M solution of various salts used in this study.

| h (cm) | U (m/s) | We=ρ U2D0σ |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | H2O | NaOH | KOH | K2CO3 |
| 1 | 0.41 | 7 | 7 | 7 | 7 |
| 2.5 | 0.65 | 16 | 17 | 17 | 17 |
| 4 | 0.82 | 26 | 27 | 27 | 27 |
| 7 | 1.09 | 46 | 47 | 47 | 48 |
| 11 | 1.36 | 72 | 74 | 74 | 75 |
| 16 | 1.64 | 104 | 107 | 107 | 110 |
| 24 | 2.01 | 156 | 161 | 161 | 164 |

Figure SI 1. The dimensionless drop rebound time and maximum spreading time, trebτ and tDmaxτ, on CP+MPL samples versus Weber number (We) at different operational temperatures for (a) water, (b) NaOH, (c) KOH, and (d) K2CO3 droplets. Dashed lines represent the linear fit with zero slope. The average rebound and spreading times for each condition are indicated on the graphs.

Figure SI 2. The dimensionless maximum spreading diameter DmaxD0 of 1M (a) NaOH, (b) KOH, and (c) K2CO3 droplets impacting CP and CP+MPL surfaces in various drop velocities. The fitting equation is indicated in (a1). Dashed lines are proportional to the fitted equation.

Figure SI 3. Galvanostatic measurements at 60 °C applying a constant current of 0.5 A cm-2. Operating conditions: T=60 °C, anode recirculation of 1 M KOH at 5 mL/s. Anode: Ni foam, AEM: 40 μm Piperion membrane. Cathode 0.1 mg cm-2 on CP (red) or CP+MPL (blue).

Figure SI 4. Electrochemical impedance spectroscopy of WE cells. T=60 °C, 0.5 A cm-2 DC, 20 mA AC, 10 kHz to 10 mHz. Anode: Ni foam, AEM: 40 μm Piperion membrane. Cathode 0.1 mg cm-2 on CP (red) or CP+MPL (blue).