A Structural and Compositional Analysis of the Customization of Ti3C2 MXenes for Enhanced Power Storage

W. A. Hussein1*, P. Ragupathy2, Raghupandiyan Naresh2, V. Varshini2, Ghalia A. Gaber1*

1 Department of Chemistry, Faculty of Science (Girls), Al-Azhar University, P.O. Box: 11754, Yousef Abbas Str., Nasr City, Cairo, Egypt

2 CSIR-Central Electrochemical Research Institute, Karaikudi-630003, India

*Correspondence:

W. A. Hussein     Email: wallaahmed@azhar.edu.eg

Ghalia A. Gaber        Email: ghaliaasaid@azhar.edu.eg

Table S1. XRD crystallite size (D), inter-planar spacing (d-Spacing), and lattice parameters of all electrodes.

| Parameters Electrodes | D (nm) | d-Spacing Å | C lattice Å |
| --- | --- | --- | --- |
| c-Ti3C2 | 2.8 | 8.8 | 17.7 |
| d-Ti3C2 | 2.3 | 9.8 | 19.6 |
| c-Ti3C2/Si | 1.9 | 9.3 | 18.7 |
| d-Ti3C2/Si | 1.0 | 10.1 | 20.2 |

Table S2. Statistical fitting parameters obtained from FT-IR deconvolution analysis of all electrodes.

| Parameters Electrodes | Reduced Chi-Sqr | R-Square (COD) | Adj. R-Square |
| --- | --- | --- | --- |
| c-Ti3C2 | 4.31798E-5 | 0.94543 | 0.94481 |
| d-Ti3C2 | 8.63468E-4 | 0.92121 | 0.91992 |
| c-Ti3C2/Si | 2.09922E-4 | 0.98168 | 0.98135 |
| d-Ti3C2/Si | 3.97427E-5 | 0.96889 | 0.96853 |

Fig. S1. FTIR spectral deconvolution for all electrodes (c-Ti₃C₂, d-Ti₃C₂, c-Ti₃C₂/Si, and d-Ti₃C₂/Si) showing the measured signal and cumulative fit peaks.

Table S3. Fraction of Ti, C, O, and F atoms of synthesized MXene

| Element (atom %) | MAX-Ti3AlC2 | c-Ti3C2 | d-Ti3C2 | c-Ti3C2/Si | d-Ti3C2/Si |
| --- | --- | --- | --- | --- | --- |
| C | 45.71 | 14.91 | 23.33 | 42.89 | 15.71 |
| O | 13.74 | 10.25 | 17.00 | 45.72 | 33.68 |
| F |  | 14.67 | 23.72 |  |  |
| Al | 16.82 | 2.33 | 1.15 | 1.46 | 1.10 |
| Ti | 23.73 | 57.84 | 34.81 | 62.74 | 48.47 |
| Si |  |  |  | 3.51 | 1.04 |