Prediction of Coal Ash Fusion Temperatures using Computational  Intelligence based Models

Makarand Naniwadekar a,b,c, Shishir Tiwarya, Ashis Mukherjee d,  Tarit Baran Das e,  Sanjeev S. Tambe a,*

aChemical Engineering and Process DevelopmentDivision, CSIR-National Chemical Laboratory, Dr. Homi Bhabha Road, Pashan, Pune 411008, India

b Chemical Engineering Department, All India Shri Shivaji Memorial Society's College of Engineering (AISSMSCOE), Kennedy Road, Pune 411001, India

c Savitribai Phule Pune University (SPPU), Ganeshkhind Road, Pune 411007, India

dCombustion Science and Technology , CSIR-Central Institute of Mining and Fuel Research (CIMFR) , Dhanbad 826015, India

eMineral Technology, CSIR-Central Institute of Mining and Fuel Research (CIMFR) , Dhanbad 826015, India

*	Corresponding author: Sanjeev S. Tambe;  email: ss.tambe@ncl.res.in;

Phone: + 91 (20) 2590 2156; Fax: + 91 (20) 2590 2621

Supplementary Data

Table S1: Composition of oxides (wt%)  and corresponding  IDT

| SiO2 | Al2O3 | Fe2O3 | CaO | MgO | TiO2 | K2O + Na2O | IDT | Reference§ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 30.884 | 17.236 | 19.829 | 19.116 | 7.256 | 0.613 | 4.995 | 1050 | Lolja et al. (2002) |
| 52.416 | 16.490 | 12.089 | 10.585 | 3.619 | 0.852 | 3.909 | 1090 | Lolja et al. (2002) |
| 40.114 | 13.455 | 23.607 | 11.035 | 5.904 | 0.713 | 5.101 | 1040 | Lolja et al. (2002) |
| 43.397 | 18.920 | 10.768 | 16.236 | 3.904 | 0.767 | 5.940 | 1100 | Lolja et al. (2002) |
| 42.405 | 16.473 | 21.543 | 7.415 | 5.862 | 0.772 | 5.421 | 1070* | Lolja et al. (2002) |
| 50.145 | 23.544 | 11.842 | 4.482 | 5.505 | 0.672 | 3.690 | 1080 | Lolja et al. (2002) |
| 51.323 | 23.953 | 10.834 | 3.468 | 5.201 | 0.792 | 4.330 | 1080* | Lolja et al. (2002) |
| 56.241 | 20.719 | 10.239 | 3.553 | 2.562 | 0.971 | 5.635 | 1080 | Lolja et al. (2002) |
| 53.195 | 13.602 | 13.000 | 12.328 | 4.895 | 0.612 | 2.217 | 1060 | Lolja et al. (2002) |
| 42.130 | 19.808 | 13.185 | 18.900 | 2.221 | 0.949 | 2.564 | 1100# | Lolja et al. (2002) |
| 49.814 | 26.655 | 5.677 | 8.791 | 4.592 | 0.754 | 3.667 | 1140 | Lolja et al. (2002) |
| 43.826 | 14.992 | 14.131 | 16.465 | 4.597 | 0.641 | 5.338 | 1080 | Lolja et al. (2002) |
| 50.511 | 16.693 | 8.858 | 12.976 | 4.800 | 0.611 | 5.521 | 1100 | Lolja et al. (2002) |
| 54.683 | 28.810 | 3.954 | 2.723 | 6.259 | 0.802 | 2.768 | 1320 | Qiu et al. (1999) |
| 39.131 | 26.327 | 11.063 | 13.829 | 6.587 | 0.697 | 2.366 | 1200 | Qiu et al. (1999) |
| 44.187 | 36.039 | 6.445 | 8.931 | 1.045 | 2.340 | 1.013 | 1335 | Hanxu et al. (2006) |
| 48.512 | 36.358 | 4.861 | 5.840 | 0.772 | 2.019 | 1.638 | 1450* | Hanxu et al. (2006) |
| 51.364 | 33.730 | 8.632 | 1.405 | 0.636 | 1.548 | 2.686 | 1425# | Hanxu et al. (2006) |
| 48.019 | 23.324 | 23.171 | 1.321 | 0.863 | 1.016 | 2.286 | 1110 | Vorres (1979) |
| 39.315 | 21.005 | 30.583 | 4.439 | 1.306 | 0.846 | 2.507 | 1110 | Vorres (1979) |
| 49.916 | 18.771 | 21.145 | 6.040 | 1.071 | 0.819 | 2.237 | 1093 | Vorres (1979) |
| 49.231 | 11.795 | 7.179 | 25.641 | 4.103 | 0.615 | 1.436 | 1126 | Vorres (1979) |
| 38.847 | 20.250 | 26.129 | 7.544 | 1.252 | 0.894 | 5.085 | 917.77# | Rees (1964) |
| 35.846 | 20.592 | 25.327 | 8.520 | 3.250 | 0.838 | 5.628 | 956.66 | Rees (1964) |
| 35.704 | 20.633 | 26.501 | 8.095 | 2.306 | 0.961 | 5.800 | 933.88# | Rees (1964) |
| 43.143 | 18.145 | 23.738 | 8.361 | 1.053 | 0.901 | 4.658 | 932.77* | Rees (1964) |
| 46.622 | 19.034 | 23.186 | 4.246 | 1.025 | 0.994 | 4.894 | 924.44# | Rees (1964) |
| 44.194 | 17.553 | 28.286 | 3.022 | 1.035 | 1.014 | 4.895 | 957.22# | Rees (1964) |
| 35.004 | 16.109 | 31.145 | 13.426 | 0.970 | 0.776 | 2.569 | 909.44* | Rees (1964) |
| 39.296 | 14.465 | 34.984 | 6.847 | 0.931 | 0.802 | 2.675 | 956.11 | Rees (1964) |
| 44.525 | 17.275 | 23.643 | 7.906 | 1.007 | 1.051 | 4.592 | 957.22 | Rees (1964) |
| 40.157 | 20.311 | 22.240 | 9.248 | 1.713 | 0.999 | 5.333 | 909.44 | Rees (1964) |
| 47.261 | 19.653 | 16.650 | 11.832 | 0.863 | 0.829 | 2.913 | 1036.11 | Rees (1964) |
| 47.763 | 20.072 | 12.984 | 14.325 | 0.937 | 0.913 | 3.006 | 986.11 | Rees (1964) |
| 40.302 | 18.205 | 21.082 | 16.142 | 0.684 | 0.861 | 2.724 | 991.11 | Rees (1964) |
| 35.282 | 20.400 | 30.310 | 9.430 | 0.765 | 0.972 | 2.841 | 1080.55* | Rees (1964) |
| 34.296 | 19.782 | 30.330 | 11.278 | 0.696 | 1.101 | 2.516 | 1077.77 | Rees (1964) |
| 52.643 | 23.955 | 13.666 | 4.378 | 0.865 | 1.074 | 3.419 | 1147.77 | Rees (1964) |
| 42.591 | 17.366 | 14.806 | 20.744 | 0.901 | 0.771 | 2.821 | 1071.66 | Rees (1964) |
| 43.258 | 17.337 | 12.924 | 21.386 | 1.094 | 0.681 | 3.319 | 1114.44* | Rees (1964) |
| 54.701 | 21.674 | 13.660 | 4.498 | 1.044 | 1.002 | 3.423 | 1147.77* | Rees (1964) |
| 52.474 | 22.708 | 14.720 | 5.149 | 0.939 | 1.087 | 2.923 | 1114.44 | Rees (1964) |
| 44.724 | 22.379 | 21.963 | 4.755 | 1.310 | 1.145 | 3.723 | 1155.55 | Rees (1964) |
| 55.775 | 28.160 | 7.209 | 1.444 | 1.282 | 1.363 | 4.766 | 1237.22 | Rees (1964) |
| 52.461 | 24.388 | 6.605 | 9.755 | 1.050 | 1.225 | 4.517 | 1089.44* | Rees (1964) |
| 46.978 | 23.008 | 12.504 | 11.324 | 1.869 | 0.634 | 3.683 | 1038.88 | Rees (1964) |
| 46.580 | 22.947 | 14.976 | 9.473 | 2.382 | 0.674 | 2.969 | 1038.88 | Rees (1964) |
| 50.729 | 22.728 | 13.345 | 6.974 | 1.839 | 0.676 | 3.709 | 1141.66* | Rees (1964) |
| 41.309 | 25.077 | 16.253 | 12.201 | 1.224 | 0.971 | 2.966 | 1149.44 | Rees (1964) |
| 49.260 | 22.622 | 19.207 | 3.499 | 0.814 | 1.268 | 3.330 | 1160.00 | Moreno (2008) |
| 48.412 | 20.275 | 20.460 | 7.904 | 0.119 | 0.998 | 1.832 | 1115.55* | Moreno (2008) |
| 40.046 | 19.550 | 32.132 | 2.806 | 0.652 | 0.904 | 3.910 | 1093.33 | Moreno (2008) |
| 55.435 | 29.577 | 6.752 | 2.265 | 0.790 | 1.612 | 3.571 | 1482.22 | Moreno (2008) |
| 57.772 | 29.465 | 4.044 | 2.117 | 1.443 | 1.411 | 3.749 | 1482.22 | Moreno (2008) |
| 62.087 | 25.120 | 4.792 | 3.453 | 1.116 | 0.956 | 2.476 | 1348.88* | Moreno (2008) |
| 52.242 | 23.494 | 9.420 | 6.850 | 1.981 | 0.917 | 5.095 | 1260.00 | Moreno (2008) |
| 63.583 | 22.641 | 6.445 | 1.908 | 1.397 | 0.897 | 3.129 | 1326.66 | Moreno (2008) |
| 64.084 | 25.679 | 4.937 | 0.539 | 0.394 | 1.203 | 3.163 | 1482.22 | Moreno (2008) |
| 50.117 | 19.456 | 20.780 | 5.277 | 0.835 | 0.907 | 2.628 | 1037.77 | Moreno (2008) |
| 45.335 | 17.165 | 24.208 | 8.891 | 0.770 | 0.825 | 2.806 | 957.222 | Moreno (2008) |
| 59.037 | 22.009 | 5.412 | 7.121 | 3.470 | 1.631 | 1.321 | 1004.44* | Moreno (2008) |
| 48.642 | 19.057 | 5.159 | 14.214 | 4.759 | 1.263 | 6.907 | 1043.33 | Moreno (2008) |
| 43.086 | 19.293 | 6.588 | 17.258 | 3.679 | 1.370 | 8.727 | 1093.33 | Moreno (2008) |
| 39.008 | 19.441 | 20.057 | 14.823 | 4.515 | 0.787 | 1.368 | 1168.88 | Moreno (2008) |
| 43.193 | 32.753 | 18.731 | 1.842 | 1.024 | 2.149 | 0.307 | 1280.00# | Bryant et al. (2000) |
| 50.563 | 32.344 | 12.078 | 1.842 | 1.024 | 1.842 | 0.307 | 1310.00 | Bryant et al. (2000) |
| 62.680 | 22.990 | 5.773 | 3.299 | 1.237 | 0.825 | 3.196 | 1240.00 | Bryant et al. (2000) |
| 62.613 | 26.533 | 4.422 | 0.402 | 0.804 | 1.206 | 4.020 | 1200.00 | Bryant et al. (2000) |
| 45.120 | 13.723 | 17.894 | 11.308 | 9.178 | 0.703 | 1.789 | 1160.00 | Akiyama et al. (2011) |
| 65.871 | 23.982 | 4.796 | 1.131 | 0.827 | 1.435 | 1.927 | 1334.00 | Akiyama et al. (2011) |
| 52.545 | 25.440 | 11.813 | 5.133 | 1.846 | 1.665 | 1.526 | 1220.00 | Steyn and Minnitt (2010) |
| 49.697 | 25.608 | 11.306 | 9.919 | 2.763 | 0.691 | 0.015 | 1174.00* | Bahrinet al. (2009) |
| 36.782 | 23.103 | 18.161 | 14.713 | 2.299 | 2.184 | 2.759 | 1195.00 | Matuszewski (2012) |
| 46.667 | 25.104 | 18.021 | 4.375 | 1.667 | 1.354 | 2.813 | 1200.00 | Matuszewski (2012) |
| 44.572 | 23.779 | 24.270 | 3.412 | 0.746 | 1.098 | 2.122 | 1237.77 | Matuszewski (2012) |
| 47.619 | 19.048 | 21.164 | 7.407 | 1.058 | 1.058 | 2.646 | 1201.11 | Matuszewski (2012) |
| 38.725 | 18.899 | 6.029 | 24.928 | 7.420 | 1.391 | 2.609 | 1187.77 | Matuszewski (2012) |
| 45.491 | 19.981 | 7.715 | 19.778 | 5.076 | 0.860 | 1.099 | 1225.55 | Matuszewski (2012) |
| 43.896 | 15.388 | 6.410 | 18.017 | 8.276 | 0.726 | 7.287 | 1118.33# | Matuszewski (2012) |
| 51.773 | 17.645 | 10.519 | 13.982 | 3.135 | 1.209 | 1.737 | 1177.77 | Matuszewski (2012) |
| 58.438 | 28.861 | 5.823 | 0.512 | 0.205 | 2.487 | 3.674 | 1504.44 | U.S.DOE (2001) |
| 59.553 | 28.515 | 5.429 | 0.110 | 0.669 | 2.040 | 3.685 | 1393.33# | U.S.DOE (2001) |
| 56.539 | 28.483 | 8.972 | 0.533 | 0.139 | 1.984 | 3.350 | 1241.66 | U.S.DOE (2001) |
| 54.065 | 26.209 | 15.229 | 0.484 | 0.165 | 1.564 | 2.284 | 1365.55 | U.S.DOE (2001) |
| 36.323 | 25.628 | 30.371 | 3.844 | 0.310 | 1.312 | 2.211 | 1065.00 | U.S.DOE (2001) |
| 64.036 | 11.751 | 13.044 | 4.420 | 1.919 | 1.843 | 2.986 | 1166.11 | U.S.DOE (2001) |
| 69.782 | 21.404 | 4.756 | 1.554 | 0.532 | 0.960 | 1.012 | 1414.00* | Kim et al. (1994) |
| 54.398 | 20.033 | 6.718 | 13.448 | 2.519 | 0.906 | 1.978 | 1154.00* | Kim et al. (1994) |
| 63.482 | 25.283 | 4.507 | 2.451 | 1.033 | 1.121 | 2.122 | 1373.00* | Kim et al. (1994) |
| 55.254 | 20.434 | 15.221 | 4.379 | 1.512 | 1.043 | 2.158 | 1165.00 | CEA Report (2012) |
| 58.924 | 33.944 | 1.612 | 1.501 | 1.007 | 1.491 | 1.521 | 1320.00 | CEA Report (2012) |
| 74.467 | 16.322 | 4.080 | 1.632 | 1.224 | 0.755 | 1.520 | 1380.00 | CEA Report (2012) |
| 73.755 | 18.439 | 4.098 | 1.024 | 0.615 | 0.840 | 1.229 | 1350.00 | CEA Report (2012) |
| 59.024 | 31.583 | 4.636 | 0.879 | 0.455 | 2.020 | 1.384 | 1270.00# | CIMFR |
| 59.572 | 28.740 | 6.426 | 1.508 | 0.442 | 1.649 | 1.649 | 1250.00* | CIMFR |
| 58.722 | 23.656 | 8.929 | 2.939 | 1.281 | 1.139 | 3.285 | 1120.00 | CIMFR |
| 62.037 | 24.247 | 6.458 | 2.628 | 0.809 | 1.132 | 2.648 | 1200.00 | CIMFR |
| 61.681 | 26.187 | 5.630 | 1.340 | 0.453 | 1.612 | 3.072 | 1220.00 | CIMFR |
| 61.679 | 27.043 | 4.875 | 1.822 | 0.723 | 1.466 | 2.341 | 1200.00# | CIMFR |
| 55.756 | 26.835 | 9.385 | 2.893 | 1.155 | 1.963 | 1.942 | 1180.00 | CIMFR |
| 66.078 | 24.923 | 4.023 | 1.633 | 0.575 | 1.129 | 1.613 | 1220.00 | CIMFR |
| 58.874 | 26.892 | 7.623 | 1.861 | 0.654 | 1.770 | 2.313 | 1180 .00# | CIMFR |
| 51.477 | 34.204 | 5.620 | 4.233 | 1.327 | 1.609 | 1.508 | 1240.00 | CIMFR |
| 63.498 | 28.237 | 4.015 | 0.875 | 0.312 | 1.449 | 1.580 | 1210.00* | CIMFR |
| 58.522 | 31.128 | 6.013 | 0.693 | 0.201 | 2.008 | 1.425 | 1280.00 | CIMFR |
| 62.270 | 28.659 | 2.415 | 1.449 | 0.403 | 1.610 | 3.160 | 1220.00* | CIMFR |
| 60.889 | 27.816 | 6.838 | 0.232 | 0.121 | 2.095 | 1.994 | 1260.00 | CIMFR |
| 62.174 | 27.276 | 5.492 | 0.703 | 0.326 | 2.527 | 1.447 | 1220.00 | CIMFR |
| 59.872 | 22.687 | 10.204 | 2.403 | 1.227 | 2.086 | 1.442 | 1240.00* | CIMFR |
| 62.217 | 27.065 | 6.475 | 1.165 | 0.253 | 1.702 | 1.094 | 1240.00* | CIMFR |
| 66.754 | 26.760 | 2.222 | 0.434 | 0.323 | 1.536 | 1.950 | 1280.00# | CIMFR |
| 61.149 | 29.563 | 4.834 | 1.467 | 0.354 | 1.214 | 1.396 | 1340.00 | CIMFR |
| 66.459 | 22.797 | 6.357 | 0.923 | 0.170 | 1.189 | 1.719 | 1320. 00 | CIMFR |
| 60.348 | 25.638 | 9.636 | 0.966 | 0.483 | 1.690 | 1.217 | 1220.00 | CIMFR |
| 59.162 | 24.158 | 12.801 | 0.401 | 0.110 | 2.085 | 1.273 | 1300.00* | CIMFR |
| 52.000 | 27.691 | 15.048 | 0.642 | 0.102 | 3.179 | 1.294 | 1180.00 | CIMFR |
| 61.773 | 27.762 | 6.800 | 0.230 | 0.100 | 2.283 | 1.042 | 1220.00 | CIMFR |
| 59.097 | 29.700 | 6.662 | 0.698 | 0.121 | 2.345 | 1.355 | 1300.00 | CIMFR |
| 61.380 | 24.597 | 8.482 | 1.164 | 0.455 | 2.753 | 1.134 | 1260.00 | CIMFR |
| 61.375 | 28.189 | 6.897 | 0.609 | 0.264 | 1.625 | 0.995 | 1200.00 | CIMFR |
| 60.646 | 29.900 | 4.825 | 1.481 | 0.655 | 1.451 | 1.017 | 1240.00 | CIMFR |
| 58.201 | 26.385 | 11.045 | 0.865 | 0.744 | 1.851 | 0.895 | 1180.00 | CIMFR |
| 59.703 | 26.735 | 9.460 | 0.666 | 0.474 | 1.896 | 1.039 | 1220.00 | CIMFR |
| 64.371 | 26.411 | 6.395 | 0.170 | 0.080 | 1.441 | 1.111 | 1260.00 | CIMFR |
| 62.428 | 25.386 | 8.074 | 0.992 | 0.223 | 1.862 | 1.002 | 1200.00 | CIMFR |
| 64.258 | 27.446 | 4.431 | 0.696 | 0.151 | 1.938 | 1.060 | 1240.00* | CIMFR |
| 62.412 | 27.348 | 6.018 | 0.713 | 0.482 | 1.849 | 1.175 | 1200.00 | CIMFR |
| 64.787 | 27.848 | 4.013 | 0.231 | 0.181 | 1.529 | 1.388 | 1230.00# | CIMFR |
| 62.409 | 24.388 | 8.400 | 1.103 | 0.381 | 1.524 | 1.784 | 1230.00 | CIMFR |
| 60.813 | 26.803 | 8.032 | 0.634 | 0.272 | 1.610 | 1.822 | 1250 .00# | CIMFR |
| 65.086 | 26.581 | 3.047 | 1.172 | 0.387 | 1.712 | 1.957 | 1260.00 | CIMFR |
| 61.844 | 27.247 | 6.635 | 0.111 | 0.101 | 2.094 | 1.943 | 1250.00 | CIMFR |
| 62.853 | 24.824 | 8.007 | 0.110 | 0.110 | 1.525 | 2.549 | 1210.00* | CIMFR |
| 63.143 | 24.478 | 6.061 | 1.346 | 0.557 | 1.619 | 2.762 | 1240.00 | CIMFR |
| 60.756 | 24.515 | 8.081 | 2.015 | 0.638 | 1.499 | 2.461 | 1240.00 | CIMFR |
| 65.463 | 24.127 | 4.803 | 1.675 | 0.441 | 1.685 | 1.805 | 1200.00 | CIMFR |
| 59.049 | 23.815 | 12.881 | 0.989 | 0.424 | 1.937 | 0.878 | 1180.00* | CIMFR |
| 59.628 | 19.071 | 9.105 | 7.269 | 1.960 | 1.825 | 0.996 | 1180.00 | CIMFR |
| 64.442 | 22.992 | 5.669 | 2.373 | 0.791 | 1.298 | 2.394 | 1100.00 | CIMFR |
| 60.632 | 21.901 | 8.621 | 3.518 | 1.132 | 1.646 | 2.438 | 1140.00* | CIMFR |
| 61.651 | 24.333 | 4.905 | 3.912 | 1.239 | 1.802 | 2.069 | 1200.00 | CIMFR |
| 64.143 | 22.793 | 6.878 | 1.894 | 0.881 | 1.621 | 1.742 | 1200.00 | CIMFR |
| 64.978 | 24.714 | 6.435 | 0.493 | 0.211 | 1.611 | 1.541 | 1220.00 | CIMFR |
| 65.837 | 26.132 | 2.032 | 1.778 | 0.691 | 1.463 | 2.022 | 1220.00 | CIMFR |
| 63.642 | 23.285 | 5.287 | 4.176 | 1.151 | 1.141 | 1.263 | 1200.00* | CIMFR |
| 63.051 | 26.205 | 5.473 | 0.142 | 0.061 | 1.868 | 3.137 | 1200.00# | CIMFR |
| 62.699 | 26.033 | 4.675 | 0.173 | 0.092 | 1.793 | 4.471 | 1240.00 | CIMFR |
| 68.281 | 21.807 | 6.095 | 0.326 | 0.142 | 1.628 | 1.659 | 1180.00 | CIMFR |
| 66.554 | 22.881 | 6.513 | 0.194 | 0.061 | 1.631 | 2.100 | 1180.00 | CIMFR |
| 59.795 | 14.665 | 11.745 | 6.786 | 1.544 | 1.849 | 3.341 | 1140.00 | CIMFR |
| 64.180 | 20.761 | 9.261 | 0.494 | 0.212 | 1.614 | 3.450 | 1220.00* | CIMFR |
| 66.549 | 20.515 | 8.037 | 1.178 | 0.423 | 1.289 | 1.984 | 1190.00 | CIMFR |
| 60.551 | 28.212 | 6.029 | 1.157 | 0.584 | 1.771 | 1.671 | 1200.00* | CIMFR |
| 70.551 | 19.243 | 5.679 | 0.843 | 0.356 | 1.626 | 1.656 | 1160.00 | CIMFR |
| 59.059 | 25.008 | 7.058 | 4.781 | 1.414 | 1.996 | 0.509 | 1190.00 | CIMFR |
| 61.359 | 21.744 | 6.941 | 2.965 | 0.961 | 1.963 | 3.997 | 1140.00 | CIMFR |
| 63.844 | 23.608 | 4.467 | 0.997 | 0.234 | 1.628 | 5.180 | 1180.00 | CIMFR |
| 64.176 | 17.360 | 10.186 | 1.704 | 0.439 | 1.960 | 4.113 | 1180.00 | CIMFR |
| 67.294 | 22.025 | 4.022 | 0.605 | 0.222 | 1.290 | 4.526 | 1220 | CIMFR |
| 68.401 | 19.043 | 4.842 | 1.304 | 0.303 | 1.456 | 4.629 | 1200 | CIMFR |
| 66.080 | 25.947 | 4.032 | 0.788 | 0.232 | 1.374 | 1.516 | 1200 | CIMFR |
| 66.713 | 19.129 | 10.085 | 1.157 | 0.364 | 1.455 | 1.081 | 1200 | CIMFR |
| 67.061 | 25.022 | 4.399 | 0.802 | 0.170 | 1.603 | 0.912 | 1220 | CIMFR |
| 63.661 | 27.378 | 5.631 | 0.342 | 0.081 | 1.934 | 0.957 | 1280 | CIMFR |
| 66.151 | 25.268 | 4.807 | 0.331 | 0.130 | 1.766 | 1.525 | 1300 | CIMFR |
| 61.503 | 26.212 | 6.835 | 1.913 | 0.221 | 1.852 | 1.450 | 1260 | CIMFR |
| 65.106 | 27.388 | 3.212 | 0.695 | 0.191 | 1.571 | 1.822 | 1270 | CIMFR |
| 66.403 | 23.872 | 5.110 | 1.270 | 0.881 | 1.311 | 1.086 | 1240 | CIMFR |
| 66.865 | 25.034 | 3.637 | 1.084 | 0.537 | 1.499 | 1.307 | 1250* | CIMFR |
| 59.201 | 23.128 | 10.173 | 3.354 | 1.019 | 1.182 | 1.876 | 1160 | CIMFR |
| 59.258 | 25.624 | 8.606 | 2.249 | 0.709 | 1.273 | 2.188 | 1260 | CIMFR |
| 66.678 | 26.639 | 3.209 | 0.523 | 0.252 | 1.449 | 1.227 | 1280# | CIMFR |
| 60.513 | 25.337 | 9.311 | 1.521 | 0.639 | 1.542 | 1.095 | 1220* | CIMFR |
| 62.306 | 28.681 | 4.042 | 1.398 | 0.760 | 1.621 | 1.155 | 1270 | CIMFR |
| 62.540 | 26.214 | 4.717 | 2.785 | 0.678 | 1.809 | 1.171 | 1280* | CIMFR |
| 63.780 | 25.452 | 5.422 | 0.755 | 0.332 | 1.207 | 3.038 | 1220* | CIMFR |
| 64.295 | 24.649 | 5.022 | 1.157 | 0.352 | 1.449 | 3.060 | 1230 | CIMFR |
| 64.696 | 26.057 | 4.198 | 0.291 | 0.230 | 1.362 | 3.146 | 1240 | CIMFR |
| 63.425 | 24.386 | 6.891 | 1.898 | 0.700 | 1.624 | 1.035 | 1220* | CIMFR |
| 63.197 | 23.990 | 7.679 | 1.682 | 0.567 | 1.783 | 1.064 | 1180 | CIMFR |
| 60.103 | 28.005 | 5.837 | 2.611 | 1.008 | 1.371 | 1.028 | 1250* | CIMFR |
| 61.349 | 28.980 | 4.226 | 1.826 | 0.857 | 1.533 | 1.190 | 1240 | CIMFR |
| 64.139 | 25.369 | 6.458 | 0.930 | 0.344 | 1.455 | 1.273 | 1230* | CIMFR |
| 61.475 | 28.722 | 4.468 | 2.209 | 0.774 | 1.303 | 1.008 | 1240# | CIMFR |

* Test data;  # Validation data ; § CIMFR:  Central Institute of Mining and Fuel  Research, Dhanbad, India from where data were sourced.

Table S2. Composition of oxides (wt%) and corresponding  ST

| SiO2 | Al2O3 | Fe2O3 | CaO | MgO | TiO2 | K2O + Na2O | ST | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 48.40 | 25.50 | 3.50 | 2.41 | 5.54 | 0.71 | 2.45 | 1350.00# | Qiu et al. (1999) |
| 38.20 | 25.70 | 10.80 | 13.50 | 6.43 | 0.68 | 2.31 | 1380.00 | Qiu et al. (1999) |
| 42.30 | 34.50 | 6.17 | 8.55 | 1.00 | 2.24 | 0.97 | 1360.00* | Hanxu et al. (2006) |
| 42.00 | 36.90 | 3.21 | 1.93 | 0.44 | 2.08 | 0.54 | 1451.00 | Hanxu et al. (2006) |
| 47.10 | 35.30 | 4.72 | 5.67 | 0.75 | 1.96 | 1.59 | 1500.00 | Hanxu et al. (2006) |
| 50.10 | 32.90 | 8.42 | 1.37 | 0.62 | 1.51 | 2.62 | 1495.00 | Hanxu et al. (2006) |
| 47.27 | 22.96 | 22.81 | 1.30 | 0.85 | 1.00 | 2.25 | 1343.00* | Vorres (1979) |
| 37.64 | 20.11 | 29.28 | 4.25 | 1.25 | 0.81 | 2.40 | 1190.00 | Vorres (1979) |
| 47.52 | 17.87 | 20.13 | 5.75 | 1.02 | 0.78 | 2.13 | 1182.00 | Vorres (1979) |
| 34.76 | 18.12 | 23.38 | 6.75 | 1.12 | 0.80 | 4.55 | 993.88 | Rees (1964) |
| 32.10 | 18.44 | 22.68 | 7.63 | 2.91 | 0.75 | 5.04 | 1016.66 | Rees (1964) |
| 31.58 | 18.25 | 23.44 | 7.16 | 2.04 | 0.85 | 5.13 | 1005.55 | Rees (1964) |
| 39.73 | 16.71 | 21.86 | 7.70 | 0.97 | 0.83 | 4.29 | 1013.33 | Rees (1964) |
| 44.58 | 18.20 | 22.17 | 4.06 | 0.98 | 0.95 | 4.68 | 1024.44 | Rees (1964) |
| 42.70 | 16.96 | 27.33 | 2.92 | 1.00 | 0.98 | 4.73 | 1024.44 | Rees (1964) |
| 30.66 | 14.11 | 27.28 | 11.76 | 0.85 | 0.68 | 2.25 | 963.88 | Rees (1964) |
| 36.73 | 13.52 | 32.70 | 6.40 | 0.87 | 0.75 | 2.50 | 1001.66* | Rees (1964) |
| 41.11 | 15.95 | 21.83 | 7.30 | 0.93 | 0.97 | 4.24 | 1024.44 | Rees (1964) |
| 35.39 | 17.90 | 19.60 | 8.15 | 1.51 | 0.88 | 4.70 | 1015.00 | Rees (1964) |
| 42.18 | 17.54 | 14.86 | 10.56 | 0.77 | 0.74 | 2.60 | 1111.11 | Rees (1964) |
| 41.31 | 17.36 | 11.23 | 12.39 | 0.81 | 0.79 | 2.60 | 1101.11 | Rees (1964) |
| 34.18 | 15.44 | 17.88 | 13.69 | 0.58 | 0.73 | 2.31 | 1101.11 | Rees (1964) |
| 32.29 | 18.67 | 27.74 | 8.63 | 0.70 | 0.89 | 2.60 | 1123.33 | Rees (1964) |
| 30.53 | 17.61 | 27.00 | 10.04 | 0.62 | 0.98 | 2.24 | 1118.88 | Rees (1964) |
| 50.50 | 22.98 | 13.11 | 4.20 | 0.83 | 1.03 | 3.28 | 1187.77 | Rees (1964) |
| 35.93 | 14.65 | 12.49 | 17.50 | 0.76 | 0.65 | 2.38 | 1114.44* | Rees (1964) |
| 35.58 | 14.26 | 10.63 | 17.59 | 0.90 | 0.56 | 2.73 | 1138.88* | Rees (1964) |
| 52.42 | 20.77 | 13.09 | 4.31 | 1.00 | 0.96 | 3.28 | 1163.33# | Rees (1964) |
| 49.73 | 21.52 | 13.95 | 4.88 | 0.89 | 1.03 | 2.77 | 1163.33# | Rees (1964) |
| 51.54 | 25.79 | 25.31 | 5.48 | 1.51 | 1.32 | 4.29 | 1222.77 | Rees (1964) |
| 55.24 | 27.89 | 7.14 | 1.43 | 1.27 | 1.35 | 4.72 | 1342.22 | Rees (1964) |
| 47.97 | 22.30 | 6.04 | 8.92 | 0.96 | 1.12 | 4.13 | 1195.00 | Rees (1964) |
| 42.98 | 21.05 | 11.44 | 10.36 | 1.71 | 0.58 | 3.37 | 1188.33 | Rees (1964) |
| 42.83 | 21.10 | 13.77 | 8.71 | 2.19 | 0.62 | 2.73 | 1156.11* | Rees (1964) |
| 48.01 | 21.51 | 12.63 | 6.60 | 1.74 | 0.64 | 3.51 | 1201.66 | Rees (1964) |
| 40.09 | 17.54 | 18.60 | 11.16 | 1.03 | 1.00 | 2.25 | 1156.11* | Rees (1964) |
| 41.59 | 18.64 | 22.48 | 7.10 | 1.20 | 1.00 | 2.15 | 1132.22 | Rees (1964) |
| 39.70 | 17.74 | 25.20 | 7.72 | 0.98 | 0.86 | 2.29 | 1105.55 | Rees (1964) |
| 39.14 | 23.76 | 15.40 | 11.56 | 1.16 | 0.92 | 2.81 | 1186.66* | Rees (1964) |
| 46.60 | 21.40 | 18.17 | 3.31 | 0.77 | 1.20 | 3.15 | 1197.22# | Moreno (2008) |
| 44.65 | 18.70 | 18.87 | 7.29 | 0.11 | 0.92 | 1.69 | 1148.88 | Moreno (2008) |
| 38.10 | 18.60 | 30.57 | 2.67 | 0.62 | 0.86 | 3.72 | 1115.55* | Moreno (2008) |
| 52.63 | 28.08 | 6.41 | 2.15 | 0.75 | 1.53 | 3.39 | 1482.22 | Moreno (2008) |
| 54.86 | 27.98 | 3.84 | 2.01 | 1.37 | 1.34 | 3.56 | 1482.22 | Moreno (2008) |
| 58.43 | 23.64 | 4.51 | 3.25 | 1.05 | 0.90 | 2.33 | 1382.22 | Moreno (2008) |
| 46.14 | 20.75 | 8.32 | 6.05 | 1.75 | 0.81 | 4.50 | 1293.33 | Moreno (2008) |
| 60.97 | 21.71 | 6.18 | 1.83 | 1.34 | 0.86 | 3.00 | 1371.11 | Moreno (2008) |
| 61.79 | 24.76 | 4.76 | 0.52 | 0.38 | 1.16 | 3.05 | 1482.22 | Moreno (2008) |
| 49.20 | 19.10 | 20.40 | 5.18 | 0.82 | 0.89 | 2.58 | 1112.77# | Moreno (2008) |
| 41.20 | 15.60 | 22.00 | 8.08 | 0.70 | 0.75 | 2.55 | 1037.77* | Moreno (2008) |
| 45.60 | 17.00 | 4.18 | 5.50 | 2.68 | 1.26 | 1.02 | 1093.33* | Moreno (2008) |
| 46.20 | 18.10 | 4.90 | 13.50 | 4.52 | 1.20 | 6.56 | 1087.77* | Moreno (2008) |
| 30.58 | 14.60 | 4.07 | 23.63 | 3.08 | 1.06 | 4.31 | 1160.00 | Moreno (2008) |
| 33.03 | 14.79 | 5.05 | 13.23 | 2.82 | 1.05 | 6.69 | 1110.00 | Moreno (2008) |
| 34.21 | 17.05 | 17.59 | 13.00 | 3.96 | 0.69 | 1.20 | 1200.00 | Moreno (2008) |
| 42.20 | 32.00 | 18.30 | 1.80 | 1.00 | 2.10 | 0.30 | 1470.00* | Bryant et al. (2000) |
| 49.40 | 31.60 | 11.80 | 1.80 | 1.00 | 1.80 | 0.30 | 1570.00 | Bryant et al. (2000) |
| 60.80 | 22.30 | 5.60 | 3.20 | 1.20 | 0.80 | 3.10 | 1330.00 | Bryant et al. (2000) |
| 26.00 | 11.40 | 12.20 | 29.60 | 5.00 | 0.80 | 5.50 | 1200.00 | Bryant et al. (2000) |
| 49.24 | 23.84 | 11.07 | 4.81 | 1.73 | 1.56 | 1.43 | 1250.00 | Steyn and Minnitt (2010) |
| 32.80 | 12.40 | 24.70 | 16.50 | 12.30 | 0.26 | 0.35 | 1650.00 | Bahrinet al. (2009) |
| 79.70 | 18.49 | 0.39 | 0.57 | 0.07 | 0.24 | 0.53 | 1512.00* | Bahrinet al. (2009) |
| 77.60 | 19.60 | 1.52 | 0.76 | 0.09 | 0.25 | 0.11 | 1650.00 | Bahrinet al. (2009) |
| 71.40 | 15.38 | 11.30 | 0.57 | 0.17 | 0.58 | 0.59 | 1281.00 | Bahrinet al. (2009) |
| 42.90 | 16.50 | 1.30 | 22.00 | 16.50 | 0.25 | 0.44 | 1650.00 | Bahrinet al. (2009) |
| 29.10 | 6.75 | 37.70 | 15.10 | 10.10 | 0.20 | 0.19 | 1356.00* | Bahrinet al. (2009) |
| 49.10 | 25.30 | 11.17 | 9.80 | 2.73 | 0.68 | 0.02 | 1650.00 | Bahrinet al. (2009) |
| 37.60 | 34.73 | 1.73 | 6.15 | 5.43 | 6.68 | 5.77 | 1414.00 | Bahrinet al. (2009) |
| 39.24 | 43.62 | 1.45 | 5.40 | 3.21 | 3.29 | 2.69 | 1283.00 | Bahrinet al. (2009) |
| 41.18 | 30.53 | 1.73 | 7.17 | 4.75 | 8.32 | 4.32 | 1326.00 | Bahrinet al. (2009) |
| 36.26 | 41.52 | 3.90 | 6.67 | 5.00 | 3.58 | 1.81 | 1116.00 | Bahrinet al. (2009) |
| 23.58 | 46.98 | 3.36 | 11.73 | 7.00 | 4.41 | 1.66 | 1650.00* | Bahrinet al. (2009) |
| 78.80 | 16.07 | 0.01 | 0.06 | 0.95 | 2.11 | 1.26 | 1032.00 | Bahrinet al. (2009) |
| 32.00 | 20.10 | 15.80 | 12.80 | 2.00 | 1.90 | 2.40 | 1226.00 | Matuszewski (2012) |
| 44.80 | 24.10 | 17.30 | 4.20 | 1.60 | 1.30 | 2.70 | 1232.00# | Matuszewski (2012) |
| 41.80 | 22.30 | 22.76 | 3.20 | 0.70 | 1.03 | 1.99 | 1287.77 | Matuszewski (2012) |
| 45.00 | 18.00 | 20.00 | 7.00 | 1.00 | 1.00 | 2.50 | 1237.77 | Matuszewski (2012) |
| 33.40 | 16.30 | 5.20 | 21.50 | 6.40 | 1.20 | 2.25 | 1198.88 | Matuszewski (2012) |
| 38.09 | 16.73 | 6.46 | 16.56 | 4.25 | 0.72 | 0.92 | 1234.44 | Matuszewski (2012) |
| 35.06 | 12.29 | 5.12 | 14.39 | 6.61 | 0.58 | 5.82 | 1140.55@ | Matuszewski (2012) |
| 44.10 | 15.03 | 8.96 | 11.91 | 2.67 | 1.03 | 1.48 | 1237.77# | Matuszewski (2012) |
| 57.10 | 28.20 | 5.69 | 0.50 | 0.20 | 2.43 | 3.59 | 1532.22 | U.S.DOE (2001) |
| 54.30 | 26.00 | 4.95 | 0.10 | 0.61 | 1.86 | 3.36 | 1357.22* | U.S.DOE (2001) |
| 53.00 | 26.70 | 8.41 | 0.50 | 0.13 | 1.86 | 3.14 | 1475.55 | U.S.DOE (2001) |
| 52.54 | 25.47 | 14.80 | 0.47 | 0.16 | 1.52 | 2.22 | 1390.55 | U.S.DOE (2001) |
| 35.15 | 24.80 | 29.39 | 3.72 | 0.30 | 1.27 | 2.14 | 1143.33 | U.S.DOE (2001) |
| 59.40 | 10.90 | 12.10 | 4.10 | 1.78 | 1.71 | 2.77 | 1365.00 | U.S.DOE (2001) |
| 74.20 | 15.78 | 3.45 | 1.69 | 0.50 | 0.80 | 0.94 | 1457.00# | Kim et al. (1994) |
| 66.90 | 20.52 | 4.56 | 1.49 | 0.51 | 0.92 | 0.97 | 1478.00# | Kim et al. (1994) |
| 49.23 | 18.13 | 6.08 | 12.17 | 2.28 | 0.82 | 1.79 | 1197.00# | Kim et al. (1994) |
| 57.75 | 23.00 | 4.10 | 2.23 | 0.94 | 1.02 | 1.93 | 1474.00 | Kim et al. (1994) |
| 32.58 | 27.49 | 21.23 | 4.11 | 1.85 | 0.25 | 1.11 | 1236.00 | Kim et al. (1994) |
| 50.00 | 27.00 | 3.50 | 9.20 | 1.50 | 1.70 | 0.80 | 1450.00 | CEA Report (2012) |
| 53.00 | 19.60 | 14.60 | 4.20 | 1.45 | 1.00 | 2.07 | 1200.00 | CEA Report (2012) |
| 58.50 | 33.70 | 1.60 | 1.49 | 1.00 | 1.48 | 1.51 | 1550.00 | CEA Report (2012) |
| 73.00 | 16.00 | 4.00 | 1.60 | 1.20 | 0.74 | 1.49 | 1450.00* | CEA Report (2012) |
| 72.00 | 18.00 | 4.00 | 1.00 | 0.60 | 0.82 | 1.20 | 1450.00 | CEA Report (2012) |

* Test data;   # Validation data

Table S3: Composition of oxides (wt%) and corresponding  HT

| SiO2 | Al2O3 | Fe2O3 | CaO | MgO | TiO2 | Na2O + K2O | RH | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 30.73 | 17.15 | 19.73 | 19.02 | 7.22 | 0.61 | 4.97 | 1070.00 | CIMFR |
| 52.29 | 16.45 | 12.06 | 10.56 | 3.61 | 0.85 | 3.90 | 1150.00* | CIMFR |
| 39.95 | 13.40 | 23.51 | 10.99 | 5.88 | 0.71 | 5.08 | 1070.00# | CIMFR |
| 44.13 | 19.24 | 10.95 | 16.51 | 3.97 | 0.78 | 6.04 | 1150.00 | CIMFR |
| 42.32 | 16.44 | 21.50 | 7.40 | 5.85 | 0.77 | 5.41 | 1100 .00* | CIMFR |
| 50.01 | 23.48 | 11.81 | 4.47 | 5.49 | 0.67 | 3.68 | 1120.00 | CIMFR |
| 51.21 | 23.90 | 10.81 | 3.46 | 5.19 | 0.79 | 4.32 | 1150.00 | CIMFR |
| 48.43 | 12.71 | 17.54 | 3.44 | 15.51 | 0.34 | 1.65 | 1230.00 * | CIMFR |
| 49.28 | 12.86 | 15.17 | 1.63 | 18.73 | 0.27 | 1.65 | 1280.00 | CIMFR |
| 56.19 | 20.70 | 10.23 | 3.55 | 2.56 | 0.97 | 5.63 | 1160.00 * | CIMFR |
| 53.23 | 20.02 | 9.01 | 6.81 | 3.50 | 0.25 | 6.88 | 1160.00 * | CIMFR |
| 53.03 | 13.56 | 12.96 | 12.29 | 4.88 | 0.61 | 2.21 | 1120.00 | CIMFR |
| 41.73 | 19.62 | 13.06 | 18.72 | 2.20 | 0.94 | 2.54 | 1170.00 | CIMFR |
| 49.58 | 26.53 | 5.65 | 8.75 | 4.57 | 0.75 | 3.65 | 1190.00# | Lolja et al. (2002) |
| 44.57 | 6.46 | 8.26 | 27.09 | 7.06 | 0.46 | 5.86 | 1290.00 | Lolja et al. (2002) |
| 43.76 | 14.97 | 14.11 | 16.44 | 4.59 | 0.64 | 5.33 | 1110.00 | Lolja et al. (2002) |
| 50.41 | 16.66 | 8.84 | 12.95 | 4.79 | 0.61 | 5.51 | 1120.00 * | Lolja et al. (2002) |
| 47.27 | 22.96 | 22.81 | 1.30 | 0.85 | 1.00 | 2.25 | 1360.00 | Vorres (1979) |
| 37.64 | 20.11 | 29.28 | 4.25 | 1.25 | 0.81 | 2.40 | 1280.00 | Vorres (1979) |
| 47.52 | 17.87 | 20.13 | 5.75 | 1.02 | 0.78 | 2.13 | 1193.00 | Vorres (1979) |
| 48.00 | 11.50 | 7.00 | 25.00 | 4.00 | 0.60 | 1.40 | 1171.00 | Vorres (1979) |
| 46.60 | 21.40 | 18.17 | 3.31 | 0.77 | 1.20 | 3.15 | 1230.55 | Moreno (2008) |
| 44.65 | 18.70 | 18.87 | 7.29 | 0.11 | 0.92 | 1.69 | 1182.22# | Moreno (2008) |
| 38.10 | 18.60 | 30.57 | 2.67 | 0.62 | 0.86 | 3.72 | 1126.66 * | Moreno (2008) |
| 52.63 | 28.08 | 6.41 | 2.15 | 0.75 | 1.53 | 3.39 | 1482.22# | Moreno (2008) |
| 54.86 | 27.98 | 3.84 | 2.01 | 1.37 | 1.34 | 3.56 | 1482.22 | Moreno (2008) |
| 58.43 | 23.64 | 4.51 | 3.25 | 1.05 | 0.90 | 2.33 | 1426.66 | Moreno (2008) |
| 60.97 | 21.71 | 6.18 | 1.83 | 1.34 | 0.86 | 3.00 | 1410.00# | Moreno (2008) |
| 61.79 | 24.76 | 4.76 | 0.52 | 0.38 | 1.16 | 3.05 | 1482.22 | Moreno (2008) |
| 49.20 | 19.10 | 20.40 | 5.18 | 0.82 | 0.89 | 2.58 | 1148.88 | Moreno (2008) |
| 41.20 | 15.60 | 22.00 | 8.08 | 0.70 | 0.75 | 2.55 | 1093.33 | Moreno (2008) |
| 45.60 | 17.00 | 4.18 | 5.50 | 2.68 | 1.26 | 1.02 | 1126.66 | Moreno (2008) |
| 46.20 | 18.10 | 4.90 | 13.50 | 4.52 | 1.20 | 6.56 | 1115.55 | Moreno (2008) |
| 30.58 | 14.60 | 4.07 | 23.63 | 3.08 | 1.06 | 4.31 | 1171.11 | Moreno (2008) |
| 33.03 | 14.79 | 5.05 | 13.23 | 2.82 | 1.05 | 6.69 | 1143.33 | Moreno (2008) |
| 34.21 | 17.05 | 17.59 | 13.00 | 3.96 | 0.69 | 1.20 | 1210.00 * | Moreno (2008) |
| 42.20 | 32.00 | 18.30 | 1.80 | 1.00 | 2.10 | 0.30 | 1490.00 | Bryant et al. (2000) |
| 49.40 | 31.60 | 11.80 | 1.80 | 1.00 | 1.80 | 0.30 | 1590.00 | Bryant et al. (2000) |
| 60.80 | 22.30 | 5.60 | 3.20 | 1.20 | 0.80 | 3.10 | 1350.00 | Bryant et al. (2000) |
| 26.00 | 11.40 | 12.20 | 29.60 | 5.00 | 0.80 | 5.50 | 1200.00 | Bryant et al. (2000) |
| 41.10 | 12.50 | 16.30 | 10.30 | 8.36 | 0.64 | 1.63 | 1180.00 | Akiyama et al. (2011) |
| 62.90 | 22.90 | 4.58 | 1.08 | 0.79 | 1.37 | 1.84 | 1548.00 | Akiyama et al. (2011) |
| 49.24 | 23.84 | 11.07 | 4.81 | 1.73 | 1.56 | 1.43 | 1280.00 | Steyn and Minnitt (2010) |
| 32.80 | 12.40 | 24.70 | 16.50 | 12.30 | 0.26 | 0.35 | 1650.00 | Bahrinet al. (2009) |
| 79.70 | 18.49 | 0.39 | 0.57 | 0.07 | 0.24 | 0.53 | 1650.00 | Bahrinet al. (2009) |
| 77.60 | 19.60 | 1.52 | 0.76 | 0.09 | 0.25 | 0.11 | 1650.00 | Bahrinet al. (2009) |
| 71.40 | 15.38 | 11.30 | 0.57 | 0.17 | 0.58 | 0.59 | 1296.00 * | Bahrinet al. (2009) |
| 42.90 | 16.50 | 1.30 | 22.00 | 16.50 | 0.25 | 0.44 | 1650.00 * | Bahrinet al. (2009) |
| 29.10 | 6.75 | 37.70 | 15.10 | 10.10 | 0.20 | 0.19 | 1367.00# | Bahrinet al. (2009) |
| 49.10 | 25.30 | 11.17 | 9.80 | 2.73 | 0.68 | 0.02 | 1650.00 | Bahrinet al. (2009) |
| 37.60 | 34.73 | 1.73 | 6.15 | 5.43 | 6.68 | 5.77 | 1466.00 | Bahrinet al. (2009) |
| 39.24 | 43.62 | 1.45 | 5.40 | 3.21 | 3.29 | 2.69 | 1352.00 * | Bahrinet al. (2009) |
| 41.18 | 30.53 | 1.73 | 7.17 | 4.75 | 8.32 | 4.32 | 1384.00 | Bahrinet al. (2009) |
| 36.26 | 41.52 | 3.90 | 6.67 | 5.00 | 3.58 | 1.81 | 1224.00 | Bahrinet al. (2009) |
| 23.58 | 46.98 | 3.36 | 11.73 | 7.00 | 4.41 | 1.66 | 1650.00 | Bahrinet al. (2009) |
| 78.80 | 16.07 | 0.01 | 0.06 | 0.95 | 2.11 | 1.26 | 1078.00 | Bahrinet al. (2009) |
| 32.00 | 20.10 | 15.80 | 12.80 | 2.00 | 1.90 | 2.40 | 1265.00 | Matuszewski (2012) |
| 44.80 | 24.10 | 17.30 | 4.20 | 1.60 | 1.30 | 2.70 | 1271.00 | Matuszewski (2012) |
| 45.00 | 18.00 | 20.00 | 7.00 | 1.00 | 1.00 | 2.50 | 1285.00 | Matuszewski (2012) |
| 33.40 | 16.30 | 5.20 | 21.50 | 6.40 | 1.20 | 2.25 | 1204.44 | Matuszewski (2012) |
| 38.09 | 16.73 | 6.46 | 16.56 | 4.25 | 0.72 | 0.92 | 1243.33 | Matuszewski (2012) |
| 35.06 | 12.29 | 5.12 | 14.39 | 6.61 | 0.58 | 5.82 | 1162.77 | Matuszewski (2012) |
| 44.10 | 15.03 | 8.96 | 11.91 | 2.67 | 1.03 | 1.48 | 1231.11 * | Matuszewski (2012) |
| 19.60 | 5.74 | 52.70 | 8.69 | 3.41 | 0.12 | 6.26 | 1460.00 | Kim et al. (2010) |
| 23.74 | 5.43 | 47.31 | 9.64 | 0.79 | 0.21 | 5.68 | 1485.00 | Kim et al. (2010) |
| 34.18 | 6.30 | 29.87 | 14.82 | 2.62 | 0.14 | 4.16 | 1390.00 | Kim et al. (2010) |
| 0.55 | 2.20 | 85.33 | 3.33 | 0.84 | 0.18 | 1.82 | 1500.00 * | Kim et al. (2010) |
| 4.93 | 3.08 | 65.71 | 12.21 | 2.25 | 0.16 | 6.14 | 1470.00 * | Kim et al. (2010) |
| 30.04 | 13.47 | 29.39 | 6.71 | 2.06 | 0.12 | 4.64 | 1480.00 | Kim et al. (2010) |
| 52.67 | 17.75 | 12.97 | 6.86 | 2.76 | 0.26 | 6.71 | 1406.00 | Kim et al. (2010) |
| 35.13 | 5.55 | 2.45 | 33.06 | 5.52 | 0.19 | 14.29 | 1325.00 | Kim et al. (2010) |
| 36.38 | 8.54 | 3.94 | 30.15 | 7.41 | 0.22 | 5.26 | 1290.00 * | Kim et al. (2010) |
| 74.20 | 15.78 | 3.45 | 1.69 | 0.50 | 0.80 | 0.94 | 1476.00# | Kim et al. (1994) |
| 66.90 | 20.52 | 4.56 | 1.49 | 0.51 | 0.92 | 0.97 | 1499.00 | Kim et al. (1994) |
| 49.23 | 18.13 | 6.08 | 12.17 | 2.28 | 0.82 | 1.79 | 1217.00# | Kim et al. (1994) |
| 57.75 | 23.00 | 4.10 | 2.23 | 0.94 | 1.02 | 1.93 | 1498.00 | Kim et al. (1994) |
| 32.58 | 27.49 | 21.23 | 4.11 | 1.85 | 0.25 | 1.11 | 1257.00 * | Kim et al. (1994) |
| 50.00 | 27.00 | 3.50 | 9.20 | 1.50 | 1.70 | 0.80 | 1480.00 | CEA Report (2012) |
| 53.00 | 19.60 | 14.60 | 4.20 | 1.45 | 1.00 | 2.07 | 1230.00 | CEA Report (2012) |
| 58.50 | 33.70 | 1.60 | 1.49 | 1.00 | 1.48 | 1.51 | 1570.00 | CEA Report (2012) |
| 73.00 | 16.00 | 4.00 | 1.60 | 1.20 | 0.74 | 1.49 | 1480.00 | CEA Report (2012) |
| 72.00 | 18.00 | 4.00 | 1.00 | 0.60 | 0.82 | 1.20 | 1470.00* | CEA Report (2012) |

*Test data ; # Validation data

Table S4: Composition of oxides (wt%) and corresponding  FT

| SiO2 | Al2O3 | Fe2O3 | CaO | MgO | TiO2 | K2O + Na2O | FT | Reference§ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 30.88 | 17.24 | 19.83 | 19.12 | 7.26 | 0.61 | 4.99 | 1090.00* | Lolja et al. (2002) |
| 52.42 | 16.49 | 12.09 | 10.59 | 3.62 | 0.85 | 3.91 | 1200.00 | Lolja et al. (2002) |
| 40.11 | 13.46 | 23.61 | 11.04 | 5.90 | 0.71 | 5.10 | 1130.00 | Lolja et al. (2002) |
| 43.40 | 18.92 | 10.77 | 16.24 | 3.90 | 0.77 | 5.94 | 1230.00 | Lolja et al. (2002) |
| 42.40 | 16.47 | 21.54 | 7.41 | 5.86 | 0.77 | 5.42 | 1130.00 | Lolja et al. (2002) |
| 50.15 | 23.54 | 11.84 | 4.48 | 5.50 | 0.67 | 3.69 | 1210.00 | Lolja et al. (2002) |
| 51.32 | 23.95 | 10.83 | 3.47 | 5.20 | 0.79 | 4.33 | 1240.00 | Lolja et al. (2002) |
| 56.24 | 20.72 | 10.24 | 3.55 | 2.56 | 0.97 | 5.64 | 1230.00 | Lolja et al. (2002) |
| 53.19 | 13.60 | 13.00 | 12.33 | 4.90 | 0.61 | 2.22 | 1200.00 | Lolja et al. (2002) |
| 42.13 | 19.81 | 13.19 | 18.90 | 2.22 | 0.95 | 2.56 | 1260.00 | Lolja et al. (2002) |
| 49.81 | 26.66 | 5.68 | 8.79 | 4.59 | 0.75 | 3.67 | 1260.00* | Lolja et al. (2002) |
| 43.83 | 14.99 | 14.13 | 16.46 | 4.60 | 0.64 | 5.34 | 1150.00* | Lolja et al. (2002) |
| 50.51 | 16.69 | 8.86 | 12.98 | 4.80 | 0.61 | 5.52 | 1180.00* | Lolja et al. (2002) |
| 54.68 | 28.81 | 3.95 | 2.72 | 6.26 | 0.80 | 2.77 | 1380.00# | Qiu et al. (1999) |
| 39.13 | 26.33 | 11.06 | 13.83 | 6.59 | 0.70 | 2.37 | 1400.00* | Qiu et al. (1999) |
| 51.36 | 33.73 | 8.63 | 1.40 | 0.64 | 1.55 | 2.69 | 1510.00 | Hanxu et al. (2006) |
| 48.02 | 23.32 | 23.17 | 1.32 | 0.86 | 1.02 | 2.29 | 1437.00 | Vorres (1979) |
| 49.92 | 18.77 | 21.14 | 6.04 | 1.07 | 0.82 | 2.24 | 1271.00* | Vorres (1979) |
| 49.23 | 11.79 | 7.18 | 25.64 | 4.10 | 0.62 | 1.44 | 1232.00 | Vorres (1979) |
| 38.85 | 20.25 | 26.13 | 7.54 | 1.25 | 0.89 | 5.08 | 1025.55 | Rees (1964) |
| 35.85 | 20.59 | 25.33 | 8.52 | 3.25 | 0.84 | 5.63 | 1075.55 | Rees (1964) |
| 35.70 | 20.63 | 26.50 | 8.09 | 2.31 | 0.96 | 5.80 | 1036.66* | Rees (1964) |
| 43.14 | 18.15 | 23.74 | 8.36 | 1.05 | 0.90 | 4.66 | 1034.44 | Rees (1964) |
| 46.62 | 19.03 | 23.19 | 4.25 | 1.02 | 0.99 | 4.89 | 1103.33# | Rees (1964) |
| 44.19 | 17.55 | 28.29 | 3.02 | 1.03 | 1.01 | 4.90 | 1103.33 # | Rees (1964) |
| 35.00 | 16.11 | 31.15 | 13.43 | 0.97 | 0.78 | 2.57 | 1015.00 | Rees (1964) |
| 39.30 | 14.46 | 34.98 | 6.85 | 0.93 | 0.80 | 2.67 | 1015.00# | Rees (1964) |
| 44.53 | 17.27 | 23.64 | 7.91 | 1.01 | 1.05 | 4.59 | 1054.44 | Rees (1964) |
| 47.26 | 19.65 | 16.65 | 11.83 | 0.86 | 0.83 | 2.91 | 1163.33 | Rees (1964) |
| 47.76 | 20.07 | 12.98 | 14.33 | 0.94 | 0.91 | 3.01 | 1154.44* | Rees (1964) |
| 40.30 | 18.21 | 21.08 | 16.14 | 0.68 | 0.86 | 2.72 | 1154.44* | Rees (1964) |
| 35.28 | 20.40 | 30.31 | 9.43 | 0.76 | 0.97 | 2.84 | 1208.88 | Rees (1964) |
| 34.30 | 19.78 | 30.33 | 11.28 | 0.70 | 1.10 | 2.52 | 1206.66 | Rees (1964) |
| 52.64 | 23.95 | 13.67 | 4.38 | 0.87 | 1.07 | 3.42 | 1243.33 | Rees (1964) |
| 42.59 | 17.37 | 14.81 | 20.74 | 0.90 | 0.77 | 2.82 | 1232.22* | Rees (1964) |
| 43.26 | 17.34 | 12.92 | 21.39 | 1.09 | 0.68 | 3.32 | 1156.66 | Rees (1964) |
| 54.70 | 21.67 | 13.66 | 4.50 | 1.04 | 1.00 | 3.42 | 1202.22 | Rees (1964) |
| 52.47 | 22.71 | 14.72 | 5.15 | 0.94 | 1.09 | 2.92 | 1177.22* | Rees (1964) |
| 44.72 | 22.38 | 21.96 | 4.76 | 1.31 | 1.15 | 3.72 | 1248.33 | Rees (1964) |
| 55.78 | 28.16 | 7.21 | 1.44 | 1.28 | 1.36 | 4.77 | 1371.11 | Rees (1964) |
| 52.46 | 24.39 | 6.61 | 9.76 | 1.05 | 1.22 | 4.52 | 1257.22 | Rees (1964) |
| 46.98 | 23.01 | 12.50 | 11.32 | 1.87 | 0.63 | 3.68 | 1288.33 | Rees (1964) |
| 46.58 | 22.95 | 14.98 | 9.47 | 2.38 | 0.67 | 2.97 | 1288.33 | Rees (1964) |
| 50.73 | 22.73 | 13.35 | 6.97 | 1.84 | 0.68 | 3.71 | 1215.00 | Rees (1964) |
| 41.31 | 25.08 | 16.25 | 12.20 | 1.22 | 0.97 | 2.97 | 1201.111 | Rees (1964) |
| 49.26 | 22.62 | 19.21 | 3.50 | 0.81 | 1.27 | 3.33 | 1261.66 | Moreno (2008) |
| 48.41 | 20.28 | 20.46 | 7.90 | 0.12 | 1.00 | 1.83 | 1254.44 | Moreno (2008) |
| 40.05 | 19.55 | 32.13 | 2.81 | 0.65 | 0.90 | 3.91 | 1148.88* | Moreno (2008) |
| 55.44 | 29.58 | 6.75 | 2.26 | 0.79 | 1.61 | 3.57 | 1482.22 | Moreno (2008) |
| 57.77 | 29.47 | 4.04 | 2.12 | 1.44 | 1.41 | 3.75 | 1482.22* | Moreno (2008) |
| 62.09 | 25.12 | 4.79 | 3.45 | 1.12 | 0.96 | 2.48 | 1482.22 | Moreno (2008) |
| 52.24 | 23.49 | 9.42 | 6.85 | 1.98 | 0.92 | 5.10 | 1376.66# | Moreno (2008) |
| 63.58 | 22.64 | 6.44 | 1.91 | 1.40 | 0.90 | 3.13 | 1476.66* | Moreno (2008) |
| 64.08 | 25.68 | 4.94 | 0.54 | 0.39 | 1.20 | 3.16 | 1482.22* | Moreno (2008) |
| 50.12 | 19.46 | 20.78 | 5.28 | 0.84 | 0.91 | 2.63 | 1193.33 | Moreno (2008) |
| 45.33 | 17.17 | 24.21 | 8.89 | 0.77 | 0.83 | 2.81 | 1115.55 | Moreno (2008) |
| 59.04 | 22.01 | 5.41 | 7.12 | 3.47 | 1.63 | 1.32 | 1148.88 | Moreno (2008) |
| 48.64 | 19.06 | 5.16 | 14.21 | 4.76 | 1.26 | 6.91 | 1143.33 * | Moreno (2008) |
| 39.01 | 19.44 | 20.06 | 14.82 | 4.52 | 0.79 | 1.37 | 1270.00 | Moreno (2008) |
| 43.19 | 32.75 | 18.73 | 1.84 | 1.02 | 2.15 | 0.31 | 1540.00 | Bryant et al. (2000) |
| 50.56 | 32.34 | 12.08 | 1.84 | 1.02 | 1.84 | 0.31 | 1615.00 | Bryant et al. (2000) |
| 62.68 | 22.99 | 5.77 | 3.30 | 1.24 | 0.82 | 3.20 | 1410.00 | Bryant et al. (2000) |
| 62.61 | 26.53 | 4.42 | 0.40 | 0.80 | 1.21 | 4.02 | 1605.00 | Bryant et al. (2000) |
| 65.87 | 23.98 | 4.80 | 1.13 | 0.83 | 1.43 | 1.93 | 1570.00 | Akiyama et al. (2011) |
| 52.55 | 25.44 | 11.81 | 5.13 | 1.85 | 1.66 | 1.53 | 1320.00 | Steyn and Minnitt (2010) |
| 49.70 | 25.61 | 11.31 | 9.92 | 2.76 | 0.69 | 0.02 | 1650.00 | Bahrinet al. (2009) |
| 36.78 | 23.10 | 18.16 | 14.71 | 2.30 | 2.18 | 2.76 | 1319.00 * | Matuszewski (2012) |
| 46.67 | 25.10 | 18.02 | 4.38 | 1.67 | 1.35 | 2.81 | 1333.00* | Matuszewski (2012) |
| 44.57 | 23.78 | 24.27 | 3.41 | 0.75 | 1.10 | 2.12 | 1332.22 | Matuszewski (2012) |
| 47.62 | 19.05 | 21.16 | 7.41 | 1.06 | 1.06 | 2.65 | 1323.88 | Matuszewski (2012) |
| 45.49 | 19.98 | 7.72 | 19.78 | 5.08 | 0.86 | 1.10 | 1258.88 | Matuszewski (2012) |
| 51.77 | 17.64 | 10.52 | 13.98 | 3.13 | 1.21 | 1.74 | 1294.44 | Matuszewski (2012) |
| 58.44 | 28.86 | 5.82 | 0.51 | 0.20 | 2.49 | 3.67 | 1537.77 | U.S.DOE (2001) |
| 59.55 | 28.52 | 5.43 | 0.11 | 0.67 | 2.04 | 3.69 | 1463.88 # | U.S.DOE (2001) |
| 56.54 | 28.48 | 8.97 | 0.53 | 0.14 | 1.98 | 3.35 | 1537.77 | U.S.DOE (2001) |
| 54.06 | 26.21 | 15.23 | 0.48 | 0.16 | 1.56 | 2.28 | 1445.00* | U.S.DOE (2001) |
| 36.32 | 25.63 | 30.37 | 3.84 | 0.31 | 1.31 | 2.21 | 1240.556 | U.S.DOE (2001) |
| 64.04 | 11.75 | 13.04 | 4.42 | 1.92 | 1.84 | 2.99 | 1480.55 | U.S.DOE (2001) |
| 69.78 | 21.40 | 4.76 | 1.55 | 0.53 | 0.96 | 1.01 | 1516.00 | Kim et al. (1994) |
| 54.40 | 20.03 | 6.72 | 13.45 | 2.52 | 0.91 | 1.98 | 1243.00 | Kim et al. (1994) |
| 63.48 | 25.28 | 4.51 | 2.45 | 1.03 | 1.12 | 2.12 | 1523.00 | Kim et al. (1994) |
| 55.25 | 20.43 | 15.22 | 4.38 | 1.51 | 1.04 | 2.16 | 1260.00# | CEA Report (2012) |
| 58.92 | 33.94 | 1.61 | 1.50 | 1.01 | 1.49 | 1.52 | 1620.00# | CEA Report (2012) |
| 74.47 | 16.32 | 4.08 | 1.63 | 1.22 | 0.75 | 1.52 | 1540.00 | CEA Report (2012) |
| 73.76 | 18.44 | 4.10 | 1.02 | 0.61 | 0.84 | 1.23 | 1500.00 | CEA Report (2012) |
| 58.72 | 23.66 | 8.93 | 2.94 | 1.28 | 1.14 | 3.28 | 1410.00 | CIMFR |
| 59.05 | 23.82 | 12.88 | 0.99 | 0.42 | 1.94 | 0.88 | 1430.00 | CIMFR |
| 59.63 | 19.07 | 9.10 | 7.27 | 1.96 | 1.83 | 1.00 | 1340.00 # | CIMFR |
| 64.44 | 22.99 | 5.67 | 2.37 | 0.79 | 1.30 | 2.39 | 1430.00 | CIMFR |
| 60.63 | 21.90 | 8.62 | 3.52 | 1.13 | 1.65 | 2.44 | 1360.00 | CIMFR |
| 59.80 | 14.67 | 11.74 | 6.79 | 1.54 | 1.85 | 3.34 | 1310.00 | CIMFR |
| 59.06 | 25.01 | 7.06 | 4.78 | 1.41 | 2.00 | 0.51 | 1380.00 | CIMFR |
| 61.36 | 21.74 | 6.94 | 2.96 | 0.96 | 1.96 | 4.00 | 1410.00 | CIMFR |
| 64.18 | 17.36 | 10.19 | 1.70 | 0.44 | 1.96 | 4.11 | 1400.00 | CIMFR |

*: Test data;  #: Validation data; § CIMFR:  Central Institute of Mining and Fuel Research, Dhanbad, India, from where data were sourced.

Table S5: Mean and Standard deviation of seven oxide weight percentages (wt%) four AFTs fusion temperature

| AFT |  | SiO2 wt (%) (x1) | Al2O3 wt (%) (x2) | Fe2O3 wt (%) (x3) | CaO wt (%) (x4) | MgO wt (%) (x5) | TiO2 wt (%) (x6) | K2O+Na2O wt (%) (x7) | y (OC)# |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| IDT | Mean | 55.75 | 23.63 | 10.51 | 4.8 | 1.37 | 1.38 | 2.56 | 1189.36 |
|  | Std. dev. | 9.53 | 4.61 | 7.32 | 5.50 | 1.69 | 0.48 | 1.47 | 113.36 |
| ST | Mean | 45.85 | 21.60 | 12.93 | 7.14 | 2.04 | 1.25 | 2.61 | 1264.87 |
|  | Std. dev. | 12.01 | 7.14 | 8.99 | 5.80 | 2.57 | 1.13 | 1.48 | 179.17 |
| HT | Mean | 45.70 | 19.05 | 13.80 | 8.95 | 3.53 | 1.08 | 3.07 | 1314.96 |
|  | Std. dev. | 14.69 | 8.39 | 14.27 | 7.73 | 3.61 | 1.26 | 2.10 | 169.95 |
| FT | Mean | 50.77 | 21.79 | 14.06 | 7.21 | 1.93 | 1.13 | 3.09 | 1300.42 |
|  | Std. dev. | 9.30 | 4.69 | 8.03 | 5.75 | 1.70 | 0.44 | 1.41 | 158.02 |

# y denotes the specific ash fusion temperature

References

Akiyama K, Pak H, Ueki Y, et al. (2011) Effect of Mg based addition to Upgraded Brown Coal on the Ash Deposition Behavior during Combustion. Chia Laguna, Cagliari, Sardinia, Italy, September 11-15.

Bahrin D, Faizal M, Ibrahim E, et al (2009) Predicting Coal Ash Fusion Temperature of South Sumatera’s Blended Coal with Coal Blending Simulation and Laboratory Analysis. SISEST 2009 - RUSNAS PEBT A IX – 1.

Bryant GW, Browning GJ, Emanuel H,  et al (2000) The Fusibility of Blended Coal Ash. Energy  Fuels , 14, 316-325.

CEA Report of The Group for Studying Range of Blending of Imported Coal with Domestic Coal (2012), Central Electricity Authority (CEA), April 2012. http://cea.nic.in/reports/others/thermal/tetd/blending_coal.pdf

Hanxu L, Ninomiya Y, Zhongbing D, et al.  (2006) Application of the FactSage to Predict the Ash Melting Behavior in Reducing Conditions. Chinese J. Chem. Eng., 14(6) 784—789.

Kim HT, Chung SW, Lee SH,  (1994) Behavior of Coal Ash Under Gasifier Environment (1994), American Chemical Society (ACS) national meeting, Washington, DC (United States), 21-26 Aug 1994, pp. 894-898. https://web.anl.gov/PCS/acsfuel/preprint%20archive/Files/39_3_WASHINGTON%20DC_08-94_0894.pdf

Kim MR, Jang JG, Lee SK, et al.  (2010). Correlation between the ash composition and melting temperature of waste incineration residue. Korean J. Chem. Eng., 27(3) 1028-1034.

Lolja SA, Haxhi H, Dhimitri R, et al (2002) Correlation between ash fusion temperatures and chemical composition in Albanian coal ashes. Fuel (81) 2257–2261.

Matuszewski M. (2012) Quality Guidelines for Energy System Studies- Detailed Coal Specifications. DOE/NETL-401/012111, Final Report, January 2012.

Moreno RX. (2008)  Development of a LIBS system for prediction of ash fusion temperature in coal-fired power plants. Theses and Dissertations (2008). Paper 1019. 
https://preserve.lehigh.edu/etd/1019

Qiu JR, Li F, Zheng Y, et al (1999) The influences of mineral behaviour on blended coal ash fusion characteristics. Fuel (78), 963–969.

Rees OW. (1964) Composition of the Ash of Illinois Coals. Illinois State Geological Survey, Urbana, Circular 365, URL: http://library.isgs.illinois.edu/Pubs/pdfs/circulars/c365.pdf.

Steyn M, Minnitt RCA. (2010) Thermal coal products in South Africa. Journal of The Southern African Institute of Mining and Metallurgy VOLUME 110, OCTOBER 2010.

U.S.DOE Award Number DE-FC 26-00NT- 40693 (2001)Quarterly Technical Progress Report, p.2-7. https://www.osti.gov/servlets/purl/788765

Vorres KS. (1979) Chemistry of coal ash melting in gasification and combustion. Paper presented to Structure of Coal. Symposium, Fuel Chemistry Division, ACS/CSJ Congress, Honolulu, April 1979, pp. 247-254,  Institute of Gas Technology, Chicago. https://web.anl.gov/PCS/acsfuel/preprint%20archive/Files/24_2_HONOLULU_04-79_0247.pdf