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Fig. S1 Survey XPS spectrum of the as-obtained Fe2O3-modified BiVO4 porous nanoplates
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Fig. S2 FE-SEM image of the as-obtained Fe2O3-modified BiVO4 porous nanoplates
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Fig. S3 Mapping images of an individual Fe2O3/BiVO4 porous nanoplate
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Fig. S4 EDX spectrum of the products
Preparation of Fe2O3 nanorods

The preparation of Fe2O3 adopted a modified method [1]. In a typical process, 10 mmol of FeCl3 was dissolved in 40 mL of ultrapure water. Then 30 mmol of NaOH was added into the solution. The resultant precipitate was washed by ultrapure water for several times. Subsequently, the precipitate was dispersed in 40 mL of NaOH aqueous solution (2M) under stirring for 1 h. Then the suspension was put in a Teflon® lined stainless steel autoclave with 50 mL of capability and heated at 160 °C for 20 h. After the autoclave was cooled to room temperature, the resultant products were separated via centrifugation and washed three times with ultrapure water and absolute ethanol, respectively. Finally, the products were dried under vacuum at 60 °C for 4 h.
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Fig. S5 XRD pattern of the products
Power XRD pattern of the products can be indexed as hexagonal Fe2O3 (JCPDS No. 89-0597).
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Fig. S6 TEM image of the products.

TEM image shows that the as-synthesized products are nanorods.
Preparation of ultrafine Fe2O3 nanoparticles loaded SiO2 nanospheres

SiO2 nanospheres were prepared through a modified Stober method [2]. In a typical process, 125 mL of ethanol and 6.25 mL of ammonia aqueous solution (28-30 %) were mixed under stir. Then 4.38 mL of TEOS was injected into the above mixture solution. The reaction was allowed to proceed at 25 (C for 24 h. The resultant products were collected, washed with distilled water and ethanol for several times, and then vacuum-dried at 60 (C. 
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Fig. S7 TEM image of the products.

TEM image shows that the as-synthesized products are SiO2 nanospheres.
For the synthesis of Fe2O3/SiO2, similar to previous report [3], 0.4 mmol of Fe(acac)3 (acac represents acetylancetone) was dissolved into the mixed solvents of ethanol (12 mL) and n-hexane (68 mL). Then 4 mmol of the as-obtained SiO2 nanospheres were added into the mixed solvents. The solvents were allowed to stand at 25 (C for 24 h. After that, the solid precipitates were washed with the same solvent to remove physisorbed complexes and then washed with ethanol for several times. Subsequently, the sample was vacuum-dried at 60 (C, followed by heating in air at 500 (C for 2 h.
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Fig. S8 TEM image of the products at different magnification
TEM images show that ultrasmall Fe2O3 nanoparticles were loaded on the surfaces of SiO2 nanospheres.
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Fig. S9 Phenol concentration changes with irradiation time over ultrafine Fe2O3 nanopartices loaded SiO2 nanospheres
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Fig. S10 The adsorption behavior of RhB (a) phenol (b) on BiVO4, Fe2O3, Bi2O3/BiVO4, and Fe2O3/BiVO4
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Fig. S11 PL emission spectra of BiVO4 and Co3O4/BiVO4 excited at λ = 400 nm at room temperature
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Fig. S12 The adsorption behavior of phenol on Fe2O3/BiVO4 and Co3O4/BiVO4
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Fig. S13 Phenol concentration changes with irradiation time 
over BiVO4, Pt/BiVO4 and Fe2O3/BiVO4
Preparation of Pt/BiVO4
The preparation of Pt loaded porous BiVO4 nanoplates adopted impregnation method [4]. In a typical process, 129.6 mg of the as-obtained porous BiVO4 nanoplates was added into 5 mL of ultrapure water containing 7 mg of H2PtCl6·6H2O in a beaker. Then the suspension was stirred evenly and dried at 60 °C under vacuum. After that, the powder was calcined in air at 400 °C for 0.5 h.
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