A novel artificial neuron-like gas sensor constructed from CuS quantum dots/Bi2S3 nanosheets

Xinwei Chen1, Tao Wang1, Jia Shi1, Shuyue Zheng2, Wen Lv1, Yutong Han1, Min Zeng1, Jianhua Yang1, Nantao Hu1, Yanjie Su1, Hao Wei1, Zhihua Zhou1, Zhi Yang1*, Yafei Zhang1*

1 Key Laboratory of Thin Film and Microfabrication (Ministry of Education), Department of Micro/Nano Electronics, Institute of Marine Equipment, School of Electronic Information and Electrical Engineering, Shanghai Jiao Tong University, Shanghai 200240, P. R. China.

2 Department of Breast Surgery, Fudan University Shanghai Cancer Center, Shanghai 200032, P. R. China.

*Corresponding authors. E-mail address: zhiyang@sjtu.edu.cn and yfzhang@sjtu.edu.cn.

Fig. S1 Photographs of Bi2S3 dispersions in various ethanol/water mixtures: a Before and b after ultrasonication treatment for 8 h. c Supernatant collection by centrifugation at 3000 rpm.

Fig. S2 SEM image of Bi2S3 samples before a and after b Liquid phase stripping. c and d TEM and HR-TEM images of Bi2S3 NSs.

Fig. S3 XRD patterns a and Raman spectra b of bulk Bi2S3 and Bi2S3 NSs.

Fig. S4 a XRD pattern b Raman spectra and c SEM image of CuS sample.

Fig. S5 Full XPS survey spectrums of a Bi2S3 NSs and b CuS.

Fig. S6 The atomic structure of CuS-Bi2S3.

Fig. S7 UPS spectra of a Bi2S3 and b CuS: the secondary electron cut-off energy region (left) and low binding energy region (right) of each.

Fig. S8 UV−vis diffuse reflectance spectra of a Bi2S3 NSs and c CuS. (αhν)2 v.s. hν curve of b Bi2S3 NSs and d CuS.

Fig. S9 Energy level diagram between interfacial materials CuS and Bi2S3 and schematic diagram of the charge transfer process.

Fig. S10 Structure diagram of the flexible interdigital electrode.

Fig. S11 Schematic diagram of the homemade gas-control system.

Fig. S12 a-k Sensitive response at a concentration to 10 ppm NO2 through a dynamic gas-sensing room temperature testing for bulk pure Bi2S3, Bi2S3 NSs, BC-2.5, BC-3, BC-4, BC-5, BC-6, BC-7.5, BC-10, BC-20, and pure CuS. l I-V curves of Bi2S3, different content of CuS QDs/Bi2S3 NSs and CuS-based gas sensors.

Fig. S13 a Response and b recovery performances of Bi2S3, different content of CuS QDs/Bi2S3 NSs, and CuS-based gas sensors to 10 ppm NO2.

Fig. S14 a The response value of BC-5 sensor to different concentrations of NO2 and its error bars. b The response of BC-5-based sensor as a function of the logarithm of the NO2 concentration. c Long-term stability of BC-5-based sensor.

Fig. S15 The selectivity of the BC-5-based sensor to 10 ppm different target gases of a H2S, b NH3, c SO2, d H2 and e NO.

Fig. S16 Sensing characteristics of the sensor to 10 ppm NO2 at different humidity levels.

Fig. S17 a Energy band structures of CuS QDs/Bi2S3 NSs heterostructure in air. b the proposed sensing mechanism of the heterostructure.

Fig. S18 The schematic circuit diagram of the flexible printed circuit board: a Data acquisition and communication circuit. b Sensor front-end circuit. c USB/Wireless charging circuit.

Fig. S19 a Photograph of the flexible circuit and electrode used in the current work (placed next to a school logo and 1 RMB coin for comparison). b Photographs of Bluetooth signal connection of wearable sensor device. c Photographs of wireless sensor signal acquisition process of the wearable sensor device.

Table S1 The bond length of M-O on NO2-CuS-Bi2S3 structure.

| Binding structure | Atoms | Bond | Length (Å) |
| --- | --- | --- | --- |
| n1 | N (from NO2) | Cu-N | 1.978 |
|  | Cu (CuS-Bi2S3) |  |  |
| n2 | O (from NO2) | Bi-O | 2.025 |
|  | Bi (CuS-Bi2S3) |  | 2.018 |
| n3 | O (from NO2) | Cu-O | 2.396 |
|  | Bi/Cu (CuS-Bi2S3) | Bi-O | 2.557 |
| n4 | O (from NO2) | Cu-O | 2.555 |
|  | Cu (CuS-Bi2S3) |  | 2.567 |

Table S2 The charge and charge transfer of NO2 correlated to Fig. 5.

| Binding structure | Atoms | Charge | Charge transfer |
| --- | --- | --- | --- |
| n2 | N | 4.4197582 | -0.5802418 |
|  | O | 6.5942103 | 0.5942103 |
|  | O | 6.6273451 | 0.6273451 |
|  | Total-NO2 |  | 0.6413136 |
| n4 | N | 4.4885298 | -0.5114702 |
|  | O | 6.598587 | 0.598587 |
|  | O | 6.6327922 | 0.6327922 |
|  | Total-NO2 |  | 0.719909 |

Table S3 The charge and charge transfer of CuS correlated to Fig. 3d.

| Binding structure | Atoms | Charge (e) | Charge transfer (e) |
| --- | --- | --- | --- |
| CuS-Bi2S3 | Cu1 | 10.59286 | -0.40714 |
|  | Cu2 | 10.59062 | -0.40938 |
|  | Cu3 | 10.58872 | -0.41128 |
|  | S1 | 6.800926 | 0.800926 |
|  | S2 | 6.751016 | 0.751016 |
|  | S3 | 6.768011 | 0.768011 |
|  | S4 | 6.763804 | 0.763804 |
|  | S5 | 6.771819 | 0.771819 |
|  | S6 | 6.74335 | 0.74335 |
|  | Total-CuS |  | 3.371122 |

Table S4 Resistance values of bulk Bi2S3, Bi2S3 NSs, CuS, and different complex amounts of CuS QDs/Bi2S3 heterostructures.

|  | R |  |  | R |
| --- | --- | --- | --- | --- |
| Bulk Bi2S3 | 6.4 MΩ |  | BC-6 | 48 MΩ |
| Bi2S3 NSs | 17 MΩ |  | BC-7.5 | 21.5 MΩ |
| BC-2.5 | 30 MΩ |  | BC-10 | 2.5 MΩ |
| BC-3 | 110 MΩ |  | BC-20 | 73 KΩ |
| BC-4 | 160 MΩ |  | CuS | 35.5 Ω |
| BC-5 | 66 MΩ |  |  |  |

Table S5 The room-temperature sensing performance comparison of NO2 flexible gas sensors with different sensing materials.

| Materials | Conc. (ppm) | Response | τres. (s) | τrec. (s) | LOD (ppb) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| MoSe2 | 10 | 4 a | 250 | 150 | 10 | 1 |
| VA-2D MoS2 | 5 | 380%b | 500 | Can’t recover | - | 2 |
| SnS2/S-rGO | 1 | 75% c | 600 | 1200 | 0.7 | 3 |
| RGO/Mesoporous ZnO NSs | 15 | 44% c | 140 | 630 | 43.5 | 4 |
| 3D SnS2-rGO | 5 | 32.1% d | 300 | Can’t recover | 2.8 | 5 |
| CuS QDs/Bi2S3 | 10 | 3.4 e | 18 | 338 | 78 | This work |

Conc.: Gas concentration; Temp.: Operating temperature; τrec.: Recovery time; RT: Room temperature.

a Ig/Ia.

b ΔI/I0

c ΔR/Ra.

d ΔG/G.

e Rg/Ra.

References

[1] S. Guo, D. Yang, S. Zhang, Q. Dong, B. Li, N. Tran, Z. Li, Y. Xiong, M.E. Zaghloul, Development of a cloud-based epidermal MoSe2 device for hazardous gas sensing. Adv. Funct. Mater. 29, 1900138 (2019). https://doi.org/10.1002/adfm.201900138

[2] M.A. Islam, H. Li, S. Moon, S.S. Han, H.-S. Chung, J. Ma, C. Yoo, T.-J. Ko, K.H. Oh, Y.J. Jung, Y.W. Jung, Vertically aligned 2D MoS2 layers with strain-engineered serpentine patterns for high-performance stretchable gas sensors: experimental and theoretical demonstration. ACS Appl. Mater. Interfaces 12(47), 53174−53183 (2020). https://doi.org/10.1021/acsami.0c17540

[3] Y. Huang, W. Jiao, Z. Chu, S. Wang, L. Chen, X. Nie, R. Wang, X. He, High sensitivity, humidity-independent, flexible NO2 and NH3 gas sensors based on SnS2 hybrid functional graphene ink. ACS Appl. Mater. Interfaces 12(1), 997−1004 (2020). https://doi.org/10.1021/acsami.9b14952

[4] W. Li, R. Chen, W. Qi, L. Cai, Y. Sun, M. Sun, C. Li, X. Yang, L. Xiang, D. Xie, T. Ren, Reduced graphene oxide/mesoporous ZnO NSs hybrid fibers for flexible, stretchable, twisted, and wearable NO2 e‑textile gas sensor. ACS Sens. 4(10), 2809−2818 (2019). https://doi.org/10.1021/acssensors.9b01509

[5] J. Wu, Z. Wu, H. Ding, Y. Wei, W. Huang, X. Yang, Z. Li, L. Qiu, X. Wang, Three-dimensional graphene hydrogel decorated with SnO2 for high-performance NO2 sensing with enhanced immunity to humidity. ACS Appl. Mater. Interfaces 12(2), 2634−2643 (2020). https://doi.org/10.1021/acsami.9b18098