Supporting Information

Enhancing Hydrophilicity of Thick Electrodes for High Energy Density Aqueous Batteries

Jungeun Lee1, Hyeonsoo Lee1, Cheol Bak2, Youngsun Hong1, Daeha Joung3, Jeong Beom Ko1, Yong Min Lee2,* and Chanhoon Kim1,*

1Sustainable Technology and Wellness R&D Group, Korea Institute of Industrial Technology (KITECH), 102 Jejudaehak-ro, Jeju-si, Jeju-do 63243, Republic of Korea

2Department of Energy Science and Engineering, Daegu Gyeongbuk Institute of Science and Technology (DGIST), Daegu 42988, Republic of Korea

3Department of Physics, Virginia Commonwealth University, Richmond, VA 23284, USA

*E-mail: ckim8608@kitech.re.kr

Keywords: thick electrodes, hydrophilic binder, sulfonation, aqueous zinc-ion batteries, high areal capacity

Fig. S1 A scheme to synthesize sulfornated PVdF (S-PVdF) from PVdF through simple chemical reaction.

Fig. S2 FT-IR spectra of S-PVdF and PVdF binders.

Fig. S3 1H NMR spectra of S-PVdF and PVdF binders.

Fig. S4 Nyquist plots of S-PVdF and PVdF binders and their ionic conductivities.

Fig. S5 FTIR spectra of binder before and after electrolyte soaking. a PVdF binders before and after electrolyte soaking. b S-PVdF binders before and after electrolyte soaking.

We have confirmed that the sulfonate groups in S-PVdF binders can provide abundant coordination sites with Zn2+ by Fourier transformation infrared spectrum (FTIR). After soaking in electrolyte for 24 h, the 1277 cm−1 symmetric O=S=O peak shifts to a wave number (1271 cm−1) in S-PVdF binders, which suggests that the Zn2+ ions interact with sulfonate groups [1].

Fig. S6 XPS spectrum of Zn 2p in PVdF binders a before and b after electrolyte soaking. XPS spectrum of Zn 2p in S-PVdF binders c before and d after electrolyte soaking.

We also measured the binding energy of PVDF and S-PVDF to zinc ions via X-ray photoelectron spectroscopy (XPS). As can be seen in Fig. S6, XPS analysis exhibits the characteristic binding energies of Zn 2p3/2 and Zn 2p1/2 of 1022.3 and 1045.4 eV in S-PVdF [2].

Fig. S7 a SEM image and b XRD pattern of NH4V4O10 (NHVO).

Fig. S8 Cross-sectional SEM image of a cathode with a S-PVdF binders and b its magnification. Cross-sectional SEM image of a cathode with c S-PVdF binders and d its magnification after the calendering process.

Fig. S9 a SEM images of cathodes with S-PVdF binders and b its magnification. SEM images of cathodes with c PVdF binders and d its magnification.

Fig. S10 CV profiles of full cells with S-PVdF and PVdF binders at 0.2 mV s−1.

Fig. S11 Rate capability of cathodes with different binders.

Fig. S12 Cycling performances of full cells with different binders at a low current density of 0.5 A g-1 (~0.1 C).

Fig. S13 a SEM image and b XRD pattern of δ-MnO2.

To prove the universality of the binder, δ-MnO2 was prepared. First, 1.2g of KMnO4 and 0.215 g of MnSO4 were dissolved in 130 ml DIW. Then, the solution was put into a Teflon-contained autoclave and heated at 160 °C for 12 h. After cooling and centrifugation, the product was rinsed with DIW several times. Finally, δ-MnO2 was obtained after drying in a convection oven at 80 °C for 12 h. Next, the δ-MnO2 was cast on stainless (SUS) foil and composed of three components: active material, conductive materials, and binders in the weight ratio of 7:2:1. Denka black was selected as the conductive material. Slurries containing the three components in N-methyl-2-pyrrolidone (NMP) were cast onto SUS foil (20 µm thick) via the doctor blading method, followed by a drying step at 80 °C for 12 h under vacuum. The active mass loadings for the cathode materials were ~ 3 mg cm-2. The full cell with S-PVdF binders showed a higher reversible capacity (282 mAh g−1) than those with PVdF binders (237 mAh g−1) at the same mass loading of 3 mg cm−2) at a current density of 0.2 A g−1. Moreover, the full cell with S-PVdF showed higher reversible capacities in the cycle test. More importantly, it retained a highly improved capacity of ~ 185 mAh g−1 with a durable capacity retention of 66% after 200 cycles at 0.2 A g−1. On the other hand, only a 20% capacity (49 mAh g−1) was obtained in the full cell with PVdF binders after the cycle test.

Fig. S14 EIS spectra of a before and b after long-term cycling (3000 cycles at 10 A g−1). c Corresponding equivalent circuit. Ri and Rs are the ohmic resistance of solution and electrodes. Rct is the charge-transfer resistance. C1 and C2 are the constant phase element of the double-layer capacitance, respectively. Zw is the Warburg impedance.

Fig. S15 1H NMR spectra of binders with different sulfonation degrees.

Fig. S16 a Galvanostatic cycling performances of cathodes with different binders at a current density of 1 A g-1. b Contact angle of the cathode with S-PVdF binder (low sulfonation degree of 5%).

Fig. S17 High-resolution XPS spectra of S-PVdF films before and after being immersed into cathode-dissolved electrolytes. a S2p and b O1s spectra peaks of immersed S-PVdF film before being immersed into cathode-dissolved electrolytes. c S2p and d O1s spectra peaks S-PVdF film after being into cathode-dissolved electrolytes.

To clarify the suppression of vanadium dissolution of vanadium-based active materials, we prepared cathode-dissolved electrolyte. First, 0.1 g of the vanadium-based active materials (NH4V4O10) were immersed into 10 ml of 2 M ZnSO4 aqueous electrolytes. Then, the solution was kept in an oven for 24 h at 70 °C and puriﬁed via ﬁltration by 0.45 µm syringe ﬁlter. S-PVdF films for measuring ionic conductivities were also used here. The films were immersed into the yellowish cathode-dissolved electrolyte for 24 h at room temperature. Then, the films were rinsed with DIW and ethanol several times. Finally, the films were dried in a convection oven at 80 °C for 12 h.

Supplementary References

[S1]	H. Fan, M. Wang, Y. Yin, Q. Liu, B. Tang, et al., Tailoring interfacial Zn2+ coordination via a robust cation conductive film enables high performance zinc metal battery. Energy Storage Materials. 49(380-389 (2022).
https://doi.org/https://doi.org/10.1016/j.ensm.2022.04.031

[S2] 	Y. Yang, C. Liu, Z. Lv, H. Yang, Y. Zhang, et al., Synergistic manipulation of Zn2+ ion flux and desolvation effect enabled by anodic growth of a 3d ZnF2 matrix for long-lifespan and dendrite-free zn metal anodes. Advanced Materials. 33(11), 2007388 (2021). 
https://doi.org/https://doi.org/10.1002/adma.202007388