Supporting Information for

Facile Semiconductor p-n Homojunction Nanowires with Strategic p-Type Doping Engineering Combined with Surface Reconstruction for Biosensing Applications

Liuan Li1,†, Shi Fang1,†, Wei Chen1, Yueyue Li2, Mohammad Fazel Vafadar3, Danhao Wang1, Yang Kang1, Xin Liu1, Yuanmin Luo1, Kun Liang1, Yiping Dang4, Lei Zhao4, Songrui Zhao3, Zongzhi Yin2,*, Haiding Sun1,*

1 iGaN Laboratory, School of Microelectronics, University of Science and Technology of China, Hefei 230026, P. R. China

2 Department of Obstetrics and Gynecology, the First Affiliated Hospital of Anhui Medical University, No 218 Jixi Road, Hefei 230022, P. R. China

3 Department of Electrical and Computer Engineering, McGill University, 3480 University Street, Montreal, Quebec H3A 0E9, Canada

4 Union Hospital, Tongji Medical College, Huazhong University of Science and Technology, No 1277 Jiefang Ave. Wuhan 430022, P. R. China

† Liuan Li and Shi Fang contributed equally to this work.

*Corresponding authors. E-mail: yinzongzhi@ahmu.edu.cn (Zongzhi Yin); haiding@ustc.edu.cn (Haiding Sun)

Supplementary Figures and Tables

Fig. S1 Scanning electron microscope (SEM) images of a n-GaN and b p-n GaN nanowires. c Open-circuit potential (OCP) measurements of the n-GaN and p-n GaN nanowires under 340 nm light illumination. The ΔOCP in p-n GaN nanowires significantly exceeds that in n-GaN nanowires, providing evidence for the superior carrier separation and extraction efficiency within p-n GaN nanowires compared to n-GaN nanowires.

Fig. S2 a Side-view and b top-view SEM images of the p-n GaN nanowires, c the corresponding selected nanowires area of the p-n GaN nanowires. The filling factor is approximately 0.76. d Side-view and e top-view SEM images of the p+-n GaN nanowires, f the corresponding selected nanowires area of the p+-n GaN nanowires. The filling factor is approximately 0.77. g Side-view and h top-view SEM images of the p++-n GaN nanowires, i the corresponding selected nanowires area of the p++-n GaN nanowires. The filling factor is approximately 0.80. The filling factors are calculated by the ratio of the nanowires area to the whole image area.

Fig. S3 Contact potential difference (CPD) mappings were obtained under dark conditions for a p-n GaN, b p+-n GaN, and c p++-n GaN nanowires, respectively. The corresponding average CPD values in a 2 μm × 2 μm region of p-n GaN, p+-n GaN, and p++-n GaN nanowires are 268.1, 97.6, and -175.1 mV, respectively. Additionally, CPD mappings were recorded under the illumination of 340 nm for d p-n GaN, e p+-n GaN, and f p++-n GaN nanowires, respectively. The corresponding average CPD values in a 2 μm × 2 μm region of p-n GaN, p+-n GaN, and p++-n GaN nanowires are 632.0, 369.3, and 26.1 mV, respectively. The difference value between the contact potential under illuminated conditions and dark conditions corresponds to surface photovoltage (SPV). The calculated SPV values of p-n GaN, p+-n GaN, and p++-n GaN nanowires are 363.9, 271.7, and 201.2 mV, respectively.

Fig. S4 valence band spectra of the a p-n GaN, b p+-n GaN, and c p++-n GaN nanowires. The relative positions of the valence band maxima referred to the Fermi level in p-n GaN, p+-n GaN, and p++-n GaN nanowires were determined as 1.53, 1.36, and 1.12 eV, respectively.

Fig. S5 The continuous on/off cycles test of p-n GaN nanowires under the illumination of 340 nm. The light intensity is kept at 0.1 mW cm−2.

Fig. S6 High-resolution TEM image of the a p-n GaN nanowires and b p-n GaN/CoNiOx nanowires. We can clearly observe the periodic lattice fringes in the GaN nanowires as well as the coated amorphous layer around the nanowires surface.

Fig. S7 The CPD mappings of p-n GaN/CoNiOx nanowires under a dark conditions and b under the illumination of 340 nm. The calculated SPV values of p-n GaN nanowire/CoNiOx nanowires were 766.8 mV.

Fig. S8 Photocurrents of the p-n GaN/CoNiOx nanowires under the illumination of 340 nm with different light intensities

Fig. S9 Chopped LSV measurements from 0.55 to −0.15 V with a scan rate of 0.03 V s−1

Fig. S10 Analysis of the response/recovery times of PEC photosensor employing p-n GaN/CoNiOx

Fig. S11 Photocurrents of the p-n GaN nanowires measured under a pure electrolyte (deionized water) and b 30 µM glucose. The photocurrent measured under pure electrolyte and 30 µM glucose is 0.080 and 0.085 µA, respectively.

Fig. S12 SEM images exhibit the morphology of the p–n GaN/CoNiOx nanowires a before and b after the 20-day test.

Fig. S13 Sequential additions of glucose, fructose, lactose, maltose, urea, and uric acid were made to the electrolyte under chopper light, and the corresponding photocurrents were recorded. The concentrations of all these compounds are 50µM. Two additions of glucose caused a significant enhancement of the photocurrent, while the intermediate addition of interfering substances showed negligible changes in the photocurrent. These results indicate the high selectivity of the glucose sensing.

Fig. S14 a Relationship between the photoresponse and the Co/Ni loading amounts. The photodeposition time is kept as 10 minutes. b Relationship between the photoresponse and the photodeposition time. The amount of Co-addition/Ni-addition is 30/30 µL. It is found that the 30 µL Co-addition, 30 µL Ni-addition, and the photodeposition for 30 minutes is the optimal photodeposition condition.

Fig. S15 Image of the as-fabricated PEC photosensor. The inset shows the fabricated GaN nanowires photoelectrode.

Table S1 Fitted parameters for the TRPL curves of p-n GaN and p-n GaN/CoNiOx nanowires

| Sample | τ1 (ns) | % | τ2 (ns) | % | τav (ns) |
| --- | --- | --- | --- | --- | --- |
| p-n GaN | 0.144 | 78.1 | 1.253 | 21.9 | 0.387 |
| p-n GaN/CoNiOx | 0.239 | 54.3 | 1.630 | 45.7 | 0.875 |

Table S2 Comparison of the performance of various glucose sensors

| Materials | Potential | Detection limit (µM) | Sensitivity (µA mM-1 cm-2) | Refs. |
| --- | --- | --- | --- | --- |
| p-n GaN/CoNiOx nanowires | 0 V vs. Ag/AgCl | 0.07 | 173 | This work |
| ITO/TiO2- Co3O4-CNT-GOx | 0 V vs. Ag/AgCl | 0.16 | 0.3 | [S1] |
| Ni/nanodiamond/BDD | 0.46 V vs. SCE | 0.05 | 120 | [S2] |
| BiOCl-G NHS | 0.5 V vs. Ag/AgCl | 220 | 127.2 | [S3] |
| Cu/ZnO | 0.1 V vs. SCE | 3.762 | 63.76 | [S4] |
| CuO/FTO | 0.6 vs. Ag/AgCl | 59.5 | 263 | [S5] |
| Au/Ni/BDD | 0.5 V vs. Ag/AgCl | 2.6 | 157.5 | [S6] |
| 3D hollow-out TiO2 NWc/GOx | 0.4 V vs. Ag/AgCl | 8.7 | 58.9 | [S7] |
| NiAl-LDH/α-Fe2O3 | 0.3 V vs. SCE | 5 | 274.7 | [S8] |
| Fe2O3NR/FTO | -0.1 V vs. SCE | 5.5 | 100.46 | [S9] |
| Fe2O3 films | 0.99 V vs. RHE | 0.05 | 17.23 | [S10] |

SCE: Saturated calomel electrode; RHE: Reversible hydrogen electrode

Supplementary References

- B. Çakıroğlu, M. Özacar, A self-powered photoelectrochemical glucose biosensor based on supercapacitor Co3O4-CNT hybrid on TiO2. Biosens. Bioelectron. 119, 34-41 (2018). https://doi.org/10.1016/j.bios.2018.07.049

- W. Dai, M. Li, S. Gao, H. Li, C. Li et al., Fabrication of nickel/nanodiamond/boron-doped diamond electrode for non-enzymatic glucose biosensor. Electrochim. Acta. 187, 413-421 (2016). https://doi.org/10.1016/j.electacta.2015.11.085

- A. I. Gopalan, N. Muthuchamy, K. P. Lee, A novel bismuth oxychloride-graphene hybrid nanosheets based non-enzymatic photoelectrochemical glucose sensing platform for high performances. Biosens. Bioelectron. 89, 352-360 (2017). https://doi.org/10.1016/j.bios.2016.07.017

- B. Yang, N. Han, S. Hu, L. Zhang, S. Yi et al., Cu/ZnO nano-thorn with modifiable morphology for photoelectrochemical detection of glucose. J. Electrochem. Soc. 168, 027516 (2021). https://doi.org/10.1149/1945-7111/abe50e

- N. J. Cory, E. Visser, J. Chamier, J. Sackey, F. Cummings et al., Electrodeposited CuO thin film for wide linear range photoelectrochemical glucose sensing. Appl. Surf. Sci. 576, 151822 (2022). https://doi.org/10.1016/j.apsusc.2021.151822

- K. Yao, B. Dai, X. Tan, V. Ralchenko, L. Yang et al., Fabrication of Au/Ni/boron-doped diamond electrodes via hydrogen plasma etching graphite and amorphous boron for efficient non-enzymatic sensing of glucose. J. Electroanal. Chem. 871, 114264 (2020). https://doi.org/10.1016/j.jelechem.2020.114264

- W. Yang, X. Wang, W. Hao, Q. Wu, J. Peng et al., 3d hollow-out TiO2 nanowire cluster/GOx as an ultrasensitive photoelectrochemical glucose biosensor. J. Mater. Chem. B. 8, 2363-2370 (2020). https://doi.org/10.1039/d0tb00082e

- M. Fan, S. Zhu, Q. Zhang, X. Wang, L. Zhang et al., Sensitive photoelectrochemical sensing of glucose using hematite decorated with NiAl-layered double hydroxides. Food Chem. 405, 134883 (2023). https://doi.org/10.1016/j.foodchem.2022.134883

- L. He, Q. Zhang, C. Gong, H. Liu, F. Hu et al., The dual-function of hematite-based photoelectrochemical sensor for solar-to-electricity conversion and self-powered glucose detection. Sens. Actuators, B 310, 127842 (2020). https://doi.org/10.1016/j.snb.2020.127842

- F. Liu, P. Wang, Q. Zhang, Z. Wang, Y. Liu et al., α‐Fe2O3 film with highly photoactivity for non‐enzymatic photoelectrochemical detection of glucose. Electroanalysis. 31, 1809-1814 (2019). https://doi.org/10.1002/elan.201900133