Supporting Information for

TiO2 Electron Transport Layer with p-n Homojunctions for Efficient and Stable Perovskite Solar Cells

Wenhao Zhao1, Pengfei Guo1, 2, 4,*, Jiahao Wu1, Deyou Lin1, Ning Jia1, Zhiyu Fang1, Chong Liu1, Qian Ye1, Jijun Zou3, Yuanyuan Zhou2 and Hongqiang Wang1, 4,*

1State Key Laboratory of Solidification Processing, Center for Nano Energy Materials, School of Materials Science and Engineering, Northwestern Polytechnical University and Shaanxi Joint Laboratory of Graphene (NPU), Xi’an 710072, P. R. China

2Department of Chemical and Biological Engineering, Hong Kong University of Science and Technology, Clear Water Bay, Hong Kong SAR, P. R. China

3Key Laboratory for Green Chemical Technology of the Ministry of Education, School of Chemical Engineering and Technology, Tianjin University, Tianjin 300072, P. R. China

4Chongqing Innovation Center of Northwestern Polytechnical University, Northwestern Polytechnical University, Chongqing 401135, P. R. China

*Corresponding authors. E-mail: guopengfei@nwpu.edu.cn (Pengfei Guo); hongqiang.wang@nwpu.edu.cn (Hongqiang Wang)

Supplementary Figures

Fig. S1 Schematic illustration of laser process of Ti0.936O2 nanocrystals and their embedding in the ETLs

Fig. S2 SEM image of the raw Ti0.936O2 powders before laser irradiation

Fig. S3 TEM images of Ti0.936O2 nanoparticles with different size under various laser fluence of a 100, b 200 and c 400 mJ/pulse cm2, respectively. TEM image of high concentration of Ti0.936O2 particles with d 0.05 and e 0.2 mg/ml

For optimization of laser fluence, Figure S3 shows TEM morphology and size evolution of Ti0.936O2 nanoparticles under different laser fluence. Normally, considering the employment of laser with the nanosecond pulse width, an increase in the laser fluence from 100 mJ/pulse cm2 to 200 mJ/pulse cm2, based on the “heat-melt-evaporation” mechanism induced by the laser in the liquid phase [S1], results in a decrease in the size of the spherical particles, as shown in Fig. S3a, b. When the laser fluence increases to 300 mJ/pulse cm2, Ti0.936O2 nanocrystals with a particle size below 10 nm are obtained, as shown in Figure 1a. However, if the laser fluence is further increased to 400 mJ/pulse cm2, it will be difficult to obtain Ti0.936O2 nanocrystals, which may be due to the strong photothermally induced evaporation effect under such conditions leading to the evaporation and further disappearance of Ti0.936O2 nanocrystals in liquid phase, as shown in Fig. S3c. Therefore, the laser fluence of 100~300 mJ/pulse cm2 can be used to prepare different sizes of Ti0.936O2 nanoparticles, and the optimal laser fluence is 300 mJ/pulse cm2.

We further explored the mechanism of the influence of target concentration on the preparation of monodisperse nanocrystals. The results shows that when the concentration of the original Ti0.936O2 particles was increased from 0.05 to 0.2 mg/ml, the laser prepared Ti0.936O2 nanoparticles would gradually change from a well-dispersed state to an agglomerated state, as shown in Fig. S3d, e. The introduction of such agglomerated Ti0.936O2 nanoparticles will keep them in the same agglomerated state in the film, which is not conducive to the preparation of smooth and flat films, and further leads to unsatisfactory interface contact and deterioration of the photoelectric performance of perovskite solar cells. Therefore, our optimal concentration of Ti0.936O2 for embedding of electron transport layer is 0.1 mg/ml.

Fig. S4 Raman spectroscopy of Ti0.936O2 with and without laser irradiation process. Raman spectroscopy of both nanoparticles and nanocrystals of Ti0.936O2 exhibits the same Raman bands at 143 cm-1, 197 cm-1, 397 cm-1, 516 cm-1, 519 cm-1 (overlapping with 516 cm-1) and 638 cm-1. These peaks can be attributed to six Raman-active modes of anatase phase with the symmetries of Eg, Eg, B1g, A1g, B1g and Eg, respectively [S2]

Fig. S5 HAADF and corresponding TEM-EDS images of different size of Ti0.936O2 nanoparticles

Fig. S6 XPS spectra of Ti0.936O2 nanocrystals. Ti 2p peaks at 458.5 eV and 464.4 eV, which are attributed to the chemical states of Ti 2p3/2 and Ti 2p1/2 of Ti4+, respectively. The O 1s peak at 529.8 eV belongs to the Ti4+-O bond, and the O 1s peak at 531.4 eV belongs to the Ti-OH bond [3], which strongly confirms that Ti and O elements exist stably in Ti0.936O2 nanocrystals, and the surface composition and chemical state of Ti0.936O2 do not change significantly after laser irradiation.

Fig. S7 Schematic illustration of embedding of Ti0.936O2 nanocrystals in the TiO2 matrix

Fig. S8 SEM images (inset: AFM images) of a 3%-Target TiO2 and b 9%-Target TiO2 films

Fig. S9 Absorption spectra a of different TiO2 films and corresponding Tauc plots b determining the optical bandgaps of TiO2 films

Fig. S10 Optical transmittance spectra of FTO and different TiO2 films based on FTO

Table S1 The dark I-V plots of different devices show VTFL (the onset voltage of the trap-filled limit region) kink point behavior, it could be extracted to determine the Nt of various ETLs. The Nt of different ETLs was evaluated using Nt=2ε0εVTFLqL2 formula, where ε0 is the vacuum permittivity, ε is the relative dielectric constant, VTFL is the onset voltage of the trap-filled limit region, q is the elemental charge, and L is the thickness of the ETLs [S4]

| ETLs | VTFL (V) | Nt (cm-3) |
| --- | --- | --- |
| Pristine TiO2 | 1.87 | 6.48 × 1016 |
| 6%-Target TiO2 | 0.40 | 1.39 × 1016 |

Fig. S11 Conduction properties of pristine TiO2 and 6%-target TiO2 films measured by a device structure of FTO/ETLs/Ag

Fig. S12 UPS spectra of different TiO2 films

The Fermi level (EF) is calculated by the equation: EF = Ecut-off - 21.22 eV, where Ecut-off represents cut-off binding energy, 21.22 eV is the photon energy of excitation light. The Ecut-off values are extracted to be 16.68 and 17.53 eV for different TiO2 layers. The EF values were calculated to be -4.54 and -3.69 eV for the pristine TiO2 and 6%-target TiO2 layers, respectively. Then the valence band (EVB) is calculated to be -7.42 and -7.34 eV for pristine TiO2 and 6%-target TiO2 layers by using the equation: EVB = EF - EF, edge (Fermi edge). The band gap (Eg) values of TiO2 are obtained from the absorption spectrum and corresponding Tauc plot, showing negligible change of Eg from 3.20 and 3.22 eV for different TiO2 layers. Then the calculated conduction bands (ECB) calculated by Eg and EVB are -4.22 and -4.12 eV for different TiO2 layers, respectively.

Fig. S13 AFM images of CsFAMA perovskite based on a the pristine TiO2 and b 6%-target TiO2 layers

Fig. S14 Cross-sectional SEM images of different devices

Fig. S15 XRD patterns of CsFAMA perovskite upon different TiO2 layers. the improved crystallinity results from gradual increment of intensity for (001) diffraction plane of XRD patterns

Table S2 Summaries of parameters extracted from the fitted plots of the corresponding TRPL spectra following bi-exponential rate law: f(t) = A1exp(-t/τ1 )+A2exp(-t/τ2 )+y0, where A1 and A2 represent the relative amplitudes, τ1 represents trap-assisted recombination, and τ2 represents free carrier recombination. The τave is calculated using τave = ∑Aiτi2∑Aiτi formula [S4]

| ETLs | A1 | τ1 (ns) | A2 | τ2 (ns) | τave (ns) |
| --- | --- | --- | --- | --- | --- |
| Pristine TiO2 | 0.40 | 7.64 | 0.60 | 135.26 | 130.63 |
| 6%-Target TiO2 | 0.35 | 6.00 | 0.65 | 39.92 | 37.38 |

Note S1: AS and Mott-Schottky Analyses

Considering the limitations of the space charge-limited current (SCLC) on defect analysis, temperature dependent admittance spectroscopy (AS) along with Mott-Schottky analysis are adopted to quantitatively analyse both shallow and deep defects in PSCs. According to the previous literature [5], the defect activation energies (Ea) is obtained by the equation:

ω0=βT2exp(-EaKbT)

where ω0is the characteristic transition angular frequency, β is a temperature dependent parameter, T is the temperature and Kbis the Boltzmann’s constant, respectively. The derivative of the capacitance spectrum can be calculated to obtain ω0 from the peak value of the [-ω×dC/dω] curve. The value of Ea can be thus obtained from the slope of the plot using the Arrhenius formula [S5]:

lnω0T2=lnβ-EaKbT

the trap density (Nt) can be obtained according to the equation [S5]:

Nt(Eω)=-VbiqWdCdωωkbT ,   Eω=KbTlnβT2ω

where Vbi is the built-in potential, C is the capacitance, ω is the applied angular frequency, q is the elementary charge, and W is the depletion width, respectively. The values of Vbi and W were extracted from the Mott-Schottky [S5]:

A2C2=2(Vbi-V)qεε0N

where A is the active area, ε is the static permittivity of perovskite, ε0 is the permittivity of free space, N is the apparent doping profile in the depleted layer, and V is the applied bias. The Mott-Schottky plot shows the intersection of a line with the bias axis for obtaining Vbi and the impurity doping density N is extracted from the slope of the line. Then, the depletion width W=2εε0VbiqN that corresponds to the zero bias can be calculated, the distribution of trap state density can be further obtained. Fig. S16a, b show the capacitance-frequency (C-f) curves of the devices upon different ETLs, which were measured at temperatures ranging from 210 to 320 K under the dark. The defect activation energies (Ea) of different devices are extracted from the corresponding Arrhenius plots that depicts the relationship between the characteristic transition frequencies and temperatures (Fig. 2e), which are calculated to be 0.277 and 0.223 eV, respectively. The built-in potential (Vbi) and the depletion width (W) are derived from the Mott-Schottky, which were measured at a frequency of 1 kHz with bias potential from 0 to 1.2 V (Fig. S16c). The Vbi are determined to be 0.90 and 0.99 V for the control and the target, respectively, and the depletion widths are calculated to be 183 and 285 nm, respectively. The density distribution and energy levels of trap states of different devices are then showed in Fig. 2f.

Fig. S16 Admittance spectra of devices based on a pristine TiO2 and b 6%-target TiO2 ETLs were measured at gradient temperatures ranging from 210 to 320 K with a step of 15 K under the dark. c Mott-Schottky analysis at 1 kHz for obtaining the Vbi

Fig. S17 Dark current density-voltage plots of devices based on different TiO2 layers

Table S3 Summaries of parameters extracted from the fitted plots of the impedance spectra of devices upon differnent ETLs using a the equivalent circuit model

| ETLs | Rs (Ω) | Rco (Ω) | CPE1-T (F) | CPE1-P (F) | Rrec (Ω) | CPE2-T (F) | CPE2-P (F) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Pristine TiO2 | 15.55 | 16544 | 5.16E-09 | 0.98 | 1.05E05 | 1.45E-06 | 0.81 |
| 6%-Target TiO2 | 7.65 | 12300 | 6.28E-09 | 0.97 | 1.64E05 | 1.27E-06 | 0.80 |

Fig. S18 Schematic illustration of fabrication process of perovskite devices with Ti0.936O2@TiO2 ETLs

Table S4 The Photovoltaic parameters of champion devices with and without defected TiO2 nanocrystals embedding under forward and reverse scanning

| Scanning direction | VOC (V) | JSC (mA/cm2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- |
| Forward control | 1.133 | 22.97 | 66.55 | 17.32 |
| Reverse control | 1.149 | 23.16 | 74.93 | 19.94 |
| Forward Target | 1.167 | 23.77 | 78.24 | 21.70 |
| Reverse Target | 1.194 | 23.72 | 77.75 | 22.02 |

Fig. S19 Cross-sectional SEM images of control FAPbI3 a and target FAPbI3 b devices, respectively. Scale Bar: 1μm

Fig. S20 SEM images of FAPbI3 perovskite based on the pristine TiO2 a and target TiO2 b layers. Scale bars: 2 µm

Fig. S21 AFM images of FAPbI3 perovskite based on a the pristine TiO2 and b 6%-target TiO2 layers. Scale bars: 1 µm

Fig. S22 XRD patterns of FAPbI3 perovskite upon different TiO2 layers

Fig. S23 PL a and TRPL b spectra of FAPbI3 perovskite based on the pristine TiO2 and target TiO2 layers

Table S5 Summaries of fitting parameters for TRPL spectra with a structure of FAPbI3/TiO2 (with and without defected TiO2 nanocrystals)/FTO substrates

| Samples | A1 | Ʈ1 (ns) | A2 | Ʈ2 (ns) | Ʈave (ns) |
| --- | --- | --- | --- | --- | --- |
| FAPbI3 | 0.25 | 204.80 | 0.75 | 1311.17 | 1256.42 |
| Target FAPbI3 | 0.21 | 154.90 | 0.79 | 845.45 | 813.38 |

Fig. S24 The Tauc plot of FAPbI3 film for obtaining bandgap

Fig. S25 Statistical distributions of the photovoltaic parameters of Voc, Jsc and FF for CsFAMA devices with different TiO2 layers. The average PCE improves from 18.28% to 21.22%, as shown in Figure 3e, with Voc from 1.147 to 1.192 V, the average Jsc from 22.41 to 23.93 mA/cm2, and the FF from 73.88 to 77.93%

Fig. S26 Statistical distributions of the photovoltaic parameters of Voc, Jsc and FF for FAPbI3 devices based on different TiO2 layers. The average PCE increases from 21.24% to 23.52%, with Voc from 1.074 to 1.125 V, the average Jsc from 25.10 to 25.86 mA/cm2, and the FF from 79.23 to 81.92%

Table S6 Reported values for the efficiency of different PSCs based on TiO2 ETLs

| Type | Device structure | Best PCE (%) | Refs. |
| --- | --- | --- | --- |
| [BMIM]BF4 | FTO/TiO2/[BMIM]BF4/MAPbI3/PTAA/Au | 19.62 | [S6] |
| GQD | FTO/TiO2@GQD/MAPbI3/Spiro- OMeTAD/Au | 19.11 | [S7] |
| CuI | FTO/TiO2@CuI/CsFAMA/Spiro-OMeTAD/Au | 19.00 | [S8] |
| Heparin sodium | FTO/TiO2/heparin sodium/MAPbI3/Spiro-OMeTAD/Au | 20.1 | [S9] |
| Dopamine | FTO/Dopamine-TiO2/Cs0.05FA0.81MA0.14PbI2.55Br0.45/Spiro-OMeTAD/Au | 20.93 | [S10] |
| Urea | ITO/TiO2-urea/Cs0.05(FA0.87MA0.13)0.95PbI2.55Br0.45/Spiro-OMeTAD/Au | 21.33 | [S11] |
| Boron | FTO/Boron-TiO2/ MAPbI3/Spiro- OMeTAD/Au | 20.51 | [S12] |
| Li2CO3 | FTO/Li2CO3-TiO2/FAPbI3/Spiro- OMeTAD/Au | 25.28 | [S13] |
| TiOxNy | FTO/TiOxNy/TiO2/PMMA:PCBM/ Cs0.05FA0.88MA0.07PbI2.56Br0.44/PMMA/P3HT:CuPC/Au | 23.28 (1cm2) | [S14] |
| Single-crystalline TiO2 | FTO/Single-crystalline TiO2/ Rb0.03Cs0.05MA0.05FA0.9PbI3/Spiro- OMeTAD/Au | 24.05 | [S15] |
| Tartaric acid | FTO/tartaric acid-TiO2/FAMAPbI3/Spiro-OMeTAD/Au | 24.81 | [S16] |
| C-PCBA | FTO/TiO2/C-PCBA/CsFAPb(IBr)3/Spiro-OMeTAD/Au | 24.80 | [S17] |
| CdTe nanocrystals | FTO/TiO2@CdTe/Cs0.05(FA0.85MA0.15)0.95PbI2.55Br0.45/Spiro-OMeTAD/Au | 22.00 | [S4] |
| CdTe nanocrystals | FTO/TiO2@CdTe/FAPbI3/Spiro-OMeTAD/Au | 25.05 | [S4] |
| Ti0.936O2 | FTO/TiO2@ Ti0.936O2/Cs0.05(FA0.85MA0.15)0.95PbI2.55Br0.45/Spiro-OMeTAD/Au | 22.02 | Our present work |
| Ti0.936O2 | FTO/TiO2@ Ti0.936O2/FAPbI3/Spiro-OMeTAD/Au | 25.50 | Our present work |

Fig. S27 UPS Fermi edge a and the cut-off energy b of CsFAMA perovskite film. The calculation of the EF, EVB and ECB of CsFAMA-based perovskite film are -4.35, -5.70 and -4.10 eV

Fig. S28 The long-term thermal stability of CsFAMA-based devices with and without Ti0.936O2 nanocrystals embedding. The excellent thermal stability of target devices presents PCE degradation of less than 30% over 500 h in contrast with that of control devices (over 60%) after continuous thermal treatment of 85 °C. The error bars represent the standard deviation for 20 devices.

Fig. S29 Schematic illustration of the effects of embedding Ti0.936O2 nanocrystals on crystallization kinetics and light-induced stability

Fig. S30 J-V curves of the champion FAPbI3 devices employing 6%-Target TiO2 layers measured both in reverse scan and forward scan

Table S7 Performance parameters of champion FAPbI3 devices employing 6%-Target TiO2 layers measured both in reverse scan and forward scan

| Scanning direction | Voc (V) | Jsc (mA/cm2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- |
| Reverse 6%-Target TiO2 | 1.185 | 25.79 | 83.45 | 25.50 |
| Forward 6%-Target TiO2 | 1.183 | 25.68 | 82.43 | 25.04 |

The hysteresis index is calculated to be 0.018 according the equation below:

Hysteresis index = (PCEReverse-PCEForward)/ PCEReverse

Supplementary References

- H. Yu, W. Zhao, L. Ren, H. Wang, P. Guo et al., Laser-generated supranano liquid metal as efficient electron mediator in hybrid perovskite solar cells. Adv. Mater. 32, e2001571 (2020). https://doi.org/10.1002/adma.202001571

- J. Zhang, M. Li, Z. Feng, J. Chen, C. Li UV Raman spectroscopic study on TiO2. I. phase transformation at the surface and in the bulk. J. Phys. Chem. B 110, 927–935 (2006). https://doi.org/10.1021/jp0552473

- S. Wang, L. Pan, J.-J. Song, W. Mi, J.-J. Zou et al., Titanium-defected undoped anatase TiO2 with p-type conductivity, room-temperature ferromagnetism, and remarkable photocatalytic performance. J. Am. Chem. Soc. 137, 2975–2983 (2015). https://doi.org/10.1021/ja512047k

- W. Zhao, P. Guo, C. Liu, N. Jia, Z. Fang et al., Laser derived electron transport layers with embedded p-n heterointerfaces enabling planar perovskite solar cells with efficiency over 25. Adv. Mater. 35, e2300403 (2023). https://doi.org/10.1002/adma.202300403

- N. Li, S. Tao, Y. Chen, X. Niu, C.K. Onwudinanti et al., Cation and anion immobilization through chemical bonding enhancement with fluorides for stable halide perovskite solar cells. Nat. Energy 4, 408–415 (2019). https://doi.org/10.1038/s41560-019-0382-6

- D. Yang, X. Zhou, R. Yang, Z. Yang, W. Yu et al., Surface optimization to eliminate hysteresis for record efficiency planar perovskite solar cells. Energy Environ. Sci. 9, 3071–3078 (2016). https://doi.org/10.1039/C6EE02139E

- J. Ryu, J.W. Lee, H. Yu, J. Yun, K. Lee et al., Size effects of a graphene quantum dot modified-blocking TiO2 layer for efficient planar perovskite solar cells. J. Mater. Chem. A 5, 16834–16842 (2017). https://doi.org/10.1039/C7TA02242E

- M.M. Byranvand, T. Kim, S. Song, G. Kang, S.U. Ryu et al., P-type CuI islands on TiO2 electron transport layer for a highly efficient planar-perovskite solar cell with negligible hysteresis. Adv. Energy Mater. 8, 1702235 (2018). https://doi.org/10.1002/aenm.201702235

- S. You, H. Wang, S. Bi, J. Zhou, L. Qin et al., A biopolymer heparin sodium interlayer anchoring TiO2 and MAPbI3 enhances trap passivation and device stability in perovskite solar cells. Adv. Mater. 30, e1706924 (2018). https://doi.org/10.1002/adma.201706924

- Y. Zhang, X. Liu, P. Li, Y. Duan, X. Hu et al., Dopamine-crosslinked TiO2/perovskite layer for efficient and photostable perovskite solar cells under full spectral continuous illumination. Nano Energy 56, 733–740 (2019). https://doi.org/10.1016/j.nanoen.2018.11.068

- W. Hu, W. Zhou, X. Lei, P. Zhou, M. Zhang et al., Low-temperature in situ amino functionalization of TiO2 nanoparticles sharpens electron management achieving over 21% efficient planar perovskite solar cells. Adv. Mater. 31, 1806095 (2019). https://doi.org/10.1002/adma.201806095

- X. Shi, Y. Ding, S. Zhou, B. Zhang, M. Cai et al., Enhanced interfacial binding and electron extraction using boron-doped TiO2 for highly efficient hysteresis-free perovskite solar cells. Adv. Sci. 6, 1901213 (2019). https://doi.org/10.1002/advs.201901213

- M. Kim, I.-W. Choi, S.J. Choi, J.W. Song, S.-I. Mo et al., Enhanced electrical properties of Li-salts doped mesoporous TiO2 in perovskite solar cells. Joule 5, 659–672 (2021). https://doi.org/10.1016/j.joule.2021.02.007

- J. Peng, F. Kremer, D. Walter, Y. Wu, Y. Ji et al., Centimetre-scale perovskite solar cells with fill factors of more than 86 per cent. Nature 601, 573–578 (2022). https://doi.org/10.1038/s41586-021-04216-5

- Y. Ding, B. Ding, H. Kanda, O.J. Usiobo, T. Gallet et al., Single-crystalline TiO2 nanoparticles for stable and efficient perovskite modules. Nat. Nanotechnol. 17, 598–605 (2022). https://doi.org/10.1038/s41565-022-01108-1

- H. Huang, P. Cui, Y. Chen, L. Yan, X. Yue et al., 24.8%-efficient planar perovskite solar cells via ligand-engineered TiO2 deposition. Joule 6, 2186–2202 (2022). https://doi.org/10.1016/j.joule.2022.07.004

- Z. Chen, Y. Li, Z. Liu, J. Shi, B. Yu et al., Reconfiguration toward self-assembled monolayer passivation for high-performance perovskite solar cells. Adv. Energy Mater. 13, 2202799 (2023). https://doi.org/10.1002/aenm.202202799