Supporting Information for

Approaching Ultimate Synthesis Reaction Rate of Ni-Rich Layered Cathodes for Lithium-Ion Batteries

Zhedong Liu1, Jingchao Zhang1, Jiawei Luo1, Zhaoxin Guo1, Haoran Jiang1, Zekun Li1, Yuhang Liu1, Zijing Song1, Rui Liu2, Wei-Di Liu3, Wenbin Hu1, *, Yanan Chen1, *

# 1 School of Materials Science and Engineering, Tianjin University, Tianjin 300072, P. R. China

2 School of Materials Science and Engineering, Shandong University of Science and Technology, Qingdao 266590, P. R. China

3Australian Institute of Bioengineering and Nanotechnology, The University of Queensland, St Lucia, QLD, Australia 4072

*Corresponding authors. E-mail: yananchen@tju.edu.cn (Yanan Chen); wbhu@tju.edu.cn (Wenbin Hu)

Supplementary Figures and Tables

Fig. S1 (a) Ex situ XRD patterns evolution of NCM523 in the HTS process at 900 ℃. (b) Evolution of the cationic disordering

Fig. S2 (a) Ex situ XRD patterns evolution of NCM811 in the HTS process at 800 ℃. (b) Evolution of the cationic disordering

Fig. S3 Evolution of lattice parameters a, c and the c/a ratio with holding time during synthesis of NCM622 at 900 ºC

Fig. S4 Evolution of lattice parameters a, c and the c/a ratio with holding time during synthesis of NCM523 at 900 ºC

Fig. S5 Evolution of lattice parameters a, c and the c/a ratio with holding time during synthesis of NCM811 at 800 ºC

Fig. S6 (a) Refined X-ray diffraction pattern of NCM523 sample (900 °C 90 s) and NCM811 sample (800 °C 210 s). (b) Rietveld refinements based on layered phase were carried out and the samples consist of the layered R3m (Li–TM–O2)

Fig. S7 (a) The calcination temperature curve of NCM622 at 900 °C for 90 s. (b) SEM images of NCM622 samples sintered under the conditions of (c) 900 ℃-0 s, (d) 10 s, (e) 20s, (f) 60 s, (g) 90 s and (h) 120 s, scale bar, 1 μm

Fig. S8 (a) SEM images of NCM622 at 900 °C for 90 s, scale bar, 1 μm. (b, c) FIB images, scale bar, 500 nm. (d) Enlarged image of internal morphology of the particles, scale bar, 200 nm

Fig. S9 (a), (a-1) SEM images of precursors, scale bar, 5 μm, 1 μm and (b), (b-1) NCM523 samples sintered under the condition of 900 ℃-90 s, scale bar, 5 μm, 1 μm

Fig. S10 (a), (a-1) SEM images of precursors, scale bar, 20 μm, 1 μm and (b), (b-1) NCM811 samples sintered under the condition of 800 ℃-210 s, scale bar, 20 μm, 1 μm

Fig. S11 N2 adsorption and desorption curves of HTS-NCM622 and TF-NCM622

Fig. S12 TEM image for NCM523 (900 °C 90 s) sample, scale bar, 2 nm. The inset images are the fast Fourier transform pattern for the TEM image, scale bar, 2 μm

Fig. S13 TEM image for NCM811 (800 °C 210 s) sample, scale bar, 10 nm. The inset images are the fast Fourier transform pattern for the TEM image, scale bar, 10 μm

Fig. S14 (a) FIB-image of NCM622 samples, scale bar, 1 μm. (b) Enlarged image of internal morphology of the particles, scale bar, 200 nm. (c) EELS-Mapping of lithium, scale bar, 200 nm

Fig. S15 Initial charge and discharge voltage profiles of LiNixCoyMnzO2 at 45℃, 2.8–4.3 V

Fig. S16 Cycle performances at 45 °C, 2.8-4.3V for the NCM523, NCM622, and NCM811 cathodes obtained using 2032-type coin cells with Li metal as a counter electrode. The cyclic performances of traditional methods are in contrast. (1C = 200 mA g−1)

Fig. S17 Initial charge and discharge voltage profiles of LiNixCoyMnzO2 at 30 ℃, 2.8–4.5 V

Fig. S18 Cycle performances at 30 °C, 2.8-4.5V for the NCM523, NCM622, and NCM811 cathodes obtained using 2032-type coin cells with Li metal as a counter electrode. The cyclic performances of traditional methods are in contrast. (1C = 200 mA g−1)

Table S1 Chemical compositions of the rapid synthesized NCM523, NCM622, NCM811 cathodes

| Sample | ICP-AES (wt%) |  |  |  |
| --- | --- | --- | --- | --- |
|  | Li | Ni | Co | Mn |
| NCM523 | 7.19 | 30.39 | 12.21 | 17.99 |
| NCM622 | 7.16 | 36.33 | 12.16 | 11.94 |
| NCM811 | 7.13 | 48.27 | 6.06 | 5.95 |
| Sample | Measured molar ration |  |  |  |
|  | Li | Ni | Co | Mn |
| NCM523 | 1.036 | 0.492 | 0.197 | 0.311 |
| NCM622 | 1.032 | 0.594 | 0.198 | 0.208 |
| NCM811 | 1.027 | 0.796 | 0.099 | 0.105 |

Table S2 Structural characteristics were determined from the Rietveld-refined XRD results at different temperatures following the heating profiles of fast synthesis of NCM622

| Material | a (Å) | c (Å) | c/a |
| --- | --- | --- | --- |
| precursor | 3.0543 | 4.5660 | 1.494 |
| 300℃ | 3.0510 | 4.5689 | 1.497 |
| 500℃ | 3.0482 | 4.5793 | 1.502 |
| 700℃ | 2.8983 | 14.2812 | 4.927 |
| 900℃ | 2.8855 | 14.2285 | 4.931 |

Table S3 The specific surface area test results

|  | HTS-NCM622 | TF-NCM622 |
| --- | --- | --- |
| BET (m2/g) | 0.7797 | 0.8125 |

Table S4 Comparison of cycling stability of LiNixCoyMnzO2 cathodes with the Ni-rich based cathodes reported before for half cells at 30 ℃

| Sample | 1st capacity (mAh g-1) | Retention | References |
| --- | --- | --- | --- |
| NCM523 | 172 | 94%（2.8-4.3V, 1C, 200 cycles） | This work |
| NCM622 | 181 | 94%（2.8-4.3V, 1C, 200 cycles） | This work |
| NCM811 | 195 | 80%（2.8-4.3V, 1C, 200 cycles） | This work |
| NCM523 | 173 | 96.9%（3-4.3V, 0.5C, 100 cycles） | [S1] |
| NCM622 | 185 | 94%（3-4.3V, 0.5C, 100 cycles） |  |
| NCM811 | 204 | 81%（3-4.3V, 0.5C, 100 cycles） |  |
| SrCO3-NCM523 | 163 | 90%（2.8-4.3V, 1C, 100 cycles） | [S2] |
| ZrB2-NCM811 | 202 | 90%（3-4.3V, 1C, 100 cycles） | [S3] |
| RHSNCM523 | 155(0.5C) | 92%（2.5-4.3V, 0.5C, 100 cycles） | [S4] |
| RHSNCM622 | 167(0.5C) | 90%（2.5-4.3V, 0.5C, 100 cycles） |  |
| Li2BO3flux-NCM523 | 175 | 80%（2.8-4.3V, 1C, 100 cycles） | [S5] |
| NCM523-IE200-PL800 | 170.3 | 86.2%（2.7-4.3V, 1C, 200 cycles） | [S6] |
| NCM811-BE-LiHMDS | 182(0.5C) | 73.9%（3.0-4.5V, 0.5C, 1000 cycles） | [S7] |
| NCM811-FETT | 200(0.5C) | 68%（3.0-4.6V, 0.5C, 150 cycles） | [S8] |
| NCM811 | 195.2 | 72.4%（2.7-4.3V, 0.5C, 200 cycles） | [S9] |

Supplementary References

- H.-J. Noh, S. Youn, C. S. Yoon, Y.-K. Sun, Comparison of the structural and electrochemical properties of layered Li[NixCoyMnz]O2 (x=1/3, 0.5, 0.6, 0.7, 0.8 and 0.85) cathode material for lithium-ion batteries. J. Power Sources 233, 121-130 (2013). https://doi.org/10.1016/j.jpowsour.2013.01.063

- G. Hu, L. Li, Y. Lu, Y. Cao, Z. Peng et al., SrCO3 assisted synthesis of disk-like micron-sized monocrystalline LiNi0.5Co0.2Mn0.3O2 with Preferred (104) plane and its enhanced cycle performance. J. Electrochem. Soc. 167, (2020). https://doi.org/10.1149/1945-7111/abc032

- Z. Feng, R. Rajagopalan, S. Zhang, D. Sun, Y. Tang et al., A three in one strategy to achieve zirconium doping, boron doping, and interfacial coating for stable LiNi(0.8)Co(0.1)Mn(0.1)O(2) Cathode. Adv. Sci. 8, 2001809 (2021). https://doi.org/10.1002/advs.202001809

- K. Jia, J. Wang, Z. Zhuang, Z. Piao, M. Zhang et al., Topotactic Transformation of Surface Structure Enabling Direct Regeneration of Spent Lithium-Ion Battery Cathodes. J. Am. Chem. Soc. 145, 7288-7300 (2023). https://doi.org/10.1021/jacs.2c13151

- T. Yamada, K. Shishino, Y. Doya, K. Fujisawa, K. Teshima, Individual effects of flux species as a reaction field on coprecipitation precursor toward the design of fine, mono-dispersed LiNi0.5Co0.2Mn0.3O2 single crystals. ACS Appl. Energy Mater. 6, 245-256 (2022). https://doi.org/10.1021/acsaem.2c02884

- Y.-h. Luo, Q.-l. Pan, H.-x. Wei, Y.-d. Huang, L.-b. Tang et al., Regulating cation mixing for enhanced structural stability of layered oxide cathodes by ion-exchange strategy. Mater. Today 69, 54-65 (2023). https://doi.org/10.1016/j.mattod.2023.08.006

- J. Huang, Y. Yang, Y. Liu, J. Ma, Lithium Hexamethyldisilazide Endows Li||NCM811 Battery with Superior Performance. Nano-Micro Lett. 15, 33 (2023). https://doi.org/10.1007/s40820-022-00998-z

- J. Liu, X. Li, J. Huang, G. Yang, J. Ma, Additive‐guided solvation-regulated flame-retardant electrolyte enables high-voltage lithium metal batteries with robust electrode electrolyte interphases. Adv. Funct. Mater. 2312762 (2024). https://doi.org/10.1002/adfm.202312762

- Y. Han, Y. Zhang, Y. Lei, D. Xiao, J. Ni et al., Regulating cathode-electrolyte interphase by confining functional aluminum compound within Ni-rich cathodes. Adv. Funct. Mater. 33, 2301642 (2023). https://doi.org/10.1002/adfm.202301642