Supporting Information for

Photo-Energized MoS2/CNT Cathode for High Performance Li–CO2 Batteries in a Wide Temperature Range

Tingsong Hu1, Wenyi Lian1, Kang Hu1, Qiuju Li1, Xueliang Cui1, Tengyu Yao1, Laifa Shen1,*

1Jiangsu Key Laboratory of Materials and Technologies for Energy Storage, College of Materials Science and Technology, Nanjing University of Aeronautics and Astronautics, Nanjing 210016, People’s Republic of China.

*Corresponding author. E-mail: lfshen@nuaa.edu.cn (Laifa Shen)

Supplementary Fiures and Tables

Fig. S1 Representations of the design of MoS2/CNT

Fig. S2 Scanning electron microscopy image of pristine CNT

Fig. S3 Raman spectra of CNT and MoS2/CNT cathode

Fig. S4 X-ray photoelectron spectroscopy image of (a) Mo and (b) S in MoS2/CNT cathode

Fig. S5 Partial Density of States of Mo and S in (a) MoS2/CNT or (b) MoS2

Fig. S6 Tauc plot corresponding to UV-vis absorption of MoS2/CNT

Fig. S7 Time-resolved transient photoluminescence decay spectra of MoS2 and MoS2/CNT

First-principles calculations were carried out using density functional theory (DFT) to calculate the kinetic processes under light and no light. According to the intensity value of the Ultraviolet curing lamp in the experiment, the applied electric field component for computation could be calculated by the following equations. According to the intensity value of the Ultraviolet curing lamp in the experiment, the applied electric field component for computation could be calculated by the following equations.

Z0 = μ0c                      (S1)

H0 = (2S/Z0)1/2                 (S2)

E0 = (2Z0S)1/2                  (S3)

Where Z0 is the impedance of free space, μ0 is the permeability of vacuum (μ0= 4π×10-7 H/m), c is the light speed (c = 3×108 m/s), S is the electromagnetic wave intensity (S = 42 mW/cm2, the intensity of Ultraviolet lamp), H0 is the magnetic field intensity, and E0 is the electric field intensity. The incident electric field component was calculated to be 563 V/m. To facilitate the subsequent calculation process, the electric field intensity applied in the computation was 600 V/m.

Table S1 Reaction path and energy changes during the charging process

| Reaction path(charge) | Reaction equation | No lighting (eV) | Lighting (eV) |
| --- | --- | --- | --- |
| a1 | *Li2CO3 + C = *LiCO3 + C + Li | 4.6250 | 4.3285 |
| a2 | *LiCO3 + C = *CO3 + C + Li | 2.9887 | 2.8845 |
| a3 | *CO3 + C = *CO + CO2 | -6.4143 | -6.2816 |
| a4 | *Li2CO3 + CO = *LiCO3 + CO + Li | 4.5535 | 4.3064 |
| a5 | *LiCO3 + CO + Li = *LiCO2 + Li + CO2 | -1.8243 | -1.8366 |
| a6 | *LiCO2 + Li + CO2 = *Li + Li + 2CO2 | -0.8993 | -0.8575 |
| a7 | *Li + Li + 2CO2 = * + 2Li + 2CO2 | 1.4534 | 1.5423 |

Table S2 Reaction path and energy changes during the discharge process

| Reaction path(discharge) | Reaction equation | No lighting (eV) | Lighting (eV) |
| --- | --- | --- | --- |
| b1 | * + 2Li + 2CO2 = *Li + Li + 2CO2 | -1.4534 | -1.5423 |
| b2 | *Li + Li + 2CO2 = *LiCO2 + Li + CO2 | 0.8993 | 0.8575 |
| b3 | *LiCO2 + Li + CO2 = *LiCO3 + CO + Li | 1.8243 | 1.8366 |
| b4 | *LiCO3 + CO + Li = *Li2CO3 + CO | -4.5535 | -4.3064 |
| b5 | *CO + CO2 = *CO3 + C | 6.4143 | 6.2816 |
| b6 | *CO3 + C + Li = *LiCO3 + C | -2.9887 | -2.8845 |
| b7 | *LiCO3 + C + Li = *Li2CO3 + C | -4.6250 | -4.3285 |

Fig. S8 (a) Charging reaction path with MoS2 under lighting and no lighting. (b) Rate-determining step in charging reaction. (c) Discharge reaction path with MoS2 under lighting and no lighting. (d) Rate-determining step in discharge reaction

Fig. S9 Cyclic voltammetry curves of Li–CO2 batteries with MoS2/CNT cathode in Ar or CO2 atmosphere at 1 mV s–1

Fig. S10 (a) Linear sweep voltammetry curves in CO2 oxidation process at 5 mV s–1 and (b) corresponding Tafel curves of Li–CO2 battery with MoS2/CNT cathode in the presence and absence of illumination

Fig. S11 Galvanostatic intermittent titration spectra during charge of Li–CO2 battery with MoS2/CNT cathode with or without illumination

Fig. S12 Differential electrochemical mass spectrometry results of discharge process (a) with and (b) without illumination in Li–CO2 battery with MoS2/CNT cathode. DEMS results of recharge process (c) with and (d) without illumination in Li–CO2 battery with MoS2/CNT cathode

Fig. S13 Discharge and charge curves of the Li–CO2 battery based on the MoS2/CNT cathode without illumination at different current density

Fig. S14 Scanning electron microscopy image of MoS2/CNT cathode collected from full-discharge Li–CO2 battery (a) with or (b) without illumination

Fig. S15 Comparison of energy efficiency and cycle performance of Li–O2 and Li–CO2 batteries with the state-of-the-art cases reported in the literature

Fig. S16 (a) Nyquist plots and (b) ionic conductivity at different temperatures (TEGEDME with 1.0 M LiTFSI is used as electrolyte)

Fig. S17 Schematic diagram of temperature gradient of Li–CO2 battery with MoS2/CNT cathode with illumination at –30 oC, without illumination at –30 oC, and without illumination at –12 oC

Fig. S18 Comparison of energy efficiency with different electrolytes (conventional electrolytes, cryo-electrolytes and solid electrolytes) at low temperature

Fig. S19 Cyclic voltammetry curves of Li–CO2 battery with MoS2/CNT cathode with illumination at –30 oC, without illumination at –30 oC, and without illumination at –12 oC

Fig. S20 Discharge/charge behaviors responding to the Li–CO2 battery with illumination at –30 oC and without illumination at –12 oC

Fig. S21 (a) Linear sweep voltammetry curves in CO2 oxidation process and (b) Corresponding Tafel curves of Li–CO2 battery with MoS2/CNT cathode with illumination at –30 oC, without illumination at –30 oC, and without illumination at –12 oC

Fig. S22 Cycling profiles at 0.01 mA cm–1 of Li–CO2 battery with MoS2/CNT cathode with illumination at –30 oC, without illumination at –30 oC, and without illumination at –12 oC

Fig. S23 (a) Discharge rate capability and (b) Charge rate capability of Li–CO2 battery with MoS2/CNT cathode with illumination at –30 oC and without illumination at –12 oC