Supporting Information for

Crystallization Modulation and Holistic Passivation Enables Efficient Two-Terminal Perovskite/CuIn(Ga)Se2 Tandem Solar Cells

Cong Geng1, Kuanxiang Zhang2, Changhua Wang2, Chung Hsien Wu2, Jiwen Jiang2, Fei Long3, Liyuan Han4,*, Qifeng Han4, Yi-Bing Cheng1, and Yong Peng1,*

1 State Key Laboratory of Advanced Technology for Materials Synthesis and Processing, Wuhan University of Technology, Wuhan 430070, P. R. China

2 Triumph Photovoltaic Materials Co., Ltd. No.1001 Yannan Avenue, High-Tech Development District, Bengbu, Anhui, P. R. China

3 College of Materials Science and Engineering, Guilin University of Technology, Guilin 541004, P. R. China

4 State Key Laboratory of Metal Matrix Composites, Shanghai Jiao Tong University, Shanghai 200240, P. R. China

*Corresponding authors. E-mail: yongpeng@whut.edu.cn (Yong Peng); han.liyuan@sjtu.edu.cn (Liyuan Han)

Supplementary Figures and Tables

Fig. S1 5 µm × 5 µm AFM topography of surface PVK thin-film as-grown on CIGS

Fig. S2 a-d Photo-voltaic (PV) parameter statistics of the control, D-HLH-treated, LiF-treated, and 2-TEAI-treated, and 2-TEAI/LiF-treated PSCs

Fig. S3 XRD intensity evolution for (100) crystal plane at 2θ = 14.00° during the annealing process

Fig. S4 13C NMR spectra of D-HLH and D-HLH/FAI

Fig. S5 XPS spectra of a Pb 4f, b I 3d, and c N 1s of the control and D-HLH-tread films

Fig. S6 PLQY of the perovskite films on a ITO/SAM/PVK stack, and b ITO/SAM/PVK/passivation layer/C60 stack

The PLQY, which is directly related to the QFLS under the presumption that all PL emission results from the radiative recombination of free charges in perovskite film, can be represented by the following equation.

QFLS=KBTIn(PLQY×JGJ0,rad)

where KB, and T represent Boltzmann constant and temperature, respectively. JG is the current density under illumination, and J0,rad is the dark radiative recombination saturation current density.

The following equations can be used to calculate the in accordance with the detailed balance theory:

J0,rad=q0∞EQEPVE∅BBEdE

∅BBE=2πE2h3c21expEKBT-1

Where q, EQEPV, ∅BB , E, h, c represents elementary charge, photovoltaic external quantum efficiency, black-body radiative spectrum, photon energy, Planck constant, and light speed in vacuum, respectively.

Fig. S7 Steady-state PL spectra of the PVK films

Fig. S8 Transient PL spectra of the glass/PVK/passivation layer /C60 stacks

Fig. S9 Schematic of the device layout used in the fabrication of the 2T PVK/CIGS TSCs. The final aperture area of 0.16 cm2 is defined by a black shadow mask used during J-V measurements

Fig. S10 Cross-section SEM images the PVK/CIGS tandem solar cells. (Scale bar: 10 μm)

Fig. S11 PV parameter statistics of PVK/CIGS tandem solar cells without NiOx

Fig. S12 a-d PV parameter statistics of the control, D-HLH-treated, LiF-treated, and 2-TEAI-treated, and 2-TEAI/LiF-treated PVK/CIGS tandem solar. cells

Fig. S13 The stability of three unencapsulated tandem devices in nitrogen and air (30-50% RH) environment

Table S1 Summary of 2-T PVK/CIGS tandem solar cells

| Year | Perovskite | Voc (V) | Jsc (mA / cm2) | FF (%) | PCE (%) | area (cm2) | Refs. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2015 | MAPbIBr | 1.45 | 12.7 | 56.6 | 10.9 | 0.4 | [S1] |
| 2017 | MAPbI3 | 1.346 | 12.9 | 63.5 | 11.03 | 0.5 | [S2] |
| 2018 | Cs0.09FA0.77MA0.14Pb(I0.86Br0.14)3 | 1.774 | 17.3 | 73.1 | 22.43 | 0.52 | [S3] |
| 2019 | Cs0.05(MA0.17FA0.83)0.95Pb(I0.83Br0.17)3 | 1.58 | 18 | 76 | 21.6 | 0.78 | [S4] |
| 2019 | Cs0.05(MA0.17FA0.83)0.95Pb(I0.83Br0.17)3 | 1.68 | 19.17 | 71.9 | 23.26 | 1.03 | [S5] |
| 2022 | Cs0.05(MA0.23FA0.77)Pb1.1(I0.77Br0.23)3 | 1.77 | 18.8 | 71.2 | 24.2 | 1.04 | [S6] |
| 2022 | Cs0.05MA0.1FA0.85Pb(I0.9Br0.1)3 | 1.59 | 19.4 | 75.5 | 23.5 | 0.5 | [S7] |
| 2024 | Cs0.05(MA0.17FA0.83)0.95Pb(I0.83Br0.17)3 | 1.742 | 20.97 | 67.3 | 24.6 | 0.16 | This Wok |

Supplementary References

- T. Todorov, T. Gershon, O. Gunawan, Y. S. Lee, C. Sturdevant et al., Monolithic perovskite-cigs tandem solar cells via in situ band gap engineering. Adv. Energy Mater. 5(23), 1500799 (2015). https://doi.org/10.1002/aenm.201500799

- Y. H. Jang, J. M. Lee, J. W. Seo, I. Kim, D.-K. Lee, Monolithic tandem solar cells comprising electrodeposited CuInSe2 and perovskite solar cells with a nanoparticulate zno buffer layer. J. Mater. Chem. A 5(36), 19439-19446 (2017). https://doi.org/10.1039/C7TA06163C

- Q. Han, Y.-T. Hsieh, L. Meng, J.-L. Wu, P. Sun et al., High-performance perovskite/Cu(In,Ga)Se2 monolithic tandem solar cells. Science 361(6405), 904-908 (2018). https://doi.org/10.1126/science.aat5055

- M. Jošt, T. Bertram, D. Koushik, J. A. Marquez, M. A. Verheijen et al., 21.6%-efficient monolithic perovskite/Cu(In,Ga)Se2 tandem solar cells with thin conformal hole transport layers for integration on rough bottom cell surfaces. ACS Energy Lett. 4(2), 583-590 (2019). https://doi.org/10.1021/acsenergylett.9b00135

- A. Al-Ashouri, A. Magomedov, M. Roß, M. Jošt, M. Talaikis et al., Conformal monolayer contacts with lossless interfaces for perovskite single junction and monolithic tandem solar cells. Energy Environ. Sci. 12(11), 3356-3369 (2019). https://doi.org/10.1039/C9EE02268F

- M. Jošt, E. Köhnen, A. Al-Ashouri, T. Bertram, Š. Tomšičet al., Perovskite/cigs tandem solar cells: From certified 24.2% toward 30% and beyond. ACS Energy Lett. 7(4), 1298-1307 (2022). https://doi.org/10.1021/acsenergylett.2c00274

- M. A. Ruiz-Preciado, F. Gota, P. Fassl, I. M. Hossain, R. Singh et al., Monolithic two-terminal perovskite/cis tandem solar cells with efficiency approaching 25%. ACS Energy Lett. 7(7), 2273-2281 (2022). https://doi.org/ https://doi.org/10.1021/acsenergylett.2c00707