Supporting Information for

Carbon Nanofiber/Polyaniline Composite Aerogel with Excellent Electromagnetic Interference Shielding, Low Thermal Conductivity, and Extremely Low Heat Release

Mingyi Chen1,2†, Jian Zhu2†, Kai Zhang2, Hongkang Zhou2, Yufei Gao2, Jie Fan1,5*, Rouxi Chen2,3*, Hsing-Lin Wang2,3,4*

1School of Textiles Science and Engineering, Tiangong University, Tianjin 300387, P. R. China

2Department of Materials Science and Engineering, Southern University of Science and Technology, Shenzhen, Guangdong 518055, P. R. China

3School of Innovation and Entrepreneurship, Southern University of Science and Technology, Shenzhen 518055, P. R. China

4Guangdong Provincial Key Laboratory of Energy Materials for Electric Power, Southern University of Science and Technology, Shenzhen, Guangdong 518055, P. R. China

5Ministry of Education Key Laboratory of Advanced Textile Composite Materials, Tiangong University, Tianjin 300387, P. R. China

†Mingyi Chen and Jian Zhu contributed equally to this work.

* Corresponding authors. E-mail: fanjie@tiangong.edu.cn (Jie Fan); chenrx@sustech.edu.cn (Rouxi Chen); wangxl3@sustech.edu.cn(Hsing-Lin Wang)

S1 Calculation

EMI SE was measured using an Agilent E5071C vector network analyzer by the wave guide method in the 8.2-12.4 GHz (X-band) range. The measured scattering parameters (Figs. S11 and S21) were used to calculate the absorption, reflection, and total shielding values. EMI SE (SET) is divided into three parts: reflection loss (SER), absorption loss (SEA), and multiple reflection loss (SEM), and can be expressed by the following formulas:

EMI SE=10lgP0P1=SER +SEA+SEM           (S1)

When SET ≥15 dB，SEM can be neglected, meanwhile，SET 、SER and SEA can be determined as follows：

SET=SEA+SER       (S2)

The power coefficients of reflection (R), transmission (T), and absorption (A) can be calculated based on the four scattering parameters (Figs. S11, S12, S21, and S22) of the network analyzer.

R=S112 = S222      （S3）

T=S122 = S212      （S4）

A=1-R-T       （S5）

SEA and SER can be obtained as：

SER =10log11-R=10log11-S112         （S6）

SEA=10log1-RT=10log1-S112S212           （S7）

The skin depth (δ), defined as the depth at which the incident electromagnetic wave decays to 1/e of its surface value, can be calculated using the following formula (Gupta, Singh, Teotia et al., 2013):

δ=1πfμσ      （S8）

where f is the frequency, μ is the permeability, and σ is the conductivity.

Hence

SEA=8.68 dπfμσ       (S9)

δ can also be obtained by the following formula：

δ=8.68 （dSEA）    (S10)

The specific SE (SE·d-1), which considers the material's density, is expressed as:

SEd=SEdensity (dB▪cm3·g-1)            (S11)

S2 Supplementary Figures and Tables

Fig. S1 Microscopic image of the CNFs after grinding

Fig. S2 SEM images and diameter distribution diagrams of a NTCA-DAB-PVP nanofiber membrane. b carbon nanofibers membrane. c CFA@PANI. d CP-1@PANI. e CP-2@PANI. f CP-3@PANI

Fig. S3 Synthetic scheme for the reaction of the NTCA and DAB monomers to BBB and derived carbon structure

Fig. S4 Comparative photos of NTCA-DAB-PVP membrane and its nanofiber membrane

Fig. S5 Photos of mechanical flexibility of CNFs membrane

Fig. S6 SEM image of PANI nanoparticles

Fig. S7 SEM image of in CFA aerogel, where the nanocellulose entangled around the CNFs and act as the binder

Fig. S8 Photographs of the color change of the aerogels and the precipitated PANI particles

Fig. S9 Photographs and cross-sectional SEM images of a CP-2 aerogel. b CP-3 aerogel c CFA@PANI aerogel. d CP-2@PANI aerogel

Fig. S10 SEM image of CP-3@PANI aerogel

Fig. S11 EDS mapping of C, N, O, P elements and their proportion of the CP-3@PANI

Fig. S12 Raman spectra of CFA, PANI Power and CNFs/PANI hybrid aerogels

Fig. S13 P 2p spectrum of CP-3@PANI

Fig. S14 TGA curves of CP-1@PANI, CP-2@PANI, and CP-3@PANI

Fig. S15 N2 adsorption–desorption isotherms and pore size distribution curves of CFA and CP-3@PANI

Fig. S16 Water contact angle (WCA) of the CFA, CP-3, and CP-3@PANI

Fig. S17 Construction of a device for testing the resistance change of CP-3@PANI aerogel during heat treatment

Fig. S18 a Temperature-resistance dependence of CP-3@PANI during heating-cooling cycle; b Time-resistance change rate curve of CP-3@PANI during heat treatment

Fig. S19 Conductivity of PANI doped with different acids in CP-3@PANI

Fig. S20 SEM images of CP-3@PANI aerogels in-situ polymerization for 4h, 8h, 12h, and 16h

Fig. S21 EMI SE of CP-3@PANI aerogels in-situ polymerization for 4h, 8h, 12h, and 16h

Fig. S22 SET, SER, and SEA values of CP-3@PANI in the 5-50 MHz

Fig. S23 SET, SER, and SEA values of CP-3@PANI in the 50-500 MHz

Fig. S24 (a) the SET, SER, and SEA value of CP-3@PANI in the K-band. (b) the R, T, and A value of CP-3@ PANI in the K-band

Fig. S25 (a) real part ε' and (b) imaginary part ε“of CFA and CP-3PANI

Fig. S26 Thermal infrared images of the CP-3@PANI on a 300 °C heating platform after 10 repeated heating cycles

Fig. S27 Thermal conductivity of CFA, CP-2@PANI, CP-3@PANI and CP-3@PANI after 10 repeated heating cycles

Fig. S28 EMI SE values of the CP-3@PANI after 10 heating and cooling cycles (from RT-300 °C)

Fig. S29 TGA curves of P-PANI and PANI

Fig. S30 a Photo of nanocellulose aerogel; b HHR curves of the nanocellulose aerogel and composite aerogels; c THR curves of the nanocellulose aerogels and composite aerogels

Fig. S31 LOI values of the pure nanocellulose, CFA, CP-3 and CP-3@PANI aerogel

Table S1 The compositions of the CNFs/PANI aerogels

| Samples | Carbon nanofiber (g) | PANI (g) | CNFs : PANI (g) | Nanocellulose Suspension (g)a | Density (g cm-3) |
| --- | --- | --- | --- | --- | --- |
| CFA | 0.32 | 0 | 1:0 | 4 | 0.01 |
| CP-1 | 0.32 | 0.32g | 1:1 | 4 | 0.02 |
| CP-2 | 0.32 | 0.64g | 1:2 | 4 | 0.034 |
| CP-3 | 0.32 | 0.96g | 1:3 | 4 | 0.043 |

- Weight concentration of the nanocellulose suspension is 1.5 wt%.

Table S2 Some Typical Data for Fiber Shell Polymerization

| Sample | Weight of ANI (g) | Weight increase of the sample (g) | % Yield of PANIb (only on the aerogel) | Conductivity (S/m) | Density (g/cm3) | PA content (wt%) |
| --- | --- | --- | --- | --- | --- | --- |
| CFA@PANI | 1 | 0.54 | 11.9 | 100 | 0.075 | 17 |
| CP-1@PANI | 1 | 0.63 | 13.9 | 120 | 0.08 | 21 |
| CP-2@PANI | 1 | 0.75 | 16.6 | 170 | 0.095 | 22.7 |
| CP-3@PANI | 1 | 0.82 | 18.2 | 199 | 0.108 | 23.8 |

b) Yield of the PANI salts was calculated based on the amount of aniline used in the reaction.

Table S3 Surface area, pore volume, and average pores size of the CFA and CP-3@PANI

| Sample | SBET (m2·g-1) | Pore volume (cm3·g-1) | Pore size (nm) |
| --- | --- | --- | --- |
| CFA | 10.98 | 0.023 | 9.053 |
| CP-3@PANI | 0.52 | 0.000976 | 7.45 |

Table S4 The sample parameters and SSE/d values of carbon-based and PANI-based aerogel

| Materials | Density [g·cm-3] | Frequency [GHz] | EMI SE [dB] | SSE/d [dB· cm3 ·g-1] | Refs. |
| --- | --- | --- | --- | --- | --- |
| PANI/MWCNT/graphene | 0.2 | 12.4-18 | 42 | 196 | [S1] |
| LSW/PVA/PANI | 0.55 | 8.2-12.4 | 40 | 73 | [S2] |
| Wood-derived carbon | 0.072 | 8.2-12.4 | 25.5 | 354 | [S3] |
| HfC-carbon fibers/graphene | 0.18 | 8.2-12.4 | 66.4 | 364.1 | [S4] |
| NbC-pyrolytic carbon | 0.48 | 8.2-12.4 | 54.8 | 114 | [S5] |
| Carbon foam | 0.15 | 8.2-12.4 | 53 | 353 | [S6] |
| Carbon-rGO | 0.31 | 8.2-12.2 | 50 | 161 | [S7] |
| GRA Carbon foam | 0.166 | 8.2-12.4 | 40 | 241 | [S8] |
| Carbon/PN resin | 0.152 | 8.2-12.4 | 51.2 | 341 | [S9] |
| Carbon fiber/nano copper | 0.317 | 8.2-12.4 | 29.3 | 92 | [S10] |
| Aerogel-like Carbon | 0.121 | 8.2-12.4 | 51 | 421 | [S11] |
| Graphene-carbon | 0.07 | 8.2-12.4 | 37 | 528 | [S12] |
| WTP-PVA Carbon | 0.057 | 8.2-12.4 | 40 | 700 | [S13] |
| Phthalonitrile-Based Carbon | 0.15 | 8.2-12.4 | 51.2 | 341.1 | [S14] |
| Sugarcane-derived carbon | 0.112 | 8.2-12.4 | 51 | 455.4 | [S15] |
| Bread-derived carbon | 0.29 | 8.2-12.4 | 17.2 | 59.3 | [S16] |
| RF/MWCNTs/Fe3O4 carbon | 0.125 | 8.2-12.4 | 62 | 493.6 | [S17] |
| Carbon/MWCNTs | 0.52 | 8.2-12.4 | 85 | 163 | [S18] |
| Wood-derived carbon/AgNWs | 0.13 | 8.2-12.4 | 60 | 465.1 | [S19] |
| Carbon honeycomb/rGO | 0.061 | 8.2-12.4 | 42 | 688.5 | [S20] |
| 3D-carbon texture/rGO | 0.07 | 8.2-12.4 | 37 | 528 | [S21] |
| Carbon foam | 0.121 | 8.2-12.4 | 20 | 165 | [S22] |
| CP-3@PANI | 0.108 | 8.2-12.4 | 85.45 | 791.2 | This work |

Table S5 Related MCC Data of CNF aerogel

| Sample | PHRR (W g-1) | Tp (℃) | THR (kJ g-1) | HRC (J g-1 K-1) |
| --- | --- | --- | --- | --- |
| CNF | 248.9 | 322.7 | 13.9 | 248.4 |

Table S6 CF-3@PANI Comparison of comprehensive performance with samples reported in literatures

| Materials | EMI SE [dB] | Thermal conductivity (W·m-1·K-1) | PHHR [W·g-1] | Refs. |
| --- | --- | --- | --- | --- |
| Carbon foams | 38.9 | 0.185 |  | [S23] |
| rGO/sugarcane derived hybrid carbon foam | 53 | 0.115 |  | [S24] |
| PCC/MXene/polyvinyl alcohol | 43.13 | 0.69 | 207.6 | [S25] |
| MXene/polyphosphamide/PA6 | 24 |  | 300 | [S26] |
| SPI/PA/GNS-co-Q | 43 |  | 315.46 | [S27] |
| (APP)/PEI/MXene/(PCL) ramie fabric | 35 |  | 66.3 | [S28] |
| UPPH-SMCs | 77 |  | 83 | [S29] |
| FRs/CNT/TPU | 32.7 |  | 28.4 | [S30] |
| PS/SiAPP/MWCNT | 11 |  | 399 | [S31] |
| P-doped PANI/AgMWs | 51.2 |  | 223 | [S32] |
| Melamine-Based MF/Fe3O4/AgNWs | 49 |  | 75.9 | [S33] |
| CoFe2O4@CNT/PDMS Foams | 48.85 | 0.106 |  | [S34] |
| MXene/CNT/Epoxy | 34.7 |  | 532 | [S35] |
| MXene/montmorillonite/CNF | 43 | 0.159 |  | [S36] |
| F-reduced graphene oxide (rGO)/paraffin | 74.6 | 0.36 | 534 | [S37] |
| PS-MWCNT-IFR | 38 |  | 171 | [S38] |
| CP-3@PANI | 85.45 | 0.104 | 7.8 | This work |

Supplementary References

- Y. Huangfu, K. Ruan, H. Qiu, Y. Lu, C. Liang et al., Fabrication and investigation on the PANI/MWCNT/thermally annealed graphene aerogel/epoxy electromagnetic interference shielding nanocomposites. Composites, Part A. 121, 265-272 (2019). https://doi.org/10.1016/j.compositesa.2019.03.041

- T. Zhang, S. Zeng, H. Jiang, Z. Li, D. Bai et al., Leather solid waste/poly(vinyl alcohol)/polyaniline aerogel with mechanical robustness, flame retardancy, and enhanced electromagnetic interference shielding. ACS Appl Mater Interfaces 13(9), 11332-11343 (2021). https://doi.org/10.1021/acsami.1c00880

- X. Liu, Y. Li, X. Sun, W. Tang, G. deng et al., Off/on switchable smart electromagnetic interference shielding aerogel. Matter. 4, (2021). https://doi.org/10.1016/j.matt.2021.02.022

- D. Jiang, S. Tian, H. Li, Z. Du, T. Liu et al., Lightweight hfc nanowire-carbon fiber/graphene aerogel composites for high-efficiency electromagnetic interference shielding. Carbon. 219, 118788 (2024). https://doi.org/10.1016/j.carbon.2024.118788

- X. Liu, H. Liu, H. Xu, W. Xie, M. Li et al., Natural wood templated hierarchically cellular nbc/pyrolytic carbon foams as stiff, lightweight and high-performance electromagnetic shielding materials. J. Colloid Interface Sci. 606, 1543-1553 (2022). https://doi.org/10.1016/j.jcis.2021.08.110

- A. Chithra, P. Wilson, S. Vijayan, R. Rajeev, K. Prabhakaran. Carbon foams with low thermal conductivity and high emi shielding effectiveness from sawdust. Industrial Crops and Products. 145, 112076 (2020). https://doi.org/10.1016/j.indcrop.2019.112076

- P. R. Agrawal, R. Kumar, S. Teotia, S. Kumari, D. P. Mondal et al., Lightweight, high electrical and thermal conducting carbon-rgo composites foam for superior electromagnetic interference shielding. Composites, Part B. 160, 131-139 (2019). https://doi.org/10.1016/j.compositesb.2018.10.033

- F. Moglie, D. Micheli, S. Laurenzi, M. Marchetti, V. Mariani Primiani. Electromagnetic shielding performance of carbon foams. Carbon. 50(5), 1972-1980 (2012). https://doi.org/10.1016/j.carbon.2011.12.053

- E. Zhou, J. Xi, Y. Guo, Y. Liu, Z. Xu et al., Synergistic effect of graphene and carbon nanotube for high-performance electromagnetic interference shielding films. Carbon. 133, 316-322 (2018). https://doi.org/10.1016/j.carbon.2018.03.023

- Y. Jiao, C. Wan, W. Zhang, W. Bao, J. Li. Carbon fibers encapsulated with nano-copper: A core‒shell structured composite for antibacterial and electromagnetic interference shielding applications. Nanomaterials (Basel). 9(3), (2019). https://doi.org/10.3390/nano9030460

- Y.-Q. Li, Y. A. Samad, K. Polychronopoulou, K. Liao, Lightweight and highly conductive aerogel-like carbon from sugarcane with superior mechanical and emi shielding properties. ACS Sustainable Chem. Eng. 3(7), 1419-1427 (2015). https://doi.org/10.1021/acssuschemeng.5b00340

- W.-L. Song, X.-T. Guan, L.-Z. Fan, W.-Q. Cao, C.-Y. Wang et al., Tuning three-dimensional textures with graphene aerogels for ultra-light flexible graphene/texture composites of effective electromagnetic shielding. Carbon. 93, 151-160 (2015). https://doi.org/10.1016/j.carbon.2015.05.033

- L. Vazhayal, P. Wilson, K. Prabhakaran, Waste to wealth: Lightweight, mechanically strong and conductive carbon aerogels from waste tissue paper for electromagnetic shielding and CO2 adsorption. Chem. Eng. J. 381, 122628 (2020). https://doi.org/10.1016/j.cej.2019.122628

- L. Zhang, M. Liu, E. Chua, K. Y. See, X. Hu, Phthalonitrile-based carbon foam with high specific mechanical strength and superior electromagnetic interference shielding performance. ACS Appl. Mater. Interfaces 8, 5b12072 (2016). https://doi.org/10.1021/acsami.5b12072

- Y. Zhang, J. Yu, J. Lu, C. Zhu, D. Qi, Facile construction of 2d mxene (ti3c2tx) based aerogels with effective fire-resistance and electromagnetic interference shielding performance. J. Alloys Compd. 870, 159442 (2021). https://doi.org/10.1016/j.jallcom.2021.159442

- Y. Yuan, Y. Ding, C. Wang, F. Xu, Z. Lin et al., Multifunctional stiff carbon foam derived from bread. ACS Appl. Mater. Interfaces 8(26), 16852-16861 (2016). https://doi.org/10.1021/acsami.6b03985

- Q. Li, L. Chen, J. Ding, J. Zhang, X. Li et al., Open-cell phenolic carbon foam and electromagnetic interference shielding properties. Carbon 104, 90-105 (2016). https://doi.org/10.1016/j.carbon.2016.03.055

- R. Kumar, S. R. Dhakate, T. Gupta, P. Saini, B. P. Singh et al., Effective improvement of the properties of light weight carbon foam by decoration with multi-wall carbon nanotubes. J. Mater. Chem. A 1(18), 5727-5735 (2013). https://doi.org/10.1039/C3TA10604G

- Y. Yuan, X. Sun, M. Yang, F. Xu, Z. Lin et al., Stiff, thermally stable and highly anisotropic wood-derived carbon composite monoliths for electromagnetic interference shielding. ACS Appl. Mater. Interfaces 9(25), 21371-21381 (2017). https://doi.org/10.1021/acsami.7b04523

- Y. Yuan, L. Liu, M. Yang, T. Zhang, F. Xu et al., Lightweight, thermally insulating and stiff carbon honeycomb-induced graphene composite foams with a horizontal laminated structure for electromagnetic interference shielding. Carbon 123, 223-232 (2017). https://doi.org/10.1016/j.carbon.2017.07.060

- W.-L. Song, X.-T. Guan, L.-Z. Fan, W.-Q. Cao, C.-Y. Wang et al., Tuning three-dimensional textures with graphene aerogels for ultra-light flexible graphene/texture composites of effective electromagnetic shielding. Carbon 93, 151 (2015). https://doi.org/10.1016/j.carbon.2015.05.033

- W. Li, L. Feng, X. Shi, Y. Wang, Mechanical and electromagnetic shielding properties of carbon foam. Adv. Engin. Mater. 23, 2100452 (2021). https://doi.org/10.1002/adem.202100452

- A. Chithra, P. Wilson, S. Vijayan, R. Rajeev, K. Prabhakaran, Thermally insulating robust carbon composite foams with high emi shielding from natural cotton. J. Mater. Sci. Technol. 94, 113-122 (2021). https://doi.org/10.1016/j.jmst.2021.02.064

- L. Wang, X. Shi, J. Zhang, Y. Zhang, J. Gu, Lightweight and robust rgo/sugarcane derived hybrid carbon foams with outstanding EMI shielding performance. J. Mater. Sci. Technol. 52, 119-126 (2020). https://doi.org/10.1016/j.jmst.2020.03.029

- S. Gong, X. Sheng, X. Li, M. Sheng, H. Wu et al., A multifunctional flexible composite film with excellent multi‐source driven thermal management, electromagnetic interference shielding, and fire safety performance, inspired by a “brick–mortar” sandwich structure. Adv. Funct. Mater. 32，2200570 (2022). https://doi.org/10.1002/adfm.202200570

- V. K. Patle, Y. Mehta, N. Dwivedi, D. P. Mondal, A. K. Srivastava et al., Thermal insulating and fire-retardant lightweight carbon-slag composite foams towards absorption dominated electromagnetic interference shielding. Sustainable Mater. Technol. 33, e00453 (2022). https://doi.org/10.1016/j.susmat.2022.e00453

- J. Liu, J. Zhang, F. Chen, X. Cui, P. Qi et al., Enhancing fire safety, electromagnetic interference shielding, and photothermal conversion performances of wearable polyamide fabrics through eco-friendly coatings. Sustainable Mater. Technol. 40, e00949 (2024). https://doi.org/10.1016/j.susmat.2024.e00949

- W. Cheng, Y. Zhang, Y. Tao, J. Lu, J. Liu et al., Durable electromagnetic interference (emi) shielding ramie fabric with excellent flame retardancy and self-healing performance. J. Colloid Interface Sci. 602, 810-821 (2021). https://doi.org/10.1016/j.jcis.2021.05.159

- C.-C. Höhne, P. Blaess, S. Ilinzeer, P. Griesbaum, New approach for electric vehicle composite battery housings: Electromagnetic shielding and flame retardancy of pur/up-based sheet moulding compound. Composites, Part A. 167, 107404 (2023). https://doi.org/10.1016/j.compositesa.2022.107404

- X. Ji, D. Chen, J. Shen, S. Guo, Flexible and flame-retarding thermoplastic polyurethane-based electromagnetic interference shielding composites. Chem. Eng. J. 370, 1341-1349 (2019). https://doi.org/10.1016/j.cej.2019.03.293

- C. Gao, Y. Shi, Y. Chen, S. Zhu, Y. Feng et al., Constructing segregated polystyrene composites for excellent fire resistance and electromagnetic wave shielding. J. Colloid Interface Sci. 606, 1193-1204 (2022). https://doi.org/10.1016/j.jcis.2021.08.091

- L. Zhang, B.-W. Liu, Y.-Z. Wang, T. Fu, H.-B. Zhao, P-doped pani/agmws nano/micro coating towards high-efficiency flame retardancy and electromagnetic interference shielding. Composites, Part B 238, 109944 (2022). https://doi.org/10.1016/j.compositesb.2022.109944

- H.-G. Shi, H.-B. Zhao, B.-W. Liu, Y.-Z. Wang, Multifunctional flame-retardant melamine-based hybrid foam for infrared stealth, thermal insulation, and electromagnetic interference shielding. ACS Appl. Mater. Interfaces 13(22), 26505-26514 (2021). https://doi.org/10.1021/acsami.1c07363

- Z. Xie, Z. Wei, Y. Meng, N. Pan, R. Zhang et al., Robust CoFe2O4@carbon nanotube/polydimethylsiloxane foams with low thermal conductivity for electromagnetic interference shielding. ACS Appl. Nano Mater. 6(23), 21733-21740 (2023). https://doi.org/10.1021/acsanm.3c03945

- R. Chang, H. Gao, P. Hao, H. Qu, J. Xu et al., Hierarchically porous mxene/carbon nanotube/epoxy composites for effective electromagnetic interference shielding and flame retardancy. ACS Appl. Nano Mater. 7(3), 3168-3178 (2024). https://doi.org/10.1021/acsanm.3c05512

- D.-D. Li, X. Pu, P. Hu, M. Han, W. Xin et al., Multifunctional Ti3C2Tx mxene/montmorillonite/cellulose nanofibril films for electromagnetic interference shielding, photothermal conversion, and thermal insulation. Cellulose 30(6), 3793-3805 (2023). https://doi.org/10.1007/s10570-023-05119-6

- Y.-R. Li, Y.-M. Li, W.-J. Hu, D.-Y. Wang. Shaped photothermal conversion phase‐change materials with excellent electromagnetic shielding performance and flame retardancy. Adv. Eng. Mater. 25((2023). https://doi.org/10.1002/adem.202201885

- D. Ponnamma, K. K. Sadasivuni, M. Strankowski, Q. Guo, S. Thomas, Synergistic effect of multi walled carbon nanotubes and reduced graphene oxides in natural rubber for sensing application. Soft Matter. 9(43), 10343-10353 (2013). https://doi.org/10.1039/C3SM51978C