Supporting Information for

Membranes of Polymer of Intrinsic Microporosity PIM-1 for Gas Separation: Modification Strategies and Meta-Analysis

Boya Qiu1, Yong Gao2, Patricia Gorgojo1, 3, 4,*, Xiaolei Fan1, 2, 5,*

1 Department of Chemical Engineering, Faculty of Science and Engineering, The University of Manchester, Manchester M13 9PL, United Kingdom

2 Institute of Wenzhou, Zhejiang University, Wenzhou 325006, P. R. China

3 Instituto de Nanociencia y Materiales de Aragón (INMA) CSIC-Universidad de Zaragoza, Mariano Esquillor, 50018 Zaragoza, Spain

4 Departamento de Ingeniería Química y Tecnologías del Medio Ambiente, Universidad de Zaragoza, Pedro Cerbuna 12, 50009 Zaragoza, Spain

5 Ningbo China Beacons of Excellence Research and Innovation Institute, University of Nottingham Ningbo China, 211 Xingguang Road, Ningbo 315048, P. R. China

*Corresponding authors.  E-mails: pgorgojo@unizar.es  (Patricia Gorgojo); xiaolei.fan@manchester.ac.uk (Xiaolei Fan)

Supplementary Figures

Table S1 Gas separation performance of thick PIM-1 membranes (at 20−40 ℃ and 1−4 bar)

|  | Membrane | Gas permeability (barrer) |  |  |  |  |  | Selectivity |  |  | Refs. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | He 2.59 Å | H2 2.90 Å | O2 3.44 Å | N2 3.66 | CH4 3.81 Å | CO2 3.63 Å | O2/N2 | CO2/N2 | CO2/ CH4 |  |
| Unmodified PIM-1 | PIM-1 | 660 | 1300 | 370 | 92 | 125 | 2300 | 4.0 | 25 | - | [S1] |
|  | PIM-1 | 760 | 1630 | 580 | 180 | 310 | 4390 | 3.2 | 24 | - | [S2] |
|  | PIM-1 | - | - | 1133 | 353 | - | 5366 | 3.2 | 15 | - | [S3] |
|  | PIM-1 | 1061 | 2332 | 786 | 238 | 360 | 3496 | 3.3 | 14.7 | 9.7 | [S4] |
|  | PIM-1 | 1500 | 3600 | 1300 | 340 | 430 | 6500 | 3.3 | 15 |  | [S5] |
|  | PIM-1 |  |  | 1017 | 342 | 555 | 5093 | 3.0 | 14.9 | 9.2 | [S6] |
|  | PIM-1 |  | 3731 | 1172 | 309 | 431 | 6601 |  |  | 15.2 | [S7] |
|  | PIM-1 |  | 2785 | 1012 | 303 | 417 | 5606 | 3.3 | 18.5 | 13.4 | [S8] |
|  | PIM-1 |  | 3195 | 1089 | 325 | 418 | 5622 | 3.4 | 17.3 | 13.5 | [S9] |
|  | PIM-1 |  |  | 1521 | 687 |  | 8461 | 2.2 | 12.3 |  | [S10] |
|  | PIM-1 | 1048 |  | 928 | 279 | 401 | 6211 | 3.3 | 22.3 | 15.5 | [S11] |
|  | PIM-1 | 800 |  | 510 | 120 | 170 | 2790 | 4.4 | 23 | 16.4 | [S12] |
|  | PIM-1 |  |  |  |  |  | 4100* |  | 15* |  | [S13] |
|  | PIM-1 | 1577 | 3365 | 985 | 248 | 362 (423*b) | 5919 (5600*b) | 4.0 | 24 | 16 (13*b) | [S14] |
|  | PIM-1 |  |  |  | 228 | 310 | 3799 |  | 16.6 | 12.2 | [S15] |
|  | PIM-1 (ethanol treated) | 1760 |  | 1950 | 660 | 1000 | 11400 | 3.0 | 17 | 11.4 | [S12] |
|  | PIM-1 |  |  | 562.2 | 163.6 | 322.2 | 3294.7 | 3.4 | 20.1 | 10.2 | [S16] |
|  | PIM-1 |  | 3537 | 1072 | 351 | 536 | 6576 | 3.0 | 18.7 | 12.3 | [S17] |
|  | PIM-1 |  |  |  |  |  | 3815 |  | 20 | 14 | [S18] |
|  | PIM-1 |  |  | 2179 | 912 | 1374 | 10683 | 2.4 | 11.7 | 7.8 | [S19] |
|  | PIM-1 |  | 1936 |  | 148 | 229 | 3425 |  | 23.1 | 15.0 | [S20] |
|  | PIM-1 |  | 4000 | 1073 | 338 | 502 | 5506 | 3.2 | 16.3 | 11.0 | [S21] |
|  | PIM-1 | 1660 | 4270 | 1620 | 540 | 1000 | 8570 | 3 | 15.9 | 8.6 | [S22] |
|  | PIM-1 |  |  |  |  |  | 2430 |  | 16.99 |  | [S23] |
|  | PIM-1 |  |  |  | 240 |  | 4700 |  | 19.3 |  | [S24] |
|  | PIM-1 |  | 3511 | 1049 | 269 | 366 | 3934 | 3.9 | 14.6 | 11.0 | [S25] |
|  | PIM-1 |  |  |  |  |  | 3672 |  | 16.5 (15.5d) | 10.6 (9.6e) | [S26] |
|  | PIM-1 | 1170 | 2710 | 875 | 219 | 286 | 4770 | 4.0 | 21.8 | 16.7 | [S27] |
|  | PIM-1 |  |  |  | 198 | 315 | 3795 |  | 19 | 12 | [S28] |
|  | PIM-1 |  |  | 1130 | 397 | 652 | 7440 | 2.8 | 19 | 11 | [S29] |
|  | PIM-1 |  | 2504 | 965.5 | 255.9 | 335.0 | 4087 | 3.77 | 16.0 | 12.2 | [S30] |
|  | PIM-1 |  | 1820 | 802 | 190 | 210 | 3054 | 4.2 | 16.1 | 14.5 | [S31] |
|  | PIM-1 |  | 1784 | 590 | 182 | 218 (239*b) | 3364 (3422*b) | 3.2 | 18.5 | 15.4 (14.3*b) | [S32] |
|  | PIM-1 |  | 7072 | 2326 | 693 | 1080 | 11371 | 3.4 | 16.4 | 10.5 | [S33] |
|  | PIM-1 | 1369 | 3580 | 1790 | 727 | - | 8310 | 2.5 | 11 |  | [S34] |
|  | PIM-1 |  |  |  | 211 |  | 3402 |  | 16.1 |  | [S35] |
|  | PIM-1 |  |  |  | (231a) | (288b) | (4020a) (3895b) |  | (15.6a) | (13.9b) | [S35] |
|  | PIM-1 |  |  |  | 297 (321a) |  | 8095 (3882a) |  | 13 (14.7a) |  | [S36] |
|  | PIM-1 |  |  |  |  | (330b) | (6400b) |  |  | (20.3b) | [S37] |
|  | PIM-1 |  |  |  | 230 |  | 3277 |  | 16.2 |  | [S38] |
|  | PIM-1 | 2000 | 4980 | 2140 | 607 | 914 | 12100 |  | 19.9 | 13.2 | [S39] |
|  | PIM-1 |  | 2219 |  | 224 | 363 | 4521 (4336e) |  | 20.2 | 12.5 (11.5e) | [S40] |
|  | PIM-1 |  |  | 1072 | 351 | 536 (408b) | 6576 (5772b) | 3.0 | 18.7 | 12.3 (12.4b) | [S41] |
|  | PIM-1 |  | 3274 | 1396 | 483 | 789 | 9896 | 2.9 | 20.5 | 12.5 | [S42] |
|  | PIM-1 |  | 2696 | 712 | 166 | 204 | 3375 | 4.3 | 20.4 | 16.6 | [S43] |
|  | PIM-1 |  | 2753 | 1028 | 375 | 644 | 5811 | 2.7 | 15.5 | 9.0 | [S44] |
|  | PIM-1 |  |  |  | 195.4 |  | 3694.5 |  | 18.9 |  | [S45] |
|  | PIM-1 |  |  |  |  |  | (8994f) (8263b) |  | (14.9f) | (13.6b) | [S46] |
|  | PIM-1 |  |  |  |  |  | 1250 |  | 19.8 |  | [S47] |
|  | PIM-1 |  |  |  | 306.2 |  | 4131 |  | 13 |  | [S48] |
|  | PIM-1 |  |  |  | 113.9 |  | 3027.7 |  | 26.6 |  | [S49] |
|  | PIM-1 | 1830 | 4710 | 2130 | 773 | 1300 | 12800 | 2.76 | 16.5 | 9.8 | [S50] |
|  | PIM-1 |  |  |  |  |  | (7500g) |  | (14g) |  | [S51] |
|  | PIM-1 |  |  | 844 | 211 |  | 4200 | 4.0 | 20 |  | [S52] |
|  | PIM-1 |  |  | 1545 | 486 |  | 7340 | 3.2 | 15.1 |  | [S53] |
|  | PIM-1 |  |  |  |  | (450b) | (5920b) |  |  | (13.1b) | [S54] |
|  | PIM-1 |  |  |  | 650 | 1490 | 11840 |  | 18.23 | 7.94 | [S55] |
|  | PIM-1 |  |  |  | 204 | 273 | 4375 |  | 21.4 | 16.0 | [S56] |
|  | PIM-1 |  | 1400 | 460 | 140 | 220 | 2800 | 3.2 | 20 | 13 | [S57] |
|  | PIM-1 |  |  |  |  | 363 | 4533 (4391e) |  |  | 12.5 (11.6e) | [S58] |
|  | PIM-1 |  |  |  |  |  | 4521 (4336e) |  |  | 12.45 (11.50e) | [S59] |
|  | PIM-1 |  |  |  | 85.9 | 104.7 | 2345.4 |  | 27.3 | 22.4 | [S60] |
|  | PIM-1 |  | 575.2 | 130.1 | 27.2 | 29.0 | 980.7 |  | 36.0 | 33.8 | [S61] |
|  | PIM-1 |  |  |  |  |  | (5917b) |  |  | (13.1b) | [S62] |
|  | PIM-1 |  |  | 802 | 229 | 258 | 4259 | 3.5 | 18.6 | 16.5 | [S63] |
|  | PIM-1 |  | 3380 | 1250 | 400 | 590 | 7200 | 3.1 | 18.0 | 12.0 | [S64] |
|  | PIM-1 |  |  |  |  |  | 7210 |  | 18 |  | [S65] |
|  | PIM-1 (sub-ambient temperature) | 1000 | 1557 | 159 | 17 | 21 | 1380 | 8 | 81.2 |  | [S66] |
|  | PIM-1 |  |  |  |  | (543b) | (6190b) |  |  | (11.7b) | [S67] |
|  | PIM-1 (methanol treated) |  | 3949 | 1257 | 337 | 472 | 6957 | 3.7 | 20.7 | 14.8 | [S43] |
|  | PIM-1 |  |  |  |  | 516 | 7135 (6007*e) |  |  | 13.8 (14.7*e) | [S68] |
|  | PIM-1 |  |  |  |  | (543b) | (6190b) |  |  | (11.7b) | [S69] |
|  | PIM-1 |  |  |  |  |  | 5800 |  |  | 11.5 | [S70] |
|  | PIM-1 |  |  |  |  | 660 (810b) | 9000 (8250b) |  |  | 13.5 (10.2b) | [S71] |
|  | PIM-1 |  |  |  | 205 |  | 4110 |  | 20 |  | [S72] |
|  | PIM-1 |  | 1530 | 880 | 273 | 380 | 5105 |  | 18.7 | 13.4 | [S73] |
|  | PIM-1 |  |  |  |  | (758b) | (6578b) |  |  | (8.7b) | [S74] |
|  | PIM-1 |  | 4330 | 1353 | 373 | 442 | 6595 | 3.63 | 17.7 | 14.9 | [S75] |
|  | PIM-1 |  | 4381 | 1686 | 434 | 527 | 8287 | 3.9 | 19.1 | 15.7 (14.3b) | [S76] |
|  | PIM-1 | 1336 | 2772 | 768 | 203 | 299 | 3760 | 3.8 | 18.5 | 12.6 | [S77] |
|  | PIM-1 |  |  |  |  |  | (4216e) |  |  | (10.1e) | [S78] |
|  | PIM-1 |  |  |  | 288.0 | 371.7 | 5181.6 |  | 18.0 | 13.9 | [S79] |
|  | PIM-1 |  |  |  |  | 1453 | 9336 |  |  | 6.43 | [S80] |
|  | PIM-1 |  |  |  | 227.5 (251.4h) |  | 3842.3 (3253.1h) |  | 16.9 (12.9h) |  | [S81] |
|  | PIM-1 |  |  |  |  |  | 6605.9 (4902g) |  | 16.1 (18.2g) | 12.0 | [S82] |
|  | PIM-1 |  |  |  |  |  | 5167 |  |  |  | [S83] |
|  | PIM-1 |  |  |  | (363a) | (563b) | (6780a) (6411b) |  | (18.6a) | (11.5b) | [S84] |
|  | PIM-1 |  |  |  |  |  | (3945e) |  |  | (12.5e) | [S85] |
|  | PIM-1 |  | 3250 |  | 249.9 | 318 | 4868 |  | 19.5 | 15.3 | [S86] |
|  | PIM-1 |  |  |  |  | (611b) | (6887b) |  |  | (11.5b) | [S87] |
|  | PIM-1 |  | 3255* |  | 364* (387a) | 632* (590b) | 7311* (7323a) (7195 b) |  | (18.9a) | (12.3b) | [S88] |
|  | PIM-1 |  |  |  |  |  | 4310 |  |  | 22.6 | [S89] |
|  | PIM-1 |  |  |  |  |  | (8000b) |  | (18d) | (10e) | [S90] |
|  | PIM-1 |  |  |  |  |  | (3980a) |  | (23.1a) |  | [S91] |
|  | PIM-1 |  |  |  | 170.9 (170.4a) |  | 3872.8 (3673.7a) |  | 22.7 (21.6a) |  | [S92] |
|  | PIM-1 |  | 2378 |  |  | 305.3 | 4822 |  | 15.8 | 11.3 | [S93] |
|  | PIM-1 |  |  |  | 309 (284f) | 416 (385b) | 6065 (4786f) (4635b) |  | 19.6 (16.1f) | 14.6 (12.3b) | [S94] |
|  | PIM-1 |  |  |  | 313.1 |  | 5360.6 |  | 17.0 |  | [S95] |
|  | PIM-1 |  |  |  | 210 (207a) | 224 (238b) | 4387 (4210a) (4270b) |  | 20.9 (17.94a) | 19.6 (20.3b) | [S96] |
|  | PIM-1 |  | 2058.2 | 589.2 | 142.2 | 199.0 | 2789.5 |  | 19.6 | 14.0 | [S97] |
|  | PIM-1 |  |  |  |  |  | (6800f) |  | (18f) |  | [S98] |
|  | PIM-1 |  |  |  |  |  | 4187 |  | 17.4 |  | [S99] |
|  | PIM-1 |  |  |  |  | 259 | 4654 |  |  | 18.1 | [S100] |
|  | PIM-1 |  |  | 787 | 299 | 511 | 4772 |  | 15.9 | 9.3 | [S101] |
|  | PIM-1 |  | 2631 |  | 578 | 832 | 7842 |  | 13.6 | 9.7 | [S102] |
|  | PIM-1 |  |  |  |  |  | 4132 |  | 13.5 |  | [S103] |
|  | PIM-1 |  |  |  |  |  | 2795 |  | 16 |  | [S104] |
| Chain modification | Carboxylated PIM-1 | 153 | 408 | 110 | 24 | - | 620 | 4.6 | 26 | - | [S34] |
|  | TZ−PIM-1 | - | - | - | - | - | - | - | 30* (40a*) | 22* (22b*) | [S105] |
|  | Thio−PIM-1 | 270 | 610 | 140 | 37 | 56 | 1120 | 3.8 | 30 | 20 | [S106] |
|  | MTZ−PIM |  |  | 269.6 | 62.7 (42.0c) |  | 1391 (1674c) | 4.3 | 22.2 (39.9c) |  | [S10] |
|  | AO−PIM-1 | 412 | 912 | 147 | 33 | 34 (35*b) | 1153 (830*b) | 4.5 | 35 | 34 (24*b) | [S14] |
|  | PIM-C1 | 2880 | 9870 | 3410 | 980 | 1300 | 18900 | 3.5 | 19.3 | 14.4 | [S22] |
|  | HCPIM(PIM-1−COOH) |  | 90.53 | 9.80 | 1.80 | 3.82 | 96.43 | 5.4 | 53.6 | 25.2 | [S25] |
|  | PIM-1−M |  | 3710 | 2180 | 850 | 1525 | 14180 | 2.6 | 17 | 9 | [S107] |
|  | PIM-1−MBr |  | 1300 | 480 | 115 | 185 | 3200 |  | 27 | 17 | [S107] |
|  | Brominated vinylated PIM-1 |  | 675 | 305 | 90 | 130 | 1890 |  | 21 | 15 | [S107] |
|  | Thiophenated vinylated PIM-1 |  | 775 | 234 | 70 | 125 | 1735 |  | 25 | 14 | [S107] |
|  | Vinylated PIM-1 |  | 1080 | 410 | 130 | 260 | 3240 |  | 26 | 12 | [S107] |
|  | PIM-1 160℃, 33 min |  |  |  |  | 694 | 7478 |  |  | 11.9 | [S108] |
|  | PIM-1 120℃, 81 min |  |  |  |  | 293.5 | 5151 |  |  | 17.65 | [S108] |
|  | Adamantane-AO−PIM-1 |  | 1360.3 | 366.5 | 79.5 | 82.5 | 2483.6 |  | 31.2 | 30.1 | [S61] |
|  | PIM-1−COOH |  | 270 | 44 | 9.0 | 9.0 | 290 | 5.0 | 32 | 33 | [S57] |
|  | PIM-1 160℃, 40 min, N2 flow |  |  |  |  |  | 4835 |  | 55.5 |  | [S109] |
|  | PIM-1−SO3H |  | 2607 | 324 | 53 | 35 | 1388 |  | 26.2 | 39.7 | [S75] |
|  | PIM-1−Py |  | 556.7 | 127.4 | 36.7 |  | 768.5 |  | 20.9 | 17.5 | [S97] |
|  | PIM-1−MePy |  | 272.5 | 53.4 | 13.6 |  | 295.1 |  | 21.8 | 15.0 | [S97] |
| Post-modification | Crosslinked PIM-1/azide |  |  | 38 | 8 |  | 219 | 4.8 | 27.4 |  | [S110] |
|  | DC-induced thermal crosslinked cPIM-1 |  |  | 231 | 49.9 | 52.6 | 1291 | 4.6 | 28.8 | 24.6 | [S6] |
|  | PIM-UV 30 min |  | 2274 | 189 | 27.7 | 23.1 (20.4b) | 724 (745b) | 6.8 | 26.1 | 31.3 (29.3b) | [S7] |
|  | Thermally crosslinked PIM-1 |  | 3872 | 582 | 96 | 73 | 4000 |  | 41.7 | 54.8 | [S43] |
|  | UV/oxidize-modified PIM-1 |  | 2104 | 513 | 84 | 85 | 2394 | 6.1 | 28.4 | 28.1 | [S9] |
|  | TOX-PIM-1 |  | 1820 | 245 | 30 | 16 | 1104 | 8.1 | 37 (45*a) | 69 (60*b) | [S111] |
|  | PIM-1(Na)-Al |  |  |  |  |  | 907 |  | 30.8 |  | [S19] |
|  | Amine-PIM-1 | 838 | 2180 | 664 | 176 | 240 | 1030 |  | 5.83 | 4.28 | [S39] |
|  | PIM-1−NH2 |  | 1450 | 430 | 134 | 210 | 840 | 3.2 | 6.3 | 4 | [S64] |
|  | PIM-1−tBOC |  | 130 | 19 | 3.6 | 5.0 | 100 | 5.3 | 28 | 20 | [S64] |
|  | PIM-1−deBOC(acid) |  | 1700 | 500 | 160 | 260 | 1400 | 3.0 | 8.6 | 5.6 | [S64] |
|  | PIM-1−deBOC(thermal) |  | 2000 | 500 | 120 | 170 | 2300 | 4.6 | 20 | 14 | [S64] |
|  | PIM-1-450 |  | 200* |  | 0.6* | 0.15* | 30* |  | 50* | 200* | [S112] |
|  | SCPIMs |  |  |  | 69 | 98 | 4008 |  | 58.1 | 40.9 | [S56] |
|  | Crosslinked PIM-1-BM-70 |  |  | 11.1 | 1.7 | 1.1 | 48.3 | 6.5 | 30.1 | 43.9 | [S63] |
|  | F-PIM-1 | 754 | 326 | 7.54 | 0.88 | 0.2 | 22.3 | 8.6 | 25.3 | 111.5 | [S77] |
|  | PIM-1/Al2O3 |  | 2492 | 188 | 21.3 | 11.1 (13.9b) | 624 (698b) | 8.8 | 29.3 | 56.2 (50.2b) | [S76] |
|  | PIM-1−NH2 |  |  |  |  | 300 (33.5b) | 1070 (845b) |  |  | 3.6 (25.2b) | [S71] |
|  | PIM-1/tannic acid |  |  |  |  |  | (3253e) |  |  | (19.0e) | [S78] |
|  | PIM-1/TiO2 |  |  |  |  |  | 10659.6 (7036g) |  | 15.5 (18.0g) | 11.3 | [S82] |
|  | PIM-1-O3 |  | 1294 |  | 13.81 | 10.7 | 443 |  | 32.08 | 41.4 | [S86] |
|  | Ester-crosslinked PIM-1−COOH |  |  | 984 | 302 | 416 | 6347 |  | 21.0 | 15.2 | [S101] |
|  | NA-PIM-1 |  |  |  | 161.4 (178.4a) |  | 4593.2 (4121.7a) |  | 28.5 (23.1a) |  | [S92] |
|  | NA-PIM-1-Zn-PEI |  |  |  | 98.9 (104.4a) |  | 3125.9 (2848.1a) |  | 31.6 (27.3a) |  | [S92] |
|  | Aminated PIM-1 |  | 1135 |  | 85 | 229 | 2590 |  | 30.8 | 13.1 | [S102] |
|  | f-PIM-1 | 710 | 741 | 27 | 3.1 | 1.6 | 102 | 8.7 | 32.9 | 63.8 | [S113] |
| Blends | PIM-1/Matrimid® (10%) |  |  | 400 |  |  | 1953 | 4.0 | 20 | 16 | [S18] |
|  | PIM-1/Matrimid® (10%)−TETA |  | 395 | 32 | 4.3 | 3.4 | 41 | 7.4 | 9.5 | 12.1 | [S114] |
|  | cPIM-1/Torlon (10%) |  |  | 185 | 42 | 42 | 1013 | 4.4 | 24.0 | 23.9 | [S115] |
|  | cPIM-1/Matrimid® |  |  |  |  | 57 (53.5b) | 982 (905b) |  |  | 17.2 (16.9b) | [S116] |
|  | PIM-1/PEG |  |  |  | 115 | 50 | 1952 |  | 17.0 | 39.0 | [S15] |
|  | PIM-1/sPPSU |  | 1257 | 257 | 57 | 61 (60*b) | 1429 (1800*b) | 4.5 | 25.1 | 23.4 (30*b) | [S21] |
|  | PIM-b-PEG |  |  | 370 | 140 | 270 | 3000 | 2.8 | 22.3 | 11.1 | [S117] |
|  | PIM-1-PEG copolymer |  |  | 101 | 27 | 43 | 812 | 3.7 | 30 | 19 | [S29] |
|  | PIM-1/[SC6mim][STf2N] |  |  | 310 | 90 | 165 | 2240 | 3.4 | 25 | 14 | [S29] |
|  | PIM/PEI (8:2) |  | 3489 | 1126 | 332 | 511 | 5765 | 3.4 | 17.4 | 11.3 | [S33] |
|  | PIM-1/MEEP80 |  | 597 | 274 | 117 | 292 | 2446 | 2.3 | 20.9 | 8.4 | [S44] |
|  | PIM-1-IL |  |  | 102 | 23 |  | 817 | 4.5 | 35.5 |  | [S53] |
|  | PIM-1/MEEP100 |  |  |  |  |  | 5340 |  | 24 |  | [S65] |
|  | PIM-1/IL |  |  |  |  |  | 2090 |  |  |  | [S83] |
|  | PIM-1/[SAPTMS][SAc] |  |  |  | 87 (90a) | 95 (94b) | 2754 (2565a) (2543b) |  | 31.7 (27.05a) | 29.0 (28.5b) | [S96] |
| MMMs | PIM-1/silica | 2000 | 5060 | 2330 | 880 | - | 10100 | 2.7 | 12.0 | - | [S118] |
|  | PIM-1/CC3 (10:1) | 740 |  | 560 | 150 | 230 | 3250 | 3.8 | 22 | 14.1 | [S12] |
|  | PIM-1/CC3 (10:3) | 820 |  | 820 | 270 | 480 | 5430 | 3.0 | 20 | 11.3 | [S12] |
|  | PIM-1/CC3 (10:1) (ethanol treated) | 2310 |  | 3150 | 1350 | 2050 | 18780 |  | 14 | 9.2 | [S12] |
|  | PIM-1/CC3 (10:3) (ethanol treated) | 4380 |  | 6810 | 3270 | 7220 | 37400 | 2.1 | 11 | 5.2 | [S12] |
|  | AO−PIM-1/UiO-66(Zr) |  | 1069 | 206 | 51 | 55 | 1380 | 4 | 27.1 | 25 | [S8] |
|  | f-SWCNTs/PIM-1 | 1355 |  | 1680 | 713 | 1483 | 12274 | 2.4 | 17.2 | 8.3 | [S11] |
|  | PIM-1/silicalite-1(MFI) |  | 894 | 351 | 83 | 183 | 2530 | 4.2 | 30 |  | [S119] |
|  | PIM-1/ZIF-8 | 1430 | 2980 | 870 | 195 | 230 | 4270 | 4.5 | 21.9* | 18.6 | [S120] |
|  | PIM-1/PAF-1 |  |  |  |  |  | 15000* |  | 11* |  | [S13] |
|  | PIM-1/POSS |  |  |  |  |  | 6730 (5650*b) |  | 16* | 11* (11*b) | [S121] |
|  | UV-PIM-1/ZIF-71 |  |  | 599.4 | 93.6 | 72.1 (67.8b) | 2545.7 (2224.3b) | 6.4 | 27.2 | 35.3 (32.8b) | [S16] |
|  | PIM-1/UiO-66 |  |  |  |  |  | 5340 |  | 21* |  | [S122] |
|  | PIM-1/Ti-UiO-66 |  |  |  |  |  | 13540 |  | 20* |  | [S122] |
|  | PIM-1/crosslinked MOF-74 |  | 11469 | 2251 | 742 | 1114 | 21269 | 3.0 | 19.1 | 28.7 | [S17] |
|  | PIM-1/g-C3N4 |  | 3830 |  | 354 | 503 | 5785 |  | 16.3 | 11.5 | [S20] |
|  | PIM-1/HCP |  |  |  | 243 |  | 4700 |  | 19.3 |  | [S123] |
|  | PIM-1/TSIL@NH2−MIL-101(Cr) |  |  |  |  |  | 2979 |  | 37.24 |  | [S23] |
|  | PIM-1/BILP-101 |  |  |  | 470 |  | 7200 |  | 15.3 |  | [S24] |
|  | PIM-1/UiO-66 | 2120 | 4560 | 1360 | 368 | 527 | 7610 | 3.7 | 20.7 | 14.4 | [S27] |
|  | PIM-1/UiO-66−NH2 | 1340 | 3130 | 1090 | 303 | 425 | 6340 | 3.6 | 20.9 | 14.9 | [S27] |
|  | PIM-1/UiO-66−(COOH)2 | 1820 | 3740 | 1220 | 296 | 401 | 6090 | 4.1 | 20.6 | 15.2 | [S27] |
|  | PIM-1/PEG-POSS |  |  |  | 43 | 44 | 1309 |  | 31 | 30 | [S28] |
|  | PIM-1/PhE-POSS |  |  | 900* | 280* | 400* | 5000* | 3.2* | 17.9* | 12.5* | [S124] |
|  | PIM-1/SNW-1 |  |  |  |  |  | 7553 |  | 22.7 (22.1d) | 13.5 (12.9e) | [S26] |
|  | PAO−PIM-1/UiO-66−NH2 |  |  |  | 306 | 366 | 8425 |  | 27.5 | 23.0 | [S125] |
|  | PIM-1/OPAS |  | 2476 | 789.5 | 157.1 | 201.2 | 3266 (3600*b) | 5.02 | 20.8 (14.9*a) | 16.2 (9.0*b) | [S30] |
|  | PIM-1/MFM-300(VIII) |  |  |  |  |  | 4450 |  | 28.04 |  | [S126] |
|  | PIM-1/UiO-66−NH2 |  | 2641 | 658 | 104 | 102 | 2869 (2573*b) |  | 27.5 (25.4*a) | 28.3 (31.4*b) | [S31] |
|  | PIM-1/β-CD |  | 3889 | 1647 | 481 | 716 (770*b) | 8812 (8907*b) | 3.5 | 18.3 | 12.3 (11.6*b) | [S32] |
|  | PIM-1/DNPC |  |  |  | 3266 |  | 40544 |  | 12.4 |  | [S35] |
|  | PIM-1/NUS-8 nanosheet |  |  |  | (389a) | (463b) | (6725a) (6462b) |  | (26.8a) | (30.1b) | [S35] |
|  | PIM-1/TPFC−CH2NH2 |  |  |  |  |  | 7730 |  | 45.9 | 36.4 | [S127] |
|  | PIM-1/Azo-DMOF-1 |  |  |  | 433 (371a) |  | 8095 (7500a) |  | 18.7 (20.2a) |  | [S36] |
|  | PIM-1/rGO−OA |  |  |  |  | (360b) | (5700b) |  |  | (17.4b) | [S37] |
|  | PIM-1/GO |  |  |  | 50 |  | 6169 |  | 123.5 |  | [S38] |
|  | PIM-1/ZIF-67 |  | 3542 |  | 215 | 310 | 5206 (5206e) |  | 24.2 | 16.8 (14.9e) | [S40] |
|  | PIM-1/crosslinked UiO-66−NH2_12h |  |  | 1942 | 555 | 828 (830b) | 15815 (15813b) | 3.5 | 28.5 | 19.1 (19.2b) | [S41] |
|  | PIM-1/crosslinked UiO-66−NH2_72h |  |  | 945 | 230 | 392 | 12498 | 4.1 | 54.2 | 31.9 | [S41] |
|  | PIM-1/ K2B12H12 |  | 4025 | 1831 | 772 | 1436 | 12954 | 2.4 | 16.8 | 9.0 | [S42] |
|  | PIM-1/MAPDA |  |  |  | 329.0 (117.7*a) |  | 7861.9 (4807.5*a) |  | 23.9 (40.1*a) |  | [S45] |
|  | PIM-1/6FDA-DAM/ZIF-8 |  |  |  |  |  | (2802f) (2891b) |  | (18.1f) | (26.6b) | [S46] |
|  | PIM-1/DMBA-Silica |  |  |  |  |  | 7930 |  | 16.8 |  | [S47] |
|  | PIM-1/PDASS |  |  |  | 47.3 |  | 1678 |  | 35 |  | [S48] |
|  | UiO-66−CN@sPIM-1 |  |  |  | 596 (225.5a) |  | 16121.3 (12063.3a) |  | 27.0 (53.5a) |  | [S49] |
|  | PIM-1/MIL-101 | 6900 |  | 6540 | 2320 | 3040 | 35600 | 2.82 | 15.3 | 11.7 | [S50] |
|  | PIM-1/pDCX |  | 9710 | 3800 | 1130 | 1650 | 20550 | 3.4 | 18.2 | 12.4 | [S128] |
|  | PIM-1/OH−pDCX |  | 5230 | 1470 | 300 | 380 | 8510 | 4.8 | 28.0 | 22.4 | [S128] |
|  | PIM-1/UiO-66 |  |  |  |  |  | (13000*g) |  | (14*g) |  | [S51] |
|  | PIM-1/azo−UiO-66 |  |  |  |  |  | (11000g) |  | (19g) |  | [S51] |
|  | PIM-1/MOF-801 |  |  | 1752 | 362 |  | 9686 | 4.8 | 27 |  | [S52] |
|  | PIM-1/LCD |  |  |  |  | (1050b) | (12510b) |  |  | (11.9b) | [S54] |
|  | PIM-1/MUF-15 |  |  |  | 810 (670a) | 1870 | 16120 (13180a) |  | 19.80 (19.57a) | 8.60 | [S55] |
|  | PIM-1-ZIF-7−NH2 |  |  |  |  | 143 | 2953 (2832e) |  |  | 20.6 (19.8e) | [S58] |
|  | PIM-1/nanosized ZIF-67 |  |  |  |  |  | 2805 (2567e) |  |  | 21.1 (19.89e) | [S59] |
|  | PIM-1/FCTF-1 |  |  |  |  |  | 7300 |  |  | 16.6 | [S70] |
|  | PIM-1/PIP-Py-X PIPs |  |  |  | 99.3 (124.2a) | 110.5 (142.8b) | 6204.8 (5300b) |  | 62.5 (41a) | 56.1 (37b) | [S60] |
|  | PIM-1/network PIM-1 nanosheet |  |  |  |  |  | (9778b) |  |  | (14.4b) | [S62] |
|  | PIM-1/QD-FCTF-1 |  |  |  |  | 222 | 4848 (4323*e) |  |  | 21.8 (22.0*e) | [S68] |
|  | PIM-1/(PIM-1-holey GO) |  |  |  |  | (360b) | (4727b) |  |  | (13.1b) | [S69] |
|  | PIM-1/(PIM-1-GO) |  |  |  |  | (176b) | (2073b) |  |  | (11.8b) | [S67] |
|  | PIM-1/IL@MOF-1 |  |  |  | 235 |  | 9420 |  | 29 |  | [S72] |
|  | cPIM-1/PPN |  | 5503 | 2008 | 474 | 519 | 11511 | 4.2 | 24.2 | 22.2 | [S73] |
|  | PIM-1/BNNS |  |  |  |  | (644b) | (5940b) |  |  | (9.3b) | [S74] |
|  | PIM-1/ZIF67 |  |  |  | 1426 | 1798 | 13256 |  | 9.3 | 7.4 | [S79] |
|  | PIM-1/TSIL-ZIF-67 |  |  |  | 936 | 1219 | 12849 (8545b) |  | 13.7 | 10.5 (9.3b) | [S79] |
|  | PIM-1/ZIF-8 |  |  |  |  | 852 | 9667 |  |  | 11.35 | [S80] |
|  | PIM-1/MOF-303 |  |  |  | 257.4 (280.9h) |  | 6602.8 (6199.2d) |  | 25.6 (22.1d) |  | [S81] |
|  | PIM-1/BcoC-ZIF |  |  |  |  |  | (7325a) |  | (32.5a) |  | [S129] |
|  | PIM-1/S-SN |  |  |  | (392a) | (771b) | (8631a) (9014b) |  | (22a) | (11.8b) | [S84] |
|  | PIM-1/KAUST-7 |  |  |  |  |  | (5928e) |  |  | (23.5e) | [S85] |
|  | PIM-1/rHGO−TAPA |  |  |  |  | (687b) | (8540b) |  |  | (12.7b) | [S87] |
|  | PIM-1/GO-POSS |  | 5004* |  | 559* (567a) | 1263* (1017b) | 11660* (11682a) (12185b) |  | (20.6a) | (12.0b) | [S88] |
|  | PIM-1/sulfonated-g-C3N4 |  | 2018 | 660 | 189 | 303 | 3740 |  | 19.8 | 12.4 | [S130] |
|  | PIM-1/[SHDBU][SIm]@ZIF-67 |  |  |  |  |  | 4721 |  |  | 14.3 | [S131] |
|  | PIM-1/[SNH2−Pmim][STf2N]@ZIF-67 |  |  |  |  |  | 9536 |  |  | 31.1 | [S89] |
|  | PIM-1/NUS-8−COOH |  |  |  |  |  | (11512b) |  | (30.95a) | (17b) | [S132] |
|  | PIM-1/NUS-8−NH2 |  |  |  |  |  | (14638b) |  | (29.2d) | (9e) | [S90] |
|  | PIM-1/UiO-66-FA |  |  |  |  |  | (16591a) |  | (23.1a) |  | [S91] |
|  | PIM-1/PAF-1+UV |  | 4769 |  | 68 | 53 | 2081 |  | 30.6 | 39.3 | [S133] |
|  | PIM-1/UiO-66−(OH)2 |  | 9168 |  |  | 1958.9 | 18017 |  | 9.2 | 6.1 | [S93] |
|  | PIM-1/HZIF-8-TA |  |  |  | 201 (292f) | 441 (398b) | 8268 (6495f) (6352b) |  | 25.1 (21.9f) | 18.7 (16.2b) | [S94] |
|  | PIM-1/PDA@TD-COF |  |  |  | 369.6 |  | 9750.6 |  | 26.3 |  | [S95] |
|  | PIM-1/Ag+@UiO-66 |  |  |  |  |  | (14943f) |  | (30f) |  | [S98] |
|  | PIM-1/CILs@PAR |  |  | 144.7 |  |  |  | 5.0 |  |  | [S134] |
|  | PIM-1/C2NxO1−x |  |  |  |  |  | 22110 (20391f) |  | 15.5 (17.1f) | 12.5 | [S135] |
|  | PIM-1/TpTta–COF |  |  |  |  |  | 9672 |  | 26.3 |  | [S99] |
|  | PIM-1/ZIF-62 |  |  |  |  | 110.8 | 5500 |  |  | 50 | [S100] |
|  | PIM-1/ZIF-62 glass |  |  |  |  | 88.7 | 5914 |  |  | 67 | [S100] |
|  | PIM-1/NH2−IL-UiO-66 |  |  |  |  |  | 10839 |  | 31.4 |  | [S136] |
|  | PIM-1-COOH/UiO-66−NH2 | 955 | 2045 | 500 | 119 | 136 | 2750 | 4.2 | 23 | 21 | [S137] |
|  | PIM-1/ (Zn-SiF6-py) |  |  |  |  |  | 6268 |  | 26.3 |  | [S103] |
|  | PIM-1/IL@COF |  |  |  |  |  | 9137.5 (8477.6g) |  | 20.2 (19.6g) |  | [S104] |
|  | PIM-1/MXene |  |  |  |  |  | 12475 (10800f) |  | 32.7 (30.5f) |  | [S138] |
|  | PIM-1/ZIF-8 gel |  | 6800 |  |  | 1002 |  |  |  |  | [S139] |
|  | PIM-1/HO−UiO-66-PLs |  |  |  |  |  | 7211 |  | 26 |  | [S140] |

* Data based on extracted values from figures in literature. Data in parentheses indicate mixture separation data, feed gases are listed as follows: a: CO2/N2 (1:1); b: CO2/CH4 (1:1); c: CO2/N2 (4:6); d: CO2/N2 (2:8); e: CO2/CH4 (3:7); f: CO2/N2 (1:9); g: CO2/N2 (15:85).

Table S2 Gas separation performance of thick PIM-1 membranes after aging (at 20−40 ℃ and 1−4 bar)

|  | Membranes | Time (days) | Normalised CO2 permeability* | Normalised CO2/N2 selectivity | Normalised CO2/CH4 selectivity | Refs. |
| --- | --- | --- | --- | --- | --- | --- |
| Unmodified PIM-1 | PIM-1 | 10 | 0.59 (CH4) | - | - | [S43] |
|  | PIM-1 | 24 | 0.3 |  |  | [S122] |
|  | PIM-1 | 30 | 0.6 | 1.57 |  | [S51] |
|  | PIM-1 | 30 | 0.47 (CH4) | - | - | [S7] |
|  | PIM-1 | 30 | 0.61 |  |  | [S28] |
|  | PIM-1 | 30 | 0.76 |  |  | [S132] |
|  | PIM-1 | 35 | 0.73 | 0.83 | 0.87 | [S55] |
|  | PIM-1 | 40 | 0.67 |  | 1.10 | [S80] |
|  | PIM-1 | 45 | 0.79 |  | 1.08 | [S79] |
|  | PIM-1 | 50 | 0.53 |  |  | [S70] |
|  | PIM-1 | 60 | 0.22 |  |  | [S68] |
|  | PIM-1 | 60 | 0.61 |  |  | [S47] |
|  | PIM-1 | 63 | 0.19 |  |  | [S94] |
|  | PIM-1 | 70 | 0.53 | 0.53 |  | [S129] |
|  | PIM-1 | 80 | 0.14 |  |  | [S125] |
|  | PIM-1 | 90 | 0.65 |  |  | [S128] |
|  | PIM-1 | 90 | 0.46 |  |  | [S30] |
|  | PIM-1 | 100 | 0.4 |  |  | [S52] |
|  | PIM-1 | 100 | 0.42 |  |  | [S72] |
|  | PIM-1 | 100 | 0.39 | 1.19 |  | [S104] |
|  | PIM-1 | 105 | 0.43 | 1.28 | 1.32 | [S82] |
|  | PIM-1 | 120 | 0.3 |  |  | [S121] |
|  | PIM-1 | 120 | 0.62 |  | 1.58 | [S35] |
|  | PIM-1 | 120 | 0.50 |  |  | [S58] |
|  | PIM-1 | 120 | 0.28 |  |  | [S136] |
|  | PIM-1 | 120 | 0.48 |  |  | [S59] |
|  | PIM-1 | 120 | 0.80 | 1.75 | 1.7 | [S32] |
|  | PIM-1 | 120 | 0.58 |  |  | [S48] |
|  | PIM-1 | 150 | 0.51 |  |  | [S67] |
|  | PIM-1 | 150 | 0.53 |  | 1.33 | [S69] |
|  | PIM-1 | 150 | 0.37 |  |  | [S84] |
|  | PIM-1 | 150 | 0.34 |  |  | [S85] |
|  | PIM-1 | 150 | 0.34 |  |  | [S123] |
|  | PIM-1 | 155 | 0.31 |  | 1.47 | [S37] |
|  | PIM-1 | 160 | 0.44 |  |  | [S88] |
|  | PIM-1 | 160 | 0.31 |  | 1.54 | [S54] |
|  | PIM-1 | 160 | 0.26 |  |  | [S91] |
|  | PIM-1 | 180 | 0.49 |  |  | [S60] |
|  | PIM-1 | 180 | 0.32 | 1.22 | 1.53 | [S73] |
|  | PIM-1 | 180 | 0.23 | 1.07 | 1.11 | [S141] |
|  | PIM-1 | 200 | 0.41 |  |  | [S20] |
|  | PIM-1 | 210 | 0.45 |  |  | [S127] |
|  | PIM-1 | 240 | 0.48 | 1.27 | - | [S13] |
|  | PIM-1 | 310 | 0.36 | - | - | [S12] |
|  | PIM-1 | 360 | 0.27 |  | 1.34 | [S87] |
|  | PIM-1 | 381 | 0.44 |  |  | [S71] |
|  | PIM-1 | 400 | 0.17 |  | 1.2 | [S41] |
|  | PIM-1 | 414 | 0.42 |  | 1.2 | [S74] |
|  | PIM-1 | 414 | 0.42 |  | 1.2 | [S74] |
|  | PIM-1 | 455 | 0.39 | 1.80 | 1.52 | [S111] |
|  | PIM-1 | 600 | 0.28 |  |  | [S130] |
|  | PIM-1 | 1000 | 0.5 |  |  | [S50] |
| Chain modification | PIM-1 120℃, 81 min | 44 | 0.74 |  |  | [S108] |
|  | PIM-1−SO3H | 60 | 0.26 |  | 1.64 | [S75] |
|  | PIM-1/Py | 87 | 0.41 |  |  | [S97] |
|  | PIM-1/MePy | 87 | 0.45 |  |  | [S97] |
|  | PIM-1 160℃, 33 min | 96 | 1.47 |  |  | [S108] |
|  | PIM-C1 | 180 | 0.39 | 0.84 | 0.91 | [S141] |
|  | PIM-1−NH2 | 448 | 0.45 |  |  | [S71] |
| Post-modification | Thermally crosslinked PIM-1 | 10 | 0.81 (CH4) | - | - | [S43] |
|  | PIM-UV 30 min | 30 | 0.85 (CH4) | - | - | [S7] |
|  | PIM-1-O3 | 30 | 0.81 | 0.95 | 0.85 | [S86] |
|  | Amine-PIM-1 | 42 | 0.88 |  |  | [S39] |
|  | f-PIM-1 | 60 | 0.98 | 1.21 | 1.31 | [S77] |
|  | NA-PIM-1 | 60 | 0.5 | 0.99 |  | [S92] |
|  | NA-PIM-1-Zn-PEI | 60 | 0.59 | 1.08 |  | [S92] |
|  | Aminated PIM-1 | 100 | 0.63 | 0.91 |  | [S102] |
|  | SCPIMs | 100 | 0.35 | 1.38 | 1.71 | [S56] |
|  | PIM-1−deBOC(acid) | 180 | 0.3 | 1.85 | 3.25 | [S64] |
|  | PIM-1−deBOC(thermal) | 180 | 0.35 | 1.05 | 1.62 | [S64] |
|  | PIM-1−deBOC | 180 | 0.4 | 1.25 | 1.6 | [S64] |
|  | PIM-1−NH2 | 180 | 0.6 | 1.7 | 2.7 | [S64] |
|  | PIM-1−tBOC | 180 | 0.8 | 0.9 | 0.99 | [S64] |
|  | f-PIM-1 | 300 | 0.75 | 0.87 | 0.46 | [S113] |
|  | TOX-PIM-1 | 455 | 0.28 | 1.03 | 1.1 | [S111] |
| Blends | PIM-1/MEEP80 | 60 | 0.65 | 0.9 |  | [S44] |
| MMMs | PIM-1/TpTta–COF | 15 | 0.99 | 0.95 |  | [S99] |
|  | PIM-1/PDA@TD-COF | 15 | 0.83 | 1.02 |  | [S95] |
|  | PIM-1/azo-UiO-66 | 30 | 0.73 | 1.36 |  | [S51] |
|  | PIM-1/NUS-8−COOH | 30 | 0.89 | 0.85 |  | [S132] |
|  | PIM-1/PEG-POSS | 30 | 0.77 |  |  | [S28] |
|  | PIM-1-COOH/UiO-66−NH2 | 31 | 0.41 | 1.14 | 1.37 | [S137] |
|  | PIM-1/MUF-15 | 35 | 0.64 | 1.28 | 1.45 | [S55] |
|  | PIM-1/ZIF-8 | 40 | 0.41 |  | 1.22 | [S80] |
|  | PIM-1/TSIL-ZIF-67 | 45 | 0.86 |  | 1.09 | [S79] |
|  | PIM-1/ZIF67 | 45 | 0.75 |  | 1.03 | [S79] |
|  | PIM-1/FCTF-1 | 50 | 0.58 |  |  | [S70] |
|  | PIM-1/QD-FCTF-1 | 60 | 0.39 |  |  | [S68] |
|  | PIM-1/PAF-1+UV | 60 | 0.78 |  |  | [S133] |
|  | PIM-1/DMBA-Silica | 60 | 0.9 | 1.03 |  | [S47] |
|  | PIM-1/HZIF-8-TA | 63 | 0.23 |  |  | [S94] |
|  | PIM-1/Ti-UiO-66 | 63 | 0.3 |  |  | [S122] |
|  | PIM-1/BcoC-ZIF | 70 | 0.7 | 1.12 |  | [S129] |
|  | PAO-PIM-1/UiO-66−NH2 | 80 | 0.69 |  |  | [S125] |
|  | PIM-1/OH-pDCX | 90 | 0.75 |  |  | [S128] |
|  | PIM-1/UiO-66 | 90 | 0.52 |  | 1.52 | [S27] |
|  | PIM-1/OAPS | 90 | 0.70 |  |  | [S30] |
|  | PIM-1/HO-UiO-66-PLs | 100 | 0.74 | 1.26 |  | [S140] |
|  | PIM-1/IL@MOF-1 | 100 | 0.74 | 0.97 |  | [S72] |
|  | PIM-1/IL@COF | 100 | 0.66 |  |  | [S104] |
|  | PIM-1/MOF-801 | 100 | 0.70 | 1.07 |  | [S52] |
|  | PIM-1/TiO2 | 105 | 0.55 | 1.24 | 1.26 | [S82] |
|  | PIM-1/PDASS | 120 | 0.77 |  |  | [S48] |
|  | PIM-1/POSS | 120 | 0.4 |  |  | [S121] |
|  | PIM-1/nanosized ZIF-67 | 120 | 0.63 |  |  | [S59] |
|  | PIM-1/NUS-8 nanosheet | 120 | 0.77 |  | 1.19 | [S35] |
|  | PIM-1/ β-CD | 120 | 0.94 | 1.05 | 1.2 | [S32] |
|  | PIM-1/NH2-IL-UiO-66 | 120 | 0.81 | 1.25 |  | [S136] |
|  | PIM-1-ZIF-7−NH2 | 120 | 0.74 |  |  | [S58] |
|  | PIM-1/S-SN | 150 | 0.68 |  | 1.35 | [S84] |
|  | PIM-1/KAUST-7 | 150 | 0.91 |  | 1.17 | [S85] |
|  | PIM-1/(PIM-1-holey GO) | 150 | 0.7 |  | 1.08 | [S69] |
|  | PIM-1/(PIM-1-GO) | 150 | 0.85 |  |  | [S67] |
|  | PIM-1/HCP | 150 | 0.60 |  |  | [S123] |
|  | PIM-1/rGO-OAa | 155 | 0.61 |  | 1.32 | [S37] |
|  | PIM-1/UiO-66-FA | 160 | 0.75 | 1.27 |  | [S91] |
|  | PIM-1/GO-POSS | 160 | 0.74 |  |  | [S88] |
|  | PIM-1/LCD | 160 | 0.71 |  | 1.50 | [S54] |
|  | PIM-1/Al2O3 | 180 | 0.46 | 0.68 | 1.08 | [S76] |
|  | cPIM-1/PPN | 180 | 0.86 | 1.12 | 0.97 | [S73] |
|  | PIM-1/PIP-Py-AC PIPs | 180 | 0.66 |  |  | [S60] |
|  | PIM-1-g-C3N4 | 200 | 0.33 |  |  | [S20] |
|  | PIM-1/TPFC−CH2NH2 | 210 | 0.78 |  |  | [S127] |
|  | PIM-1/network PIM-1 nanosheet | 210 | 0.20 |  | 1.84* | [S62] |
|  | PIM-1/PAF-1 | 240 | 0.93 | 1.62 | - | [S13] |
|  | PIM-1-COOH | 330 | 0.26 |  | 1.21 | [S57] |
|  | PIM-1/UiO-66−NH2 | 350 | 0.52 | 1.05 |  | [S27] |
|  | PIM-1/in-situ crosslinked UiO-66-NH2 | 400 | 0.76 |  | 1.03 | [S41] |
|  | PIM-1/CC3 | 400 | 0.34 | 1.36 | - | [S12] |
|  | PIM-1/BNNS | 414 | 0.78 |  | 1.3 | [S74] |
|  | PIM-1/sulfinated-g-C3N4 | 600 | 0.25 | 1.04 | 1.21 | [S130] |
|  | PIM-1/rHGO-TAPA | 611 | 0.45 |  | 1.09 | [S87] |
|  | PIM-1/MIL-101 | 2555 | 0.11 | 1.76 |  | [S50] |

*Normalisation was conducted using the values from the same references for fresh membranes at day 0.

Table S3 Gas separation performance of PIM-1 TFC/TFN membranes after aging (at 20−40 ℃ and 1−4 bar)

| Membranes | Aging time (days) | Normalised CO2 permeance | Normalised CO2/N2 selectivity | Normalised CO2/CH4 selectivity | Refs. |
| --- | --- | --- | --- | --- | --- |
| PIM-1/CuBDC NS | 4 | 1.01 |  |  | [S142] |
| PIM-1 | 28 | 0.03 |  | 0.97 | [S84] |
| PIM-1/SN | 28 | 0.05 |  | 0.90 | [S84] |
| PIM-1/S-SN | 28 | 0.14 |  | 1.18 | [S84] |
| PIM-1, #3b, network content 7.8 wt.% | 28 | 0.08 | 0.71 |  | [S108] |
| PIM-1. #1, network content 0.8 wt.% | 28 | 0.03 | 0.32 |  | [S109] |
| PIM-1. #3, network content 85.3 wt.% | 28 | 0.91 | 0.43 |  | [S109] |
| Blended 20%PIM-1#3 in PIM-1#1 | 28 | 0.59 | 0.90 |  | [S109] |
| PIM-1 | 28 | 0.29 | 0.73 | 0.93 | [S143] |
| PIM-1/OAPS | 30 | 0.14 |  |  | [S30] |
| PIM-1/OAPS | 30 | 0.02 |  |  | [S30] |
| PIM-1 | 30 | 0.11 |  |  | [S30] |
| PIM-1 | 30 | 0.01 |  |  | [S30] |
| PIM-1 | 56 | 0.11 | 1.63 |  | [S144] |
| PIM-1/Ni-MOF-74 | 56 | 0.24 | 0.97 |  | [S144] |
| PIM-1/UiO-66−NH2 | 56 | 0.12 | 1 |  | [S144] |
| B-cPIM-1 | 60 | 1.56 | 1.72 | 1.47 | [S145] |
| B-PIM-1 | 60 | 0.35 | 1.05 | 1.09 | [S145] |
| D-PIM-1 | 60 | 0.15 | 1.64 | 2.53 | [S145] |
| D-cPIM-1 | 60 | 0.48 | 0.71 | 0.76 | [S145] |
| PIM-1 | 63 | 0.46 |  |  | [S94] |
| PIM-1/ZIF-8 | 63 | 0.27 |  |  | [S94] |
| PIM-1/HZIF-8-TA | 63 | 0.14 |  |  | [S94] |
| PIM-1/C-UiO-66−NH2/cPIM-1 | 63 | 0.94 | 1.16 | 1.08 | [S143] |
| PIM-1 | 90 | 0.12 | 1.73 |  | [S146] |
| PIM-1/HCP | 90 | 0.32 | 1.52 |  | [S146] |
| PIM-1/C-HCP | 90 | 0.35 | 1.71 |  | [S146] |
| PIM-1/PTMSP | 98 | 0.03 | 0.97 |  | [S147] |
| PIM-1 | 360 | 0.27 |  |  | [S87] |
| PIM-1/rHGO-TAPA | 365 | 0.81 |  |  | [S87] |
| PIM-1 | 360 | 0.27 |  |  | [S87] |

Supplementary References

[S1] P. M. Budd, K. J. Msayib, C. E. Tattershall, B. S. Ghanem, K. J. Reynolds et al., Gas separation membranes from polymers of intrinsic microporosity. J. Membr. Sci. 251, 263–269 (2005). https://doi.org/10.1016/j.memsci.2005.01.009

[S2] P. M. Budd, N. B. McKeown, B. S. Ghanem, K. J. Msayib, D. Fritsch et al., Gas permeation parameters and other physicochemical properties of a polymer of intrinsic microporosity: Polybenzodioxane PIM-1. J. Membr. Sci. 325, 851–860 (2008). https://doi.org/10.1016/j.memsci.2008.09.010

[S3] N. Du, G. P. Robertson, J. Song, I. Pinnau, S. Thomas et al., Polymers of intrinsic microporosity containing trifluoromethyl and phenylsulfone groups as materials for membrane gas separation. Macromolecules 41, 9656–9662 (2008). https://doi.org/10.1021/ma801858d

[S4] C. L. Staiger, S. J. Pas, A. J. Hill, C. J. Cornelius, Gas separation, free volume distribution, and physical aging of a highly microporous spirobisindane polymer. Chem. Mater. 20, 2606–2608 (2008). https://doi.org/10.1021/cm071722t

[S5] S. Thomas, I. Pinnau, N. Du, M. D. Guiver, Pure- and mixed-gas permeation properties of a microporous spirobisindane-based ladder polymer (PIM-1). J. Membr. Sci. 333, 125–131 (2009). https://doi.org/10.1016/j.memsci.2009.02.003

[S6] N. Du, M. M. Dal-Cin, G. P. Robertson, M. D. Guiver, Decarboxylation-induced cross-linking of polymers of intrinsic microporosity (PIMs) for membrane gas separation. Macromolecules 45, 5134–5139 (2012). https://doi.org/10.1021/ma300751s

[S7] F. Y. Li, Y. Xiao, Y. K. Ong, T.-S. Chung, UV-rearranged PIM-1 polymeric membranes for advanced hydrogen purification and production. Adv. Energy Mater. 2, 1456–1466 (2012). https://doi.org/10.1002/aenm.201200296

[S8] I.-D. Carja, S. R. Tavares, O. Shekhah, A. Ozcan, R. Semino et al., Insights into the enhancement of MOF/polymer adhesion in mixed-matrix membranes via polymer functionalization. ACS Appl. Mater. Interfaces 13, 29041–29047 (2021). https://doi.org/10.1021/acsami.1c03859

[S9] Q. Song, S. Cao, P. Zavala-Rivera, L. Ping Lu, W. Li et al., Photo-oxidative enhancement of polymeric molecular sieve membranes. Nat. Commun. 4, 1918 (2013). https://doi.org/10.1038/ncomms2942

[S10] N. Du, G. P. Robertson, M. M. Dal-Cin, L. Scoles, M. D. Guiver, Polymers of intrinsic microporosity (PIMs) substituted with methyl tetrazole. Polymer 53, 4367–4372 (2012). https://doi.org/10.1016/j.polymer.2012.07.055

[S11] M. M. Khan, V. Filiz, G. Bengtson, S. Shishatskiy, M. M. Rahman et al., Enhanced gas permeability by fabricating mixed matrix membranes of functionalized multiwalled carbon nanotubes and polymers of intrinsic microporosity (PIM). J. Membr. Sci. 436, 109–120 (2013). https://doi.org/10.1016/j.memsci.2013.02.032

[S12] A. F. Bushell, P. M. Budd, M. P. Attfield, J. T. A. Jones, T. Hasell et al., Nanoporous organic polymer/cage composite membranes. Angew. Chem. Int. Ed. 52, 1253–1256 (2013). https://doi.org/10.1002/anie.201206339

[S13] C. H. Lau, P. T. Nguyen, M. R. Hill, A. W. Thornton, K. Konstas et al., Ending aging in super glassy polymer membranes. Angew. Chem. Int. Ed. 53, 5322–5326 (2014). https://doi.org/10.1002/anie.201402234

[S14] R. Swaidan, B. S. Ghanem, E. Litwiller, I. Pinnau, Pure- and mixed-gas CO₂/CH₄ separation properties of PIM-1 and an amidoxime-functionalized PIM-1. J. Membr. Sci. 457, 95–102 (2014). https://doi.org/10.1016/j.memsci.2014.01.055

[S15] X. Mei Wu, Q. Gen Zhang, P. Ju Lin, Y. Qu, A. Mei Zhu et al., Towards enhanced CO₂ selectivity of the PIM-1 membrane by blending with polyethylene glycol. J. Membr. Sci. 493, 147–155 (2015). https://doi.org/10.1016/j.memsci.2015.05.077

[S16] L. Hao, K.-S. Liao, T.-S. Chung, Photo-oxidative PIM-1 based mixed matrix membranes with superior gas separation performance. J. Mater. Chem. A 3, 17273–17281 (2015). https://doi.org/10.1039/C5TA03776J

[S17] N. Tien-Binh, H. Vinh-Thang, X. Y. Chen, D. Rodrigue, S. Kaliaguine, Crosslinked MOF-polymer to enhance gas separation of mixed matrix membranes. J. Membr. Sci. 520, 941–950 (2016). https://doi.org/10.1016/j.memsci.2016.08.045

[S18] W. F. Yong, F. Y. Li, Y. C. Xiao, P. Li, K. P. Pramoda et al., Molecular engineering of PIM-1/Matrimid blend membranes for gas separation. J. Membr. Sci. 407, 47–57 (2012). https://doi.org/10.1016/j.memsci.2012.03.038

[S19] H. Zhao, Q. Xie, X. Ding, J. Chen, M. Hua et al., High performance post-modified polymers of intrinsic microporosity (PIM-1) membranes based on multivalent metal ions for gas separation. J. Membr. Sci. 514, 305–312 (2016). https://doi.org/10.1016/j.memsci.2016.05.013

[S20] Z. Tian, S. Wang, Y. Wang, X. Ma, K. Cao et al., Enhanced gas separation performance of mixed matrix membranes from graphitic carbon nitride nanosheets and polymers of intrinsic microporosity. J. Membr. Sci. 514, 15–24 (2016). https://doi.org/10.1016/j.memsci.2016.04.019

[S21] W. F. Yong, Z. K. Lee, T.-S. Chung, M. Weber, C. Staudt et al., Blends of a polymer of intrinsic microporosity and partially sulfonated polyphenylenesulfone for gas separation. ChemSusChem 9, 1953–1962 (2016). https://doi.org/10.1002/cssc.201600354

[S22] J. Zhang, H. Kang, J. Martin, S. Zhang, S. Thomas et al., The enhancement of chain rigidity and gas transport performance of polymers of intrinsic microporosity via intramolecular locking of the spiro-carbon. Chem. Commun. 52, 6553–6556 (2016). https://doi.org/10.1039/C6CC02308H

[S23] J. Ma, Y. Ying, X. Guo, H. Huang, D. Liu et al., Fabrication of mixed-matrix membrane containing metal–organic framework composite with task-specific ionic liquid for efficient CO₂ separation. J. Mater. Chem. A 4, 7281–7288 (2016). https://doi.org/10.1039/C6TA02611G

[S24] A. K. Sekizkardes, V. A. Kusuma, G. Dahe, E. A. Roth, L. J. Hill et al., Separation of carbon dioxide from flue gas by mixed matrix membranes using dual phase microporous polymeric constituents. Chem. Commun. 52, 11768–11771 (2016). https://doi.org/10.1039/C6CC04811K

[S25] J. W. Jeon, D.-G. Kim, E.-h. Sohn, Y. Yoo, Y. S. Kim et al., Highly carboxylate-functionalized polymers of intrinsic microporosity for CO₂-selective polymer membranes. Macromolecules 50, 8019–8027 (2017). https://doi.org/10.1021/acs.macromol.7b01332

[S26] X. Wu, Z. Tian, S. Wang, D. Peng, L. Yang et al., Mixed matrix membranes comprising polymers of intrinsic microporosity and covalent organic framework for gas separation. J. Membr. Sci. 528, 273–283 (2017). https://doi.org/10.1016/j.memsci.2017.01.042

[S27] M. R. Khdhayyer, E. Esposito, A. Fuoco, M. Monteleone, L. Giorno et al., Mixed matrix membranes based on UiO-66 MOFs in the polymer of intrinsic microporosity PIM-1. Sep. Purif. Technol. 173, 304–313 (2017). https://doi.org/10.1016/j.seppur.2016.09.036

[S28] L. Yang, Z. Tian, X. Zhang, X. Wu, Y. Wu et al., Enhanced CO₂ selectivities by incorporating CO₂-philic PEG-POSS into polymers of intrinsic microporosity membrane. J. Membr. Sci. 543, 69–78 (2017). https://doi.org/10.1016/j.memsci.2017.08.050

[S29] K. Halder, M. M. Khan, J. Grünauer, S. Shishatskiy, C. Abetz et al., Blend membranes of ionic liquid and polymers of intrinsic microporosity with improved gas separation characteristics. J. Membr. Sci. 539, 368–382 (2017). https://doi.org/10.1016/j.memsci.2017.06.022

[S30] Y. Kinoshita, K. Wakimoto, A. H. Gibbons, A. P. Isfahani, H. Kusuda et al., Enhanced PIM-1 membrane gas separation selectivity through efficient dispersion of functionalized POSS fillers. J. Membr. Sci. 539, 178–186 (2017). https://doi.org/10.1016/j.memsci.2017.05.072

[S31] B. Ghalei, K. Sakurai, Y. Kinoshita, K. Wakimoto, Ali P. Isfahani et al., Enhanced selectivity in mixed matrix membranes for CO₂ capture through efficient dispersion of amine-functionalized MOF nanoparticles. Nat. Energy 2, 17086 (2017). https://doi.org/10.1038/nenergy.2017.86

[S32] J. Liu, Y. Xiao, K.-S. Liao, T.-S. Chung, Highly permeable and aging resistant 3D architecture from polymers of intrinsic microporosity incorporated with beta-cyclodextrin. J. Membr. Sci. 523, 92–102 (2017). https://doi.org/10.1016/j.memsci.2016.10.001

[S33] S. Zhao, J. Liao, D. Li, X. Wang, N. Li, Blending of compatible polymer of intrinsic microporosity (PIM-1) with Tröger's base polymer for gas separation membranes. J. Membr. Sci. 566, 77–86 (2018). https://doi.org/10.1016/j.memsci.2018.08.010

[S34] N. Du, G. P. Robertson, J. Song, I. Pinnau, M. D. Guiver, High-performance carboxylated polymers of intrinsic microporosity (PIMs) with tunable gas transport properties. Macromolecules 42, 6038–6043 (2009). https://doi.org/10.1021/ma9009017

[S35] Y. Cheng, S. R. Tavares, C. M. Doherty, Y. Ying, E. Sarnello et al., Enhanced polymer crystallinity in mixed-matrix membranes induced by metal–organic framework nanosheets for efficient CO₂ capture. ACS Appl. Mater. Interfaces 10, 43095–43103 (2018). https://doi.org/10.1021/acsami.8b16386

[S36] N. Prasetya, B. P. Ladewig, New azo-DMOF-1 MOF as a photoresponsive low-energy CO₂ adsorbent and its exceptional CO₂/N₂ separation performance in mixed matrix membranes. ACS Appl. Mater. Interfaces 10, 34291–34301 (2018). https://doi.org/10.1021/acsami.8b12261

[S37] M. Alberto, R. Bhavsar, J. M. Luque-Alled, A. Vijayaraghavan, P. M. Budd et al., Impeded physical aging in PIM-1 membranes containing graphene-like fillers. J. Membr. Sci. 563, 513–520 (2018). https://doi.org/10.1016/j.memsci.2018.06.026

[S38] M. Chen, F. Soyekwo, Q. Zhang, C. Hu, A. Zhu et al., Graphene oxide nanosheets to improve permeability and selectivity of PIM-1 membrane for carbon dioxide separation. J. Ind. Eng. Chem. 63, 296–302 (2018). https://doi.org/10.1016/j.jiec.2018.02.030

[S39] B. Satilmis, M. Lanč, A. Fuoco, C. Rizzuto, E. Tocci et al., Temperature and pressure dependence of gas permeation in amine-modified PIM-1. J. Membr. Sci. 555, 483–496 (2018). https://doi.org/10.1016/j.memsci.2018.03.039

[S40] X. Wu, W. Liu, H. Wu, X. Zong, L. Yang et al., Nanoporous ZIF-67 embedded polymers of intrinsic microporosity membranes with enhanced gas separation performance. J. Membr. Sci. 548, 309–318 (2018). https://doi.org/10.1016/j.memsci.2017.11.038

[S41] N. Tien-Binh, D. Rodrigue, S. Kaliaguine, In-situ cross-interface linking of PIM-1 polymer and UiO-66-NH₂ for outstanding gas separation and physical aging control. J. Membr. Sci. 548, 429–438 (2018). https://doi.org/10.1016/j.memsci.2017.11.054

[S42] M. M. Khan, S. Shishatskiy, V. Filiz, Mixed matrix membranes of boron icosahedron and polymers of intrinsic microporosity (PIM-1) for gas separation. Membranes 8, (2018). https://doi.org/10.3390/membranes8010001

[S43] F. Y. Li, Y. Xiao, T.-S. Chung, S. Kawi, High-performance thermally self-cross-linked polymer of intrinsic microporosity (PIM-1) membranes for energy development. Macromolecules 45, 1427–1437 (2012). https://doi.org/10.1021/ma202667y

[S44] A. K. Sekizkardes, V. A. Kusuma, J. S. McNally, D. W. Gidley, K. Resnik et al., Microporous polymeric composite membranes with advanced film properties: Pore intercalation yields excellent CO₂ separation performance. J. Mater. Chem. A 6, 22472–22477 (2018). https://doi.org/10.1039/C8TA07424K

[S45] G. Yu, Y. Li, Z. Wang, T. X. Liu, G. Zhu et al., Mixed matrix membranes derived from nanoscale porous organic frameworks for permeable and selective CO₂ separation. J. Membr. Sci. 591, 117343 (2019). https://doi.org/10.1016/j.memsci.2019.117343

[S46] J. Sánchez-Laínez, A. Pardillos-Ruiz, M. Carta, R. Malpass-Evans, N. B. McKeown et al., Polymer engineering by blending PIM-1 and 6FDA-DAM for ZIF-8 containing mixed matrix membranes applied to CO₂ separations. Sep. Purif. Technol. 224, 456–462 (2019). https://doi.org/10.1016/j.seppur.2019.05.035

[S47] N. Sakaguchi, M. Tanaka, M. Yamato, H. Kawakami, Superhigh CO₂-permeable mixed matrix membranes composed of a polymer of intrinsic microporosity (PIM-1) and surface-modified silica nanoparticles. ACS Appl. Polym. Mater. 1, 2516–2524 (2019). https://doi.org/10.1021/acsapm.9b00624

[S48] G. Dong, J. Zhang, Z. Wang, J. Wang, P. Zhao et al., Interfacial property modulation of PIM-1 through polydopamine-derived submicrospheres for enhanced CO₂/N₂ separation performance. ACS Appl. Mater. Interfaces 11, 19613–19622 (2019). https://doi.org/10.1021/acsami.9b02281

[S49] G. Yu, X. Zou, L. Sun, B. Liu, Z. Wang et al., Constructing connected paths between UiO-66 and PIM-1 to improve membrane CO₂ separation with crystal-like gas selectivity. Adv. Mater. 31, 1806853 (2019). https://doi.org/10.1002/adma.201806853

[S50] M. Khdhayyer, A. F. Bushell, P. M. Budd, M. P. Attfield, D. Jiang et al., Mixed matrix membranes based on MIL-101 metal–organic frameworks in polymer of intrinsic microporosity PIM-1. Sep. Purif. Technol. 212, 545–554 (2019). https://doi.org/10.1016/j.seppur.2018.11.055

[S51] N. Prasetya, B. P. Ladewig, An insight into the effect of azobenzene functionalities studied in UiO-66 frameworks for low-energy CO₂ capture and CO₂/N₂ membrane separation. J. Mater. Chem. A 7, 15164–15172 (2019). https://doi.org/10.1039/C9TA02096A

[S52] W. Chen, Z. Zhang, L. Hou, C. Yang, H. Shen et al., Metal-organic framework MOF-801/PIM-1 mixed-matrix membranes for enhanced CO₂/N₂ separation performance. Sep. Purif. Technol. 250, 117198 (2020). https://doi.org/10.1016/j.seppur.2020.117198

[S53] M. D. Guiver, M. Yahia, M. M. Dal-Cin, G. P. Robertson, S. Saeedi Garakani et al., Gas transport in a polymer of intrinsic microporosity (PIM-1) substituted with pseudo-ionic liquid tetrazole-type structures. Macromolecules 53, 8951–8959 (2020). https://doi.org/10.1021/acs.macromol.0c01321

[S54] M. Tamaddondar, A. B. Foster, M. Carta, P. Gorgojo, N. B. McKeown et al., Mitigation of physical aging with mixed matrix membranes based on cross-linked PIM-1 fillers and PIM-1. ACS Appl. Mater. Interfaces 12, 46756–46766 (2020). https://doi.org/10.1021/acsami.0c13838

[S55] H. Yin, A. Alkaş, Y. Zhang, Y. Zhang, S. G. Telfer, Mixed matrix membranes (MMMs) using an emerging metal-organic framework (MUF-15) for CO₂ separation. J. Membr. Sci. 609, 118245 (2020). https://doi.org/10.1016/j.memsci.2020.118245

[S56] S. Zhou, Y. Sun, B. Xue, S. Li, J. Zheng et al., Controlled superacid-catalyzed self-cross-linked polymer of intrinsic microporosity for high-performance CO₂ separation. Macromolecules 53, 7988–7996 (2020). https://doi.org/10.1021/acs.macromol.0c01590

[S57] K. Mizrahi Rodriguez, A. X. Wu, Q. Qian, G. Han, S. Lin et al., Facile and time-efficient carboxylic acid functionalization of PIM-1: Effect on molecular packing and gas separation performance. Macromolecules 53, 6220–6234 (2020). https://doi.org/10.1021/acs.macromol.0c00933

[S58] Y. Wang, Y. Ren, H. Wu, X. Wu, H. Yang et al., Amino-functionalized ZIF-7 embedded polymers of intrinsic microporosity membrane with enhanced selectivity for biogas upgrading. J. Membr. Sci. 602, 117970 (2020). https://doi.org/10.1016/j.memsci.2020.117970

[S59] C. Ye, X. Wu, H. Wu, L. Yang, Y. Ren et al., Incorporating nano-sized ZIF-67 to enhance selectivity of polymers of intrinsic microporosity membranes for biogas upgrading. Chem. Eng. Sci. 216, 115497 (2020). https://doi.org/10.1016/j.ces.2020.115497

[S60] C. Wang, F. Guo, H. Li, J. Xu, J. Hu et al., A porous ionic polymer bionic carrier in a mixed matrix membrane for facilitating selective CO₂ permeability. J. Membr. Sci. 598, 117677 (2020). https://doi.org/10.1016/j.memsci.2019.117677

[S61] Z. Wang, Q. Shen, J. Liang, Y. Zhang, J. Jin, Adamantane-grafted polymer of intrinsic microporosity with finely tuned interchain spacing for improved CO₂ separation performance. Sep. Purif. Technol. 233, 116008 (2020). https://doi.org/10.1016/j.seppur.2019.116008

[S62] M. Tamaddondar, A. B. Foster, J. M. Luque-Alled, K. J. Msayib, M. Carta et al., Intrinsically microporous polymer nanosheets for high-performance gas separation membranes. Macromol. Rapid Commun. 41, 1900572 (2020). https://doi.org/10.1002/marc.201900572

[S63] X. Chen, Z. Zhang, L. Wu, X. Liu, S. Xu et al., Polymers of intrinsic microporosity having bulky substitutes and cross-linking for gas separation membranes. ACS Appl. Polym. Mater. 2, 987–995 (2020). https://doi.org/10.1021/acsapm.9b01193

[S64] K. Mizrahi Rodriguez, S. Lin, A. X. Wu, G. Han, J. J. Teesdale et al., Leveraging free volume manipulation to improve the membrane separation performance of amine-functionalized PIM-1. Angew. Chem. Int. Ed. 60, 6593–6599 (2021). https://doi.org/10.1002/anie.202012441

[S65] A. K. Sekizkardes, S. Budhathoki, L. Zhu, V. Kusuma, Z. Tong et al., Molecular design and fabrication of PIM-1/polyphosphazene blend membranes with high performance for CO₂/N₂ separation. J. Membr. Sci. 640, 119764 (2021). https://doi.org/10.1016/j.memsci.2021.119764

[S66] W. Ji, K. Li, Y.-G. Min, W. Shi, J. Li et al., Remarkably enhanced gas separation properties of PIM-1 at sub-ambient temperatures. J. Membr. Sci. 623, 119091 (2021). https://doi.org/10.1016/j.memsci.2021.119091

[S67] J. M. Luque-Alled, A. W. Ameen, M. Alberto, M. Tamaddondar, A. B. Foster et al., Gas separation performance of MMMs containing (PIM-1)-functionalized GO derivatives. J. Membr. Sci. 623, 118902 (2021). https://doi.org/10.1016/j.memsci.2020.118902

[S68] H. Jiang, Z. Guo, H. Wang, X. Liu, Y. Ren et al., Solvent-processable 0D covalent organic framework quantum dot engineered composite membranes for biogas upgrading. J. Membr. Sci. 640, 119803 (2021). https://doi.org/10.1016/j.memsci.2021.119803

[S69] J. M. Luque-Alled, M. Tamaddondar, A. B. Foster, P. M. Budd, P. Gorgojo, PIM-1/holey graphene oxide mixed matrix membranes for gas separation: Unveiling the role of holes. ACS Appl. Mater. Interfaces 13, 55517–55533 (2021). https://doi.org/10.1021/acsami.1c15640

[S70] H. Jiang, J. Zhang, T. Huang, J. Xue, Y. Ren et al., Mixed-matrix membranes with covalent triazine framework fillers in polymers of intrinsic microporosity for CO₂ separations. Ind. Eng. Chem. Res. 59, 5296–5306 (2020). https://doi.org/10.1021/acs.iecr.9b04632

[S71] K. Mizrahi Rodriguez, F. M. Benedetti, N. Roy, A. X. Wu, Z. P. Smith, Sorption-enhanced mixed-gas transport in amine functionalized polymers of intrinsic microporosity (PIMs). J. Mater. Chem. A 9, 23631–23642 (2021). https://doi.org/10.1039/D1TA06530K

[S72] W. Chen, Z. Zhang, C. Yang, J. Liu, H. Shen et al., PIM-based mixed-matrix membranes containing MOF-801/ionic liquid nanocomposites for enhanced CO₂ separation performance. J. Membr. Sci. 636, 119581 (2021). https://doi.org/10.1016/j.memsci.2021.119581

[S73] W. Han, C. Zhang, M. Zhao, F. Yang, Y. Yang et al., Post-modification of PIM-1 and simultaneously in situ synthesis of porous polymer networks into PIM-1 matrix to enhance CO₂ separation performance. J. Membr. Sci. 636, 119544 (2021). https://doi.org/10.1016/j.memsci.2021.119544

[S74] A. W. Ameen, J. Ji, M. Tamaddondar, S. Moshenpour, A. B. Foster et al., 2D boron nitride nanosheets in PIM-1 membranes for CO₂/CH₄ separation. J. Membr. Sci. 636, 119527 (2021). https://doi.org/10.1016/j.memsci.2021.119527

[S75] H. Dong, Z. Zhu, K. Li, Q. Li, W. Ji et al., Significantly improved gas separation properties of sulfonated PIM-1 by direct sulfonation using SO₃ solution. J. Membr. Sci. 635, 119440 (2021). https://doi.org/10.1016/j.memsci.2021.119440

[S76] X. Chen, L. Wu, H. Yang, Y. Qin, X. Ma et al., Tailoring the microporosity of polymers of intrinsic microporosity for advanced gas separation by atomic layer deposition. Angew. Chem. Int. Ed. 60, 17875–17880 (2021). https://doi.org/10.1002/anie.202016901

[S77] X. Ma, K. Li, Z. Zhu, H. Dong, J. Lv et al., High-performance polymer molecular sieve membranes prepared by direct fluorination for efficient helium enrichment. J. Mater. Chem. A 9, 18313–18322 (2021). https://doi.org/10.1039/D1TA04099E

[S78] Z. Gao, Y. Wang, H. Wu, Y. Ren, Z. Guo et al., Surface functionalization of polymers of intrinsic microporosity (PIMs) membrane by polyphenol for efficient CO₂ separation. Green Chem. Eng. 2, 70–76 (2021). https://doi.org/10.1016/j.gce.2020.12.003

[S79] J. Han, L. Bai, H. Jiang, S. Zeng, B. Yang et al., Task-specific ionic liquids tuning ZIF-67/PIM-1 mixed matrix membranes for efficient CO₂ separation. Ind. Eng. Chem. Res. 60, 593–603 (2021). https://doi.org/10.1021/acs.iecr.0c04830

[S80] M. Yahia, Q. N. Phan Le, N. Ismail, M. Essalhi, O. Sundman et al., Effect of incorporating different ZIF-8 crystal sizes in the polymer of intrinsic microporosity, PIM-1, for CO₂/CH₄ separation. Micropor. Mesopor. Mater. 312, 110761 (2021). https://doi.org/10.1016/j.micromeso.2020.110761

[S81] Q. Shen, S. Cong, J. Zhu, Y. Zhang, R. He et al., Novel pyrazole-based MOF synergistic polymer of intrinsic microporosity membranes for high-efficient CO₂ capture. J. Membr. Sci. 664, 121107 (2022). https://doi.org/10.1016/j.memsci.2022.121107

[S82] X. Niu, G. Dong, D. Li, Y. Zhang, Y. Zhang, Atomic layer deposition modified PIM-1 membranes for improved CO₂ separation: A comparative study on the microstructure-performance relationships. J. Membr. Sci. 664, 121103 (2022). https://doi.org/10.1016/j.memsci.2022.121103

[S83] G. Ferraro, C. Astorino, M. Bartoli, A. Martis, S. Lettieri et al., Ionic liquids-polymer of intrinsic microporosity (PIMs) blend membranes for CO₂ separation. Membranes 12, (2022). https://doi.org/10.3390/membranes12121262

[S84] S. Mohsenpour, Z. Guo, F. Almansour, S. M. Holmes, P. M. Budd et al., Porous silica nanosheets in PIM-1 membranes for CO₂ separation. J. Membr. Sci. 661, 120889 (2022). https://doi.org/10.1016/j.memsci.2022.120889

[S85] K. Chen, L. Ni, H. Zhang, C. Xiao, L. Li et al., Incorporating KAUST-7 into PIM-1 towards mixed matrix membranes with long-term stable CO₂/CH₄ separation performance. J. Membr. Sci. 661, 120848 (2022). https://doi.org/10.1016/j.memsci.2022.120848

[S86] W. Ji, H. Geng, Z. Chen, H. Dong, H. Matsuyama et al., Facile tailoring molecular sieving effect of PIM-1 by in-situ O₃ treatment for high performance hydrogen separation. J. Membr. Sci. 662, 120971 (2022). https://doi.org/10.1016/j.memsci.2022.120971

[S87] F. Almansour, M. Alberto, A. B. Foster, S. Mohsenpour, P. M. Budd et al., Thin film nanocomposite membranes of superglassy PIM-1 and amine-functionalised 2D fillers for gas separation. J. Mater. Chem. A 10, 23341–23351 (2022). https://doi.org/10.1039/D2TA06339E

[S88] S. Mohsenpour, A. W. Ameen, S. Leaper, C. Skuse, F. Almansour et al., PIM-1 membranes containing POSS - graphene oxide for CO₂ separation. Sep. Purif. Technol. 121447, (2022). https://doi.org/10.1016/j.seppur.2022.121447

[S89] Z. Zhang, X. Cao, C. Geng, Y. Sun, Y. He et al., Machine learning aided high-throughput prediction of ionic liquid@MOF composites for membrane-based CO₂ capture. J. Membr. Sci. 650, 120399 (2022). https://doi.org/10.1016/j.memsci.2022.120399

[S90] Y. Pu, Z. Yang, V. Wee, Z. Wu, Z. Jiang et al., Amino-functionalized NUS-8 nanosheets as fillers in PIM-1 mixed matrix membranes for CO₂ separations. J. Membr. Sci. 641, 119912 (2022). https://doi.org/10.1016/j.memsci.2021.119912

[S91] C. Geng, Y. Sun, Z. Zhang, Z. Qiao, C. Zhong, Mitigated aging in a defective metal–organic framework pillared polymer of an intrinsic porosity hybrid membrane for efficient gas separation. ACS Sustainable Chem. Eng. 10, 3643–3650 (2022). https://doi.org/10.1021/acssuschemeng.1c08485

[S92] J. Guan, X. Wang, J. Du, Q. Liang, W. He et al., Surface-engineered PIM-1 membranes for facile CO₂ capture. Chem. Eng. J. 477, 147017 (2023). https://doi.org/10.1016/j.cej.2023.147017

[S93] Y. Sun, F. Fan, L. Bai, T. Li, J. Guan et al., Hydrogen-bonded hybrid membranes based on hydroxylated metal-organic frameworks and PIM-1 for ultrafast hydrogen separation. Results Eng. 20, 101398 (2023). https://doi.org/10.1016/j.rineng.2023.101398

[S94] B. Zhu, S. He, Y. Yang, S. Li, C. H. Lau et al., Boosting membrane carbon capture via multifaceted polyphenol-mediated soldering. Nat. Commun. 14, 1697 (2023). https://doi.org/10.1038/s41467-023-37479-9

[S95] X. Chang, H. Guo, Q. Chang, Z. Tian, Y. Zhang et al., Mixed-matrix membranes composed of dopamine modified covalent organic framework and PIM-1 for efficient CO₂/N₂ separation. J. Membr. Sci. 686, 122017 (2023). https://doi.org/10.1016/j.memsci.2023.122017

[S96] H. Amir, R. Tamime, Z. Shamair, A. L. Khan, H. AlMohamadi et al., Enhanced gas separation performance of PIM-1 blend membranes incorporating ionic liquid (3-(trimethoxysilyl) propan-1-aminium acetate ([SAPTMS][SAc])) as filler: Investigation of morphology, compatibility and transport properties. Fuel 349, 128669 (2023). https://doi.org/10.1016/j.fuel.2023.128669

[S97] S. Kang, G. Huo, Z. Zhang, T. Guo, Z. Dai et al., Polymers of intrinsic porosity with bulky side groups on the spirobisindane moieties for gas separation. ACS Appl. Polym. Mater. 5, 8660–8669 (2023). https://doi.org/10.1021/acsapm.3c01762

[S98] Z. Lin, Z. Yuan, K. Wang, X. He, Synergistic tuning mixed matrix membranes by Ag⁺-doping in UIO-66-NH₂/polymers of intrinsic microporosity for remarkable CO₂/N₂ separation. J. Membr. Sci. 681, 121775 (2023). https://doi.org/10.1016/j.memsci.2023.121775

[S99] G. Dai, Q. Zhang, S. Xiong, L. Deng, Z. Gao et al., Building interfacial compatible PIM-1-based mixed-matrix membranes with β-ketoenamine-linked COF fillers for effective CO₂/N₂ separation. J. Membr. Sci. 676, 121561 (2023). https://doi.org/10.1016/j.memsci.2023.121561

[S100] Y. Feng, W. Yan, Z. Kang, X. Zou, W. Fan et al., Thermal treatment optimization of porous MOF glass and polymer for improving gas permeability and selectivity of mixed matrix membranes. Chem. Eng. J. 465, 142873 (2023). https://doi.org/10.1016/j.cej.2023.142873

[S101] Y. Sun, J. Zhang, H. Li, F. Fan, Q. Zhao et al., Ester-crosslinked polymers of intrinsic microporosity membranes with enhanced plasticization resistance for CO₂ separation. Sep. Purif. Technol. 314, 123623 (2023). https://doi.org/10.1016/j.seppur.2023.123623

[S102] L. Chen, P. Su, J. Liu, S. Chen, J. Huang et al., Post-synthesis amination of polymer of intrinsic microporosity membranes for CO₂ separation. AIChE J. 69, e18050 (2023). https://doi.org/10.1002/aic.18050

[S103] Z. Liu, S. Cong, J. Zhang, G. Dong, Y. Zhang, Mixed matrix membrane with amorphous metal-based complexes displays high CO₂ separation performance. Sep. Purif. Technol. 330, 125349 (2024). https://doi.org/10.1016/j.seppur.2023.125349

[S104] Q. Chang, H. Guo, Z. Shang, C. Zhang, Y. Zhang et al., PIM-based mixed matrix membranes containing covalent organic frameworks/ionic liquid composite materials for effective CO₂/N₂ separation. Sep. Purif. Technol. 330, 125518 (2024). https://doi.org/10.1016/j.seppur.2023.125518

[S105] N. Du, H. B. Park, G. P. Robertson, M. M. Dal-Cin, T. Visser et al., Polymer nanosieve membranes for CO₂-capture applications. Nat. Mater. 10, 372–375 (2011). https://doi.org/10.1038/nmat2989

[S106] C. R. Mason, L. Maynard-Atem, N. M. Al-Harbi, P. M. Budd, P. Bernardo et al., Polymer of intrinsic microporosity incorporating thioamide functionality: Preparation and gas transport properties. Macromolecules 44, 6471–6479 (2011). https://doi.org/10.1021/ma200918h

[S107] K. Halder, S. Neumann, G. Bengtson, M. M. Khan, V. Filiz et al., Polymers of intrinsic microporosity postmodified by vinyl groups for membrane applications. Macromolecules 51, 7309–7319 (2018). https://doi.org/10.1021/acs.macromol.8b01252

[S108] A. B. Foster, M. Tamaddondar, J. M. Luque-Alled, W. J. Harrison, Z. Li et al., Understanding the topology of the polymer of intrinsic microporosity PIM-1: Cyclics, tadpoles, and network structures and their impact on membrane performance. Macromolecules 53, 569–583 (2020). https://doi.org/10.1021/acs.macromol.9b02185

[S109] A. B. Foster, J. L. Beal, M. Tamaddondar, J. M. Luque-Alled, B. Robertson et al., Importance of small loops within PIM-1 topology on gas separation selectivity in thin film composite membranes. J. Mater. Chem. A 9, 21807–21823 (2021). https://doi.org/10.1039/D1TA03712A

[S110] N. Du, M. M. Dal-Cin, I. Pinnau, A. Nicalek, G. P. Robertson et al., Azide-based cross-linking of polymers of intrinsic microporosity (PIMs) for condensable gas separation. Macromol. Rapid Commun. 32, 631–636 (2011). https://doi.org/10.1002/marc.201000775

[S111] Q. Song, S. Cao, R. H. Pritchard, B. Ghalei, S. A. Al-Muhtaseb et al., Controlled thermal oxidative crosslinking of polymers of intrinsic microporosity towards tunable molecular sieve membranes. Nat. Commun. 5, 4813 (2014). https://doi.org/10.1038/ncomms5813

[S112] S. He, X. Jiang, S. Li, F. Ran, J. Long et al., Intermediate thermal manipulation of polymers of intrinsic microporous (PIMs) membranes for gas separations. AIChE J. 66, e16543 (2020). https://doi.org/10.1002/aic.16543

[S113] N. A. Belov, A. Y. Alentiev, R. Y. Nikiforov, S. V. Chirkov, D. A. Bezgin et al., Gas separation properties of PIM-1 films treated by elemental fluorine in liquid perfluorodecalin. Polymer 280, 126033 (2023). https://doi.org/10.1016/j.polymer.2023.126033

[S114] W. F. Yong, F. Y. Li, T.-S. Chung, Y. W. Tong, Highly permeable chemically modified PIM-1/Matrimid membranes for green hydrogen purification. J. Mater. Chem. A 1, 13914–13925 (2013). https://doi.org/10.1039/C3TA13308G

[S115] W. F. Yong, F. Y. Li, T. S. Chung, Y. W. Tong, Molecular interaction, gas transport properties and plasticization behavior of cPIM-1/Torlon blend membranes. J. Membr. Sci. 462, 119–130 (2014). https://doi.org/10.1016/j.memsci.2014.03.046

[S116] W. F. Yong, T.-S. Chung, Miscible blends of carboxylated polymers of intrinsic microporosity (cPIM-1) and Matrimid. Polymer 59, 290–297 (2015). https://doi.org/10.1016/j.polymer.2015.01.013

[S117] G. Bengtson, S. Neumann, V. Filiz, Membranes of polymers of intrinsic microporosity (PIM-1) modified by poly(ethylene glycol). Membranes 7, (2017). https://doi.org/10.3390/membranes7020028

[S118] J. Ahn, W.-J. Chung, I. Pinnau, J. Song, N. Du et al., Gas transport behavior of mixed-matrix membranes composed of silica nanoparticles in a polymer of intrinsic microporosity (PIM-1). J. Membr. Sci. 346, 280–287 (2010). https://doi.org/10.1016/j.memsci.2009.09.047

[S119] C. R. Mason, M. G. Buonomenna, G. Golemme, P. M. Budd, F. Galiano et al., New organophilic mixed matrix membranes derived from a polymer of intrinsic microporosity and silicalite-1. Polymer 54, 2222–2230 (2013). https://doi.org/10.1016/j.polymer.2013.02.032

[S120] A. F. Bushell, M. P. Attfield, C. R. Mason, P. M. Budd, Y. Yampolski et al., Gas permeation parameters of mixed matrix membranes based on the polymer of intrinsic microporosity PIM-1 and the zeolitic imidazolate framework ZIF-8. J. Membr. Sci. 427, 48–62 (2013). https://doi.org/10.1016/j.memsci.2012.09.035

[S121] W. F. Yong, K. H. A. Kwek, K.-S. Liao, T.-S. Chung, Suppression of aging and plasticization in highly permeable polymers. Polymer 77, 377–386 (2015). https://doi.org/10.1016/j.polymer.2015.09.075

[S122] S. J. D. Smith, B. P. Ladewig, A. J. Hill, C. H. Lau, M. R. Hill, Post-synthetic Ti-exchanged UiO-66 metal-organic frameworks that deliver exceptional gas permeability in mixed matrix membranes. Sci. Rep. 5, 7823 (2015). https://doi.org/10.1038/srep07823

[S123] T. Mitra, R. S. Bhavsar, D. J. Adams, P. M. Budd, A. I. Cooper, PIM-1 mixed matrix membranes for gas separations using cost-effective hypercrosslinked nanoparticle fillers. Chem. Commun. 52, 5581–5584 (2016). https://doi.org/10.1039/C6CC00261G

[S124] N. Konnertz, Y. Ding, W. J. Harrison, P. M. Budd, A. Schönhals et al., Molecular mobility and gas transport properties of nanocomposites based on PIM-1 and polyhedral oligomeric phenethyl-silsesquioxanes (POSS). J. Membr. Sci. 529, 274–285 (2017). https://doi.org/10.1016/j.memsci.2017.02.007

[S125] Z. Wang, H. Ren, S. Zhang, F. Zhang, J. Jin, Polymers of intrinsic microporosity/metal–organic framework hybrid membranes with improved interfacial interaction for high-performance CO₂ separation. J. Mater. Chem. A 5, 10968–10977 (2017). https://doi.org/10.1039/C7TA01773A

[S126] C. G. Morris, N. M. Jacques, H. G. W. Godfrey, T. Mitra, D. Fritsch et al., Stepwise observation and quantification and mixed matrix membrane separation of CO₂ within a hydroxy-decorated porous host. Chem. Sci. 8, 3239–3248 (2017). https://doi.org/10.1039/C6SC04343G

[S127] C. Wang, F. Guo, H. Li, J. Xu, J. Hu et al., Porous organic polymer as fillers for fabrication of defect-free PIM-1-based mixed matrix membranes with facilitating CO₂-transfer chain. J. Membr. Sci. 564, 115–122 (2018). https://doi.org/10.1016/j.memsci.2018.07.018

[S128] R. Hou, S. J. D. Smith, C. D. Wood, R. J. Mulder, C. H. Lau et al., Solvation effects on the permeation and aging performance of PIM-1-based MMMs for gas separation. ACS Appl. Mater. Interfaces 11, 6502–6511 (2019). https://doi.org/10.1021/acsami.8b19207

[S129] Y. Sun, C. Geng, Z. Zhang, Z. Qiao, C. Zhong, Two-dimensional basic cobalt carbonate supported ZIF-67 composites towards mixed matrix membranes for efficient CO₂/N₂ separation. J. Membr. Sci. 661, 120928 (2022). https://doi.org/10.1016/j.memsci.2022.120928

[S130] B. K. Voon, H. Shen Lau, C. Z. Liang, W. F. Yong, Functionalized two-dimensional g-C₃N₄ nanosheets in PIM-1 mixed matrix membranes for gas separation. Sep. Purif. Technol. 296, 121354 (2022). https://doi.org/10.1016/j.seppur.2022.121354

[S131] J. Han, H. Jiang, S. Zeng, Y. Bai, X. Zhang et al., CO₂ separation performance for PIM-based mixed matrix membranes embedded by superbase ionic liquids. J. Mol. Liq. 359, 119375 (2022). https://doi.org/10.1016/j.molliq.2022.119375

[S132] D. Wang, Y. Ying, Y. Zheng, Y. Pu, Z. Yang et al., Induced polymer crystallinity in mixed matrix membranes by metal-organic framework nanosheets for gas separation. J. Membr. Sci. Lett. 2, 100017 (2022). https://doi.org/10.1016/j.memlet.2022.100017

[S133] R. Hou, S. J. D. Smith, K. Konstas, C. M. Doherty, C. D. Easton et al., Synergistically improved PIM-1 membrane gas separation performance by PAF-1 incorporation and UV irradiation. J. Mater. Chem. A 10, 10107–10119 (2022). https://doi.org/10.1039/D2TA00138A

[S134] H. Zhao, T. Song, X. Ding, R. Cai, X. Tan et al., PIM-1 mixed matrix membranes incorporated with magnetic responsive cobalt-based ionic liquid for O₂/N₂ separation. J. Membr. Sci. 679, 121713 (2023). https://doi.org/10.1016/j.memsci.2023.121713

[S135] Z. Tian, D. Li, W. Zheng, Q. Chang, Y. Sang et al., Heteroatom-doped noble carbon-tailored mixed matrix membranes with ultrapermeability for efficient CO₂ separation. Mater. Horiz. 10, 3660–3667 (2023). https://doi.org/10.1039/D3MH00463E

[S136] C. Geng, Y. Sun, Z. Zhang, Z. Qiao, C. Zhong, Mixed matrix metal-organic framework membranes for efficient CO₂/N₂ separation under humid conditions. AIChE J. 69, e18025 (2023). https://doi.org/10.1002/aic.18025

[S137] W.-N. Wu, K. Mizrahi Rodriguez, N. Roy, J. J. Teesdale, G. Han et al., Engineering the polymer–MOF interface in microporous composites to address complex mixture separations. ACS Appl. Mater. Interfaces 15, 52893–52907 (2023). https://doi.org/10.1021/acsami.3c11300

[S138] K. Wang, D. Chen, J. Tang, Z. Hong, Z. Zhu et al., PIM-1-based membranes mediated with CO₂-philic MXene nanosheets for superior CO₂/N₂ separation. Chem. Eng. J. 483, 149305 (2024). https://doi.org/10.1016/j.cej.2024.149305

[S139] K. Zhang, X. Luo, S. Li, X. Tian, Q. Wang et al., ZIF-8 gel/PIM-1 mixed matrix membranes for enhanced H₂/CH₄ separations. Chem. Eng. J. 484, 149489 (2024). https://doi.org/10.1016/j.cej.2024.149489

[S140] F. Wang, Z. Wang, J. Yu, S. Han, X. Li et al., Mixed matrix membranes with intrinsic microporous/UiO-66 post-synthesis modifications with no defects for efficient CO₂/N₂ separation. Sep. Purif. Technol. 333, 125892 (2024). https://doi.org/10.1016/j.seppur.2023.125892

[S141] M. Liu, X. Lu, M. D. Nothling, C. M. Doherty, L. Zu et al., Physical aging investigations of a spirobisindane-locked polymer of intrinsic microporosity. ACS Materials Lett. 2, 993–998 (2020). https://doi.org/10.1021/acsmaterialslett.0c00184

[S142] Y. Cheng, X. Wang, C. Jia, Y. Wang, L. Zhai et al., Ultrathin mixed matrix membranes containing two-dimensional metal-organic framework nanosheets for efficient CO₂/CH₄ separation. J. Membr. Sci. 539, 213–223 (2017). https://doi.org/10.1016/j.memsci.2017.06.011

[S143] B. Qiu, M. Yu, J. M. Luque-Alled, S. Ding, A. B. Foster et al., High gas permeability in aged superglassy membranes with nanosized UiO-66-NH₂/CPIM-1 network fillers. Angew. Chem. Int. Ed. 63, e202316356 (2024). https://doi.org/10.1002/anie.202316356

[S144] M. Liu, M. D. Nothling, P. A. Webley, J. Jin, Q. Fu et al., High-throughput CO₂ capture using PIM-1@MOF-based thin film composite membranes. Chem. Eng. J. 396, 125328 (2020). https://doi.org/10.1016/j.cej.2020.125328

[S145] M. Yu, A. B. Foster, M. Alshurafa, J. M. Luque-Alled, P. Gorgojo et al., CO₂ separation using thin film composite membranes of acid-hydrolyzed PIM-1. J. Membr. Sci. 679, 121697 (2023). https://doi.org/10.1016/j.memsci.2023.121697

[S146] R. S. Bhavsar, T. Mitra, D. J. Adams, A. I. Cooper, P. M. Budd, Ultrahigh-permeance PIM-1-based thin film nanocomposite membranes on PAN supports for CO₂ separation. J. Membr. Sci. 564, 878–886 (2018). https://doi.org/10.1016/j.memsci.2018.07.089

[S147] I. Borisov, D. Bakhtin, J. M. Luque-Alled, A. Rybakova, V. Makarova et al., Synergistic enhancement of gas selectivity in thin film composite membranes of PIM-1. J. Mater. Chem. A 7, 6417–6430 (2019). https://doi.org/10.1039/C8TA10691F