Supporting Information for

Light-Management in 2D Perovskite towards High-Performance Optoelectronic Applications

Kailian Dong1, Tao Jiang1, Guoyi Chen1, Hongsen Cui1, Shuxin Wang1, Shun Zhou1, Chen Wang1, Yi Yang1, *, Fang Yao2, Chen Tao 2, Weijun Ke1, *, Guojia Fang 1, 2 *

1Key Lab of Artificial Micro- and Nano-Structures of Ministry of Education of China,School of Physics and Technology, Wuhan University, Wuhan 430072, P. R. China

2School of Electronic and Electrical Engineering, Wuhan Textile University, Wuhan 430200, P. R. China

Corresponding authors. E-mail: weijun.ke@whu.edu.cn (Weijun Ke); gjfang@whu.edu.cn (Guojia Fang)

Supplementary Figures and Tables

Fig. S1 a-c Schematic diagram of the BPB structure. Hirshfeld dnorm surface of BDA2+ cation d. The hydrogen bonds within BPB e. Corresponding 2D fingerprint plots of BPB f

Fig. S2 Top SEM images of surface-patterned MPs a-b and its magnified ones c-d

Fig. S3 EDS mapping of Br a and Pb b distribution

Fig. S4 Enlarged cross-sectional SEM of patterned BPB MPs

Fig. S5 AFM and corresponding height of nanochannels

Fig. S6 Simulated XRD patten of BPB a. XRD patten and FWHM of flat BPB b

Fig. S7 Photoconductivity measurement of flat BPB MPs

Fig. S8 XRD patterns of BPB MPs before and after storage under ambient with approximately 70% humidity a. TGA curve of the BPB perovskite b

Fig. S9 Optical microscope images of the patterned PD a and flat PD b

Fig. S10 Transient photocurrents of the optimized surface-patterned BPB PD under different light intensity at 5V a and 10 b bias

Fig. S11 Long-term dark current of patterned BPB PD under different biases

Fig. S12 -3 dB curves of patterned BPB PD at different biases

Fig. S13 a R, b D*, and c EQE curves of patterned BPB PD as function of wavelength under different voltages

Fig. S14 The photocurrent response of the patterned BPB PD a under modulated light illumination and b continuous light illumination. I - t curves of the patterned BPB PD after storage c under approximately 70% relative humidity and d post-annealing at 150 ℃

Table S1 Comparison of our PD with other 2D DJ-type perovskite SCs-based PDs

| Material | Responsivity (mA/W) | Detectivity (Jones) | LDR (dB) | Detection Limit (nW/cm2) | On/off ratio | Dark current (A) | Refs. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| BDAPbI4 | 927 | 1.2×1011 | 150 | 8.8 | 2×104 | 4.2×10-12 | [S1] |
| PDAPbBr4 | 7.92 | 8.3×1010 | - | - | 246 | 5.7×10-11 | [S2] |
| DPAPbBr4 | 2444 | 3.85×1011 | 154 | 7.1 | 4.89×104 | 4.55×10-13 | [S3] |
| DMPDPbBr4 | 29.2 | 1.73×1012 | - | - | 5.3×103 | 2.69×10-12 | [S4] |
| 2AMPYPbBr4 | 36 | 3.2×1011 | - | - | 103 | 2.87×10-11 | [S5] |
| (NMPD)PbBr4 | 386 | 5.26×1012 | - | - | 9×103 | 3.4×10-11 | [S6] |
| (HDA)CsPb2Br7 | 0.21 | 1.5×109 | - | - | < 4×103 | 2.34×10-11 | [S7] |
| (NMPDA)Pb2I4Br2 | 280 | 3.05×1012 | - | 1.094×104 | 3.92×103 | 4.2×10-11 | [S8] |
| (3AMPY)(MA)Pb2Br7 | 81.1 | 1.78×1012 | - | 70 | 103 | 1.1×10-10 | [S9] |
| (3AMPY)(EA)Pb2Br7 | 827.4 | 8.67×1012 | - | ~25 | 2.3×104 | 3.49×10-11 | [S10] |
| BDAPbBr4 | 2240 | 7.91×1012 | 134.13 | 68.7 | 4.79×103 | 4.47×10-13 | This work |

Supplementary References

- Y. Zhang, Y. Liu, Z. Xu, Z. Yang, S. Liu, 2D Perovskite Single Crystals with Suppressed Ion Migration for High-Performance Planar-Type Photodetectors. Small 16, 2003145 (2020). https://doi.org/10.1002/smll.202003145

- W. Yang, J. Hu, J. Chen, Y. Xu, G. Tong, H. Fan, X. Chai, J. Chen, Y. He, Diamine tailored smooth and continuous perovskite single crystal with enhanced photoconductivity. J. Mater. Chem. C 9, 1303-1309 (2021). https://doi.org/10.1039/d0tc04746e

- K. Dong, X. Yang, F. Yao, H. Cong, H. Zhou, S. Zhou, H. Cui, S. Wang, C. Tao, C. Sun, H. Fu, W. Ke, G. Fang, Spacer Conformation Induced Multiple Hydrogen Bonds in 2D Perovskite toward Highly Efficient Optoelectronic Devices. Adv. Mater. 36, 2313889 (2024). https://doi.org/10.1002/adma.202313889

- G. Tong, Y. Chen, X. Xiao, J. Tang, B. He, S. Cao, M. Li, Y. He, J. Chen, Asymmetric Diammonium Directed In-Plane Charge Transport Enhancement in Two-Dimensional Lead Bromide Perovskite for Weak-Light Detection. ACS Appl. Mater. Inter. 14, 53065-53073 (2022). https://doi.org/10.1021/acsami.2c15570

- D. Fu, S. Wu, W. Cao, Z. Chen, X.-M. Zhang, Interlayer cation engineering to regulate the photoelectric properties of lead bromide Dion-Jacobson hybrid perovskites. J. Mater. Chem. C 10, 9613-9620 (2022). https://doi.org/10.1039/d2tc01623k

- D. Fu, Y. Ma, C.-Y. Su, Z. Chen, D.-W. Fu, Amplification of polarization ratio is observed in monolayer Dion–Jacobson hybrid perovskites. J. Mater. Chem. C 11, 11492-11499 (2023). https://doi.org/10.1039/d3tc01926h

- T. Yang, Y. Li, S. Han, Z. Xu, Y. Liu, X. Zhang, X. Liu, B. Teng, J. Luo, Z. Sun, Highly-Anisotropic Dion-Jacobson Hybrid Perovskite by Tailoring Diamine into CsPbBr3 for Polarization-Sensitive Photodetection. Small 16, 1907020 (2020). https://doi.org/10.1002/smll.201907020

- B. He, K. Kuang, G. Tong, J. Tang, S. Cao, Z. Yu, M. Li, Y. He, J. Chen, Halide Ordering Enables Superior Charge Transport in 3D (NMPDA)Pb2I4Br2 Perovskitoid Single Crystal. Small 20, 2305990 (2023). https://doi.org/10.1002/smll.202305990

- Z. Hou, Y. He, W. Cao, D. Fu, Incorporating an Aromatic Diammonium To Assemble Bilayered Dion-Jacobson Perovskite Crystals for Weak Light Detection. J. Phys. Chem. Lett. 14, 4304-4312 (2023). https://doi.org/10.1021/acs.jpclett.3c00755

- D. Fu, W. Jia, S. Wu, J. Chang, Z. Chen, J. Luo, Bilayered Dion–Jacobson Hybrid Perovskite Bulk Single Crystals Constructed with Aromatic Diammonium for Ultraviolet–Visible–Near-Infrared Photodetection. Chem. Mater. 35, 2541-2548 (2023). https://doi.org/10.1021/acs.chemmater.2c03815