Supporting Information for

Multifunctional Carbon Foam with Nanoscale Chiral Magnetic Heterostructures for Broadband Microwave Absorption in Low Frequency

Hao Zhang1, Kaili Kuang1, Yifeng Zhang1, Chen Sun1, Tingkang Yuan1, Ruilin Yin1, Zeng Fan1, Renchao Che2, * and Lujun Pan1, *

1 School of Physics, Dalian University of Technology, Dalian, Liaoning 116024, P. R. China

2 Laboratory of Advanced Materials, Shanghai Key Lab of Molecular Catalysis and Innovative Materials, Department of Materials Science, Fudan University, Shanghai 200438, P. R. China

*Corresponding authors. E-mail: lpan@dlut.edu.cn (Lujun Pan), rcche@fudan.edu.cn (Renchao Che)

Supplementary Figures and Tables

Fig. S1  SEM images of (a-c) CF samples and (d-f) FCF samples

Fig. S2  (a) XRD patterns, (b, c) Raman spectra, and (d) magnetic hysteresis loops of the FCCF-1 and  FCCF-3 samples

Fig. S3 Electromagnetic parameters of (a) CF composites, (b) CCF composites, (c) FCF composites, (d) FCCF-1 composites, (e) FCCF-2 composites and (f) FCCF-2 composites

Fig. S4 Impedance matching contour maps of (a) FCCF-1 and (b) FCCF-3 samples

Fig. S5 3D RL and 3D projection plots of (a, c) CF and (b, d) CCF samples

Fig. S6 (a) Optical image, (b) Magnetic properties, and (c) Structural robustness of the FCCF samples

Fig. S7 Infrared radiation images of surface temperature of FCCF-2 sample at different times on a platform with the temperature of 150 °C

Fig. S8 (a) Dielectric loss tangent curves and (b) Magnetic loss tangent curves of the samples

Fig. S9 (a) Top and (b) side views of C/FeNi DFT models

Fig. S10 Integration of ρ in planes parallel to the surface and plotted as a function of the z coordination

Fig. S11 Enlarged magnetic hysteresis loops of the FCCF-1 and FCCF-3 samples

Fig. S12 Reflection loss contour maps with quarter-wavelength matching curves of the samples

Fig. S13 Impedance matching contour maps with quarter-wavelength matching curves of the samples

Fig. S14 2D impedance matching images of the samples

Fig. S15 2D reflection loss images of the samples

Table S1 Detailed information on the concentration of the composites for electromagnetic measurement

| Sample | Fe2+ (mmol) | Ni2+ (mmol) | HMT (mmol) | Solvent (H2O/C2H5OH) | Annealing Temperature (℃) |
| --- | --- | --- | --- | --- | --- |
| FCF | 1.5 | 3 | 6 | 20 mL/20 mL | 700 |
| FCCF-1 | 1 | 2 | 4 | 20 mL/20 mL | 700 |
| FCCF-2 | 1.5 | 3 | 6 | 20 mL/20 mL | 700 |
| FCCF-3 | 2 | 4 | 8 | 20 mL/20 mL | 700 |

Synthesis mechanisms of CCF and FCCF samples

The synthesis mechanisms of CCF and FCCF are concluded as follows:

a.	The CCF samples are prepared by growing CNCs on carbon foam (CF) via a CVD process. First, a type of efficient bimetallic catalyst (α-Fe2O3/SnO2) in the form of nanoparticles is loaded onto carbon foam by a dip coating process. The α-Fe2O3/SnO2/CF samples are preheated to 710 °C in an Ar atmosphere for 30 min. The CNCs are then synthesized on the CF samples with the introduction of additional C2H2 gases at 710 °C. During the CNC growth process, Fe-containing particles are the main catalytic components in the catalyst system, decomposing C2H2 and depositing a carbon filament. The presence of Sn and SnO2 reduces the catalytic activity of Fe-containing particles. The mechanism of CNC growth is attributed to the multiple particles at the tip of a CNC with different catalytic activities corresponding to different growth rates of the carbon filaments. In our previous work (Nano-Micro Lett. (2020) 12:23; Carbon 166 (2020) 101-112), the mechanism of CNC growth was investigated in detail.

b.	The FCCF samples are prepared by growing FeNi-based nanoparticles on the CCF sample via a solvothermal reaction and a subsequent annealing treatment. In the solvothermal reaction, the hydrolysis of the hexamethylenetetramine (HMT) provides a mild basic environment (pH∼9). Hence, Ni2+ and Fe2+ couple with OH-, resulting in the formation of Ni(OH)2 and Fe(OH)2 structures on CCF sample. During the annealing treatment, the Ni(OH)2 and Fe(OH)2 structures are first transformed into NiFe2O4 structures, then the NiFe2O4 structures are partially reduced by carbon, resulting in the formation of the FeNi/NiFe2O4 structures. Following chemical equations explicitly interpreted the aforementioned reaction mechanism:

;

;

;

;

.

Density Functional Theory (DFT) calculations

The FeNi nanoparticles doped carbon model was constructed using first-principle calculation DFT via CP2K [S1-S6]. Diag procedure was used for the wave function optimization and the SCF convergence. The PBE functional [S7] was used with the D3 dispersion correction scheme [S8]. DZVP-MOLOPT-SR-GTH basis sets were used alongside planewaves expanded to a 600 Ry energy cutoff. Electronic cores were represented by Geodecker-Teter-Hutter pseudopotentials [S9, S10]. The 3s, 3p and 3d electrons of Fe/ Ni and 2s, 2p electrons of C are treated as valence. The k-point was set as 3×3×1. The periodic images were separated by vacuum layers 15 Å to eliminate image interactions.

Micromagnetic Simulation Methods

The micromagnetic simulation is performed by Mumax3 software, an open-source GPU-accelerated program. The space and time dependent magnetization dynamics in nano- to micro-sized ferromagnets can be calculated by the Mumax3 through the finite difference discretization. Based on the Landau-Lifshitz-Gilbert equation and the minimum energy principle, the finite difference algorithm simulates the dynamic physical process and solves the 3D model.

In this work, the dynamic spin structures of the FCCF-2 sample, FCF sample, and FeNi/NiFe2O4 heterostructures are simulated by the Mumax3. According to the VSM results, the saturation magnetizations of the magnetic particles in FCF and FCCF-2 samples are 2×105 and 4×105 A/m, respectively. The saturation magnetizations of the FeNi and NiFe2O4 in magnetic heterostructures are 4×105 and 2×105 A/m, respectively. The micromagnetic exchange constants of the magnetic particles in FCF and FCCF-2 samples are both 1.5×10-11 J/m. The micromagnetic exchange constants of the FeNi and NiFe2O4 in magnetic heterostructures are 1.5×10-11 and -1.5×10-11 J/m. The spin precession damping factor is 0.01. The frequency of the external magnetic field is 6 GHz. The diameters of the nanoparticles in FCCF-2 sample and FeNi/NiFe2O4 heterostructures are both 50 nm. The diameter of the nanoparticles in FCF sample is 500 nm.

Supplementary References

- CP2K version 7.0 (Development Version), The CP2K developers group (2019). https://www.cp2k.org/

- T.D. Kühne, M. Iannuzzi, M. Del Ben, V.V. Rybkin, P. Seewald et al., CP2K: an electronic structure and molecular dynamics software package - quickstep: efficient and accurate electronic structure calculations. J. Chem. Phys. 152, 194103 (2020). https://doi.org/10.1063/5.0007045

- J. VandeVondele, J. Hutter, An efficient orbital transformation method for electronic structure calculations. 118, 4365–4369 (2003). https://doi.org/10.1063/1.1543154

- J. VandeVondele, M. Krack, F. Mohamed, M. Parrinello, T. Chassaing et al., Quickstep: Fast and accurate density functional calculations using a mixed Gaussian and plane waves approach. Comput. Phys. Commun. 167, 103–128 (2005). https://doi.org/10.1016/j.cpc.2004.12.014

- J. Hutter, M. Iannuzzi, F. Schiffmann, J. VandeVondele, cp2k: atomistic simulations of condensed matter systems. Wiley Interdiscip. Rev. Comput. Mol. Sci. 4, 15–25 (2014). https://doi.org/10.1002/wcms.1159

- B.G. Lippert, J.H.A.M. Parrinello, A hybrid Gaussian and plane wave density functional scheme. mol Phys.  92, 477–488 (1997). https://doi.org/10.1080/002689797170220

- J.P. Perdew, K. Burke, M. Ernzerhof, Generalized gradient approximation made simple. Phys. Rev. Lett. 77, 3865–3868 (1996). https://doi.org/10.1103/PhysRevLett.77.3865

- S. Grimme, J. Antony, S. Ehrlich, H. Krieg, A consistent and accurate ab initio parametrization of density functional dispersion correction (DFT-D) for the 94 elements H-Pu. J. Chem. Phys. 132, 154104 (2010). https://doi.org/10.1063/1.3382344

- S. Goedecker, M. Teter, J. Hutter, Separable dual-space Gaussian pseudopotentials. Phys. Rev. B Condens. Matter 54, 1703–1710 (1996). https://doi.org/10.1103/physrevb.54.1703

- C. Hartwigsen, S. Goedecker, J. Hutter, Relativistic separable dual-space Gaussian pseudopotentials from H to Rn. Phys. Rev. B 58, 3641–3662 (1998). https://doi.org/10.1103/physrevb.58.3641