Supporting Information for

Design of Ultra-Stable Solid Amine Adsorbents and Mechanisms of Hydroxyl Group-Dependent Deactivation for Reversible CO2 Capture from Flue Gas

Meng Zhao1,2, Liang Huang1,2, Yanshan Gao1,2*, Ziling Wang1,2, Shuyu Liang1,2, Xuancan Zhu3, Qiang Wang1,2*, Hong He4, Dermot O’Hare5*

1College of Environmental Science and Engineering, Beijing Forestry University; Beijing 100083, P. R. China

2State Key Laboratory of Efficient Production of Forest Resources, Beijing Forestry University; Beijing 100083, P. R. China

3Research Center of Solar Power & Refrigeration, Institute of Refrigeration and Cryogenics, Shanghai Jiao Tong University, Shanghai 200240, P. R. China

4State Key Joint Laboratory of Environment Simulation and Pollution Control, Research Centre for Eco-Environmental Sciences, Chinese Academy of Sciences; Beijing 100085, P. R. China

5Chemistry Research Laboratory, Department of Chemistry, University of Oxford, Mansfield Road, Oxford OX1 3TA, United Kingdom

*Corresponding authors. E-mail: yanshan_gao@bjfu.edu.cn (Yanshan Gao); qiangwang@bjfu.edu.cn (Qiang Wang); dermot.ohare@chem.ox.ac.uk (Dermot O’Hare)

Supplementary Figures and Tables

Fig. S1 N2 isotherms for the pristine and PEI/PEG-functionalized a Mg0.55Al (60 oC) and b SBA-15 samples. Pore distributions for the pristine and PEI/PEG-functionalized c Mg0.55Al (60 oC) and d SBA-15 samples

Fig. S2 XRD patterns of the pristine and PEI/PEG-functionalized a Mg0.55Al (60 oC) and b SBA-15 samples

Fig. S3 In-situ DRIFTS spectra recorded at 120 oC of passing pure O2 over the a 60PEI-SBA-15 and b 60PEI-Mg0.55Al (60 °C)

Fig. S4 XPS spectra of a Al 2p for Mg0.55Al (60 °C), b Si 2p for SBA-15, and c, d O 1s for Mg0.55Al (60 °C) and SBA-15, respectively, before and after 60 wt% PEI impregnation

Fig. S5 In-situ DRIFTS spectra of passing 10% CO2 + 5% O2 over the 60PEI-Mg0.55Al (60 °C) sample while continuously increasing the temperature from 80 °C to 150 °C

Fig. S6 In-situ DRIFTS spectra recorded at 120 oC of passing 10% CO2 + 5% O2 over the 60PEI-SBA-15 adsorbents

Fig. S7 TG curves of passing a 10% CO2, and b 100% N2 over the 60PEI-Mg0.55Al (60 °C) and 60PEI-SBA-15 samples

Fig. S8 In-situ DRIFTS spectra of passing 10% CO2 over the 33PEI-SiO2 and 33PEI-Al2O3

Fig. S9 CO2 uptakes at 75 °C under 10% CO2 for 33PEI-Al2O3 and 33PEI-SiO2 before and after aging at 120 °C in 10% CO2 + 5% O2 + 3% H2O

Fig. S10 CO2 uptakes of 40PEI-20PEG-Mg0.55Al (60 °C) and 40PEI-20PEG-SBA-15 over 30 cycles (adsorption at 75 °C in 10% CO2 + 5% O2 for 10 min and desorption at 120 °C in 100% N2 for 15 min

Fig. S11 In-situ DRIFTS spectra of passing 10% CO2 over the supported PEI/PEG adsorbents while continuously increasing the temperature from 80 to 180 °C

Fig. S12 In-situ DRIFTS spectra recorded at 120 °C of passing 100% O2 over the supported PEI/PEG adsorbents

Fig. S13 XPS spectra of N 1s of a 60PEI-SBA-15, b 56PEI-4PEG-SBA-15, c 48PEI-12PEG-SBA-15, and d 40PEI-20PEG-SBA-15 sample

Fig. S14 In-situ DRIFTS spectra recorded at 70 °C of passing 10% CO2 + 5% O2 + 3 vol% H2O over the supported PEI/PEG adsorbents

Fig. S15 CO2 breakthrough curves of 40PEI-20PEG-SBA-15

Table S1 Textural properties of the pristine and PEI/PEG-functionalized Mg0.55Al (60 °C) samples

| Sample | Specific surface area (m2 g-1) | Average pore size (cc g-1) | Average pore volume (nm) |  |
| --- | --- | --- | --- | --- |
| Mg0.55Al (60 °C) | 328.1 | 1.50349 |  | 7.96 |
| 60PEI-Mg0.55Al (60 °C) | 6.1622 | 0.027186 |  | 6.28 |
| 40PEI-20PEG- Mg0.55Al (60 °C) | 8.5496 | 0.08757 |  | 17.79 |

Table S2 Textural properties of the pristine and PEI/PEG-functionalized SBA-15 samples

| Sample | Specific surface area (m2 g-1) | Average pore size (cc g-1) | Average pore volume (nm) |  |
| --- | --- | --- | --- | --- |
| SBA-15 | 420.0883 | 1.430324 |  | 5.95 |
| 60PEI-SBA-15 | 16.5764 | 0.123793 |  | 13.43 |
| 40PEI-20PEG-SBA-15 | 19.123 | 0.167791 |  | 16.4 |