Supporting Information for

An Engineered Heterostructured Trinity Enables Fire-Safe, Thermally Conductive Polymer Nanocomposite Films with Low Dielectric Loss

Qiang Chen1, Jiabing Feng3, Yijiao Xue4, Siqi Huo5, Toan Dinh5, Hang Xu1,2, *, Yongqian Shi6, Jiefeng Gao7, Long-Cheng Tang8, Guobo Huang9, *, Weiwei Lei10, Pingan Song11, *

1Key Laboratory of Integrated Regulation and Resource Development on Shallow Lakes, Ministry of Education, College of Environment, Hohai University, No.1 Xikang Road, Nanjing 210098, P. R. China

2Suzhou Research Institute of Hohai University, Suzhou 215000, P. R. China

3College of Biological, Chemical Sciences and Engineering, Jiaxing University, Jiaxing 314001, P. R. China

4Institute of Chemical Industry of Forest Products, Chinese Academy of Forestry (CAF), Nanjing 210042, P. R. China

5Centre for Future Materials, School of Engineering, University of Southern Queensland, Springfield, 4300 Australia

6 College of Environment and Safety Engineering, Fuzhou University, 2 Xueyuan Road, Fuzhou 350116, P. R. China

7School of Chemistry and Chemical Engineering, Yangzhou University, Yangzhou 225002, P. R. China

8Key Laboratory of Organosilicon Chemistry and Material Technology of MoE, College of Material, Chemistry and Chemical Engineering, Hangzhou Normal University, Hangzhou 311121, P. R. China

9School of Pharmaceutical and Chemical Engineering, Taizhou University, Taizhou 318000, P. R. China

10School of Science, RMIT University, Melbourne, VIC, 3000, Australia

11Centre for Future Materials, University of Southern Queensland, Springfield, 4300 Australia

*Corresponding authors. E-mail: pingansong@gmail.com and pingan.song@usq.edu.au (Pingan Song); xuhang810826@163.com (Hang Xu ); huangguobo@tzc.edu.cn (Guobo Huang)

S1 Supplementary Experimental Section

S1.1 Materials Characterizations

Transmission electron microscopy (TEM) measurements were carried out on a JEOL JEM-2100F equipment (Nippon Electric Motor, Japan). Scanning electron microscope (SEM, Hitachi S-2360N, Japan) with an attachment of Energy Dispersive spectrometer (EDS) was used to observe morphologies, and the samples were sprayed with gold before testing. Fourier transform infrared (FTIR) spectra of the samples were captured on QUINOX 55 equipment (Bruker, Germany) to characterize the chemical groups composition. X-ray diffraction (XRD) analysis was performed using a Rigaku diffractometer with Cu Kα radiation at 40 kV. X-ray photoelectron spectroscopy (XPS) spectra of the samples were tested by the thermo Scientific K-Alpha (USA). A laser particle size analyzer (Mastersizer 3000, Malvern Panalytical, England) was used to measure the size distribution of FG and FG@CuP@ZTC.

The limited oxygen index (LOI) measurement was conducted using the LOI instrument (HC-2, China) according to according to GB/T 2406-2009 standard. The heat release rate was observed by a microscale combustion calorimeter (MCC, GOVMARK MCC-2, USA) to assess the flame resistance. 3-5 mg of samples were added into sample cell and heated with a rate of 1 °C s-1 under the protection of a carried gas which was made up of nitrogen (80 mL min-1) and oxygen (20 mL min-1). Thermogravimetric-Fourier transform infrared spectroscopy (TG-IR) was performed on a thermal gravimeter (NETZSCH 209F3, Germany) and fourier transform infrared spectrometer (Bruker TENSOR27, Germany) from 30 to 700 °C with a heating rate of 20 °C/min in N2, and the sample weight was in the range of 5-10 mg.

The tensile strengths were tested on an AG-X plus universal tensile machine (Shimadzu Instruments, Japan) with a rectangle sample size of 200 × 100 mm and loading rate of 13.3 mm/min at room temperature, and the final tensile strengths were averaged from at least five-times results. For the resilience measurement, the samples are subjected to a cyclic strain of 50% for 5 times on an electromechanical universal testing machine (E44.104, MTS, China).

The thermal diffusivity values (α, mm2/s) of the samples were obtained by a “laser flash” technique (LFA-467, NETZSCH, Germany). The specific heat capacity (Cp, J g-1 K-1) was measured using a differential scanning calorimetry (DSC214, NETZSCH, Germany), and the density (ρ, g cm-3) was measured by a density balance following the Archimedes principle with ethanol as the medium. The thermally conductivity (λ, W m-1 K-1) was calculated according to the following equation: λ = α × Cp × ρ, and three specimens of each material were measured. Surface temperature responses were measured with an infrared thermograph (FLIR, E5, USA).

The dielectric properties (dielectric constant and dielectric loss) of samples were tested by a Broadband Dielectric Spectroscopy (Novocontrol Concept 80, Germany) at room temperature over a wide frequency range from 102 to 107 Hz.

S1.2 Synthesis of FG@ZTC

Briefly, FG, 0.1 g of NaCMC and 300 mL H2O were added to a ball milling tank containing zirconium beads. After 12 h of ball milling at a rotation speed of 1000 rpm, the FG aqueous dispersion was obtained. Afterward, 3,5-diamino-1,2,4-triazole was placed into 100 ml H2O with ultrasonication for 0.5 h, followed by the addition of the FG aqueous dispersion and stirred for 0.5 h. After that, ZnSO4·7H2O aqueous solution was added dropwise into above FG dispersion with 3,5-diamino-1,2,4-triazole, and reacted for another 8 h under. Finally, the target FG@ZTC with a weight ratio of FG and ZTC ca. 1: 2 was collected by centrifugation from the slurry, washing with the H2O, and freeze-drying (pressure: 10 Pa and temperature: -80 °C) for 48 h.

S2 Supplementary Figures and Tables

Fig. S1 The SEM image of a FG, b CuP, and c ZTC

Fig. S2 The size distributions of a FG and b FG@CuP@ZTC

Here, D refers to the volume median diameter, and it is derived from the laser diffraction results to reflect the cumulative distribution of the particle size. The number indicates how many percentages of the particles are smaller than this value (e.g., Dv50 means half of the particles are smaller than a certain size). And Dav is the De Brouckere mean diameter, which is the volume moment mean diameter.

Fig. S3 TEM image of FG@CuP after the secondary ball milling

Fig. S4 a Tensile stress-stain curves, b tensile strength, c tensile modulus, and d toughness of different WPU samples

Fig. S5 The cyclic loading-unloading curves of a pure WPU film and b WPU/30FG@CuP@ZTC nanocomposite film

Fig. S6 SEM images of fracture surfaces for a pure WPU, b WPU/10FG@CuP@ZTC, and c WPU/20FG@CuP@ZTC

Fig. S7 Photographs of the WPU/30FG@CuP@ZTC nanocomposite film during ultrasonication (using a 100 W, 40 kHz sonicator) in water

Fig. S8 Digital photographs of a WPU/10FG@CuP@ZTC, b WPU/20FG@CuP@ZTC, c WPU/30FG/CuP/ZTC, d WPU/30FG@CuP, and e WPU/30FG@ZTC during flame burning test

Fig. S9 a LOI values, b HRR curves, and c THR curves for different WPU samples

Fig. S10 SEM images of char residues for a WPU/10FG@CuP@ZTC, b WPU/20FG@CuP@ZTC, c WPU/30FG@CuP, d WPU/30FG@ZTC, and e WPU/30FG/CuP/ZTC

Fig. S11 EDS mappings of WPU/30FG@CuP@ZTC

Fig. S12 a FTIR spectra of pyrolysis products for pure WPU and WPU/30FG@CuP@ZTC at the temperature of the maximum loss rate. FTIR spectra of b hydrocarbons, c CO2, d HNCO, e carbonyl compounds, and f ethers for pure WPU and WPU/30FG@CuP@ZTC at different temperatures

Fig. S13 In-plane λ of different WPU samples as a function of temperature

Fig. S14 The schematic diagram of thermal conductive mechanism for WPU/FG@CuP@ZTC nanocomposite film

Fig. S15 a Dielectric constant and b dielectric loss curves of different WPU samples. c dielectric constants of different WPU samples at 106 Hz

Table S1 Formulations of different WPU samples

| Sample code | WPU (wt%) | FG (wt%) | CuP (wt%) | ZTC (wt%) | FG@CuPa (wt%) | FG@ZTCb (wt%) | FG@CuP@ZTCc (wt%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| WPU | 100 | - | - | - | - | - | - |
| WPU/10FG@CuP@ZTC | 90 | - | - | - | - | - | 10 |
| WPU/20FG@CuP@ZTC | 80 | - | - | - | - | - | 20 |
| WPU/30FG@CuP@ZTC | 70 | - | - | - | - | - | 30 |
| WPU/30FG/CuP/ZTC | 70 | 10 | 18 | 2 | - | - | - |
| WPU/30FG@CuP | 70 | 10 | - | - | 20 | - | - |
| WPU/30FG@ZTC | 70 | 10 | - | - | - | 20 | - |

FG@CuPa: a weight ratio of FG and CuP ca. 1: 2

FG@ZTCb: a weight ratio of FG and ZTC ca. 1: 2

FG@CuP@ZTCc: a weight ratio of FG, CuP, and ZTC ca. 1: 1.8: 0.2

Table S2 Tensile strength and elongation at break of different WPU samples

| Sample | Tensile strength (MPa) | Tensile modulus (MPa) | Toughness (MJ/m3) | Elongation at break (%) |
| --- | --- | --- | --- | --- |
| WPU | 10.5 ± 0.8 | 24 ± 2 | 63 ± 4 | 858 ± 86 |
| WPU/10FG@CuP@ZTC | 13.7 ± 1.1 | 54 ± 4 | 60 ± 4 | 702 ± 70 |
| WPU/20FG@CuP@ZTC | 15.9 ± 1.3 | 68 ± 5 | 56 ± 3 | 546 ± 55 |
| WPU/30FG@CuP@ZTC | 20.3 ± 1.4 | 102 ± 7 | 45 ± 3 | 375 ± 38 |
| WPU/30FG/CuP/ZTC | 17.8 ± 1.3 | 72 ± 5 | 55 ± 4 | 493 ± 49 |

Table S3 MCC test of pure WPU film and WPU composite films

| Sample code | PHRR (W/g) | THR (KJ/g) | EHC (KJ/g·K) | Char yield (%) |
| --- | --- | --- | --- | --- |
| WPU | 488 ± 24 | 27.9 ± 1.4 | 0.3712 ± 0.0186 | 0 |
| WPU/10FG@CuP@ZTC | 286 ± 14 | 24.3 ± 1.2 | 0.2259 ± 0.0113 | 7.5 |
| WPU/20FG@CuP@ZTC | 233 ± 12 | 21.1 ± 1.1 | 0.1942 ± 0.0097 | 12.4 |
| WPU/30FG@CuP@ZTC | 166 ± 8 | 16.6 ± 0.8 | 0.1475 ± 0.0073 | 21.2 |
| WPU/30FG/CuP/ZTC | 211 ± 11 | 19.5 ± 1.0 | 0.1795 ± 0.0090 | 15.6 |
| WPU/30FG@CuP | 194 ± 10 | 18.3 ± 0.9 | 0.1724 ± 0.0086 | 18.1 |
| WPU/30FG@ZTC | 339 ± 17 | 25.9 ± 1.3 | 0.2978 ± 0.0149 | 13.9 |

Table S4 Quantitative assessment of the fire safety and main flame-retardant modes for WPU film and WPU composite films

| Sample | Flame inhibition (%) | Charring effect (%) | Barrier and protective effect (%) |
| --- | --- | --- | --- |
| WPU | - | - | - |
| WPU/10FG@CuP@ZTC | 39.1 | 7.5 | 32.7 |
| WPU/20FG@CuP@ZTC | 47.7 | 12.4 | 36.9 |
| WPU/30FG@CuP@ZTC | 60.3 | 21.2 | 42.8 |
| WPU/30FG/CuP/ZTC | 51.6 | 15.6 | 38.1 |
| WPU/30FG@CuP | 53.6 | 18.1 | 39.4 |
| WPU/30FG@ZTC | 19.8 | 13.9 | 25.2 |