Supporting Information for

Catalysis-Induced Highly-Stable Interface on Porous Silicon for High-Rate Lithium-Ion Batteries

Zhuobin Han1,†, Phornphimon Maitarad1,8,†, Nuttapon Yodsin2, Baogang Zhao1, Haoyu Ma1, Kexin Liu1, Yongfeng Hu3, Siriporn Jungsuttiwong4, Yumei Wang5, Li Lu5, Liyi Shi1,7, Shuai Yuan1, Yongyao Xia6,* and Yingying Lv1,*

1 Research Centre of Nanoscience and Nanotechnology, Shanghai University, Shanghai 200444, People’s Republic of China

2 Department of Chemistry, Faculty of Science, Silpakorn University, Nakhon Pathom 73000, The Kingdom of Thailand

3 Sinopec Shanghai Research Institute of Petrochemical Technology Co., Ltd., Shanghai 201208, People’s Republic of China

4 Department of Chemistry and Center of Excellence for Innovation in Chemistry Faculty of Science, Ubon Ratchathani University, Ubon Ratchathani 34190, The Kingdom of Thailand

5 National University of Singapore (Chongqing) Research Institute, Chongqing 401123, People’s Republic of China

6 Department of Chemistry, Fudan University, Shanghai 200433, People’s Republic of China

7 Emerging Industries Institute Shanghai University, Jiaxing, Zhejiang 314006, People’s Republic of China

8Program in Bioinformatics and Computational Biology, Graduate School, Chulalongkorn University, Bangkok 10330, The Kingdom of Thailand

† Zhuobin Han and Phornphimon Maitarad contributed equally to this work.

*Corresponding authors. E-mail: yyinglv@shu.edu.cn (Yingying Lv); yyxia@fudan.edu.cn (Yongyao Xia)

Supplementary Figures and Tables

Fig. S1 (a, b) SEM images of pristine AlSi20 alloy; (b) The particle size distribution of pristine AlSi20 alloy

Fig. S2 TEM and elemental mapping images of AlSi20 alloy

Fig. S3 SEM images of commercial Si

Fig. S4 Elemental mapping images of p-Si@ATO

Fig. S5 Nitrogen sorption/desorption isotherms and the corresponding pore size distribution of p-Si. SSA: 98.5 m2 g−1

Fig. S6 Nitrogen sorption/desorption isotherms of commercial Si. SSA: 10.1 m2 g−1

Fig. S7 TEM and elemental mapping images of p-Si obtained from acid etching of pristine AlSi20 alloy

Fig. S8 HRTEM and elemental mapping images of surface oxide layer on the p-Si

Fig. S9 The Al 2p and Si 2p XPS of AlSi20 alloy (a, b), p-Si@ATO (c, d) and p-Si (e, f)

Fig. S10 The Si 2p XPS of commercial Si

Fig. S11 EPR spectroscopy of p-Si@ATO, p-Si, commercial Si and commercial Si with TiOx

Commercial Si with TiOx: commercial Si replaces AlSi20 alloy for hydrolysis of TBOT under the alkaline conditions provided by TMAOH. The results indicate the presence of only oxygen vacancies, and no Ti3+ signal was detected in the absence of Al.

Fig. S12 Comparison of performance of p-Si@ATO with different TBOT mass at 2 A g−1

Fig. S13 (a) Cycling performance of different FEC concentrations at 2 A g−1 after 2 cycles at 0.2 A g−1; (b) Galvanostatic first cycle charge/discharge voltage profiles at 0.2 A g−1

Fig. S14 Galvanostatic first cycle charge/discharge voltage profiles of p-Si@ATO, p-Si and commercial Si at 0.2 A g−1

Fig. S15 Cycling performance of p-Si@ATO, p-Si and commercial Si at 25 °C

Fig. S16 Cycling performance of p-Si@ATO, p-Si and commercial Si at 50 °C

Fig. S17 Cycling performance of p-Si@ATO electrode with a load of 1.8 mg cm−2 at 25 ℃

The high loading anode of 1.8 mg cm−2 (without additional conductive agent is added) displays an area capacity of approximately 3.2 mAh cm−2 at 0.2 A g−1, and can withstand high current density cycles.

Fig. S18 Capacity-voltage curves of p-Si@ATO||LFP pouch-cell at first cycle

Fig. S19 (a) Cycling performance of p-Si@ATO||LFP and p-Si||LFP coin-type full-cell; (b) Capacity-voltage curves of first cycle at 0.2 C

The coin-type full-cell has an N/P ratio of approximately 1.05, with a voltage range of 2.5–3.9 V and 1 C =160 mAh g−1. The negative electrode is pre-cycled 5 times at 0.2 A g−1 before being assembled into the full-cell.

Fig. S20 Cycling performance of coin-type full-cell p-Si@ATO/Gr||LFP at 25 ℃

The p-Si@ATO/Gr electrode slurry was fabricated by mixing 76.5 wt% graphite, 8.5 wt% p-Si@ATO powder, 10 wt% polyacrylic acid, and 5 wt% acetylene black in N-methyl-2-pyrrolidone. The initial Coulombic efficiency is 94.3% at 0.2 C.

Fig. S21 EIS after 1 cycle measured at 100% SOC

Fig. S22 (a) EIS of Li-Li symmetric cells and (b) the corresponding DRT

Fig. S23 HRTEM images of p-Si electrodes after 100 cycles

Fig. S24 F at% of LiF in F 1s XPS at different voltages

Fig. S25 Raman spectroscopy of p-Si@ATO powder and p-Si@ATO electrode before cycle

Fig. S26 F at% of LiF in F 1s XPS after 1, 50 and 100 cycles

Fig. S27 ToF-SIMS results of the Si electrode after 100 cycles: depth profiles of various species

The ions composition and distribution of the anode surface and depth sputtering area (70×70 μm2) were characterized by Time-of-Flight secondary ion mass spectrometry (ToF-SIMS, ToF-SIMS 5 ION-ToF GmbH, Germany). ToF-SIMS was equipped with a 30 keV Bi3+ primary ion gun and a 1 keV Cs+ sputter gun, and an electron flood gun was used for charge neutralization. The silicon-based electrodes were tested after 100 cycles and subsequently washed repeatedly with DMC.

Fig. S28 PDOS without FEC on SiO2, Al2O3 and ATO surfaces

Table S1 Content of elements in p-Si@ATO

| Element | EDS Mapping (wt%) | ICP (wt%) |
| --- | --- | --- |
| Si | 46.2 | 85.11 |
| Al | 35.3 | 5.58 |
| Ti | 0.14 | 0.32 |

Table S2 Content of elements after the etching process with alkaline solution

| Element | After TMAOH etching (wt%) |
| --- | --- |
| Si | 46.16 |
| Al | 35.28 |
| Ti | 0.14 |

Table S3 Comparison of the electrochemical characteristics for Si-base anode materials at high temperture

| Anode material | Electrolytes | Specific capacity (temperature) | Capacity retention | References |
| --- | --- | --- | --- | --- |
| p-Si@ATO | 1 M LiPF6 in EC/DEC (1:1) + 15% FEC | 2423 mAh g−1 at 0.2 A g−1, 270 mAh g−1 at 25 A g−1 (50 ℃) | 80.0% after 500 cycles at 2 A g−1 | This work |
| Microsized Si | 2 M LiFSI in Pyr14FSI | ~3500 mAh g−1 at 0.4 A g−1 (80 ℃) | 85% after 100 cycles at 4 A g−1 | [S1] |
| Si@GCA13 | 1 M LiPF6 in EC/DEC (1:1) + 10% FEC and 1%VC | 2302 mAh g−1 at 0.8 A g−1 after 55 cycles (60 ℃) | \ | [S2] |
| MFG/PNSi@C | 1 M LiPF6 in EC/DC/DMC (1:1:1) | 851 mAh g−1 at 0.4 A g−1 (50 ℃) | \ | [S3] |
| Si@C@Al2O3 | 1 M LiPF6 in EC/EMC (3:7) + 5% FEC | 1276 mAh g−1 at 8 A g−1 (80 ℃) | \ | [S4] |
| 3D-Si@SiOx/C | 1 M LiPF6 in EC/EMC (1:2) + 2% FEC | 1746 mAh g−1 at 0.2 A g−1 (60 ℃) | 79.4% after 70 cycles at 0.2 A g−1 | [S5] |
| Si@BaTiOx-600@C | 1.3 M LiPF6 in EC/DEC (3:7) + 10% FEC | 2021 mAh g−1 at 1 C (60 °C) | 64% after 600 cycles at 1 C | [S6] |
| Si-C@Al2O3 | 1 M LiPF6 in EC/DMC (1:1) + 10% FEC | 668.6 mAh g−1 at 0.5 A g−1 (60 °C) | 80.4% after 100 cycles at 0.5 A g−1 | [S7] |
| Si@PAA-B-HPR | 1 M LiPF6 in EC/DEC (1:1) + 5% FEC and 0.5% VC | 2106 mAh g−1 at 1.4 A g−1 (55 °C) | 50.14% after 500 cycles at 1.4 A g−1 | [S8] |
| Si@C-5CNTs | 1 M LiPF6 in EC/DMC (1:1) | 819 mAh g−1 at 2 A g−1 (40 °C) | 83.6% after 100 cycles at 0.1 A g−1 | [S9] |

Supplementary References

- Q. Liu, T. Meng, L. Yu, S. Guo, Y. Hu et al., Interface engineering to boost thermal safety of microsized silicon anodes in lithium-ion batteries. Small Methods. 6, 2200380 (2022). https://doi.org/10.1002/smtd.202200380

- Y. Tong, S. Jin, H. Xu, J. Li, Z. Kong et al., An energy dissipative binder for self-tuning silicon anodes in lithium-ion batteries. Adv Sci 10, 2205443 (2023). https://doi.org/10.1002/advs.202205443

- H. Chen, X. Hou, F. Chen, S. Wang, B. Wu et al., Milled flake graphite/plasma nano-silicon@carbon composite with void sandwich structure for high performance as lithium ion battery anode at high temperature. Carbon. 130, 433-440 (2018). https://doi.org/10.1016/j.carbon.2018.01.021

- L. Fu, A. Xu, Y. Song, J. Ju, H. Sun et al., Pinecone-like silicon@carbon microspheres covered by Al2O3 nano-petals for lithium-ion battery anode under high temperature. Electrochim Acta. 387, 138461 (2021). https://doi.org/10.1016/j.electacta.2021.138461

- J. Lee, J. Moon, S. A. Han, J. Kim, V. Malgras et al., Everlasting living and breathing gyroid 3D network in Si@SiOx/C nanoarchitecture for lithium ion battery. ACS Nano. 13, 9607-9619 (2019). https://doi.org/10.1021/acsnano.9b04725

- H. Park, S. Choi, S.-J. Lee, Y.-G. Cho, G. Hwang et al., Design of an ultra-durable silicon-based battery anode material with exceptional high-temperature cycling stability. Nano Energy. 26, 192-199 (2016). https://doi.org/10.1016/j.nanoen.2016.05.030

- C. Zhang, F. Ji, D. Li, T. Bai, H. Zhang et al., Interface engineering enables wide-temperature Li-ion storage in commercial silicon-based anodes. Small. 2310633 (2024). https://doi.org/10.1002/smll.202310633

- Z. H. Xie, M. Z. Rong, M. Q. Zhang, Dynamically cross-linked polymeric binder-made durable silicon anode of a wide operating temperature Li-ion battery. ACS Appl Mater Interfaces. 13, 28737-28748 (2021). https://doi.org/10.1021/acsami.1c01472

- M. Zhang, L. Zhao, D. Sun, Y. Sun, C. Xu et al., S doped CNTs scaffolded Si@C spheres anode toward splendid high-temperature performance in lithium-ion battery. Appl Surf Sci. 626, 157254 (2023). https://doi.org/10.1016/j.apsusc.2023.157254