Supporting Information for

Highest Solar-to-Hydrogen Conversion Efficiency in Cu2ZnSnS4 Photocathodes and Its Directly Unbiased Solar Seawater Splitting

Muhammad Abbas1, Shuo Chen1*, Zhidong Li1, Muhammad Ishaq1, Zhuanghao Zheng1, Juguang Hu1, Zhenghua Su1, Yanbo Li2, Liming Ding3*, Guangxing Liang1*

1Institute of Thin Film Physics and Applications, Shenzhen Key Laboratory of Advanced Thin Films and Applications, Key Laboratory of Optoelectronic Devices and Systems of Ministry of Education and Guangdong Province, State Key Laboratory of Radio Frequency Heterogeneous Integration, College of Physics and Optoelectronic Engineering, Shenzhen University, Shenzhen 518060, P. R. China

2Institute of Fundamental and Frontier Sciences, University of Electronic Science and Technology of China, Chengdu 610054, P. R. China

3School of Chemical Engineering and Light Industry, Guangdong University of Technology, Guangzhou 510006, P. R. China

*Corresponding authors. E-mail: chensh@szu.edu.cn (Shuo Chen); ding@nanoctr.cn (Liming Ding); lgx@szu.edu.cn (Guangxing Liang)

Note S1 Preparation of BiVO4

S1.1 Preparation of BiOI Precursor Film

The BiOI precursor film was electrodeposited on an FTO glass substrate in a three-electrode system, where a Pt-foil was used as the counter electrode and an Ag/AgCl with saturated KCl solution was used as the reference electrode. The BiOI precursor deposition solution was fabricated by dissolving lactic acid (0.03 M), KI (0.4 M), and Bi(NO3)3.5H2O (0.015 M) in deionized water (100 mL), with 1,4-Benzoquinone (0.046 M) in ethanol (40 mL) solution. The pH of the mixed solution was adjusted to 3.5 by adding 0.1 M nitric acid aqueous solution after stirring for 30 min. Initially, a 60 s deposition was conducted at -0.40 VAg/AgCl to prevent the falling off of BiOI films from the surface of the FTO substrate. After the initial deposition, the BiOI film was obtained at a constant voltage of -0.28 VAg/AgCl with different deposition durations, then rinsed thoroughly with deionized water and dried in a drying oven.

S1.2 Preparation of BiVO4 Electrode

The vanadium source solution was prepared by dissolving VO(acac)2 (0.5 M) in dimethylsulfoxide (10 mL). The as-prepared BiOI precursor film was dropped into the superfluous vanadium source solution. The electrode was then shifted to a muffle furnace and annealed for about 12 h. The heating rate was 3 oC/min to 120 oC, 0.67 oC/min to 280 oC, and 1.41 oC/min to 450 oC, and then held at 450 oC for 1 h. All the annealing processes ended with furnace cooling. After annealing, the electrodes were immersed in a 1.0 M NaOH solution for 15 min with gentle stirring to wash off the V2O5 on the BiVO4 surface. The prepared BiVO4 electrodes were rinsed thoroughly with deionized water and dried in a drying oven.

S1.3 Photo-Assisted Electrodeposition of CoPi Cocatalyst

The CoPi co-catalyst was electrodeposited on the BiVO4 electrode under AM 1.5 G simulated sunlight by using the three-electrode system containing the solutions of NaH2PO4 (0.1 M), Na2HPO4 (0.1 M), Co(NO3)2.6H2O (0.001 M), and deionized water (100 mL). Similarly, an Ag/AgCl with a saturated KCl solution was used as the reference electrode and a Pt-foil as the counter electrode. The deposition voltage and time were -0.20 VAg/AgCl and 90 s, respectively.

Table S1 A comparison of this work to those of previously reported CZTS-based photocathodes

| Photocathode | Electrolyte | Method | Jph (mA cm−2 at 0 VRHE) | Von (VRHE) |  | HC-STH (%) | Year | Refs. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Mo/CZTS/CdS/TiO2/Pt | 0.5 M H2SO4 | Spin Coating | 29.44 | 0.73 | 9.91 |  | 2025 | This work |
| Mo/CZTS/In2S3-Pt | 0.25 M KH2PO4/0.25 M K2HPO4 | Co-electrodeposition | 6.8 | 0.50 | - |  | 2023 | [S1] |
| Mo/CZTS/CdS/ITO/Pt | 1 M K2HPO4/KH2PO4 | Spin Coating | 29 | 0.75 | - |  | 2023 | [S2] |
| Mo/CZTS-S | 1M Na2SO3 | Thermal evaporation | 3.0 | 0.20 | 0.31 |  | 2022 | [S3] |
| Mo/ACZTS/Ag | Na2HPO4/ NaH2PO4 | Spray deposition | 10 | 0.65 | 2.46 |  | 2022 | [S4] |
| CZTS/HfO2/CdS/HfO2/Pt | 0.2M NaH2PO4/Na2HPO4 | Spray deposition | 28 | 0.72 | 7.27 |  | 2021 | [S5] |
| CZTS/CdS/TiO2-NB/Pt | 0.2M NaH2PO4/Na2HPO4 | Spray deposition | 17.2 | 0.70 | 3.70 |  | 2020 | [S6] |
| Mo/CZTS/CdS/MoSX | 0.2 M Na2HPO4/NaH2PO4 | Spray pyrolysis | 18 | 0.60 | 3.0 |  | 2019 | [S7] |

Table S2 A comparison of this work to those of previously reported state of the art chalcogenide-based photocathodes

| Photocathode | Electrolyte | Jph (mA cm−2 at 0 VRHE) | Von (VRHE) | HC-STH (%) | Year | Refs. |
| --- | --- | --- | --- | --- | --- | --- |
| Mo/CZTS/CdS/TiO2/Pt | 0.5 M H2SO4 | 29.44 | 0.73 | 9.91 | 2025 | This work |
| Mo/Cu2ZnSn(S,Se)4/CdS/TiO2/Pt | 0.5 M H2SO4 | 40.40 | 0.50 | 6.47 | 2023 | [S8] |
| SLG/Mo/Sb2Se3/CdS (In)/Pt | 0.5 M H2SO4 | 35.70 | 0.54 | 5.60 | 2022 | [S9] |
| Mo/Cu2BaSn(S,Se)4/CdS/TiO2/Pt | 0.5M KH2PO4/Na2SO4 | 5.54 | 0.39 | 0.49 | 2021 | [S10] |
| a-Si(p-i-n)/Fh/Ni | 1M KOH | 15.60 | 0.67 | 4.08 | 2021 | [S11] |
| FTO/Au/Sb2Se3/PABA/TiO2/Pt | 0.1M H2SO4 | 35 | 0.50 | 4.70 | 2021 | [S12] |
| Mo/(CuInS2)0.81(ZnS)0.19/CdS/Pt | 0.5M KPi | 16.70 | 0.84 | 5.60 | 2019 | [S13] |
| Mo/Cu(In,Ga)Se2/CdS/Al2O3/TiO2/Pt | 1M HClO4 | 28 | 063 | 9.30 | 2018 | [S14] |
| Au/Cu/CdTe/CdS/Pt | 1 M K2HPO4/KH2PO4 | 22 | 0.60 | 3.70 | 2017 | [S15] |

Table S3 Summary of the PEIS fitted parameters

| Device | Rs(Ω) |  | R1 (Ω) | C1(F) | R2 (Ω) | C2(F) |
| --- | --- | --- | --- | --- | --- | --- |
| CZTS-1 |  | 3.971 | 270.8 | 2.192×10-3 | 25.09 | 3.411×10-3 |
| CZTS-2 |  | 4.974 | 47.87 | 3.67×10-3 | 67.92 | 5.22×10-3 |
| CZTS-3 |  | 16.02 | 123.2 | 7.07×10-4 | 90.10 | 4.70×10-4 |

Table S4 A comparison of Jph in this work to those of previously reported CZTS-based photocathodes in seawater or neutral electrolyte

| Photocathode | Electrolyte | Jph (mA cm−2 at 0 VRHE) | Von (VRHE) | Year | Refs. |
| --- | --- | --- | --- | --- | --- |
| Mo/CZTS/CdS/TiO2/Pt | Seawater | 16.54 | 0.78 | 2025 | This work |
| Mo/CZTS/CdS/In2S3/Pt | 6.5 | 5 | 0.63 | 2023 | [S16] |
| FTO/2D-CZTS | 8.0 | 0.041 | 0.30 | 2022 | [S17] |
| Mo/CZTS/CdS/A-TiO2/Pt | 6.5 | 11.9 | 0.42 | 2021 | [S18] |
| Mo/CZTS/CdS/TiO2-NB/Pt | 6.85 | 14.6 | 0.70 | 2020 | [S6] |
| Mo/CZTS/CdS-MoSx | 6.5 | 14 | 0.60 | 2020 | [S7] |
| Mo/CZTS/CdS/HfO2/Pt | Seawater | 12 | 0.75 | 2018 | [S19] |
| Mo/CZTS/Mo/TiO2-s/Pt | 6.85 | 13 | 0.63 | 2016 | [S20] |
| Mo/CZTS/CdS/Pt | 6.0 | 3 | 0.58 | 2010 | [S21] |

Fig. S1 Schematic illustration of PSLE based Mo/CZTS/CdS/TiO2/Pt photocathode preparation. a spin Coating of CZTS Precursor Films b Sulfurization of CZTS thin films c Chemical bath deposition (CBD) method for CdS buffer layer deposition d Final CZTS photocathode after TiO2 and Pt depositions

Fig. S2 Device preparation and testing a, b PSLE treated Spin coated 4×4 and 2×2 CZTS precursor films over Mo substrate c represents sulfurization, CdS, TiO2 and Pt deposition on CZTS precursor film respectively. d Preparation of photocathode by adding Ag, e Prominent H2 bubbles are emerging while testing of as prepared Mo/CZTS/CdS/TiO2/Pt Photocathode and f Schematic of typical 3-electrode PEC water-splitting configuration

Fig. S3 Dark and continuous light illumination derived J-V curves of CZTS-0,1,2 and 3 photocathodes

Fig. S4 Stability test of Mo/CZTS-2/CdS/TiO2/Pt photocathode in 0.5M H2SO4 electrolyte

Fig. S5 Light harvesting related characterizations results of CZTS-1, CZTS-2 and CZTS-3 thin films. a Absorbance, b absorbance coefficient, c reflectance, and d transmittance

Fig. S6 UPS characterizations derived VB positions and SEC edges of a CZTS-2 b CdS c CZTS-1 and d CZTS-3 thin films

Fig. S7 Schematic illustration of energy band alignment of a CZTS-1/CdS and b CZTS-3/CdS hetrostructures

Fig. S8 M–S plots of a CZTS-2 and b CZTS-1 and c CZTS-3 at frequency of 1-kHz

Fig. S9 Charge separation efficiency calculations using Transient photocurrent response of, a CZTS-1, and b CZTS-2, and c CZTS-3 photocathodes

Fig. S10 Nyquist plot of CZTS-1, CZTS-2, and CZTS-3 photocathodes

Fig. S11 Microstructure and elemental mapping information. aTEM-coupled EDS elemental mappings of Cu, Zn, Sn, S, Cd b,c CdS/TiO2 and d,e CZTS/CdS interfaces

Fig. S12 Crystal structure information. a XRD of CZTS-1, 2 and 3 thin films after spin coating and b after sulfurization. c Raman spectroscopy of CZTS-1, 2 and 3 thin films after spin coating and d after sulfurization

Fig. S13 The cross sectional SEM images of precursor seed layers at a 100 seconds, b 150 seconds and c 200 seconds annealing duration at 295 oC temperature

Fig. S14 The SEM analyses of PSLE strategy based prepared CZTS thin films depict the re-crystallization process from seed layer to sulfurized thin films and corresponding schematic diagrams. a-d CZTS-1, e-h CZTS-2 and i-l CZTS-3

Fig. S15 SEM analyses of cross section and surface of CZTS thin films after sulfurization at a-c 50 seconds, d-f 250 seconds, g-i 300 seconds, and j-l 350 seconds annealing duration

Fig. S16 Grain size calculation a FWHM vs, hkl graph of CZTS-1,2 and 3 thin films and b calculated grain sizes of these thin films

Fig. S17 XPS characterization. a-d comparison of elemental composition of CZTS-1,2 and 3 thin films, e Full scan spectra of CZTS-2 thin film

Fig. S18 KPFM scanning surface topography, potential, CPD maps and corresponding schematic diagrams of the energy band structure of a-d CZTS-3, e-h CZTS-2 and i-l CZTS-1 thin films

Fig. S19 3D potential mapping of a CZTS-1, b CZTS-2 and c CZTS-3

Fig. S20 a TRPL plot of CZTS-0 thin film and b PL spectra of CZTS-1,2 and 3 thin films

Fig. S21 Arrhenius plots of the characteristic frequencies to obtain the defect activation energy. a PV-CZTS-2, b PV-CZTS-1 and c PV-CZTS-3 photovoltaic devices

Fig. S22 PEC performance of Mo/CZTS-2/CdS/TiO2/Pt photocathode in pH4, pH7 and seawater electrolytes, a photocurrent density and b HC-STH efficiency

Fig. S23 Stability test of champion CZTS-2 photocathode in seawater electrolyte under AM 1.5G solar simulated illumination

Supplementary References

- M. Tanaka, Y. Hirose, Y. Harada, M. Takahashi, Y. Sakata et al., Fabrication of Cu2ZnSnS4 (CZTS) by co-electrodeposition of Cu-Zn-Sn alloys, and effect of chemical composition of CZTS on their photoelectrochemical water splitting. Results Chem. 5, 100900 (2023). https://doi.org/10.1016/j.rechem.2023.100900

- Y.F. Tay, M. Zhang, S. Zhang, S. Lie, S.Y. Chiam et al., Charge transfer enhancement at the CZTS photocathode interface using ITO for efficient solar water reduction. J. Mater. Chem. A 11, 26543-26550 (2023). https://doi.org/10.1039/D3TA05227C

- L. Abeykoon, H. Tan, C. Yan, J. Bandara, Significant role of the initial precursor sulfur concentration in the photoelectrochemical hydrogen production of Cu2ZnSnS4 photocathode prepared by thermal evaporation. J. Nanophotonics 16, 016001 (2022). https://doi.org/10.1117/1.JNP.16.016001

- S. Ikeda, T.H. Nguyen, R. Okamoto, M. Remeika, I. Abdellaoui et al., Effects of incorporation of Ag into a kesterite Cu2ZnSnS4 thin film on its photoelectrochemical properties for water reduction. Phys. Chem. Chem. Phys. 24, 468-476 (2022). https://doi.org/10.1039/D1CP04075H

- D. Huang, K. Wang, L. Li, K. Feng, N. An et al., 3.17% efficient Cu2ZnSnS4–BiVO4 integrated tandem cell for standalone overall solar water splitting. Energy Environ. Sci. 14, 1480-1489 (2021). https://doi.org/10.1039/D0EE03892J

- L. Li, K. Feng, D. Huang, K. Wang, Y. Li et al., Surface plasmon resonance effect of a Pt-nano-particles-modified TiO2 nanoball overlayer enables a significant enhancement in efficiency to 3.5% for a Cu2ZnSnS4-based thin film photocathode used for solar water splitting. Chem. Engin. J. 396, 125264 (2020). https://doi.org/10.1016/j.cej.2020.125264

- K. Feng, D. Huang, L. Li, K. Wang, J. Li et al., MoSx-CdS/Cu2ZnSnS4-based thin film photocathode for solar hydrogen evolution from water. Appl. Catalysis B: Environ. 268, 118438 (2020). https://doi.org/10.1016/j.apcatb.2019.118438

- G. Liang, Z. Li, M. Ishaq, Z. Zheng, Z. Su et al., Charge separation enhancement enables record photocurrent density in Cu2ZnSn(S,Se)4 photocathodes for efficient solar hydrogen production. Adv. Energy Mater. 13, 2300215 (2023). https://doi.org/10.1002/aenm.202300215

- S. Chen, T. Liu, M. Chen, M. Ishaq, R. Tang et al., Crystal growth promotion and interface optimization enable highly efficient Sb2Se3 photocathodes for solar hydrogen evolution. Nano Energy 99, 107417 (2022). https://doi.org/10.1016/j.nanoen.2022.107417

- J. Song, B. Teymur, Y. Zhou, E. Ngaboyamahina, D.B. Mitzi, Porous Cu2BaSn(S,Se)4 film as a photocathode using non-toxic solvent and a ball-milling approach. ACS Appl. Energy Mater. 4, 81-87 (2021). https://doi.org/10.1021/acsaem.0c01892

- D. Zhang, M. Du, P. Wang, H. Wang, W. Shi et al., Hole-storage enhanced a-Si photocathodes for efficient hydrogen production. Angew. Chem. Int. Ed. 60, 11966-11972 (2021). https://doi.org/10.1002/anie.202100078

- J. Tan, W. Yang, H. Lee, J. Park, K. Kim et al., Surface restoration of polycrystalline Sb2Se3 thin films by conjugated molecules enabling high-performance photocathodes for photoelectrochemical water splitting. Appl. Catalysis B: Environ. 286, 119890 (2021). https://doi.org/10.1016/j.apcatb.2021.119890

- J. Zhao, T. Minegishi, H. Kaneko, G. Ma, M. Zhong et al., Efficient hydrogen evolution on (CuInS2)x(ZnS)1−x solid solution-based photocathodes under simulated sunlight. Chem. Commun. 55, 470-473 (2019). https://doi.org/10.1039/C8CC08623K

- C.-M. Jiang, S.E. Reyes-Lillo, Y. Liang, Y.-S. Liu, G. Liu et al., Electronic structure and performance bottlenecks of CuFeO2 photocathodes. Chem. Mater. 31, 2524-2534 (2019). https://doi.org/10.1021/acs.chemmater.9b00009

- M. Chen, Y. Liu, C. Li, A. Li, X. Chang et al., Spatial control of cocatalysts and elimination of interfacial defects towards efficient and robust CIGS photocathodes for solar water splitting. Energy Environ. Sci. 11, 2025-2034 (2018). https://doi.org/10.1039/C7EE03650G

- F. Jiang, Gunawan, T. Harada, Y. Kuang, T. Minegishi et al., Pt/In2S3/CdS/Cu2ZnSnS4 thin film as an efficient and stable photocathode for water reduction under sunlight radiation. J. Am. Chem. Soci. 137, 13691-13697 (2015). https://doi.org/10.1021/jacs.5b09015

- V. Mahalakshmi, D. Venugopal, K. Ramachandran, R. Ramesh, Synthesis of 2D-CZTS nanoplate as photocathode material for efficient PEC water splitting. J. Mater. Sci. Mater. Electron. 33, 1-11 (2022). https://doi.org/10.1007/s10854-021-06400-9

- L. Li, C. Wang, K. Feng, D. Huang, K. Wang et al., Kesterite Cu2ZnSnS4 thin-film solar water-splitting photovoltaics for solar seawater desalination. Cell Rep. Phys. Sci. 2, 100468 (2021). https://doi.org/10.1016/j.xcrp.2021.100468

- L. Wu, Cu-based mutlinary sulfide nanomaterials for photocatalytic applications. AIMS Mater. Sci. 10, 909-933 (2023). https://doi.org/10.3934/matersci.2023049

- W. Yang, Y. Oh, J. Kim, M.J. Jeong, J.H. Park et al., Molecular chemistry-controlled hybrid ink-derived efficient Cu2ZnSnS4 photocathodes for photoelectrochemical water splitting. ACS Energy Lett. 1, 1127-1136 (2016). https://doi.org/10.1021/acsenergylett.6b00453

- D. Kang, J.C. Hill, Y. Park, K.-S. Choi, Photoelectrochemical properties and photostabilities of high surface area CuBi2O4 and Ag-doped CuBi2O4 photocathodes. Chem. Mater. 28, 4331-4340 (2016). https://doi.org/10.1021/acs.chemmater.6b01294