Supporting Information for

From Coils to Crawls: A Snake-Inspired Soft Robot for Multimodal Locomotion and Grasping

He Chen1, Zhong Chen2,*, Zonglin Liu1, Jinhua Xiong1, Qian Yan1, Teng Fei1, Xu Zhao1, Fuhua Xue1, Haowen Zheng1, Huanxin Lian1, Yunxiang Chen1, Liangliang Xu1, Qingyu Peng1,3,*, and Xiaodong He1,*

1 National Key Laboratory of Science and Technology on Advanced Composites in Special Environments, Center for Composite Materials and Structures, Harbin Institute of Technology, Harbin 150080, P. R. China

2 Dongfang Electric Academy of Science and Technology Co., Ltd, Chengdu 611731, P. R. China

3 Suzhou Research Institute of HIT, Suzhou 215104, P. R. China

*Corresponding authors. E-mail: pengqingyu@hit.edu.cn (Qingyu Peng); nick.chenzhong@outlook.com (Zhong Chen); hexd@hit.edu.cn (Xiaodong He)

S1 Characterization

The morphology of MXene nanosheets, MXene-CNF layer surface, and MXene-CNF/PE bilayer film cross-section were recorded by scanning electron microscopy (FIB-SEM, TESCAN AMBER) with an energy dispersive spectrometer (EDS) detector.

The thickness of MXene nanosheets was recorded by atomic force microscopy (AFM, Dimension Fastscan, Brucker.).

The structures of MXene and MXene-CNF were characterized using Fourier transform infrared spectroscopy (FT-IR, Thermo Scientific Nicolet iS20), X-ray photoelectron spectroscopy (XPS, ESCALAB 250Xi), and X-ray diffraction (XRD, Bruker D8 Advance).

The water contact angles of PE film before and after plasma treatment, as well as the water contact angles of MXene, CNF, and MXene-CNF, were measured using a contact angle (Datophysics DCAT21).

The optical absorption spectrum of CNF and MXene-CNF were measured using a UV/Vis/IR spectrometer (Shimadzu UV-3600i Plus).

The rheological properties of MXene ink and MXene-CNF ink were measured using flat plate rheometer (TA Instruments DHR-3).

The mechanical properties of MXene film, MXene-CNF film, and PE film were measured using a mechanical tensile machine (Instron 5944).

The thermal shrinkage performance of MXene-CNF film and the thermal expansion performance of anisotropic PE film were measured by a thermomechanical analyzer (TMAQ400).

The photothermal conversion performance of MXene-CNF film and the light-driven actuation performance of ICSBot were evaluated using an 808 nm NIR laser, and the NIR light intensity was measured using an optical power meter (Ceaulight, GEL-NP2000). The infrared thermal images are recorded with a VARIOCAM HD infrared camera (Infratech).

The humidity-driven actuation performance of the ICSBot was measured in an airtight chamber. The relative humidity was controlled by using saturated aqueous solutions of CH3COOK, MgCl2, K2CO3, NaBr, NaCl, KCl, and K2SO4 in an enclosed container, which generated ∼23%, 33%, 44%, 57%, 75%, 86%, and 97% RH, respectively. Besides, the RH value was recorded with a hydrometer.

S2 Supplementary Notes

Note S1 The single layer of MXene was obtained by a modified HCl/LiF etching method (Fig. S1). Figure S1a shows the X-ray diffraction (XRD) patterns of the obtained Ti3C2Tx MXene and Ti3AlC2 MAX phase, the characteristic diffraction peak corresponding to the (002) lattice plane of Ti3C2Tx MXene is 6.59°, which is significantly smaller than that of Ti3AlC2 (9.67°). The characteristic diffraction peak at 38.89° corresponds to the (104) lattice plane of Ti3AlC2, which disappears in the XRD pattern of Ti3C2Tx MXene, indicating that the aluminum atomic layers have been selectively etched [S1]. The SEM image (Fig. S1b) and atomic force microscopy (AFM) image (Fig. S1c) indicate the successful synthesis of single-layer MXene.

Note S2 MXene-CNF ink was successfully fabricated for DIW by uniformly mixing the concentrated MXene dispersion with CNF. The obvious Tyndall effect indicates the uniform dispersion of MXene-CNF ink (Fig. S2). The crystal structure, intermolecular hydrogen bonding, and chemical composition of MXene-CNF inks were analyzed using XRD, FT-IR spectroscopy, and XPS (Fig. S3). The XRD spectra of MXene, CNF, and MXene CNF are shown in Fig. S3a. The introduction of CNF shifts the characteristic peak of the (002) crystal plane of MXene from 6.59° to 5.94°, indicating that the introduction of 1D CNF further expands the interlayer spacing of 2D MXene flakes, promotes the adsorption/desorption of water molecules, and effectively avoids the re-stacking of MXene nanosheets. The FT-IR spectrum is shown in Fig. S3b, the CNF in MXene-CNF shows typical peaks at 2931 cm-1 and 1644 cm-1, corresponding to C–H stretching and –OH bending, respectively. The distinctive peaks of MXene in MXene-CNF are 1428 and 580 cm-1 for C–F and –OH groups, respectively. The XPS spectrum further confirms the presence of a large number of oxygen-containing functional groups in MXene-CNF (Fig. S3c, d).

Note S3 The rheological properties of MXene-CNF ink are the key factors determining the successful fabrication of ICSBot through DIW technology [S2]. Specifically, MXene-CNF ink obviously presents a low-viscosity gel state (Fig. S4a). As the shear rate increases (from 10-2 s-1 to 103 s-1), MXene-CNF inks with different solid contents exhibit shear thinning non-Newtonian fluid behavior, which ensures continuous and smooth flow of ink at the nozzle, thereby ensuring its extrusiveness (Fig. S4b). As the solid content increases, the viscosity of MXene-CNF ink also increases, indicating that adjusting the solid content can easily and effectively control the ink viscosity. Under the same solid content, MXene-CNF ink has a much higher viscosity than MXene ink, indicating that the addition of CNF forms a strong encapsulation network with MXene. Furthermore, the thixotropy of ink was studied through alternating changes in shear rate (0.1 s-1/100 s-1) (Fig. S4c). With the alternation of shear rate from 0.1 s-1 to 100 s-1, the gel network of MXene-CNF ink was destroyed, and the viscosity of gel with different solid content decreased rapidly. After the shear rate recovered to 0.1 s-1, the viscosity of the ink quickly returned to its initial value, indicating that the ink extruded from the nozzle has the ability to maintain a stable shape. In summary, the excellent rheological properties of MXene-CNF provide a solid foundation for the fabrication of ICSBot using DIW technology.

Note S4 We calculated the overall deformation of ICSBot using laminated composite plates theory, with only thickness being involved in the geometric parameters [S3, S4].

The generation of deformation can be attributed to the stress generated by thermal expansion, and its constitutive relationship can be expressed as:

σ=i=12Diε-εti#S1

Where i=1 represents the PE layer and i=2 represents the MXene-CNF layer, Di and εti represent the material stiffness and thermal strain of the i-th layer, respectively. σ is the stress and ε is the strain.

The z-direction is defined as the thickness direction of the bilayer film. It is possible to describe the total strain at distance z from the bottom plane (z0=0) as ε(z)=ε0+κz under Kirchoff assumption, where ε0 is the bottom plane strain and κ the curvature. The forces and moments can be expressed as:

F=Aϵ0+B κ #(S2)

M=Bϵ0+C κ #S3

where F and M are the force matrix and moment matrix, respectively. A, B and C are the extensional stiffness, coupling stiffness and bending stiffness, respectively, which defined as:

A=k=12Dkzk+1-zk#S4

B=12k=12Dkzk+12-zk2#S5

C=13k=12Dkzk+13-zk3#S6

where k is the k-th layer definition and D is the stiffness matrix defined as:

D=RH-1R-1E111-υ12υ21E11υ211-υ12υ210E22υ121-υ12υ21E221-υ12υ21000G12#S7

=E1-υ21υ0υ10001-υ2

where the PE layer and MXene-CNF layer are assumed to be isotropic with E and ν being respectively Young’s modulus and Poisson’s ratio, and H is transformation matrix, R is Reuter's matrix, where θ is the printing angle:

H=cos2θsin2θ2sinθcosθsin2θcos2θ-2sinθcosθ-sinθcosθsinθcosθcos2θ-sin2θ#S8

R=100010002#S9

Since deformation is induced by thermal expansion, the total strain can be modeled according to the definition of CTE, which represents the amount of strain generated per percentage unit of temperature change.

The thermal stress can be expressed as ϵt=α ΔT= α (T- T0), where 𝜶 is the linear CTE, T is the pre-heating platform temperature at which the bilayer film shows a curvature 𝜿 = 0 and T0 is the room temperature.

α=αxxαyyαxy=RH-1R-1α1α2α0#S10

Next, F and M can be represented as:

F=0hD α ΔT dz#S11

M=0hD α ΔT z dz#S12

where h is the whole thickness of the bilayer film and ΔT is the temperature variations.

Since D and α are independent of z-axis, F and M can be written as:

F=k=12Dk αk ΔT zk+1-zk#S13

M=12k=12Dkαk ΔT zk+12-zk2#S14

The strain and the curvature vector can be calculated using the definition of F and M:

ε0κ=ABBC-1FM#S15

The curvature vector κ=(κxx κyy κxy)T can be transformed in the matrix form:

b=κxxκxyκxyκyy#S16

From Kirchoff’s theory of thin plates, the maximum eigenvalue of the curvature tensor b represents the principal curvature 𝜅0, which determines the shape of ICSBot.

Finally, the diameter D and the pitch P of the ICSBot are finally calculated as:

D=2κ0##S17

P=2πtanθκ0#S18

S3 Supplementary Figures and Tables

Fig. S1 Characterization of single-layer MXene. a XRD patterns of Ti3AlC2 and MXene, b SEM image of single-layer MXene, c AFM image of single-layer MXene

Fig. S2 Optical image of the stability of MXene-CNF ink

Fig. S3 Characterization of MXene-CNF layer. a XRD patterns of MXene, CNF, and MXene-CNF, b FT-IR spectra of MXene, CNF, and MXene-CNF, c XPS spectra of MXene, CNF, and MXene-CNF, d O1s XPS spectra of MXene-CNF

Fig. S4 The rheological properties of MXene-CNF ink. a Optical image of MXene-CNF ink, b Viscosity as a function of shear rate, c Viscosity evolution over time for alternating shear rates of 0.1 s−1 and 100 s−1

Fig. S5 Optical images of MXene-CNF ink printed on different polymer substrates using DIW technology. a PLA film, b PET film, c PI film. Scale bars, 10 mm

Fig. S6 The water contact angle of PE film before and after plasma treatment

Fig. S7 Optical images of the MXene-CNF/PE bilayer film. a coiling status, b uncoiling status

Fig. S8 Cross-sectional SEM image of MXene-CNF/PE bilayer film. a-c Printing ply number of MXene-CNF film (a) One ply number, (b) Two ply numbers, and (c) Three ply numbers

Fig. S9 Cross-sectional SEM image of MXene-CNF layer

Fig. S10 Morphology of the surface of MXene-CNF layer after drying. a SEM image, b EDS element mapping of Ti, O, and C

Fig. S11 Dependence of MXene-CNF layer thickness on the printing ply number.

Fig. S12 ICSBot fabricated with different printing speeds and pressures. a, b different printing speeds, c, d different pressures. Scale bars, 10 mm

Fig. S13 a, b Optical image of the cyclic bending test of the MXene-CNF/PE bilayer film. c, d Cross-sectional SEM images of the MXene-CNF/PE bilayer film before (c) and after (d) 15000 times cyclic bending tests

Fig. S14 Thermal expansion/contraction behaviors of MXene-CNF layer and PE layer. a MXene-CNF layer, b AD and TD direction of PE layer

Fig. S15 Mechanical properties of MXene, MXene-CNF, and PE. a Stress-strain curves of MXene and MXene-CNF, b Stress-strain curves of PE layer

Fig. S16 Schematics of the anisotropic composite plates

Fig. S17 Dependence of pitch and diameter of ICSBot on printing angles (ΔT = 30 °C) under laminated composite material model

Fig. S18 FEA result of ICSBot fabricated with different lengths of printed rectangular patterns

Fig. S19 FEA result of ICSBot fabricated with different widths of printed rectangular patterns

Fig. S20 FEA result of ICSBot fabricated with rectangular pattern width D greater than pitch P

Fig. S21 FEA and optical images of ICSBot at printing angles of 45° and -45°. a FEA, b optical image

Fig. S22 Comparison between FEA and experimental results in pitch and diameter of ICSBot as a function of temperature variation. a printing angle θ = 75°, b printing angle θ = 60°, c printing angle θ = 30°, d printing angle θ = 15°

Fig. S23 Comparison between FEA and experimental results in pitch and diameter of ICSBot as a function of printing angle. a temperature variation ΔT = 20 °C, b temperature variation ΔT = 30 °C

Fig. S24 FEA and optical images of ICSBot fabricated with different thicknesses of PE layer. Scale bars, 5 mm

Fig. S25 Design and fabrication of ICSBot with complex initial structure. a X shape, b U shape

Fig. S26 Programmable ICSBot with complex geometric structures. a complex geometric structure, b, c Optical image of “ant” structured ICSBot. Scale bars, 10 mm

Fig. S27 Ultraviolet-visible-near-infrared absorption spectra of the MXene-CNF layer and CNF

Fig. S28 The photothermal conversion performance of MXene-CNF layer. a Infrared thermal image of MXene-CNF layer under different light intensity irradiation, b The equilibrium temperature of the MXene-CNF layer at various light intensities, c Temperature change of MXene-CNF layer under different light intensity irradiation on/off conversion cycles, d Maximum temperature under different light intensity irradiation

Fig. S29 Water contact angle of CNF, MXene, and MXene-CNF

Fig. S30 Time-dependent ATR-FTIR spectra for MXene-CNF film after exposure to D2O vapor for 1minute followed by rapid release of D2O in air.

Fig. S31 Cyclic test with repeated exposure to light irradiation (200 mW cm-2).

Fig. S32 Real-time pitch and diameter of ICSBot with different printing angles and temperature variations under NIR light irradiation (100 mW cm-2). a printing angle θ = 75°, b printing angle θ = 60°, c printing angle θ = 45°, d printing angle θ = 30°, e printing angle θ = 15°

Fig. S33 Dependence of changes in pitch and diameter of the ICSBot on temperature variation under NIR light irradiation (100 mW cm-2). a printing angle θ = 75°, b printing angle θ = 60°, c printing angle θ = 30°, d printing angle θ = 15°

Fig. S34 Optical images of the coiling deformation of the ICSBot under different temperatures (50 °C, 60 °C, 70 °C and 80 °C). Scale bars, 10 mm

Fig. S35 Optical images of sidewinding crawling of ICSBot with different printing angles. a printing angle θ = 60°, b printing angle θ = 45°, c printing angle θ = 30°. Scale bars, 10 mm

Fig. S36 Application of ICSBot based on sidewinding crawling. a Escaping from complex environments, b Crawling under the condition of pushing objects. Scale bars, 10 mm

Fig. S37 Optical images of sidewinding crawling of ICSBot in high-noise environments. Scale bars, 10 mm

Fig. S38 Optical images of accordion crawling of ICSBot inside the S shape and U shape rubber tube. Scale bars, 10 mm

Fig. S39 Optical images of winding climbing of ICSBot outside the trembling rubber tube. Scale bars, 10 mm

Table S1 Properties of the MXene-CNF and PE layers

|  | MXene-CNF layer | PE layer |  |
| --- | --- | --- | --- |
|  |  | AD | TD |
| Young’s Modulus (GPa) | 2.984 | 0.239 |  |
| Poisson’s coefficient | 0.23[S5] | 0.46 [S6] |  |
| Thickness (μm) | 10 | 30/50/80 |  |
| CTE (ppm K-1) | -49 | 430 | 156 |

Table S2 Comparison between ICSBot and other soft robots

| Types | Materials | Structure | Stimulation | Locomotion mode | Refs. |
| --- | --- | --- | --- | --- | --- |
| Snake-inspired soft robot | modular snake robot | self-repeating | Electric | Sidewinding | [S7] |
|  | polyester plastic /Ecoflex | kirigami | Pneumatic | Rectilinear | [S8] |
|  | elastic bellow | two winding actuators, a telescopic actuator | Pneumatic | Winding climbing | [S9] |
|  | LCE | Coiling | Heat | Sidewinding | [S10] |
|  | GO-PDA/rGO/GO-PDA | Triple-layer | NIR Light | Accordion | [S11] |
| Coiling structure soft robot | LCE | Coiling | Heat | Rolling | [S12] |
|  | LCN/PI | Coiling | Electric | Grasping, Crawling | [S13] |
|  | LCE/PP | Coiling | UV Light | Rolling | [S14] |
|  | GO/BOPP | Coiling | IR Light | Grasping | [S15] |
|  | Vitrimer-A/Vitrimer-B | Coiling | Light, Humidity | Grasping | [S16] |
| Multimodal locomotion soft robot | PDMS/PI | Coiling | Light, Magnetic | Flipping, Rolling, Rotating | [S17] |
|  | PDMS/ Metal scales | Bilayer | Magnetic | Rolling, Tumbling | [S18] |
|  | LCE/ PDMS | Bilayer | Light | Crawling, Turning, Rotating | [S19] |
|  | LCE/ MXene | Bilayer | NIR Light | Crawling, Jumping | [S20] |
| This work | MXene-CNF/PE | Coiling | NIR Light, Humidity, Heat | Grasping, Sidewinding, Accordion, Winding | This work |

Supplementary References

- J. Xiong, X. Zhao, Z. Liu, H. Chen, Q. Yan et al., Multifunctional nacre-like nanocomposite papers for electromagnetic interference shielding via heterocyclic aramid/MXene template-assisted in situ polypyrrole assembly. Nano-Micro Lett. 17(1), 53 (2024). https://doi.org/10.1007/s40820-024-01552-9

- Z. Chen, X. Zhao, B. Gao, L. Xu, H. Chen et al., Biobased inks based on cuttlefish ink and cellulose nanofibers for biodegradable patterned soft actuators. ACS Appl. Mater. Interfaces 16(17), 22547–22557 (2024). https://doi.org/10.1021/acsami.4c02775

- J. Ha, S.M. Choi, B. Shin, M. Lee, W. Jung et al., Hygroresponsive coiling of seed awns and soft actuators. Extreme Mech. Lett. 38, 100746 (2020). https://doi.org/10.1016/j.eml.2020.100746

- L. Cecchini, S. Mariani, M. Ronzan, A. Mondini, N.M. Pugno et al., 4D printing of humidity-driven seed inspired soft robots. Adv. Sci. 10(9), 2205146 (2023). https://doi.org/10.1002/advs.202205146

- L. Xu, H. Zheng, F. Xue, Q. Ji, C. Qiu et al., Bioinspired multi-stimulus responsive MXene-based soft actuator with self-sensing function and various biomimetic locomotion. Chem. Eng. J. 463, 142392 (2023). https://doi.org/10.1016/j.cej.2023.142392

- S. Wang, Y. Gao, A. Wei, P. Xiao, Y. Liang et al., Asymmetric elastoplasticity of stacked graphene assembly actualizes programmable untethered soft robotics. Nat. Commun. 11(1), 4359 (2020). https://doi.org/10.1038/s41467-020-18214-0

- H. Marvi, C. Gong, N. Gravish, H. Astley, M. Travers et al., Sidewinding with minimal slip: snake and robot ascent of sandy slopes. Science 346(6206), 224–229 (2014). https://doi.org/10.1126/science.1255718

- A. Rafsanjani, Y. Zhang, B. Liu, S.M. Rubinstein, K. Bertoldi, Kirigami skins make a simple soft actuator crawl. Sci. Robot. 3(15), eaar7555 (2018). https://doi.org/10.1126/scirobotics.aar7555

- B. Liao, H. Zang, M. Chen, Y. Wang, X. Lang et al., Soft rod-climbing robot inspired by winding locomotion of snake. Soft Robot. 7(4), 500–511 (2020). https://doi.org/10.1089/soro.2019.0070

- Y.B. Kim, S. Yang, D.S. Kim, Sidewinder-inspired self-adjusting, lateral-rolling soft robots for autonomous terrain exploration. Adv. Sci. 11(14), 2308350 (2024). https://doi.org/10.1002/advs.202308350

- Y. Yang, M. Zhang, D. Li, Y. Shen, Graphene-based light-driven soft robot with snake-inspired Concertina and serpentine locomotion. Adv. Mater. Technol. 4(1), 1800366 (2019). https://doi.org/10.1002/admt.201800366

- Y. Zhao, Y. Chi, Y. Hong, Y. Li, S. Yang et al., Twisting for soft intelligent autonomous robot in unstructured environments. Proc. Natl. Acad. Sci. USA 119(22), e2200265119 (2022). https://doi.org/10.1073/pnas.2200265119

- Y.-Y. Xiao, Z.-C. Jiang, X. Tong, Y. Zhao, Biomimetic locomotion of electrically powered “Janus” soft robots using a liquid crystal polymer. Adv. Mater. 31(36), 1903452 (2019). https://doi.org/10.1002/adma.201903452

- X. Lu, S. Guo, X. Tong, H. Xia, Y. Zhao, Tunable photocontrolled motions using stored strain energy in malleable azobenzene liquid crystalline polymer actuators. Adv. Mater. 29(28), 1606467 (2017). https://doi.org/10.1002/adma.201606467

- Q. Li, Y. Jiao, Ultrafast photothermal actuators with a large helical curvature based on ultrathin GO and biaxially oriented PE films. ACS Appl. Mater. Interfaces 14(50), 55828–55838 (2022). https://doi.org/10.1021/acsami.2c18478

- Q. Chen, X. Qian, Y. Xu, Y. Yang, Y. Wei et al., Harnessing the day-night rhythm of humidity and sunlight into mechanical work using recyclable and reprogrammable soft actuators. ACS Appl. Mater. Interfaces 11(32), 29290–29297 (2019). https://doi.org/10.1021/acsami.9b09324

- Z. Tian, J. Xue, X. Xiao, C. Du, Y. Liu, Optomagnetic coordination helical robot with shape transformation and multimodal motion capabilities. Nano Lett. 24(9), 2885–2893 (2024). https://doi.org/10.1021/acs.nanolett.4c00047

- R.H. Soon, Z. Yin, M.A. Dogan, N.O. Dogan, M.E. Tiryaki et al., Pangolin-inspired untethered magnetic robot for on-demand biomedical heating applications. Nat. Commun. 14(1), 3320 (2023). https://doi.org/10.1038/s41467-023-38689-x

- N. Qian, H.K. Bisoyi, M. Wang, S. Huang, Z. Liu et al., A visible and near-infrared light-fueled omnidirectional twist-bend crawling robot. Adv. Funct. Mater. 33(16), 2214205 (2023). https://doi.org/10.1002/adfm.202214205

- W. Cho, D.J. Kang, M.J. Hahm, J. Jeon, D.-G. Kim et al., Multi-functional locomotion of collectively assembled shape-reconfigurable electronics. Nano Energy 118, 108953 (2023). https://doi.org/10.1016/j.nanoen.2023.108953