Supporting Information for

Tellurium Terminated MXene Synthesis via One-Step Tellurium Etching

Guoliang Ma1, Zongbin Luo1, Hui Shao2*, Yanbin Shen2, Zifeng Lin1*, Patrice Simon3*

1College of Materials Science and Engineering, Sichuan University, Chengdu 610065, P. R. China

2 i-Lab, CAS Center for Excellence in Nanoscience, Suzhou Institute of Nano-Tech and Nano-Bionics (SINANO), Chinese Academy of Sciences (CAS), Suzhou 215123, P. R. China

3CIRIMAT, Université de Toulouse, CNRS, France

*Corresponding authors. E-mail: simon@chimie.ups-tlse.fr (Patrice Simon); linzifeng@scu.edu.cn  (Zifeng Lin); hshao2023@sinano.ac.cn (Hui Shao)

S1 Materials

Ti3AlC2, V2AlC, Ti2AlC, Nb2AlC, Ta2AlC, Ti2AlN, Ti3AlCN, Ti4AlN3, V4AlC3, Cr2AlC, Zr2AlC etc. MAX (99% purity, 400 mesh-600 mesh) was purchased from Jilin Yiyi Technology Co. Ltd, Te (99.99% purity, 300 mesh) was purchased from Hebei Jincan Metals New Material Co. Ltd., HCl solution was purchased from Chengdu Kelong Company, 1 m NaPF6 in ethylene glycol dimethyl ether (DME, battery-grade) electrolyte was purchased from DuoDuo ElectroChemical Reagent, and glass fibers (GF/D and GF/A) was purchased from Kelude Company, all the chemicals and reagents were used directly after purchase.

S2 Synthesis of Te-MXene

Taking the synthesis of Ti3C2Tex MXene as an example, the precursor materials, Ti3AlC2 (0.5 g) and Te powder (0.975 g), are weighed in a stoichiometric ratio of 1:3. A small amount of ethanol is added to facilitate mixing, and the mixture is manually homogenized until ethanol evaporates. The mixture is then transferred to a quartz boat and placed in a tube furnace. To ensure an inert Ar atmosphere, the system is first flushed with argon gas at a flow rate of 600 mL min-1 for 10 minutes to expel any residual air from the quartz tube. The flow rate is subsequently adjusted to 100 mL min-1 to maintain the inert environment. The furnace is then heated to 700°C at a rate of 10°C min-1 and held at this temperature for 1 hour before being cooled to room temperature. Post-treatment involves washing the product with 100 mL of 1 m HCl solution for 1 hour to remove residual impurities. This is followed by multiple washes with deionized water using a filtration system to eliminate any floating impurities on the surface. Finally, the material is vacuum-dried at 60°C for 8–12 hours to obtain the Ti3C2Tex MXene. The preparation of other MXene materials follows a similar procedure, with variations in temperature and precursor ratios depending on the specific MAX phase. Detailed information on these variations is provided in Table S7 of the Supporting Information.

S3 Material characterization

The phase composition of the MXene products was analyzed using X-ray diffraction (XRD) with a Cu target on a DX-2700 diffractometer. The scanning range was 5°–70°, with an operating tube voltage of 40 kV and a tube current of 30 mA. The microstructure and surface elemental composition of the products were examined using a JEOL field emission scanning electron microscope (FE-SEM, JSM-7900F) equipped with an energy-dispersive X-ray spectrometer (EDS, UltimMax65). Focused ion beam (FIB) sample preparation for particle cross-sections was performed using an FEI HELIOS NanoLab 600i system. Atomic-level analysis of the products was carried out using an FEI Titan Themis 80-300 spherical aberration-corrected transmission electron microscope, which is equipped with two aberration correctors. The elemental valence states of the MXene products were analyzed via X-ray photoelectron spectroscopy (XPS) using an AXIS Supra system (Kratos) with a monochromatic Al Kα X-ray source. The binding energy data were calibrated to the C 1s peak at 284.6 eV. The contents of Ti and Te elements were quantified using an ICAP 7000 series inductively coupled plasma atomic emission spectrometer (ICP-AES). The C content was determined with a CS600 carbon and sulfur analyzer, while the oxygen content of the MXene materials was measured using a TCH600 oxygen, nitrogen, and hydrogen analyzer.

S4 Theoretical calculation

The theoretical calculations based on Density Functional Theory (DFT) were performed using the DS-PAW software package integrated within Device Studio [S1]. For the pseudopotential, the exchange-correlation functional was treated using the Perdew-Burke-Ernzerhof generalized gradient approximation (GGA-PBE). A vacuum layer of 20 Å was added in the structure to minimize periodicity effects along the c-axis. Geometry optimizations were carried out using a 5x5x1 Monhkorst-Pack k-point grid, while electronic structure calculations employed a 7x7x1 grid. The convergence criterion for forces was set to 0.02 eV Å-1, with a plane-wave energy cutoff of 600 eV and an energy convergence threshold of less than 10-6 eV. Long-range van der Waals interactions were accounted for using the DFT-D3 method with Becke-Jonson damping corrections.

Gibbs Free Energy Calculation:  The Gibbs free energy (ΔGr) was calculated using the HSC Chemistry software (version 9.5), with the following reaction Equation S1:

∆Gr=∆Hr+T∆Sr                       (S1)

∆Hr represents the reaction enthalpy change, ∆Sr represents the entropy change, T represents the reaction temperature. Additionally, ∆Hfand ∆Sfvalues can be obtained from HSC thermodynamic software. Based on prior research experience, the entire preparation process can be viewed as a dynamic equilibrium at constant pressure. Furthermore, to predict the etching effect of Te on MAX precursors, we selected elements A from MAX and Te as the initial reactants [S2, S3]. The etching process equations are as follows:

2A+3Te=Al2Te3                        (S2)

Here, the A elements mainly include Al, In, and Ga (Equation S2).

A+Te=ATe                            (S3)

In this case, the A elements primarily include Si, Zn, Sn, Ge, and Pb (Eq. S2).

The details are listed in Tables S1 and S2.

S5 Supplementary Figures and Tables

Table S1 Gibbs free energy (Gr) for the reaction of Te with A-site elements in MAX

| A-site | Te | S | Se | P | Sb | As |
| --- | --- | --- | --- | --- | --- | --- |
| Al | -279.96 | 73.63 | 79.29 | -85.02 | -37.88 | -109.61 |
| Si | 60.02 | -201.09 | -118.40 | -35.52 | None | None |
| Ga | -206.05 | -174.10 | -125.44 | -68.68 | -16.51 | -44.42 |
| In | -135.79 | -102.67 | -63.68 | -34.14 | -17.92 | -35.02 |
| Zn | -99.20 | -177.44 | -70.40 | -2.91 | -15.41 | -6.98 |
| Pb | -55.147 | -84.71 | -87.00 | None | None | None |
| Sn | -49.43 | -92.52 | -69.61 | None | None | None |
| Ge | -52.40 | -104.44 | -98.02 | 39.97 | None | -83.09 |

Fig. S1 The Gibbs free energy of the reaction between different A- site elements (Al, Ga, In, Zn, Pb, Sn, Ge) and Te at different temperatures

Table S2 Gibbs free energy (Gr) for the reaction of Te with A-site elements in different MAX at different temperatures

| Gibbs Free Energy (∆G) of different A-site elements (kJ mol-1) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A | 100 ℃ | 200 ℃ | 300 ℃ | 400 ℃ | 500 ℃ | 600 ℃ | 700 ℃ | 800 ℃ | 900 ℃ | 1000 ℃ |
| Al | -312.630 | -310.806 | -308.866 | -306.830 | -300.965 | -291.049 | -279.963 | -267.317 | -254.984 | -246.552 |
| Zn | -7.979 | -8.287 | -8.633 | -9.130 | -45.479 | -46.760 | -47.605 | -48.281 | -48.818 | -49.240 |
| Sn | -62.435 | -62.508 | -61.550 | -60.115 | -57.435 | -53.448 | -49.430 | -45.401 | -44.302 | -43.410 |
| In | -180.654 | -176.793 | -171.923 | -167.003 | -158.356 | -145.805 | -135.794 | -131.836 | -127.901 | -123.988 |
| Ga | -264.734 | -258.530 | -252.086 | -245.492 | -235.071 | -220.646 | -206.051 | -191.351 | -176.588 | -161.798 |
| Ge | -51.699 | -52.653 | -53.715 | -54.927 | -54.993 | -53.725 | -52.405 | -54.453 | -57.408 | -58.640 |
| Pb | -67.478 | -67.105 | -66.678 | -65.619 | -63.048 | -59.130 | -55.147 | -51.124 | -47.077 | -46.670 |

Fig. S2 a Ti3C2Tex different ratios XRD, different ratios SEM b 1-2, c 1-2.5, d 1-3, e 1-3.5

Fig. S3 a Ti3C2Tex XRD at different temperatures b XRD patterns of Ti3C2Tex synthesized at 700 °C during different reaction times

Fig. S4 The XRD of -F, -Cl, -Br, -Te functional groups Ti3C2 MXene

Fig. S5 Ti3C2Tex SEM microstructure a 300x, b 500x

Fig. S6 Ti3C2Tex EDS surface element distribution data

Fig. S7 Ti3C2Tex products before and after HCl post-treatment. a XRD, b-c SEM of the product before acid washing, d-e SEM of the product after acid washing

Table S3 Composition of the Ti3C2Tex MXene

| Element | wt.% | mol% |
| --- | --- | --- |
| Ti | 25.81 | 3 |
| C | 3.63 | 1.69 |
| Te | 67.13 | 2.93 |
| O | 1.85 | 0.64 |
| Composition | Ti3C1.69Te2.93O0.64 |  |

Fig. S8 Ti3C2Tex XPS data a total spectrum, b O-fraction, c Al-fraction

Table S4 XPS Peak position information of Ti3C2Tex

| Region | BE(eV) | FWHM(eV) | Assigned | Reference |
| --- | --- | --- | --- | --- |
| Ti 2p3/2(2p1/2) | 454.92(460.97) | 0.92(0.96) | Ti-C | [4, 5] |
|  | 455.82(461.99) | 2.37(1.02) | Ti-Te | [S4, S5] |
|  | 459.16(464.6) | 1.75(2.69) | Ti-O | [S4, S5] |
| C 1s | 281.97 | 0.92 | C-Ti | [S4, S5] |
|  | 284.47 | 1.38 | C-C | [S4, S5] |
|  | 285.85 | 2.06 | C-H | [S4, S5] |
|  | 288.67 | 2.03 | -COO | [S4, S5] |
| Te 3d | 572.95(583.33) | 1.24(1.18) | Te-Ti | [S4, S5] |
|  | 572.91(583.27) | 2.84(2.84) | Te | [S4, S5] |
|  | 576.21(587.16) | 2.49(2.49) | Teδ+ | [S4, S5] |
| O 1s | 530.56 | 2.33 | O-Ti | [S4, S5] |
|  | 531.96 | 1.69 | O-Al | [S4, S5] |

Fig. S9 Ti3C2Tex products after 9 months in room temperature air environment. a XRD, b SEM of the product, c SEM of the product after 9 months

Fig. S10 a Experimental and theoretically calculated XRD of Ti3C2Cl2, b Theoretical structure of Ti3C2Cl2

Fig. S11 Lewis acid salt CuCl2 etching of V2AlC. a-b SEM microstructure

Fig. S12 Microscopic morphology of V2CTex MXene without post-treatment SEM, a 1000x, b 200x

Fig. S 13 V2CTex MXene. a XRD before and after etching. b SEM macrostructure after acid cleaning

Fig. S14 V2CTex MXene EDS data a Te. b V. c C

Table S5 Composition of the V2CTex MXene

| Element | wt% | mol% |
| --- | --- | --- |
| V | 26.78 | 2 |
| C | 2.7 | 0.85 |
| Te | 67.1 | 2 |
| O | 1.33 | 0.31 |
| Composition | V2C0.85Te2O1.71 |  |

Fig. S15 V2CTex XPS data a total spectrum, b V-fraction, c Te-fraction, d C-fraction

Table S6 XPS Peak position information of V2CTex

| Region | BE(eV) | FWHM(eV) | Assigned | References |
| --- | --- | --- | --- | --- |
| V 2p3/2(2p1/2) | 513.0(520.56) | 1.01(1.01) | V-C | [S4, S5] |
|  | 513.74(521.74) | 1.94(1.71) | V-Te | [S4, S5] |
|  | 516.4(524.01) | 2.44(2.42) | V-O | [S4, S5] |
| C 1s | 282.63 | 0.79 | C-Ti | [S4, S5] |
|  | 284. 54 | 1.34 | C-C | [S4, S5] |
|  | 286.01 | 1.87 | C-H | [S4, S5] |
|  | 288.62 | 1.65 | -COO | [S4, S5] |
| Te 3d | 572.79(583.19) | 1.24(1.24) | Te2- | [S4, S5] |
|  | 572.90(583.05) | 3.26(3.26) | Teδ+ | [S4, S5] |
|  | 576.13(587.08) | 2.72(2.72) | Te | [S4, S5] |
| O 1s | 530.7 | 1.56 | O-V | [S4, S5] |
|  | 533.0 | 2.06 | O-Al | [S4, S5] |

Fig. S16 Microscopic morphology of Nb2CTex MXene without post-treatment SEM. a 4000x. b1000

Fig. S17 Nb2CTex MXene. a XRD before and after etching. b SEM macrostructure after acid cleaning

Fig. S18 Ta2CTex MXene. a XRD before and after etching. b SEM macrostructure after acid cleaning 1000x

Fig. S19 Ti2NTex MXene. a XRD before and after etching. b SEM macrostructure after acid cleaning 500x

Fig. S20 Ti2CTexMXene. a XRD before and after etching. b SEM macrostructure after acid cleaning 200x

Fig. S21 V4C3Tex MXene. a XRD before and after etching. b SEM macrostructure after acid cleaning 500x

Fig. S22 Ti4N3Tex MXene. a XRD before and after etching. b SEM macrostructure after acid cleaning 500x

Fig. S23 Ti3CNTex MXene. a XRD before and after etching. b SEM macrostructure after acid cleaning 1000x

Fig. S24 Cr2CTex MXene. a XRD before and after etching. b SEM macrostructure after acid cleaning 150x

Fig. S25 Zr2CTex MXene. a XRD before and after etching. b SEM macrostructure after acid cleaning 5000x

Table S7 Types of etching MAX and process parameters

| Raw materials | proportion | Temperature-Time |
| --- | --- | --- |
| Ti3AlC2-Te | 1:3 | 700- 1h |
| V2AlC-Te | 1:2 | 700-1h |
| Nb2AlC-Te | 1:2 | 700-1h |
| Ti2AlC-Te | 1:2 | 700-1h |
| Ti2AlN-Te | 1:2 | 700-1h |
| Ti3AlCN-Te | 1:3 | 700-1h |
| Ta2AlC-Te | 1:2 | 700-1h |
| Ti4AlN3-Te | 1:3 | 700-1h |
| V4AlC3-Te | 1:3 | 700-1h |
| Cr2AlC-Te | 1:2 | 700-1h |
| Zr2AlC-Te | 1:2 | 700-1h |

Fig. S26 Elemental etch extension, a Se, S etched Ti3SiC2 XRD pattern, b SEM macrostructure of Ti3SiC2, c SEM macrostructure of S etched Ti3SiC2, d SEM macrostructure of Se etched Ti3SiC2

Fig. S27 a Lithium storage and sodium storage charge-discharge curves of Ti3C2Tex and V2CTex, b Lithium storage rate performance of Ti3C2Tex and V2CTex

Fig. S28 Sodium storage dQ/dV curves of different Te-based MXene materials

Fig. S29 V2CTex MXene Long-cycle performance at 2 A g-1

Fig. S30 Long cycle performance of Te elemental sodium storage

Fig. S31 DFT theory calculation of V2CTex sodium storage. a Structure before optimization. b Structure after optimization. c Side view of optimized MXene material surface. d Top view of optimized MXene surface

Fig. S32 V2CTex electrode after cycling, a Disassembled electrode plate and separator, b XRD of separator

Fig. S33 V2CTex electrode after cycling, a Microstructure of electrode powder, b Te spectrum in V2CTex electrode XPS

Fig. S34 Full cell data, a Charge and discharge curves of positive and negative materials for half cells, b Full cell cycle Data

Supplementary References

- P. Blöchl, Projector augmented-wave method. Phys. Rev. B 50(24), 17953–17979 (1994). https://doi.org/10.1103/physrevb.50.17953

- Y. Li, H. Shao, Z. Lin, J. Lu, L. Liu et al., A general Lewis acidic etching route for preparing MXenes with enhanced electrochemical performance in non-aqueous electrolyte. Nat. Mater. 19(8), 894–899 (2020). https://doi.org/10.1038/s41563-020-0657-0

- J. Zhu, S. Zhu, Z. Cui, Z. Li, S. Wu et al., Solvent-free one-step green synthesis of MXenes by “gas-phase selective etching”. Energy Storage Mater. 70, 103503 (2024). https://doi.org/10.1016/j.ensm.2024.103503

- H. Ding, Y. Li, M. Li, K. Chen, K. Liang et al., Chemical Scissor-mediated structural editing of layered transition metal carbides. Science 379(6637), 1130–1135 (2023). https://doi.org/10.1126/science.add5901

- V. Kamysbayev, A. S. Filatov, H. Hu, X. Rui, F. Lagunas, et al.Covalent surface modifications and superconductivity of two-dimensional metal carbide MXenes. Science, 369(6506): 979–983 (2020). https://www.science.org/doi/10.1126/science.aba8311