Supporting Information for

BaTiO3 Nanoparticle-Induced Interfacial Electric Field Optimization in Chloride Solid Electrolytes for 4.8 V All-Solid-State Lithium Batteries

Qingmei Xiao1, Shiming Huang1, Donghao Liang1, Cheng Liu1, Ruonan Zhang1, Wenjin Li1*, Guangliang Gary Liu1*

1Guangdong Provincial Key Laboratory of New Energy Materials Service Safety, College of Materials Science and Engineering, Shenzhen University, Shenzhen 518060, P. R. China

*Corresponding authors. E-mails: liwj@szu.edu.cn (Wenjin Li); ggliu@szu.edu.cn (Guangliang Gary Liu)

Supplementary Figures and Tables

Fig. S1 The Rietveld refinement of LYZC@xBTO (a) x = 0, (b) x = 2.5, (c) x = 5, and (d) x = 7.5

Fig. S2 XPS characterization of Ti 2p, Ba 3d for (a, b) LYZC and (c, d) LYZC@5BTO

Fig. S3 The XPS characterization of (a) Y 3d, (b) Zr 3d, and (c) Cl 2p for LYZC and LYZC@5BTO

Fig. S4 (a, b) SEM images of nano BTO particles

Fig. S5 The TEM image of (a) LYZC and (b) LYZC@5BTO. High-resolution TEM image of (c) LYZC and (d) LYZC@5BTO. In Figure (d), Region I corresponds to the morphology of BTO, while Region Ⅱ corresponds to LYZC

Fig. S6 (a, b) The TEM images of LYZC@5BTO

Fig. S7 (a) The Nyquist plots of LYZC@xBTO (x = 0, 2.5, 5, 7.5, 10, 20) measured at 25 ℃. (b) Schematic diagram of measured thickness for LYZC@xBTO (x = 0, 2.5, 5, 7.5, 10, 20) pellets

Fig. S8 The Nyquist plots of (a) LYZC and (b) LYZC@5BTO measured over the temperature range of 0 ℃ to 110 ℃

Fig. S9 DC polarization curves of (a) LYZC and (c) LYZC@5BTO at different voltages from 0.1-0.5 V. Equilibrium current response of (b) LYZC and (d) LYZC@5BTO at different voltages. The electronic conductivity of LYZC and LYZC@5BTO determined by direct current (DC) polarization measurements from 0.1-0.5 V are 5.4 × 10-9 S cm-1 and 7.3 × 10-9 S cm-1, respectively

Fig. S10 (a) Cycling performance of LYZC and LYZC@5BTO at 1 C within the voltage range of 2.8-4.3 V vs. Li+/Li and (b, c) corresponding discharge profiles at different cycle numbers of LYZC and LYZC@5BTO respectively

Fig. S11 Discharge profiles of (a) LYZC and (b) LYZC@5BTO at 1 C at different cycle numbers

Fig. S12 (a) Cycling performance of LYZC@5BTO at 1 C within the voltage range of 2.8-5.0 V vs. Li+/Li and (b) corresponding discharge profiles at different cycle numbers

Fig. S13 dQ/dV curves of (a) LYZC and (b) LYZC@5BTO at 1 C for the ASSBs at different cycle numbers

Fig. S14 (a) High-resolution TEM image of SCNCM811/LYZC composite after 200 cycles with (a1, a2) lattice plane images of Rock-salt (Rs) phase-(111) and (200). The lattice spacing of (b) NCM-(003), (c) Rs phase-(111), and (d) Rs phase-(200) obtained by FFT transformation of high-resolution TEM

Fig. S15 SEM images of (a) the SCNCM811/LYZC composite cathode and (b) SCNCM811/LYZC@5BTO composite cathode after 200 cycles

Table S1 The Rietveld refinement result of LYZC@xBTO (x = 0, 2.5, 5, 7.5)

| Samples | Phase 1 (wt) | Phase 2 (wt) | a (Å) | b (Å) | c (Å) | c/a |
| --- | --- | --- | --- | --- | --- | --- |
| LYZC | 1.000 | 0.000 | 11.125 | 11.125 | 6.007 | 0.540 |
| LYZC@2.5BTO | 0.976 | 0.024 | 11.127 | 11.127 | 5.994 | 0.539 |
| LYZC@5BTO | 0.948 | 0.052 | 11.139 | 11.139 | 6.010 | 0.540 |
| LYZC@7.5BTO | 0.922 | 0.078 | 11.121 | 11.121 | 6.008 | 0.540 |

Table S2 Atomic coordinates, atomic proportions, and isotropic displacement parameters of SCNCM811/LYZC composite after 200 cycles obtained from Rietveld refinement

| Atom ncm | Type | x | y | z | Occ. | Uiso(Å2) |
| --- | --- | --- | --- | --- | --- | --- |
| Li1 | Li+1 | 0 | 0 | 0.00000 | 0.943 | 0.0021 |
| Li2 | Li+1 | 0 | 0 | 0.50000 | 0.057 | 0.0384 |
| Ni1 | Ni+3 | 0 | 0 | 0.00000 | 0.057 | 0.0164 |
| Ni2 | Ni+3 | 0 | 0 | 0.50000 | 0.743 | 0.0019 |
| Co1 | Co+3 | 0 | 0 | 0.50000 | 0.100 | 0.0030 |
| Mn1 | Mn+3 | 0 | 0 | 0.00000 | 0.100 | 0.0093 |
| O1 | O-2 | 0 | 0 | 0.23172 | 1.000 | 0.0059 |

a = b = 2.84036 Å, c=14.38932 Å

Table S3 Atomic coordinates, atomic proportions, and isotropic displacement parameters of SCNCM811/LYZC@5BTO composite after 200 cycles obtained from Rietveld refinement

| Atom ncm | Type | x | y | z | Occ. | Uiso(Å2) |
| --- | --- | --- | --- | --- | --- | --- |
| Li1 | Li+1 | 0 | 0 | 0.00000 | 0.952 | 0.0530 |
| Li2 | Li+1 | 0 | 0 | 0.50000 | 0.048 | 0.0037 |
| Ni1 | Ni+3 | 0 | 0 | 0.00000 | 0.048 | 0.0041 |
| Ni2 | Ni+3 | 0 | 0 | 0.50000 | 0.752 | 0.0127 |
| Co1 | Co+3 | 0 | 0 | 0.50000 | 0.100 | 0.0364 |
| Mn1 | Mn+3 | 0 | 0 | 0.00000 | 0.100 | 0.0084 |
| O1 | O-2 | 0 | 0 | 0.23172 | 1.000 | 0.0022 |

a = b = 2.83689 Å, c=14.43864 Å