Supporting Information for

Radiative Coupled Evaporation Cooling Hydrogel for Above-Ambient Heat Dissipation and Flame Retardancy

Qin Ye1,#, Yimou Huang1,#, Baojian Yao1,#, Zhuo Chen1, Changming Shi2, Brian W. Sheldon2, Meijie Chen*

1 School of Energy Science and Engineering, Central South University, Changsha 430001, P. R. China

2 School of Engineering, Brown University, RI 02912, U.S.A.

# Qin Ye, Yimou Huang, and Baojian Yao contributed equally to this work.

* Corresponding authors. E-mail: chenmeijie@csu.edu.cn (Meijie Chen)

S1 Calculation model

A theoretical model was built to calculate the temperature drop based on the energy balance law, which could also be found in our previous work [S1]. To simplify the calculation, a zero-dimensional model is considered here, where radiative coupled evaporative cooling and heating occur on the surface, which can be described as:

PREC=PRC+PEC=Pheating	(S1)

where PRC was the radiative cooling power, PEC was the evaporation cooling power of the hydrogel, PREC was the radiative coupled evaporation cooling power, Pheating is the heater's power.

Heat transfer model

PRC can be calculated as follows:

PRC=Prad-Psun-Patm-Pnonrad	(S2)

where Prad was the radiative power, Psun was the absorbed solar power,Patm was the absorbed radiative power from the atmospheric irradiation, Pnonrad was the non-radiative heat transfer power between the hydrogel and the ambient.

Prad can be calculated as:

(S3)

where εθ,λ is the spectral directional emittance, IBBT,λ is the spectral intensity of a blackbody at the temperature T, which can be calculated by Planck’s law:

IBBT,λ=2hc2λ5ehcλkT-1	(S4)

whereh=6.626×10-34J sis the Planck constant, k=1.381×10-23J K-1is the Boltzmann constant, c=3×108 m s-1is the speed of light in a vacuum, and  is the wavelength.

Psun can be expressed as：

(S5)

where Isolarλ is the spectral solar intensity at AM 1.5.

Patm can be expressed as:

(S6)

where εatmθ,λ is atmospheric emittance as a function of incident zenith angle θ and wavelength, which can be approximated by:

εatmθ,λ=1-[τλ]1/cosθ	(S7)

where τλ is the atmospheric transmittance in the zenith direction, and it depends on the ambient temperature Tatm and relative humidity φ. Here we first converted the parameter pair (Tatm,φ) to the precipitable water vapor (PWV) [S2] and then input PWV to MODTRAN to achieve the atmospheric transmittance [S3].

Pnonrad was defined as:

Pnonrad=hcTamb-T	(S8)

where  is the non-radiative heat transfer coefficient, including the conductive and convective processes.

Mass transfer model

PEC can be calculated based on the mass change rate：

Δm=PECHvT	(S9)

where  is the vapor mass flux, which can be calculated in the mass transfer model, HvT is vaporization latent heat at the temperature T.

HvT is phase change latent heat at the temperature T, which can be calculated by [S4]：

HvT=1918460(TT-33.91)2	(S10)

is the vapor mass flux, which can be calculated by the water vapor concentration difference between the ambient and the surface, can be written as [S5]:

Δm=gm,H2OmH2O,ambient-mH2O,surface	(S11)

where  was the mass transfer coefficient of the water vapor,  and  were the vapor concentration of water vapor in the ambient and near the hydrogel surface, respectively, which can be calculated based on the Ideal Gas Law:

mH2O=RH×PH2OMH2OP∞Mair	(S12)

where  was the atmospheric pressure, and  were the molecular mass of water and air, respectively,  was the saturation vapor pressure in units of [10-3 bar], which can be determined by 6:

PH2O=10A-B/t+C	(S13)

For T in 0  60 °C, A = 8.10765, B = 1750.286, C = 235.

Supplementary Figures

Fig. S1 Effect of RH on the heat dissipation performance. a Atmospheric transmittance spectra, b temperature, and c mass changes of the ideal REC at different RH

Fig. S2 Effect of Tamb on the heat dissipation performance. a Atmospheric transmittance spectra, b temperature, and c mass changes of the ideal REC at different Tamb

Fig. S3 Water capture performance calculation. a Vapor pressure at different mLiCl. Mass change of the sample at different b mLiCl, c Tamb, and d RH

Fig. S4 Calculated water change in the nighttime (Tamb = 25 oC, RH = 90%), daytime (Tamb = 35 oC, RH = 30%), and all day at different heating powers based on different LiCl mass fractions (a for 10%, b for 20%, c for 30%, and d for 40%)

Fig. S5 Optical images of the hydrogel after soaking a pure water, b 4 M LiCl solution, and c their mass changes

Fig. S6 a Spectral reflectance and b water capture performance of photonic hydrogels after soaking in different LiCl aqueous solutions

Fig. S7 a SEM and b EDS mapping images of the photonic hydrogel at the cross-section

Fig. S8 a X-ray diffraction results (XRD) and b Fourier-transform infrared (FTIR) spectroscopy results of the photonic hydrogel

Fig. S9 a Spectral reflectance of hydrogels, b average solar reflectance (Rsolar) and mid-infrared thermal emittance (εLWIR) with different hBN mass fractions (mhBN) at a water content of 20 wt.%

Fig. S10 Tensile strain of the photonic hydrogel with Al2O3 or without Al2O3

Fig. S11 a Spectral reflectance and b water capture performance of photonic hydrogels with different Al2O3 mass fractions

Fig. S12 Spectral reflectance of hydrogels with different thicknesses at a water content of 20 wt.%. Backgrounds are the normalized solar irradiance (yellow) and atmospheric transmittance windows (cyan)

Fig. S13 Spectral reflectance of hydrogels with different water contents. Backgrounds are the normalized solar irradiance (yellow) and atmospheric transmittance windows (cyan)

Fig. S14 90º peel test for interfacial toughness measurement on different substrates

Fig. S15 Schematic diagram of the indoor experimental setup in the constant temperature and humidity chamber

Fig. S16 Water capture and release cycle of the photonic hydrogel (initial water content of 15 %). Here, water capture under RH = 90%, and Tamb = 15 oC with a low workload of 100 W m-2, and water release under RH = 30%, and Tamb = 25 oC with a high workload of 1020 W m-2

Fig. S17 Saturated mass change of REC hydrogel at different a Tamb, and b RH in the nighttime with a low workload

Fig. S18 Schematic diagram of flame retardancy experiment setup and its optical images at 1200s

Fig. S19 Schematic diagram of the outdoor experimental setup

Fig. S20 Spectral reflectance of the reference substrate heater and SEBS@hBN radiative cooler from Ref. 7

Fig. S21 Continuous all-day cycle performance of REC hydrogel (initial water content 10 wt.%), and RC paint from 2025-06-15 to 2025-06-16 (Pheating = 200 W m-2 in the all day), including solar intensity, RH, and ambient temperature

Fig. S22 a Optical images of the dried hydrogel, b its cross-section SEM image, and c the substrate

Fig. S23 a Spectral reflectance and b water capture performance of photonic hydrogels after being placed outdoors for ten days

Fig. S24 a to c Spectral reflectance and b water capture performance of different hydrogels at a water content of ~ 10 wt.%. Here, PVA, PAAm, and HPMC hydrogels were prepared based on ref. 1, 8, and 9

Table S1 Average temperature in daytime and nighttime for the all-day experiment

|  | Tamb / oC | Tsubstrate / oC | TREC / oC | TRC / oC |
| --- | --- | --- | --- | --- |
| Daytime | 10.1 | 70.8 | 49.9 | 61.9 |
| Nighttime | 6.0 | 6.4 | 5.7 | 6.0 |

Table S2 Total cost of materials in the design hydrogels

| Reagent | DMAPS | hBN | Al2O3 | APS | PEGDA | LiCl | Total |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Price / $ m-2 mm-1 | 32.44 | 1.11 | 0.19 | 0.10 | 0.15 | 32.05 | 66.04 |

Table S3 A comparison of cooling performance for different materials at sub-ambient and above-ambient conditions

| Refs. | Materials | Solar reflectance | Mid-infrared emittance | Temperature drop | Reference |
| --- | --- | --- | --- | --- | --- |
| [S10] | Bilayer Aerogel-hydrogel | 0.98 (50 wt% h-BN) | 0.95 | 8.2 oC | Ambient |
| [S11] | Bilayer P(VdF-HFP)-P(VdF-HFP)@CaCl2 | 0.90 | 0.83 | 10.8 °C | Ambient |
| [S12] | Bilayer Fiber-PVA@CaCl2 | 0.93 (Top) 0.78 (Bottom) | 0.94 | 10 °C | Ambient |
| [S13] | Single layer ZrO2@PAAm-LiBr | 0.90 (without water) | 0.88 | 5.0 oC | Ambient |
| [S14] | Singe layer PDMS-S@LiCl | 0.92 (Visible) | 0.93 | 4.7°C | Ambient |
| [S15] | Single layer Li-PAAm | None | None | 13−17 °C | Device substrate |
| [S16] | Single layer PNAH | 0.98 (Transmittance) | 0.95 | 9.14 °C | Device substrate |
| This work | Single layer NP@PDMAPS@LiCl | 0.87 (5% water) | 0.94 (5% water) | 20.9 oC | Device substrate |

Supplementary References

- L. Yu, Y. Huang, Y. Zhao, Z. Rao, W. Li et al., Self-sustained and insulated radiative/evaporative cooler for daytime subambient passive cooling. ACS Appl. Mater. Interfaces 16(5), 6513–6522 (2024). https://doi.org/10.1021/acsami.3c19223

- C.H. Reitan, Surface dew point and water vapor aloft. J. Appl. Meteor. 1962 1982 2(6), 776–779 (1963). https://doi.org/10.2307/26169602

- Algorithms and Technologies for Multispectral, Hyperspectral, and Ultraspectral Imagery XII. in Society of Photo-Optical Instrumentation Engineers (SPIE) Conference Series 6233, (2006).

- I. Ibrahim, D.H. Seo, A.M. McDonagh, H.K. Shon, L. Tijing, Semiconductor photothermal materials enabling efficient solar steam generation toward desalination and wastewater treatment. Desalination 500, 114853 (2021). https://doi.org/10.1016/j.desal.2020.114853

- Lienhard, J. H. I. & Lienhard, J. H. V. A Heat Transfer Textbook, fifth edition (2020).

- G.W. Thomson, The antoine equation for vapor-pressure data. Chem. Rev. 38(1), 1–39 (1946). https://doi.org/10.1021/cr60119a001

- Q. Ye, N. Guo, M. Chen, Reversible solar heating and radiative cooling coupled with latent heat for self-adaptive thermoregulation. Appl. Phys. Lett. 126(11), 113903 (2025). https://doi.org/10.1063/5.0262028

- V. Penkavova, A. Spalova, J. Tomas, J. Tihon, Polyacrylamide hydrogels prepared by varying water content during polymerization: Material characterization, reswelling ability, and aging resistance. Polym. Eng. Sci. 62(3), 901–916 (2022). https://doi.org/10.1002/pen.25895

- K. Wang, S. Liu, J. Yu, P. Hong, W. Wang et al., Hofmeister effect-enhanced, nanoparticle-shielded, thermally stable hydrogels for anti-UV, fast-response, and all-day-modulated smart windows. Adv. Mater. 37(14), 2418372 (2025). https://doi.org/10.1002/adma.202418372

- X. Dong, K.-Y. Chan, X. Yin, Y. Zhang, X. Zhao et al., Anisotropic hygroscopic hydrogels with synergistic insulation-radiation-evaporation for high-power and self-sustained passive daytime cooling. Nanomicro Lett. 17(1), 240 (2025). https://doi.org/10.1007/s40820-025-01766-5

- Y. Sun, Y. Ji, M. Javed, X. Li, Z. Fan et al., Preparation of passive daytime cooling fabric with the synergistic effect of radiative cooling and evaporative cooling. Adv. Mater. Technol. 7(3), 2100803 (2022). https://doi.org/10.1002/admt.202100803

- J. Li, X. Wang, D. Liang, N. Xu, B. Zhu et al., A tandem radiative/evaporative cooler for weather-insensitive and high-performance daytime passive cooling. Sci. Adv. 8(32), eabq0411 (2022). https://doi.org/10.1126/sciadv.abq0411

- L. Xu, D.-W. Sun, Y. Tian, L. Sun, Z. Zhu, Self-rehydrating and highly entangled hydrogel for sustainable daytime passive cooling. Chem. Eng. J. 479, 147795 (2024). https://doi.org/10.1016/j.cej.2023.147795

- N. Xu, S. Ren, J. Chen, Q. Gou, G. Xue et al., Bio-inspired radiative-evaporative cooling polymer: a dual-functional composite for energy-efficient building cooling. Chem. Eng. J. 512, 162301 (2025). https://doi.org/10.1016/j.cej.2025.162301

- S. Pu, J. Fu, Y. Liao, L. Ge, Y. Zhou et al., Promoting energy efficiency via a self-adaptive evaporative cooling hydrogel. Adv. Mater. 32(17), 1907307 (2020). https://doi.org/10.1002/adma.201907307

- J. Shang, J. Zhang, Y. Zhang, X. Zhang, Q. An, Highly potent transparent passive cooling coating via microphase-separated hydrogel combining radiative and evaporative cooling. Nano Lett. 24(23), 7055–7062 (2024). https://doi.org/10.1021/acs.nanolett.4c01621