Supporting Information for

Deep Learning Assisted Organogel Pressure Sensor for Alphabet Recognition and Bio-Mechanical Motion Monitoring

Kusum Sharma1#, Kousik Bhunia1#, Subhajit Chatterjee2, Muthukumar Perumalsamy1, Anandhan Ayyappan Saj1, Theophilus Bhatti6, Yung-Cheol Byun3, Sang-Jae Kim1,4,5,7, *

1 Nanomaterials & System Lab, Major of Mechatronics Engineering, Faculty of Applied Energy System, Jeju National University, Jeju 63243, Republic of Korea

2 Department of Computer Engineering, Jeju National University, Jeju-si, 63243, Republic of Korea

3 Department of Computer Engineering, Major of Electronic Engineering, Jeju National University, Institute of Information Science & Technology, Jeju 63243, Republic of Korea

4 Nanomaterials & System Lab, Major of Mechanical System Engineering, College of Engineering, Jeju National University, Jeju 63243, Republic of Korea

5 Research Institute of Energy New Industry (RINEI), Jeju National University, Jeju 63243, Republic of Korea

6 Interdisciplinary Graduate Program in Advanced Convergence Technology & Science, Jeju National University, Republic of Korea

7 Green Hydrogen Glocal Leading Research Center (gH2-RC), Jeju National University, Jeju 63243, Republic of Korea

# Kusum Sharma and Kousik Bhunia contributed equally to this article.

*Corresponding author. E-mail: kimsangj@jejunu.ac.kr (Sang-Jae Kim)

S1 Synthesis of CoN CNT

In a typical synthesis method, 1 mmol of Co(NO3)3.6H2O is dissolved in 50 mL absolute ethanol. Subsequently, 10 g of melamine is added under continuous stirring. The mixture was placed over a preheated hotplate at 80 C to evaporate the solvent. The dried mixture was collected in a semi-closed crucible and annealed in a muffle furnace at 550 °C for 2 h at a heating rate of 5 °C min-1. Subsequently, the sample was collected and crushed to powder. Obtained powder is placed in a tubular furnace and heated under an argon atmosphere for 2 h at 850 C with a heating rate of 5C min-1. The synthesized CoN CNT has been directly used for the organogel preparation.

S2 Characterization

The surface morphology and cross-sectional parts were analyzed using a Field Emission Scanning Electron Microscope (FE-SEM, TESCAN MIRA3). The high-resolution transmission electron micrograph (HR-TEM) for the CoN CNT was carried out on an HR-TEM, at Korea basic science institute (KBSI), Busan. The X-ray diffractions (XRD) were carried out using Malvern PANalytical, Empyrean, with a Cu K-alpha source. The vibrational modes and functional groups were analyzed using Fourier Transform Infrared spectroscopy (Bruker, Alpha II). X-Ray Spectroscopy measurements were performed (XPS, Nexa, ThermoFisher Scientific, UK) with x-ray source Al Ka (1486.6 eV) from Busan Center Korea Basic Science Institute (KBSI), South Korea. The pressure-dependent capacitive measurements were performed using an impedance analyzer (HIOKI 3570). The EIS measurements were performed on VIONIC in the frequency range from 1MHz to 100 mHz with a 10 mV test signal. The resistive response measurements were systematically measured using a semiconductor device analyzer (Agilent B1500) and electrometer (Keithley 6514).

S3 Deep Learning-Based Models and Validation

3.1 1D-CNN Model

One-dimensional convolutional neural networks (1D-CNN) are very suitable for extracting spatial patterns from time series data. This model used a single convolutional layer with 64 filters and a kernel size of 2. The convolutional layer was followed by a max pooling layer to reduce dimensionality. The 1D-CNN performed well on its own but was further improved when combined with an LSTM layer to capture the temporal dependence of the data.

3.2 LSTM Model

Given that time-series tasks require capturing temporal patterns, LSTMs are very powerful as they hold entity memory units. LSTM involves input, forget and output gates which control the information that flows. The LSTM has memory cells that can help the model capture dependencies in time-series data making it particularly valuable for identifying sequential patterns within organogel sensor signals. In these experiments, the LSTM model with two stacked LSTM layers of 64 hidden units had been used to capture long-term dependency in the signal patterns across letters. Dropout was applied through the LSTM layers for regularization against overfitting. Diagram of the LSTM network architecture as shown in Scheme S1.

Scheme S1 Network architecture of LSTM

3.3 XGBoost Model

XGBoost leverages gradient boosting to combine multiple decision trees, where each subsequent tree corrects the mistakes of the previous one. XGBoost is well known for its efficiency and accuracy in structured data tasks. It was configured with 100 estimators and a learning rate of 0.1. The XGBoost model performed remarkably well in this task, significantly boosting the accuracy compared to deep learning models alone. The architecture of the XGBoost classifier used in this study is shown in Scheme S2. This method is particularly efficient in handling structured time-series data, allowing for robust classification of resistance signals from the organogel sensor. The model's ability to optimize both accuracy and speed makes it a valuable tool in classifying the distinct signal patterns associated with each letter.

Scheme S2 Architecture of XGBoost classifier

3.4 Stacking Classifier

Finally, we combined the CNN-LSTM and XGBoost models in a stacking classifier. The stacking approach employed a logistic regression model as the meta-learner to integrate the predictions from both base models. This ensemble strategy leverages the complementary strengths of deep temporal modeling (via CNN-LSTM) and gradient boosting (via XGBoost), thereby enhancing the overall classification performance.

Fig. S1 Powder XRD pattern of a CoN CNT, and b pure PVA and gelatin powder.

Pristine PVA powder exhibits sharp reflections at 19.5° and 22.7°, representing the (101) and (101*) planes of the monoclinic unit cell of PVA and a small peak at 40.5°, exhibiting the semicrystalline nature of PVA resulting from the strong intermolecular hydrogen bonding. Gelatin powder displays a halo at 20° and a sharp peak at 8°, corresponding to the triple helix molecule of gelatin.

Fig. S2 FTIR spectra of a pure PVA, and gelatin powder, b Ethylene glycol (EG)

All the characteristics peak 3278 cm-1, 2932/2901 cm-1, 1411 cm-1, 1316 cm-1, 1133 cm-1, 916 cm-1, and 853 cm-1 respectively represent the OH stretching, CH stretching, CH2 bending, OH rocking with CH wagging, C-O stretching, CH3 rocking and C-C stretching.

Fig. S3 a Survey spectrum, high resolution XPS of b C1s, c N1s, and d Co 2p of pristine CoN CNT

Fig. S4 High resolution spectra of O 1s of CoN CNT/PVA/GLE and PVA/GLE

Fig. S5 FESEM images of the synthesized CoN CNT at different magnifications

Fig. S6 FESEM image showing the surface morphology of PVA/GLE organogel at various magnifications

Fig. S7 a-b Cross-sectional view of PVA/GLE matrix at various magnification

Fig. S8 a-d Cross-sectional view of CoN CNT/PVA/GLE matrix at various magnification

Table S1 Summarized anti-fatigue results.

| No. of Cycle (n) | ED (Original) kJ/m3 | ED (10 min) kJ/m3 | RED (Original) % | RED (10 min) % |
| --- | --- | --- | --- | --- |
| 1 | 8.93 | 3.63 | 100 | 40.6495 |
| 2 | 2.79 | 1.62 | 31.243 | 18.1411 |
| 3 | 2.2 | 1.37 | 24.6361 | 15.3416 |
| 4 | 1.96 | 1.3 | 21.9485 | 14.5577 |
| 5 | 1.81 | 1.19 | 20.2688 | 13.3259 |
| 6 | 1.73 | 1.16 | 19.3729 | 12.9899 |
| 7 | 1.65 | 1.15 | 18.477 | 12.8779 |
| 8 | 1.6 | 1.14 | 17.9171 | 12.766 |
| 9 | 1.54 | 1.13 | 17.2452 | 12.654 |
| 10 | 1.49 | 1.1 | 16.6853 | 12.318 |

#ED : Energy dissipation & RED: Relative Energy Dissipation

Fig. S9 Magnified view of resistance variation upon cut and attach, exhibiting the base resistance value while healing process

Fig. S10 The magnified view of self-healing process exhibiting the time to recover electrically along with digital images

Fig. S11 Digital images show the instantons self-healing process for the gel stored under sub-zero conditions

Fig. S12 Adhesion test of CoN CNT/PVA/GLE organogel on various materials at various angles

Fig. S13 Adhesion test of CoN CNT/PVA/GLE organogel on various materials at various angles

Fig. S14 Adhesion test of CoN CNT/PVA/GLE organogel on various materials at various angles

Fig. S15 Weight retention analysis of a-c PVA/GLE, and d-f CoN CNT/PVA/GLE organogel under ambient conditions over three days. Images show the mass measurements on Day 1, Day 2, and Day 3

Fig. S16 Weight retention analysis of a-c PVA/GLE, and d-f CoN CNT/PVA/GLE organogel under ambient conditions over three days. Images show the mass measurements on Day 4, Day 5, and Day 7

Fig. S17 Weight retention analysis of a-c PVA/GLE, and d-f CoN CNT/PVA/GLE organogel under ambient conditions over three days. Images show the mass measurements on Day 8, Day 9, and Day 10

Fig. S18 Weight retention analysis of a-c PVA/GLE, and d-f CoN CNT/PVA/GLE organogel under ambient conditions over three days. Images show the mass measurements on Day 11, Day 13, and Day 14

Fig. S19 Weight retention analysis of a-c PVA/GLE, and d-f CoN CNT/PVA/GLE organogel under ambient conditions over three days. Images show the mass measurements on Day 15, Day 16, and day 17

Fig. S20 Weight retention analysis of a-c PVA/GLE, and d-f CoN CNT/PVA/GLE organogel under ambient conditions over three days. Images show the mass measurements on Day 18, Day 20, and Day 21

Fig. S21 Weight retention analysis of a-c PVA/GLE, and d-f CoN CNT/PVA/GLE organogel under ambient conditions over three days. Images show the mass measurements on Day 22, Day 30, and Day 38

Fig. S22 Weight retention analysis of a-c PVA/GLE, and d-f CoN CNT/PVA/GLE organogel under ambient conditions over three days. Images show the mass measurements on Day 49, Day 74, and Day 76

Fig. S23 Nyquist plot from -20 ºC to 60 ºC for PVA/GLE organogel

The impedance of PVA/GLE is much higher compared to CoN CNT/PVA/GLE organogel. Higher temperatures improve the conductivity of the PVA/GLE material, but it remains significantly more resistive than CoN CNT PVA/GLE organogel.

Fig. S24 Nyquist plot from 40% RH to 95% RH for PVA/GLE organogel

Table S2 Nyquist plots fitting parameter

| CoN CNT/PVA/GLE |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Sr. No. | RH | Rs (ohm) | Rp (k-ohm) | W Y0 (Mho*S1/2) | CPE Y0 (nMho*SN), N |
| 1 | 40 | 642 | 1.2 | 5.12 | 8.99, 0.818 |
| 2 | 50 | 684 | 1.16 | 4.97 | 1.22, 0.926 |
| 3 | 60 | 783 | 1.23 | 4.20 | 0.567, 0.969 |
| 4 | 70 | 857 | 1.32 | 4.71 | 0.264, 1.02 |
| 5 | 80 | 720 | 1.50 | 4.20 | 0.344, 0.979 |
| 6 | 90 | 720 | 1.42 | 4.20 | 0.324, 0.987 |
| 7 | 95 | 998 | 0.998 | 5.96 | 0.334, 1.02 |

Table S3 Nyquist plots fitting parameter

| PVA/GLE |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Sr. No. | RH | Rs (ohm) | Rp (k-ohm) | W Y0 (Mho*S1/2) | CPE Y0 (nMho*SN), N |
| 1 | 40 | 835 | 12.0 | 3.15 | 2.63, 0.788 |
| 2 | 50 | 577 | 10.9 | 3.17 | 3.92, 0.758 |
| 3 | 60 | 630 | 8.44 | 3.92 | 3.97, 0.765 |
| 4 | 70 | 508 | 6.08 | 4.22 | 10.4, 0.709 |
| 5 | 80 | 455 | 4.09 | 4.65 | 13.4, 0.702 |
| 6 | 90 | 350 | 2.05 | 5.41 | 25.5, 0.679 |
| 7 | 95 | 80 | 820 | 7.33 | 1.84, 0.479 |

Fig. S25 a-c Pressure sensing mechanism

Fig. S26 Capacitive response plot at a 60% RH, b 80% RH. Optical images of the pressure sensing set up in humid conditions

Fig. S27 Sensitivity plot at a 45 °C, b 0 °C, and c -20 °C. d-f respective optical images of the sensing setup

Fig. S28 a organogel stored at -20 ºC, b Photograph of the CoN CNT/PVA/GLE organogel, c-d in bending condition exhibiting flexibility

Fig. S29 Temperature endurance of organogel

Fig. S30 Capacitive response to pressure sensing in the detection range 0 – 20 kPa a Day 1, b Day 5, c Day 10, d Day 15, e Day 20, f Day 25, g Day 30, h cumulative capacitive response over a period of one-month, i long term stability plot

Table S4 Summary of the sensitivity data for the CoN CNT/PVA/GEL organogel

| Sr. No. | Days | Sensitivity (%) | Linearity Coefficient (r2) |
| --- | --- | --- | --- |
| 1 | 1 | 7.62 | 0.994 |
| 2 | 5 | 5.71 | 0.979 |
| 3 | 10 | 5.73 | 0.978 |
| 4 | 15 | 5.74 | 0.976 |
| 5 | 20 | 5.74 | 0.978 |
| 6 | 25 | 5.83 | 0.983 |
| 7 | 30 | 5.79 | 0.983 |

Fig. S31 CoN CNT/PVA/GLE sensor response to finger bending a as prepared, b after 1 week

Fig. S32 The response characteristics while speaking the letters 'N', 'M', 'S,' and 'L' respectively

Fig. S33 a Response characteristics for the downward and upward movement of the wrist. b magnified version showcasing an individual wrist bending cycle

Fig S34 Zone of inhibition for E. coli treated with CoN CNT/PVA/GLE over 3 days. The bar graph presents the mean zone of inhibition (cm) against Escherichia coli observed at 12-, 24-, and 72 h following treatment. N.C (Normal Control); PBS, Amp.; Ampicillin (10µg/ml). Independent t-tests were used to compare the zone of inhibition between the normal control and antibiotic drug i.e. ampicillin, and between PVA/GLE and CoN CNT/PVA/GLE treated groups. All values are means ± SD, n=3. ***p<0.0001

Table S5 Zone of Inhibition (ZOI) measurement details for E. coli treated with CoN CNT/PVA/GLE over 3 days

|  | 24hr |  |  |  | 48hr |  |  |  |  | 72hr |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | N.C | Amp. | PVA/GLE | CoN CNT/ PVA/GLE |  | N.C | Amp. | PVA/GLE | CoN CNT/ PVA/GLE |  | N.C | Amp. | PVA/GLE | CoN CNT/ PVA/GLE |
| ZOI (cm) 1 | 0 | 2.5 | 0 | 1.4 |  | 0 | 2.7 | 0 | 1.7 |  | 0 | 2.9 | 0 | 2.2 |
| ZOI (cm) 2 | 0 | 2.5 | 0 | 1.5 |  | 0 | 2.9 | 0 | 1.8 |  | 0 | 3.1 | 0 | 2.3 |
| ZOI (cm) 3 | 0 | 2.5 | 0 | 1.5 |  | 0 | 2.7 | 0 | 1.8 |  | 0 | 2.9 | 0 | 2.1 |

Fig S35 a Samples preparation in DMEM media, b Treatment of RAW264.7 cells with samples in a 96-well plate, c Process of MTT assay

Cytotoxicity Test:

Table S6 Absorbance taken at 24 h after treatment of RAW264.7 cells with different concentrations of CoN CNT for MTT assay

| Absorbance at 24 h after treatment with CoN CNT concentrations |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Nil | LPS (1µg/ml) | 100 (µg/ml) | 50 (µg/ml) | 25 (µg/ml) | 12.5 (µg/ml) | 6.25 (µg/ml) |
| 3.6767 | 3.201 | 1.7967 | 2.3938 | 2.509 | 2.707 | 2.896 |
| 3.9807 | 2.8022 | 1.7152 | 2.0339 | 2.3496 | 2.6498 | 2.8441 |
| 3.7157 | 3.6295 | 1.5544 | 2.2388 | 2.6093 | 2.7959 | 3.2499 |

Fig. S36 PVA/GLE and CoN CNT/PVA/GLE a before degradation, b after degradation in oxidative media (H2O2)

Table S7 Environmental Comparison of CoN-CNT Synthesis Routes

| Parameter | Conventional CVD Method | This Work (Solid State Route) |
| --- | --- | --- |
| Carbon Source | Toxic hydrocarbons (CH₄, C₂H₂) | Melamine (non-volatile, solid organic source) |
| Catalyst Requirement | Requires Fe, Ni, Co metals | Co(NO₃)₃·6H₂O (homogeneous precursor) |
| Reaction Atmosphere | Vacuum, inert/reducing gas flows (H₂, Ar) | Ambient air + Argon (no vacuum) |
| Temperature | >900 °C | 550 °C & 850 °C (lower, two-step) |
| Energy & Safety | High energy, flammable gases | Moderate energy, safer lab setup |
| Environmental Risk | Catalyst residues, gas emissions | Minimal waste; no toxic gases |
| Cost & Scalability | Capital intensive | Low-cost, batch-scalable process |
| End-of-Life | CNTs persistent in soil/water | CoN-CNT remains embedded in degradable gel |

Fig. S37 Patterns of writing the letter ‘N’, ‘M’, ‘S’ and ‘L’ along with response for 10 cycles

Fig. S38 Resistive response for English alphabet A-Z

Fig. S39 Resistive response for numerals 0-9

Table S8 Number of total, training, and testing samples for each letter (L, M, N, and S) used in the classification models

| Letter | Total Samples | Training Samples | Testing Samples |
| --- | --- | --- | --- |
| L | 1507 | 1205 | 302 |
| M | 1606 | 1285 | 321 |
| N | 1486 | 1189 | 297 |
| S | 1725 | 1380 | 345 |

Table S9 Comparing the performance of various classifier models

| Classification Model | Accuracy | Precision | Recall | F1-score |
| --- | --- | --- | --- | --- |
| 1D-CNN-LSTM | 0.8656 | 0.8681 | 0.8656 | 0.8650 |
| Stacking Model | 0.9810 | 0.9811 | 0.9810 | 0.9810 |
| XGBoost | 0.9826 | 0.9827 | 0.9826 | 0.9825 |

Fig. S40 Resistance signal for writing variability-such as changes in writing speed and pressure