Supporting Information for

Boron-Insertion-Induced Lattice Engineering of Rh Nanocrystals towards Enhanced Electrocatalytic Conversion of Nitric Oxide to Ammonia

Peng Han1,, Xiangou Xu2, , Weiwei Chen3, Long Zheng1, Chen Ma1, Gang Wang1, Lei Xu1, Ping Gu1, Wenbin Wang4, Qiyuan He4, Zhiyuan Zeng5, Jinlan Wang2, Dong Su3, Chongyi Ling2,*, Zhengxiang Gu6,*, and Ye Chen1,*

1 Department of Chemistry, The Chinese University of Hong Kong, Hong Kong, P. R. China

2 Key Laboratory of Quantum Materials and Devices of Ministry of Education, School of Physics, Southeast University, Nanjing 211189, P. R. China

3 Beijing National Laboratory for Condensed Matter Physics, Institute of Physics, Chinese Academy of Sciences, Beijing 100190, P. R. China

4 Department of Materials Science and Engineering, City University of Hong Kong, Hong Kong, P. R. China

5 Department of Materials Science and Engineering, and State Key Laboratory of Marine Pollution, and Center of Super-Diamond and Advanced Films, City University of Hong Kong, Hong Kong, P. R. China

6 School of Chemistry and Materials Science, Nanjing Normal University, Nanjing 210023, P. R. China

Peng Han and Xiangou Xu contributed equally to this work.

*Corresponding authors. E-mail: lingchy@seu.edu.cn (Chongyi Ling); zxgu16@fudan.edu.cn (Zhengxiang Gu); yechen@cuhk.edu.hk (Ye Chen)

S1 Experimental Section

S1.1 Chemicals and reagents

All chemicals were used as received without further purification. L-Ascorbic acid (AA, BioXtra, ≥99.0%, crystalline), potassium bromide (KBr, ≥99.0%), polyvinylpyrrolidone (PVP, powder, MW ~55000), sodium hexachlororhodate(III) (Na3RhCl6, 97%), rhodium(III) chloride hydrate (RhCl3⸱xH2O, Rh 38-40%) tetrahydrofuran (THF, 99.9%, anhydrous), sodium sulfate (Na2SO4, ≥99.0%), sodium citrate tribasic dihydrate (≥99.0%), ammonium chloride (NH4Cl, ≥99.5%), sodium hydroxide (NaOH, ACS reagent, ≥97.0%), hydrazine hydrate (N2H4, reagent grade, 50-60%), potassium hydroxide (KOH, 99.99%), p-dimethylaminobenzaldehyde (C9H11NO, 99%), dimethylamine borane (DMAB, (CH3)2NH·BH3, 97%), and ethylene glycol (EG, 99.8%, anhydrous) were all purchased from Sigma-Aldrich. Borane–tetrahydrofuran (BH3-THF, 1 M in THF), sodium nitroferricyanide dihydrate (C5FeN6Na2O·2H2O), salicylic acid (≥99%), sodium hypochlorite (NaClO, available chlorine ≥30%), and carbon (C, Cabot Vulcan XC-72) were purchased from Macklin. Nafion 115 membrane was purchased from Aladdin. Nafion D-521 dispersion (5% w/w in water and 1-propanol) was purchased from Thermo Scientific Chemicals. Fumasep FBM-bipolar membrane was purchased from Fuel Cell Store. Ethanol (HPLC, 99.9%) and acetone (HPLC, 99.9%), and hydrochloric acid (HCl, AR, 37%) were purchased from RCI Labscan (Thailand). N2 gas (99.95%) and Ar (99.95%) were provided by Industrial from Linde HKO Limited (Hong Kong). All aqueous solutions are prepared using Milli-Q water with a resistivity of 18.2 MΩ·cm at room temperature.

S1.2 Structural characterizations

The transmission electron microscopy (TEM) images are acquired on an FEI Tecnai Spirit 12 microscope operated at 120 kV. High-resolution TEM (HRTEM) images are carried out on an FEI Tecnai F20 microscope operated at 200 kV. The high-angle annular dark-field scanning transmission electron microscopy (HAADF-STEM) and energy-dispersive X-ray spectroscopy (EDS) elemental mapping images are performed on a JEOL JEM-NeoAEM-200F TEM performed at 200 kV. X-ray diffraction (XRD) patterns are measured by a Rigaku SmartLab diffractometer with Cu Kα radiation (λ=1.5406 Å). X-ray photoelectron spectroscopy (XPS) is conducted on PHI 5000 Versaprobe III system. A Bruker 600 M nuclear magnetic resonance (NMR) instrument with water suppression was used to record the 1H-NMR spectra. The X-ray absorption fine structures (XAFS) of Rh NCs, a-Rh4B NPs, hcp RhB NPs, Rh foil and Rh2O3 were measured at BL14W1 beamline in Shanghai Synchrotron Radiation Facility (Shanghai, China). The edge energy of the X-ray absorption near edge structure (XANES) spectra were determined from the maximum value in the first derivative of the leading edge of the XANES spectrum. The coordination parameters were obtained by fitting the R-space Fourier transformed data using the least square in Artemis. XAS data normalization and background subtraction were performed using Demeter 0.9.26 software package. The inductively coupled plasma optical emission spectrometry (ICP-OES) is taken on an ICPE 9820 model.

S1.3 Quantification of products concentration

NH4+ quantification. The produced NH3 was quantitatively determined using the indophenol blue method [S1]. Typically, 5 ml of electrolyte was withdrawn from the reaction cell and diluted to 2 ml. Then, 2 ml of 1 M NaOH solution containing sodium citrate and salicylic acid (stored at 4 °C) together with 1 ml of freshly prepared 0.05 M NaClO were added. The mixed solution was shaken for a few seconds. Finally, 0.2 ml of a 1 wt.% sodium nitroferricyanide solution (stored at 4 °C) was added for the color reaction. After keeping at room temperature for 1 h, the resulting solution was measured using an ultraviolet–visible (UV–Vis) spectrophotometer. The absorbance at ~655 nm was used to determine the concentration of NH3. To quantify the amount of NH3, a calibration curve was built using a standard NH4Cl (≥99.5%) solution in 0.5 M Na2SO4. The fitting curve (y = 0.420x − 0.0018, R2 = 0.9998) showed a good linear relation of absorbance value with NH3 concentrations.

N2H4 quantification. The N2H4 was quantitatively determined by Watt and Chrisp method [S2]. A mixed solution of 1.97 g C9H11NO, 10 mL concentrated HCl, and 100 mL ethanol was used as a color reagent. The calibration curve was plotted as follow: (i) collecting the electrolyte from the cathode compartment or preparing a series of N2H4 solutions of known concentration as standards; (ii) adding 4 mL color reagent into above solutions separately and standing 20 min at room temperature; (iii) measuring the absorbance of the resulting solution at 460 nm in 10 mm glass cuvette by the Ultraviolet-visible (UV-Vis) spectrophotometer. The fitting curve shows a good linear relation of absorbance with N2H4 concentration (y = 0.425x + 0.055, R2 = 0.9998).

Gas chromatography (Agilent Technologies 7890B) and mass chromatography (Pfeiffer GSD 320 O2) were used to quantify gas products, including H2, N2, NO and N2O.

S1.4 Calculation of Faradaic efficiency (FE) and the NH3 yield rate

The FE for NH3 electrosynthesis was defined as the amount of electric charge used for producing NH3 divided by the total charge passed through the electrodes during electrolysis. The FE was calculated according to the following equation:

FE = n × F × c × V / (M × Q) 		           (S1)

The NH3 yield was calculated using the following equation:

NH3 yield = CNH3 × V / (17 × t × S) 		(S2)

where n is the number of electrons needed to produce one product molecule, F is the Faraday constant (96485 C mol–1), C is the measured mass concentration of the product, V is the volume of the cathodic reaction electrolyte (50 mL), M is the relative molecular mass of a specific product, Q is the quantity of applied charge/electricity, t is the duration for applying the potential (1 h), and S is the geometric area of the working electrode (1 cm2).

S1.5 In-situ attenuated total reflection infrared (ATR-IR) spectroscopy measurements

The crystalline Ge substrates were used to increase the reflected signals. The catalyst-loaded gold film supported by crystalline silicon, platinum wire, and Ag/AgCl electrode served as the working electrode, counter electrode, and reference electrode, respectively. NO flow was constantly purged before and during the tests. LSV curves were performed in the range of 0.0 to –0.7 V with a scan rate of 1 mV s-1.

S1.6 Zn-NO battery assembly and measurement

The electrocatalysts were employed as the cathode in a cathodic electrolyte (0.2 M Na2SO4). A polished Zn plate was employed in an anodic electrolyte (1.0 M KOH), and a bipolar membrane was used to separate the two electrolytes. During the battery discharge process, NORR occurs at the cathode side, while Zn converts to ZnO at the anode side. The electrochemical reaction on each electrode was described from the following equations:

Cathode: NO + 5H+ + 5e– → NH3 + H2O  		(S3)

Anode: Zn + 2OH– → ZnO + H2O + 2e–  		(S4)

Overall: 5Zn + 2NO + 3H2O → 5ZnO + 2NH3 	(S5)

The NH3 yield was quantified using a colorimetric method. The power density was calculated from the equation (P = U × j) using the polarization results, where U is the voltage and j the current density.

S2 Supplementary Figures

Fig. S1 (a) Low-magnification TEM image with size distribution histogram, (b) Size distribution diagram, (c) Selected area electron diffraction (SAED) pattern, and (d) The HRTEM image of Rh NCs

Fig. S2 (a) SAED pattern of a-Rh4B NPs. (b) Elemental analysis result of a-Rh4B NPs from ICP-OES

Fig. S3 (a) SAED pattern, (b) HRTEM image (c) The corresponding fast Fourier transform (FFT) pattern of the selected square area marked in (b), and (d) ICP-OES result of hcp RhB NPs. The HRTEM image (Fig. S3b) of a representative hcp RhB NP show the typical atomic stacking mode of a hcp phase: i.e., “ABAB” along the [001]h close-packed direction

Fig. S4 The crystal structure model of hcp RhB. The lattice parameters are derived from the inter-planer spacing dhkl obtained by the XRD pattern and Bragg’s Law (λ = 2dhklsinθ).

Note that hcp RhB crystallizes in the hexagonal P6₃/mmc space group. Rh is bonded in a 6-coordinate geometry to six equivalent B atoms. B is bonded in a distorted body-centered cubic geometry to six equivalent Rh and two equivalent B atoms [S3, S4].

Fig. S5 (a) HAADF-STEM image of one typical hcp RhB NP and (b) the corresponding line-scan STEM-EDS elemental analysis of Rh and EELS elemental analysis of B along the white arrow in (a)

Fig. S6 Structural characterizations of B-inserted Rh nanocrystals obtained using DMAB as an alternative B source. The synthesis temperature is increased, and other conditions are the same as those using BH3-THF. (a) TEM image and (b) SAED pattern of a-Rh4B NPs prepared at reaction temperature of 110 ○C. (c) TEM image and (d) SAED pattern of hcp RhB NPs prepared at reaction temperature of 170 ○C

Fig. S7 XRD patterns of B-inserted Rh nanomaterials synthesized at different reaction temperatures while other conditions are unchanged

Fig. S8 HRTEM images of B-inserted Rh nanocrystals synthesized at (a) 60 °C, (c) 100 °C, and (e) 120 °C, respectively. ICP-OES results of B-inserted Rh nanocrystals synthesized at (b) 60 °C, (d) 100 °C, and (f) 120 °C, respectively.

Fig. S9 Temperature-composition correlation analysis of B-inserted Rh nanocrystals synthesized at different reaction temperatures while other conditions are unchanged. At 60 °C, B content was neglectable (1.22 at.%) and the obtained sample maintains the fcc phase, while an fcc-to-amorphous transition initiates between 60-80 °C. The coexistence of a-RhₓB and hcp RhB phases (a-RhₓB/hcp RhB heterophase, 33.1 at.% B) at 100 °C captures the intermediate transition state during B insertion. Furthermore, the complete transformation to phase-pure hcp RhB occurs above 120 °C, as the B content approximately exceeds 43.4 at.%

Fig. S10 (a, d) TEM images of large Rh NCs and large hcp RhB NPs. (b, c) Size distribution diagrams of large Rh NCs and large hcp RhB NPs. (e, f) SAED patterns of large Rh NCs and large hcp RhB NPs. (g) XRD patterns of large Rh NCs and large hcp RhB NPs

Fig. S11 (a) HRTEM image and (b) The corresponding FFT pattern of the selected square area marked in (a) of large Rh NCs. (c) HRTEM image and (d) The corresponding FFT pattern of the selected square area marked in (c) of large hcp RhB NPs.

Fig. S12 High-resolution XPS spectra of B 1s of a-Rh4B NPs and hcp RhB NPs. Note that mild surface B oxidation is commonly observed in B-inserted metal-based nanomaterials and a B oxidation peak is often present in XPS test [S5]

Fig. S13 The differential charge density analysis of RhB(002), RhB(100), and RhB(101) facets (isovalue = 0.008 a.u.)

Fig. S14 EXAFS fitting results of k2-weighted R space (a) Rh foil, (b) Rh2O3, (c) Rh NCs, (d) a-Rh4B NPs and (e) hcp RhB NPs

Fig. S15 TEM images of (a) Rh NCs, (b) a-Rh4B NPs, (c) hcp RhB NPs, (d) large hcp RhB NPs loaded on carbon black

Fig. S16 Quantification of NH3 using the indophenol blue by colorimetric method. (a) UV−Vis absorption spectra for NH4+ (a detectable amount of NH3, in the form of NH4+) at various concentrations. (b) A calibration curve for estimating the concentrations of NH4+

Fig. S17 Quantification of N2H4 using colorimetric method. (a) UV-Vis absorption spectra of a series of N2H4 solutions at different concentrations after incubated for 20 min at room temperature and corresponding (b) calibration curve used for estimating N2H4

Fig. S18 Chronoamperometry curves for hcp RhB NPs at various potentials in NO (20 vol.%) with 0.5 M Na2SO4 electrolyte

Fig. S19 Chronoamperometry curves for Rh NCs at various potentials in NO (20 vol.%) with 0.5 M Na2SO4 electrolyte

Fig. S20 Chronoamperometry curves for a-Rh4B NPs at various potentials in NO (20 vol.%) with 0.5 M Na2SO4 electrolyte

Fig. S21 Electrocatalytic NORR performance of Rh NCs. (a) FEs of all possible products including NH3, H2, N2O and N2 for Rh NCs at each given potential. (b) NH3 yield and FENH3 of Rh NCs at different potentials. (c) Alternating electrolysis test of Rh NCs at −0.6 V vs. RHE. (d) FENH3 and NH3 yield rate in 10 consecutive cycles over Rh NCs for NORR at −0.6 V vs. RHE

Fig. S22 Electrocatalytic NORR performance of a-Rh4B NPs. (a) FEs of all possible products including NH3, H2, N2O and N2 for a-Rh4B NPs at each given potential. (b) NH3 yield and FENH3 of a-Rh4B NPs at different potentials. (c) Alternating electrolysis test of a-Rh4B NPs at −0.6 V vs. RHE. (d) FENH3 and NH3 yield rate in 10 consecutive cycles over a-Rh4B NPs for NORR at −0.6 V vs. RHE

Fig. S23 Electrocatalytic NORR performance of large hcp RhB NPs. (a) FEs of all possible products including NH3, H2, N2O and N2 at each given potential. (b) NH3 yield and FENH3 measured at different potentials. (c) Alternating electrolysis test at −0.6 V vs. RHE. (d) FENH3 and NH3 yield rate in 10 consecutive cycles for NORR at −0.6 V vs. RHE

Fig. S24 Alternating electrolysis test of hcp RhB NPs at −0.6 V vs. RHE by switching between NO-saturated and air-saturated electrolytes

Fig. S25 XRD pattern of hcp RhB NPs/C after the long-term electrocatalytic stability test

Fig. S26 (a) HAADF-STEM image and the size distribution diagram (inset), (b) HRTEM image, (c) The corresponding FFT pattern of the selected area in (b), and (d) ICP-OES result of the hcp RhB NPs after the long-term electrocatalytic stability test

Fig. S27 High-resolution XPS spectra of hcp RhB NPs before and after NORR test in (a) Rh 3d region, and (b) B 1s region

Fig. S28 3D potential-dependent in situ attenuated total reflection infrared spectra of (a) hcp RhB NPs, (b) a-Rh4B NPs, and (c) Rh NCs for NORR in the range from 0 to −0.7 V vs. RHE

Fig. S29 Schematic illustration of the first possible NORR pathway of “NO → *NO → *NOH → *NHOH → *NH2OH → *NH2 → *NH3”

Fig. S30 Schematic illustration of the second possible NORR pathway of “NO → *NO → *HNO → *NHOH → *NH2OH → *NH2 → *NH3”

Fig. S31 Top views of the possible adsorption configurations of NO molecules on the surfaces of (a) Rh(100); (b) RhB(002), (c) RhB(100), and (d) RhB(101) facets

Fig. S32 The PDOSs of Rh sites over (a) hcp RhB(101)h, (b) hcp RhB(100)h, (c) hcp RhB(002)h, and (d) Rh(100)f surfaces before and after NO adsorption

Fig. S33 Top views of calculated Charge of Density and Bader Charge analysis of NO molecules on (a) Rh(100), (b) RhB(002), (c) RhB(100), and (d) RhB(101) facets

Fig. S34 Reaction Gibbs free energy (G) diagram of “*NO → *HNO” step or “*NO → *NOH” step on (a) Rh(100), (b) RhB(002), (c) RhB(100), and (d) RhB(101) facets

Fig. S35 Side views of adsorption configurations of intermediates along the NORR steps on Rh(100) and RhB (002) facets

Fig. S36 Calculated adsorption energies of *NO, *H, and *H2O on Rh(100), RhB(002), RhB(101), and RhB(100) facets

Fig. S37 LSV curves of Rh NCs and hcp RhB NPs in Ar-saturated 0.5 M Na2SO4 electrolyte. The hcp RhB NPs exhibit a 38.6 mV higher overpotential than Rh NCs at the current density of −25 mA cm−2, demonstrating effective suppression of HER activity

Fig. S38 Open circuit voltage (OCV) measurement of the Zn-NO battery with hcp RhB NPs as the cathode

Fig. S39 (a) TEM image, (b) Size distribution diagram, (c) XRD pattern, and (d) ICP-OES result of hcp RhB NPs after the Zn-NO battery test

S3 Supplementary Tables

| Sample | Shell | C.N. | R (Å) | σ2 (×10-3 Å2) | ΔE0 (eV) | R-factor |
| --- | --- | --- | --- | --- | --- | --- |
| Rh foil | Rh-Rh | 12.0* | 2.72 | 3.6 | -8.6 | 0.005 |
| Rh2O3 | Rh-O | 6.0 | 2.04 | 4.0 | -3.7 | 0.011 |
|  | Rh-Rh | 3.0 | 3.05 | 11.3 |  |  |
| hcp RhB NPs | Rh-Rh | 8.7 ± 0.70 | 2.64 ± 0.05 | 7.9 ± 0.26 | -5.5 ± 1.05 | 0.018 |
|  | Rh-B | 5.3 ± 0.80 | 1.96 ± 0.04 | 2.0 ± 0.11 |  |  |
| Rh NCs | Rh-Rh | 10.4 ± 0.16 | 2.70 ± 0.03 | 3.8 ± 0.14 | -3.0 ± 0.35 | 0.007 |
| a-Rh4B NPs | / | / | / | / | / | / |

Table S1 A summary of the Rh K-edge EXAFS fitting results of Rh NCs, a-Rh4B NPs, and hcp RhB NPs in reference to Rh foil and Rh2O3.

C.N.: coordination numbers; R: bond distance; σ2: Debye-Waller factors (a measure of thermal and static disorder in absorber-scatterer distances); ΔE0: the inner potential correction. R-factor: goodness of fit. *These values were fixed during the EXAFS fitting, based on the known structures of Rh foil.

Table S2 Comparison of NH3 yield rate and FENH3 of our catalysts with the reported nanocatalysts for electrocatalytic NORR performed in H-type electrochemical systems

| Catalysts | Electrolyte (pH value) | CNO | NH3 yield (µmol h-1 cm-2) | FE (%) | Potential (V vs. RHE) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| hcp RhB NPs | 0.5 M Na2SO4 (pH = 7.0) | 20 vol.% | 629.5 | 92.1 | −0.60/−0.50a | This work |
| Rh NCs | 0.5 M Na2SO4 (pH = 7.0) | 20 vol.% | 514.7 | 83.2 | −0.60 | This work |
| a-Rh4B NPs | 0.5 M Na2SO4 (pH = 7.0) | 20 vol.% | 403.8 | 73.7 | −0.60/−0.50 | This work |
| Defective TiO2−x | 0.2 M PBS (pH = 7.4) | 10 vol.% | 72.41 | 92.5 | −0.70/−0.40 | Small 2023, 19, 2300291 [S6] |
| MoC/NCS | 0.1 M HCl + 0.5 mM Fe(II) sodium benzoate (FeII-SB) (pH = 1.0) | 99.99 vol.% | 79.27 | 89 | −0.80 | Nano Res. 2022,15, 8890 [S7] |
| CoB/Co@C | 0.5 M Na2SO4 (pH = 7.0) | 99.99 vol.% | 315.4 | 70.3 | −0.60 | Nano Lett. 2023, 23, 7120−7128 [S8] |
| NiO nanosheet | 0.1 M Na2SO4 + 0.5 mM FeII-EDTA (pH = 7.0) | 10 vol.% | 125.07 | 90.0 | −0.60 | Chem. Commun. 2021, 57, 13562–13565 [S9] |
| MoS2 nanosheet | 0.1 M HCl + 0.5 mM FeII-SB (pH = 1.0) | 10 vol.% | 99.6 | 76.6 | −0.70 | Angew. Chem. Int. Ed. 2021, 60, 25263–25268 [S10] |
| Ni2P nanosheet | 0.1 M HCl (pH = 1.0) | 10 vol.% | 33.47 | 76.9 | −0.20 | J. Mater. Chem. A 2021, 9, 24268–24275 [S11] |
| a-B2.6C@TiO2 | 0.2 M Na2SO4 + FeII-EDTA (pH = 7.0) | 10 vol.% | 216.01 | 87.6 | −0.90 | Angew. Chem. Int. Ed. 2022, 61, e202202087 [S12] |
| Cu foam | 0.25 M Li2SO4 (pH = ~7.0) | 99.99 vol.% | 517.1 | 93.5 | −0.90 | Angew. Chem. Int. Ed. 2020, 59, 9711–9718 [S13] |
| Fe2O3 nanorod | 0.1 M Na2SO4 + 0.5 mM FeII-EDTA (pH = ~7.0) | 10 vol.% | 78.02 | 86.7 | −0.60/−0.40 | J. Mater. Chem. A 2022, 10, 6454–6462 [S14] |
| CuFe alloy | 0.1 M PBS (pH = 7.4) | 95 vol.% NO + 5 vol.%NO2 | 136.81 | 90.6 | −0.80 | Chem Catal. 2022, 2, 622-638 [S15] |
| CoP nanowire | 0.2 M Na2SO4 (pH = 7.0) | 10 vol.% | 47.22 | 88.3 | −0.20 | Inorg. Chem. Front. 2022, 9, 1366-1372 [S16] |
| Ru0.05Cu0.95 | 0.5 M Na2SO4 (pH = 7.0) | 25 vol.% | 17.68 | 64.9 | −0.50 | Sci. China Chem. 2021, 64, 1493 [S17] |
| Mo2C nanosheets | 0.5 M Na2SO4 (pH = 7.0) | 99.99 vol.% | 122.7 | 86.3 | −0.40 | Inorg. Chem. 2023, 62, 653−658 [S18] |
| bcc RuGa | 0.1 M K2SO4 (pH = 7.0) | 20 vol.% | 160.3 µmol h-1 cm-2 b | 72.3 | −0.20 | Angew. Chem. Int. Ed. 2023, 62, e202213351 [S19] |
| Cu@Co | 0.1 M Na2SO4 (pH = 7.0) | 1.0 vol.% | 36.89 | 76.5 | −0.50 | Adv. Mater. 2023, 36, e2309470 [S20] |
| Cu nanosheets | 0.1 M K2SO4 (pH = 7.0) | 99.99 vol.% | 187.5 | 93.2 | −0.59 | Angew. Chem. Int. Ed. 2024, 63, e202319135 [S21] |
| FeOCl-VCl | 0.1 M HCl + 50 mM sodium benzenesulfonate (SB) (pH = 1.0) | 1.0 vol.% | 26.79 | 91.1 | −0.50 | Angew. Chem. Int. Ed. 2024, 63, e202318792 [S22] |
| CuFe DS/NC | 0.1 M Na2SO4 (pH = 7.0) | 99.99 vol.% | 112.52 | 90.0 | −0.60 | Adv. Mater. 2023, 35, 2304646 [S23] |
| hcp Co | 0.1 M Na2SO4 (pH = 7.0) | 99.99 vol.% | 439.5 | 72.6 | −0.60 | J. Am. Chem. Soc. 2023, 145, 6899−6904 [S24] |
|  | 0.1 M Na2SO4 + 0.5 mM FeII-EDTA (pH = 7.0) | 99.99 vol.% | 463.4 | 75.8 | −0.60 |  |
| low-coordinated Ru | 0.5 M Na2SO4 (pH = 7.0) | 1.0 vol.% | 45.02 | 66.0 | −0.20 | ACS Energy Lett. 2022, 7, 1187−1194 [S25] |
| MnO2-x nanowire array | 0.2 M Na2SO4 (pH = 7.0) | 10 vol.% | 9.90 | 82.8 | −0.70 | Mater. Today Phys. 2022, 22, 100586 [S26] |
| FeNC | 0.1 M HClO4 (pH = 1.0) | 10 vol.% | ~20.2 | 5.1 | −0.20 | Nat. Commun. 2021, 12, 1856 [S27] |
| NiNC@CF | 0.5 M PBS (pH = 7.4) | 99.99 vol.% | 108 | 87.0 | −0.90/−0.50 | J. Mater. Chem. A 2022, 10, 6470 [S28] |
| FeB2 | 0.5 M Na2SO4 (pH = 7.0) | 99.9 vol.% | 289.3 | 93.8 | −0.40 | Inorg. Chem. 2023, 62, 8487−8493 [S29] |
| Cu1/MoS2 | 0.5 M Na2SO4 (pH = 7.0) | 99.99 vol.% | 337.5 | 90.6 | −0.60 | Nano Res. 2023, 16, 5857–5863 [S30] |
| Sb1/MoO3 | 0.5 M Na2SO4 (pH = 7.0) | 99.9 vol.% | 273.5 | 91.7 | −0.60 | ACS Energy Lett. 2023, 8, 1281−1288 [S31] |
| Pd1Cu | 0.5 M Na2SO4 (pH = 7.0) | 99.99 vol.% | 305.8 | 96.7 | −0.40 | Nano Lett. 2024, 24, 541-548 [S32] |
| Ir1/MoO3 | 0.5 M Na2SO4 (pH = 7.0) | 99.9 vol.% | 438.8 | 93.2 | −0.47 | Nano Res. 2023, 16, 8737-8742 [S33] |
| Fe1/MoS2-x | 0.5 M Na2SO4 (pH = 7.0) | 99.99 vol.% | 288.2 | 82.5 | −0.60 | Appl. Catal., B 2023, 324, 122241 [S34] |
| W1/MoO3−x | 0.5 M Na2SO4 (pH = 7.0) | 99.99 vol.% | 308.6 | 91.2 | −0.50/−0.40 | Nano Lett. 2023, 23, 1735-1742 [S35] |
| Cu@Cu/C NWAs | 0.05 M H2SO4 (pH = 7.0) | 3.0 vol.% | 69.3 | 93.0 | −0.10 | J. Am. Chem. Soc. 2024, 146, 10044 [S36] |
| VO-TiO2-x | 1 M KOH + 50 mM SB (pH = 14.0) | 1.0 vol.% | 37.2 µmol h-1 mgcat.-1 c | 76.4 | −0.50 | Angew. Chem. Int. Ed. 2024, e202420346 [S37] |

a: This catalyst achieves the maximum NH3 yield rate and FENH3 at different potential.

b: The NH3 yield rate of bcc RuGa was re-calculated in the unit of µmol h-1 cm-2.

c: The NH3 yield rate of VO-TiO2-x was calculated in the unit of µmol h-1 mgcat.-1.

Table S3 The NO adsorption energy (Eads) of different configurations on Rh(100), RhB(002), RhB(100) and RhB(101) facets

| Model | Adsorption Site | NO adsorption energy (Eads) |
| --- | --- | --- |
| Rh(100) | RhNt | -2.429 eV |
|  | Rh2Nb | -2.797 eV |
|  | Rh4Nh | -2.640 eV |
| RhB(002) | RhNt | -2.136 eV |
|  | Rh2Nb | -2.088 eV |
|  | Rh3Nf | -2.255 eV |
|  | Rh3Nh | -2.088 eV |
| RhB(101) | RhNt | -2.063 eV |
|  | Rh2Nb | -1.806 eV |
|  | Rh3Nh | -1.806 eV |
|  | Rh3Nf | -2.371 eV |
| RhB(100) | RhNt | -2.334 eV |
|  | Rh2Nb | -2.988 eV |
|  | Rh3Nh | -3.097 eV |
|  | Rh3Nf | -2.350 eV |

Note: The Eads calculation results reveal that NO prefers to adopt Rh3Nf sites on RhB(002) and RhB(101), Rh3Nh site on RhB(100), and Rh2Nb site on Rh(100).

Table S4 Adsorbent charge transfer in Bader analysis (+ represents adsorbate gain electrons from slab, − is the opposite)

| System | Rh(100) | RhB(002) | RhB(100) | RhB(101) |
| --- | --- | --- | --- | --- |
| Sum electrons | +0.37 e− | +0.47 e− | +0.56 e− | +0.44 e− |

Table S5 Calculated Gibbs free energies (ΔG) of adsorption species for NORR on Rh(100), RhB(002), RhB(100) and RhB(101) surfaces with respect to the reference NO + * (in eV)

| Rh (100) | * | *NO | *HNO | *NHOH | *NH2OH | *NH2 | *NH3 |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 0.00 | -2.253 | -1.677 | -1.370 | -1.910 | -4.078 | -4.242 |
|  | * | *NO | *NOH |  |  |  |  |
|  | 0.00 | -2.253 | -1.590 |  |  |  |  |
| RhB (002) | * | *NO | *HNO | *NHOH | *NH2OH | *NH2 | *NH3 |
|  | 0.00 | -1.693 | -1.214 | -1.443 | -1.725 | -3.476 | -4.001 |
|  | * | *NO | *NOH |  |  |  |  |
|  | 0.00 | -1.693 | -0.882 |  |  |  |  |
| RhB (101) | * | *NO | *HNO | *NHOH | *NH2OH | *NH2 | *NH3 |
|  | 0.00 | -1.807 | -1.396 | -1.410 | -1.730 | -3.675 | -4.245 |
|  | * | *NO | *NOH |  |  |  |  |
|  | 0.00 | -1.807 | -1.295 |  |  |  |  |
| RhB (100) | * | *NO | *HNO |  |  |  |  |
|  | 0.00 | -2.824 | -2.104 |  |  |  |  |
|  | * | *NO | *NOH | *NHOH | *NH2OH | *NH2 | *NH3 |
|  | 0.00 | -2.824 | -2.130 | -1.970 | -1.856 | -4.062 | -4.121 |

Table S6 Comparison of peak power density of our battery with the reported Zn-NO battery systems

| Catalysts | Catholyte | Power density (mW cm-2) | Refs. |
| --- | --- | --- | --- |
| hcp RhB NPs | 0.2 M Na2SO4 | 4.33 | This work |
| Rh NCs | 0.2 M Na2SO4 | 2.91 | This work |
| a-Rh4B NPs | 0.2 M Na2SO4 | 1.94 | This work |
| NiO nanosheet | 0.1 M Na2SO4 | 0.88 | Chem. Commun. 2021, 57, 13562−13565 [S9] |
| MoS2 nanosheet | 0.1 M HCl + 0.5 mM FeII-SBa | 1.04 | Angew. Chem. Int. Ed. 2021, 60, 25263–25268 [S10] |
| Fe2O3 nanorod | 0.1 M Na2SO4 | 1.18 | J. Mater. Chem. A, 2022, 10, 6454–6462 [S14] |
| Ni2P nanosheet | 0.1 M HCl | 1.53 | J. Mater. Chem. A, 2021, 9, 24268–24275 [S11] |
| a-B2.6C@TiO2 | 0.1 M Na2SO4 | 1.7 | Angew. Chem. Int. Ed. 2022, 61, e202202087 [S12] |
| CuFe DS/NC | 0.1 M Na2SO4 | 2.3 | Adv. Mater. 2023, 35, 2304646 [S23] |
| Cu@Co | 0.1 M Na2SO4 | 3.08 | Adv. Mater. 2023, 2309470 [S20] |
| CoB/Co@C | 0.5 M Na2SO4 | 3.68 | Nano Lett. 2023, 23, 7120−7128 [S8] |
| hcp Co | 0.1 M Na2SO4 | 4.66 | J. Am. Chem. Soc. 2023, 145, 6899−6904 [S24] |
| FeOCl-VCl | 0.1 M HCl + 50 mM SBa | 6.2 | Angew. Chem. Int. Ed. 2024, e202318792 [S22] |
| NiFe LDH | 0.1 M HCl + 0.5 mM FeII-SBa | 1.8 | Chem. Commun. 2022, 58, 8097–8100 [S38] |
| Bi NDs | 0.1 M Na2SO4 + 0.5 mM FeII-EDTAa | 2.33 | Mater. Today Phys. 2022, 22, 100611 [S39] |
| Bi NPs@C | 0.1 M Na2SO4 | 2.35 | Nano Res. 2022, 151 5032-5037 [S40] |
| CoP nanowire | 0.2 M Na2SO4 | 0.496 | Inorg. Chem. Front. 2022, 9, 1366-1372 [S16] |
| MoC/NCS | 0.1 M HCl + 0.5 mM FeII-SBa | 1.8 | Nano Res. 2022,15, 8890-8896 [S7] |
| CoSx nanosheet | 0.2 M Na2SO4 | 2.06 | Inorg. Chem. 2022, 61, 8096−8102 [S41] |

a: FeII-SB, SB, and FeII-EDTA are electrolyte additives for rapid NO capture [S42, S43].

Supplementary References

- D. Zhu, L. Zhang, R.E. Ruther, R.J. Hamers, Photo-illuminated diamond as a solid-state source of solvated electrons in water for nitrogen reduction. Nat. Mater. 12(9), 836–841 (2013). https://doi.org/10.1038/nmat3696

- G.W. Watt, J.D. Chrisp, Spectrophotometric method for determination of hydrazine. Anal. Chem. 24(12), 2006–2008 (1952). https://doi.org/10.1021/ac60072a044

- B. Aronsson, J. Åselius, E. Stenberg, Borides and silicides of the platinum metals. Nature 183(4671), 1318–1319 (1959). https://doi.org/10.1038/1831318b0

- Z. Li, X. Ai, H. Chen, X. Liang, X. Li et al., Asymmetrically strained hcp rhodium sublattice stabilized by 1D covalent boron chains as an efficient electrocatalyst. Chem. Commun. 57(41), 5075–5078 (2021). https://doi.org/10.1039/D1CC00774B

- D. Chen, R. Yu, H. Zhao, J. Jiao, X. Mu et al., Boron-induced interstitial effects drive water oxidation on ordered Ir−B compounds. Angew. Chem. Int. Ed. 63(35), e202407577 (2024). https://doi.org/10.1002/anie.202407577

- Z. Li, Q. Zhou, J. Liang, L. Zhang, X. Fan et al., Defective TiO2−x for high-performance electrocatalytic NO reduction toward ambient NH3 production. Small 19(24), 2300291 (2023). https://doi.org/10.1002/smll.202300291

- G. Meng, M. Jin, T. Wei, Q. Liu, S. Zhang et al., MoC nanocrystals confined in N-doped carbon nanosheets toward highly selective electrocatalytic nitric oxide reduction to ammonia. Nano Res. 15(10), 8890–8896 (2022). https://doi.org/10.1007/s12274-022-4747-y

- B. Wu, L. Huang, L. Yan, H. Gang, Y. Cao et al., Boron-modulated electronic-configuration tuning of cobalt for enhanced nitric oxide fixation to ammonia. Nano Lett. 23(15), 7120–7128 (2023). https://doi.org/10.1021/acs.nanolett.3c01994

- P. Liu, J. Liang, J. Wang, L. Zhang, J. Li et al., High-performance NH3 production via NO electroreduction over a NiO nanosheet array. Chem. Commun. 57(99), 13562–13565 (2021). https://doi.org/10.1039/D1CC06113E

- L. Zhang, J. Liang, Y. Wang, T. Mou, Y. Lin et al., High-performance electrochemical NO reduction into NH3 by MoS2 nanosheet. Angew. Chem. Int. Ed. 60(48), 25263–25268 (2021). https://doi.org/10.1002/anie.202110879

- T. Mou, J. Liang, Z. Ma, L. Zhang, Y. Lin et al., High-efficiency electrohydrogenation of nitric oxide to ammonia on a Ni2P nanoarray under ambient conditions. J. Mater. Chem. A 9(43), 24268–24275 (2021). https://doi.org/10.1039/D1TA07455E

- J. Liang, P. Liu, Q. Li, T. Li, L. Yue et al., Amorphous boron carbide on titanium dioxide nanobelt arrays for high-efficiency electrocatalytic NO reduction to NH3. Angew. Chem. 134(18), e202202087 (2022). https://doi.org/10.1002/ange.202202087

- J. Long, S. Chen, Y. Zhang, C. Guo, X. Fu et al., Direct electrochemical ammonia synthesis from nitric oxide. Angew. Chem. Int. Ed. 59(24), 9711–9718 (2020). https://doi.org/10.1002/anie.202002337

- J. Liang, H. Chen, T. Mou, L. Zhang, Y. Lin et al., Coupling denitrification and ammonia synthesis via selective electrochemical reduction of nitric oxide over Fe2O3 nanorods. J. Mater. Chem. A 10(12), 6454–6462 (2022). https://doi.org/10.1039/D2TA00744D

- R. Hao, L. Tian, C. Wang, L. Wang, Y. Liu et al., Pollution to solution: a universal electrocatalyst for reduction of all NOx-based species to NH3. Chem Catal. 2(3), 622–638 (2022). https://doi.org/10.1016/j.checat.2022.01.022

- J. Liang, W.-F. Hu, B. Song, T. Mou, L. Zhang et al., Efficient nitric oxide electroreduction toward ambient ammonia synthesis catalyzed by a CoP nanoarray. Inorg. Chem. Front. 9(7), 1366–1372 (2022). https://doi.org/10.1039/D2QI00002D

- J. Shi, C. Wang, R. Yang, F. Chen, N. Meng et al., Promoting nitric oxide electroreduction to ammonia over electron-rich Cu modulated by Ru doping. Sci. China Chem. 64(9), 1493–1497 (2021). https://doi.org/10.1007/s11426-021-1073-5

- K. Chen, P. Shen, N. Zhang, D. Ma, K. Chu, Electrocatalytic NO reduction to NH3 on Mo2C nanosheets. Inorg. Chem. 62(2), 653–658 (2023). https://doi.org/10.1021/acs.inorgchem.2c03714

- H. Zhang, Y. Li, C. Cheng, J. Zhou, P. Yin et al., Isolated electron-rich ruthenium atoms in intermetallic compounds for boosting electrochemical nitric oxide reduction to ammonia. Angew. Chem. Int. Ed. 62(4), e202213351 (2023). https://doi.org/10.1002/anie.202213351

- Z. Wu, Y. Liu, D. Wang, Y. Zhang, K. Gu et al., Cu@Co with dilatation strain for high-performance electrocatalytic reduction of low-concentration nitric oxide. Adv. Mater. 36(11), e2309470 (2024). https://doi.org/10.1002/adma.202309470

- L. Xiao, S. Mou, W. Dai, W. Yang, Q. Cheng et al., Identification of Cu(111) as superior active sites for electrocatalytic NO reduction to NH(3) with high single-pass conversion efficiency. Angew. Chem. Int. Ed. 63(11), e202319135 (2024). https://doi.org/10.1002/anie.202319135

- X. Guo, P. Wang, T. Wu, Z. Wang, J. Li et al., Aqueous electroreduction of nitric oxide to ammonia at low concentration via vacancy engineered FeOCl. Angew. Chem. Int. Ed. 63(6), e202318792 (2024). https://doi.org/10.1002/anie.202318792

- D. Wang, X. Zhu, X. Tu, X. Zhang, C. Chen et al., Oxygen-bridged copper–iron atomic pair as dual-metal active sites for boosting electrocatalytic NO reduction. Adv. Mater. 35(39), 2304646 (2023). https://doi.org/10.1002/adma.202304646

- D. Wang, Z.-W. Chen, K. Gu, C. Chen, Y. Liu et al., Hexagonal cobalt nanosheets for high-performance electrocatalytic NO reduction to NH3. J. Am. Chem. Soc. 145(12), 6899–6904 (2023). https://doi.org/10.1021/jacs.3c00276

- Y. Li, C. Cheng, S. Han, Y. Huang, X. Du et al., Electrocatalytic reduction of low-concentration nitric oxide into ammonia over Ru nanosheets. ACS Energy Lett. 7(3), 1187–1194 (2022). https://doi.org/10.1021/acsenergylett.2c00207

- Z. Li, Z. Ma, J. Liang, Y. Ren, T. Li et al., MnO2 nanoarray with oxygen vacancies: an efficient catalyst for NO electroreduction to NH3 at ambient conditions. Mater. Today Phys. 22, 100586 (2022). https://doi.org/10.1016/j.mtphys.2021.100586

- D.H. Kim, S. Ringe, H. Kim, S. Kim, B. Kim et al., Selective electrochemical reduction of nitric oxide to hydroxylamine by atomically dispersed iron catalyst. Nat. Commun. 12(1), 1856 (2021). https://doi.org/10.1038/s41467-021-22147-7

- T. Muthusamy, S. Sethuram Markandaraj, S. Shanmugam, Nickel nanoparticles wrapped in N-doped carbon nanostructures for efficient electrochemical reduction of NO to NH3. J. Mater. Chem. A 10(12), 6470–6474 (2022). https://doi.org/10.1039/D2TA00623E

- G. Zhang, F. Wang, Y. Wan, Y. Guo, K. Chu, Iron diboride (FeB2) for the electroreduction of NO to NH3. Inorg. Chem. 62(22), 8487–8493 (2023). https://doi.org/10.1021/acs.inorgchem.3c01207

- K. Chen, G. Zhang, X. Li, X. Zhao, K. Chu, Electrochemical NO reduction to NH3 on Cu single atom catalyst. Nano Res. 16(4), 5857–5863 (2023). https://doi.org/10.1007/s12274-023-5384-9

- K. Chen, Y. Zhang, J. Xiang, X. Zhao, X. Li et al., P-block antimony single-atom catalysts for nitric oxide electroreduction to ammonia. ACS Energy Lett. 8(3), 1281–1288 (2023). https://doi.org/10.1021/acsenergylett.2c02882

- K. Chen, J. Xiang, Y. Guo, X. Liu, X. Li et al., Pd1Cu single-atom alloys for high-current-density and durable NO-to-NH3 electroreduction. Nano Lett. 24(2), 541–548 (2024). https://doi.org/10.1021/acs.nanolett.3c02259

- K. Chen, G. Wang, Y. Guo, D. Ma, K. Chu, Iridium single-atom catalyst for highly efficient NO electroreduction to NH3. Nano Res. 16(7), 8737–8742 (2023). https://doi.org/10.1007/s12274-023-5556-7

- K. Chen, J. Wang, J. Kang, X. Lu, X. Zhao et al., Atomically Fe-doped MoS2−x with Fe-Mo dual sites for efficient electrocatalytic NO reduction to NH3. Appl. Catal. B Environ. 324, 122241 (2023). https://doi.org/10.1016/j.apcatb.2022.122241

- K. Chen, J. Wang, H. Zhang, D. Ma, K. Chu, Self-tandem electrocatalytic NO reduction to NH3 on a W single-atom catalyst. Nano Lett. 23(5), 1735–1742 (2023). https://doi.org/10.1021/acs.nanolett.2c04444

- J. Meng, C. Cheng, Y. Wang, Y. Yu, B. Zhang, Carbon support enhanced mass transfer and metal–support interaction promoted activation for low-concentrated nitric oxide electroreduction to ammonia. J. Am. Chem. Soc. 146(14), 10044–10051 (2024). https://doi.org/10.1021/jacs.4c00898

- X. Guo, T. Wu, H. Li, L. Chai, M. Liu, Enhancing low-concentration electroreduction of NO to NH3 via potential-controlled active site-intermediate interactions. Angew. Chem. Int. Ed. 64(8), e202420346 (2025). https://doi.org/10.1002/anie.202420346

- G. Meng, T. Wei, W. Liu, W. Li, S. Zhang et al., NiFe layered double hydroxide nanosheet array for high-efficiency electrocatalytic reduction of nitric oxide to ammonia. Chem. Commun. 58(58), 8097–8100 (2022). https://doi.org/10.1039/D2CC02463B

- Y. Lin, J. Liang, H. Li, L. Zhang, T. Mou et al., Bi nanodendrites for highly efficient electrocatalytic NO reduction to NH3 at ambient conditions. Mater. Today Phys. 22, 100611 (2022). https://doi.org/10.1016/j.mtphys.2022.100611

- Q. Liu, Y. Lin, L. Yue, J. Liang, L. Zhang et al., Bi nanoparticles/carbon nanosheet composite: a high-efficiency electrocatalyst for NO reduction to NH3. Nano Res. 15(6), 5032–5037 (2022). https://doi.org/10.1007/s12274-022-4283-9

- L. Zhang, Q. Zhou, J. Liang, L. Yue, T. Li et al., Enhancing electrocatalytic NO reduction to NH3 by the CoS nanosheet with sulfur vacancies. Inorg. Chem. 61(20), 8096–8102 (2022). https://doi.org/10.1021/acs.inorgchem.2c01112

- K. Ogura, H. Ishikawa, Electrochemical conversion of nitrous oxide into ammonia in the presence of iron complexes. J. Chem. Soc., Faraday Trans. 1 80(8), 2243 (1984). https://doi.org/10.1039/f19848002243

- E.K. Pham, S.-G. Chang, Removal of NO from flue gases by absorption to an iron(ii) thiochelate complex and subsequent reduction to ammonia. Nature 369(6476), 139–141 (1994). https://doi.org/10.1038/369139a0