Supporting Information for

Solid-State Hydrogen Storage Materials with Excellent Selective Hydrogen Adsorption in the Presence of Alkanes, Oxygen, and Carbon Dioxide by Atomic Layer Amorphous Al2O3 Encapsulation

Fanqi Bu 1, Zhenyu Wang 1 *, Ali Wajid 2, Rui Zhai 1, Ting Liu 3, Yaohua Li 1, Xin Ji 1, Xin Liu 1, Shujiang Ding 2, Yonghong Cheng 1, Jinying Zhang 1 *

1 State Key Laboratory of Electrical Insulation and Power Equipment, Center of Nanomaterials for Renewable Energy (CNRE), School of Electrical Engineering, Xi'an Jiaotong University, Xi'an, Shaanxi 710049, P. R. China

2 School of Chemistry, Xi’an Key Laboratory of Sustainable Energy Materials Chemistry, State Key Laboratory for Mechanical Behavior of Materials, Xi’an Jiaotong University, Xi’an 710049, P. R. China

3 Aviation Engineering school, Air Force Engineering University, Xi’an 710038, P. R. China

*Corresponding authors. E-mail: z.wang@mpi-susmat.de (Zhenyu Wang); jinying.zhang@mail.xjtu.edu.cn (Jinying Zhang)

S1 Material Characterizations

Transmission electron microscopy (TEM) images, high-resolution TEM (HRTEM) images, high-angle annular dark-field scanning transmission electron microscopy (HAADF-STEM), and elemental mapping were acquired by Lorenz Transmission Electron Microscope (Talos F200X). Scanning electron microscopy (SEM) images were recorded by Quanta 250FEG equipment. X-ray diffraction (XRD) spectra were obtained from a Bruker D2 PHASER using Cu/Kα radiation (λ =1.5418Å) at 40 kV and 30 mA. The deposited thickness of amorphous ZrO2/Al2O3 from ALD was measured by ellipsometry (SE401adv-C, SENTECH, Germany). The hydrogen storage properties of MgH2-based materials were tested using a homemade HPSA-auto apparatus [S1]. The blank MgH2-ZrTi used for comparison was subjected to all the sample preparation processes of MgH2-ZrTi@10nmAl2O3, only the ALD process without TMA pulses.

S2 Hydrogen Sorption Measurements

The isothermal cyclic adsorption was repeatedly performed at target temperature (75℃ or 100℃) in different atmospheres (30 bar 10%CH4+90%H2, 16 bar 0.1%O2+0.4%N2+99.5%H2, or 16 bar 0.1%CO2+0.4%N2+99.5%H2) for 0.5 h, followed by dehydrogenation treatment at 275 ℃ for 15min. The isothermal dehydrogenation of MgH2-ZrTi@10nmAl2O3 at different temperature (250, 275, or 300 ℃) was conducted after re-hydrogenation at 100 ℃ for 1 h under impure hydrogen atmosphere (30 bar 10%CH4+90%H2 or 16 bar 0.1%O2+0.4%N2+99.5%H2). Temperature programmed desorption (TPD) was tested from 100 to 400 ℃ at a heating rate of 3 ℃/min. The isothermal desorption kinetic of hydrogen storage materials was measured at different temperatures (250, 275, or 300 ℃) after re-hydrogenation under 30 bar H2 at different temperatures (250, 275, or 300 ℃), where the starting hydrogen pressures was set to be below 0.05 bar. The isothermal hydrogen absorption kinetic of hydrogen storage materials was tested at different temperatures (75, 100, or 125 ℃) under different atmospheres (30 bar H2, 30 bar 10%CH4+90%H2, 16 bar 0.1%O2+0.4%N2+99.5%H2, or 16 bar 0.1%CO2+99.9%H2) for 0.5h. The isothermal dehydrogenation (0.05 bar H2) and re-hydrogenation (30 bar H2) tests of the samples under pure H2 were performed repeatedly at 275 ℃ for the cycling measurements.

S3 Machine Learning Molecular Dynamics

All simulations were carried out using the LAMMPS package [S2]. Interatomic interactions were described using the Graph Atomic Cluster Expansion (GRACE) framework, specifically the GRACE-2L-OMAT model. This semi-local, two-layer machine learning potential was trained on the OMat24 dataset, which comprises over 101 million structures spanning 3.23 million materials. The dataset ensures comprehensive coverage of elemental combinations and bonding environments, with Al2O3 well-represented in both bulk and surface forms. Gas molecules such as H2, CH4, O2, N2, and CO2 consist of light elements (H, C, N, O) that are explicitly included in the training set and validated through Matbench Discovery benchmarks. The GRACE-2L-OMAT model has demonstrated high accuracy in predicting thermodynamic and transport properties, including thermal conductivity and diffusion behaviour (key factors in gas permeation studies). To assess the reliability of the GRACE-2L-OMAT potential for our system, we performed geometry optimizations on key molecular and solid-state structures. The results (Table S1) were consistent with density functional theory (DFT) calculations using the GGA-PBE functional, a widely accepted benchmark for structural accuracy.

Supplementary Table and Figures

Table S1 Validation of GRACE-2L-OMAT via Geometry Optimization

| System | Property | GRACE-2L-OMAT Result | DFT (GGA-PBE) Reference Range |
| --- | --- | --- | --- |
| α-Al2O3 | a = b | 4.806 Å | ~4.76–4.81 Å |
|  | c | 13.134 Å | ~13.0–13.2 Å |
|  | α, β, γ | 90°, 90°, 120° | 90°, 90°, 120° |
| O2 molecule | O–O bond length | 1.256 Å | ~1.21–1.26 Å |
| CH4 molecule | C–H bond length | 1.09 Å | ~1.09 Å |
|  | H–C–H angle | 109.47° | ~109.5° |
| H2 molecule | H–H bond length | 0.732 Å | ~0.74 Å |
| H2O molecule | O–H bond length | 0.973 Å | ~0.96–0.98 Å |
|  | H–O–H angle | 105.36° | ~104.5–106° |
| CO2 molecule | C–O bond length | 1.178 Å | ~1.16–1.18 Å |
| N2 | N–N | 1.112 Å | ~1.10–1.12 |

Fig. S1 Particle size distribution of (a) MgH2-ZrTi and (b) MgH2-ZrTi@10nmAl2O3

Fig. S2 (a) TEM and (b) HRTEM of MgH2-ZrTi@10nmAl2O3

Fig. S3 (a) Isothermal dehydrogenation (275 ℃) and (b) TPD curves of MgH2-ZrTi before and after exposure to air for 1 day [S3]

Fig. S4 XRD patterns of MgH2-ZrTi after exposure to air (15 ℃ and 25% RH) for 1 week and then heated at 200℃ for 48 h in an air atmosphere

Fig. S5 XRD patterns of MgH2-ZrTi@5nmAl2O3 after air exposure for different times

Fig. S6 XRD pattern of MgH2-ZrTi@10nmAl2O3 after exposure to air at 30 ℃ and 50% RH for 3 weeks

Fig. S7 XRD patterns of Mg-ZrTi@10nmAl2O3 in non-hydrogen state after exposure to air at 30 ℃ and 50% RH for 3 weeks

Fig. S8 Isothermal hydrogenation curves of MgH2-ZrTi@10nmAl2O3 at 30 bar pure H2 as well as at 35 bar 10%CH4+90%H2 atmosphere

Fig. S9 XRD patterns of MgH2-ZrTi (red) and MgH2-ZrTi@10nmAl2O3 (black) after hydrogenation in 10%CH4+90%H2 atmosphere

Fig. S10 The isothermal hydrogenation curves in pure H2 and isothermal cyclic hydrogenation curves in 10%CH4+90%H2 atmosphere for MgH2-ZrTi at 75 ℃

Fig. S11 SEM image of MgH2-ZrTi after hydrogenation in 10%CH4+90%H2 atmosphere

Fig. S12 HAADF-STEM and elemental mapping analysis of blank MgH2-ZrTi after hydrogenation in 10%CH4+90%H2 atmosphere

Fig. S13 HAADF-STEM and elemental mapping analysis of MgH2-ZrTi before hydrogenation in 10%CH4+90%H2 atmosphere

Fig. S14 (a) Isothermal adsorption curves and (b) isothermal cyclic adsorption curves of MgH2-ZrTi@10nmAl2O3 under 10%CH4+90%H2 atmosphere (75 ℃)

Fig. S15 SEM images of MgH2-ZrTi@10nmAl2O3 after hydrogenation at 125 ℃ under 10%CH4+90%H2 atmosphere

Fig. S16 HAADF-STEM and the elemental mapping analysis of MgH2-ZrTi@10nmAl2O3 after hydrogenation at 125 ℃ under 10%CH4+90%H2 atmosphere

Fig. S17 Detailed isothermal cyclic adsorption curve of MgH2-ZrTi@10nmAl2O3 under 10%CH4+90%H2 atmosphere

Fig. S18 The isothermal hydrogenation curves in pure H2 and isothermal cyclic hydrogenation curves in 0.1%O2+0.4%N2+99.5%H2 atmosphere for blank MgH2-ZrTi at 100℃

Fig. S19 (a) Isothermal adsorption curves and (b) isothermal cyclic adsorption curve of MgH2-ZrTi@10nmAl2O3 under 0.1%O2+0.4%N2+99.5%H2 atmosphere (100 ℃)

Fig. S20 (a) XRD patterns and (b) partially enlarged XRD patterns of MgH2-ZrTi and MgH2-ZrTi@10nmAl2O3 after hydrogenation in 0.1%O2+0.4%N2+99.5%H2 atmosphere

Fig. S21 Isothermal hydrogenation curves in pure H2 and isothermal cyclic hydrogenation curves in 0.1%CO2+0.4%N2+99.5%H2 atmosphere (16 bar) for (a) MgH2-ZrTi and (b) MgH2-ZrTi@10nmAl2O3 at 100 ℃

Fig. S22 (a) Side and (b) top views of the double-wall α- Al2O3 model consisting of two parallel slabs. (c-h) The simulation of the penetration of different gas molecule (H2, CO2, H2O, O2, CH4, and N2) between the two Al2O3 slabs

Fig. S23 Normalized isothermal dehydrogenation (275 °C) curves of MgH2, MgH2-ZrTi@5nmAl2O3, MgH2-ZrTi@10nmAl2O3, and MgH2-ZrTi@20nmAl2O3 by MgH2 theoretical capacity

Fig. S24 (a) Isothermal dehydrogenation curves of MgH2-ZrTi@10nmAl2O3 after re-hydrogenation at 100 ℃ for 1 h under 30 bar 10%CH4+90%H2 at different temperature and (b) the relationships of (t/t0.5)theo vs. (t/t0.5)exp at 275 ℃ according to various kinetic models

Fig. S25 (a) Isothermal dehydrogenation curves of MgH2-ZrTi@10nmAl2O3 after re-hydrogenation at 100 ℃ for 1 h under 16 bar 0.1%O2+0.4%N2+99.5%H2 at different temperature and (b) the relationships of (t/t0.5)theo vs. (t/t0.5)exp at 275 ℃ according to various kinetic models

Fig. S26 Dehydrogenation capacity of MgH2-ZrTi@10nmAl2O3 at 250 °C (within 30 min), 275 °C (within 20 min), and 300 °C (within 10 min) after re-hydrogenation in different hydrogen atmospheres

Fig. S27 (a) TEM and (b) HRTEM of MgH2-ZrTi@10nmAl2O3 after rehydro-genation

Fig. S28 High-resolution XPS spectra of (a) Al 2p and (b) Mg 1s from the as-produced, dehydrogenated, and re-hydrogenated MgH2-ZrTi@10nmAl2O3

Fig. S29 HAADF-STEM and the corresponding elemental analyses of MgH2-ZrTi@10nmAl2O3 after dehydrogenation

Fig. S30 HAADF-STEM and the corresponding elemental analyses of MgH2-ZrTi@10nmAl2O3 after rehydrogenation

Fig. S31 SEM images of MgH2-ZrTi@10nmAl2O3 after dehydrogenation at different scales

Fig. S32 SEM images of MgH2-ZrTi@10nmAl2O3 after rehydrogenation at different scales

Supplementary References

- C. Wu, Y. Wang, Y. Liu, W. Ding, C. Sun, Enhancement of hydrogen storage properties by in situ formed LaH3 and Mg2NiH4 during milling MgH2 with porous LaNiO3. Catal. Today 318, 113–118 (2018). https://doi.org/10.1016/j.cattod.2017.09.037

- A.P. Thompson, H.M. Aktulga, R. Berger, D.S. Bolintineanu, W.M. Brown et al., LAMMPS - a flexible simulation tool for particle-based materials modeling at the atomic, meso, and continuum scales. Comput. Phys. Commun. 271, 108171 (2022). https://doi.org/10.1016/j.cpc.2021.108171

- F. Bu, A. Wajid, M. Gu, T. Liu, S. Liu et al., Synergistic effect of multivalent Ti, Zr, and oxygen vacancies to significantly enhance the hydrogen sorption properties of MgH2. J. Mater. Chem. A 13(21), 16102–16111 (2025). https://doi.org/10.1039/D5TA01302J