Supporting Information for

Ultrafast Sulfur Redox Dynamics Enabled by a PPy@N-TiO2 Z-Scheme Heterojunction Photoelectrode for Photo-assisted Lithium-Sulfur Batteries

Fei Zhao1, 2, Yibo He1, 2, *, Xuhong Li1, Ke Yang1, 2, Shuo Chen1, 2, Yuanzhi Jiang3, Xue-Sen Wang4, Chunyuan Song1, 2, and Xuqing Liu1, 2

1 State Key Laboratory of Solidification Processing, Center of Advanced Lubrication and Seal Materials, School of Materials Science and Engineering, Northwestern Polytechnical University, Xi’an, Shaanxi 710072, P. R. China

2 Research & Development Institute of Northwestern Polytechnical University in Shenzhen, Shenzhen 518063, P. R. China

3 Key Laboratory of Advanced Energy Materials Chemistry (Ministry of Education), Nankai University, Tianjin 300071, P. R. China

4 Department of Physics, National University of Singapore, Singapore 117543, Singapore

*Corresponding author. E-mail: heyibo@nwpu.edu.cn (Yibo He)

Supplementary Figures and Table

Fig. S1 Low-magnification SEM image of CC

Fig. S2 SEM image of TiO2/CC

Fig. S3 Low-magnification SEM image of PPy@N-TiO2/CC

Fig. S4 Element mapping of PPy@N-TiO2/CC

Fig. S5 N 1s XPS spectrum of N-TiO2/CC

Fig. S6 a C 1s, b Ti 2p XPS spectra of PPy@N-TiO2/CC

Fig. S7 a UV-vis absorption spectra and b the band gap of N-TiO2/CC and PPy@CC

Fig. S8 Band energy diagram of N-TiO2/CC and PPy@CC vs. Li/Li+

Fig. S9 PL emission spectra of various samples

Fig. S10 Average planar electron density difference Δρ(z) for PPy@N-TiO2

Fig. S11 a Discharge and b charge curves of PPy@N-TiO2/CC battery at 0.2 C by altering the light on/off

Fig. S12 a GCD curves of PPy@N-TiO2/CC battery at 0.2 C without the illumination. Corresponding b Raman spectra and c XRD patterns of PPy@N-TiO2/CC photocathode without the illumination

Fig. S13 EIS spectra of the PPy@N-TiO2 battery at 0.2 C (a) with and (b) without the illumination

Fig. S14 Schematic diagram of DRT analysis

Fig. S15 Schematic diagram and optical photograph of PALSB assembly

Fig. S16 LSV curves of Li||PPy@N-TiO2/CC battery with the illumination

Fig. S17 UV-vis absorption spectra of Li2S6 solution with different samples (inset: the digital photo of polysulfides adsorption)

Fig. S18 CV curves of symmetric batteries without Li2S6 at 0.5 mV s–1 with PPy@N-TiO2/CC electrode with and without the illumination

Fig. S19 EIS curves of PPy@N-TiO2/CC assembled PALSB with and without the illumination

Fig. S20 EIS curves of PPy@N-TiO2/CC assembled PALSB under photothermal

Fig. S21 CV curves of PPy@N-TiO2/CC battery with and without the illumination at a 0.1 mV s–1, b 0.2 mV s–1, c 0.3 mV s–1, and d 0.4 mV s–1

Fig. S22 CV curves of PPy@N-TiO2/CC battery a with and b without the illumination at different scan rates. Plots of CV peak current versus square root of scan rate c with and d without the illumination

Fig. S23 GCD curves of PPy@N-TiO2/CC battery at 0.2 C with and without the illumination

Fig. S24 The SEM images of PPy@N-TiO2/CC electrode after being initially discharged a with and b without the illumination (Schematic diagram of discharge product morphology with and without the illumination)

Fig. S25 Rate performance of PPy@N-TiO2/CC battery under photothermal

Fig. S26 Partially enlarged GCD curves by altering the illumination periodically: a,b initial cycle, c,d final cycle

Fig. S27 GCD curves with sulfur loading of 3 mg cm–2 at 0.2 C

Fig. S28 Cycling performance of PPy@N-TiO2/CC without the Li2S6 solution

Fig. S29 a, b Tafel curves of PPy@N-TiO2/CC, N-TiO2/CC and TiO2/CC electrodes with the illumination

Fig. S30 Cycling performance of PPy@N-TiO2/CC battery at 3 C without the illumination

Fig. S31 Cycling performance with a sulfur loading of 3 mg cm–2 at 0.5 C

Fig. S32 Evaluation of the practicability of PPy@N-TiO2/CC assembled PALSB: in series with an electronic thermometer

Tabel S1 The fitted results from EIS analysis

| Cathode | Test condition | R1 (ohm) | R2 (ohm) | R3(ohm) |
| --- | --- | --- | --- | --- |
| PPy@N-TiO2/CC | Dark | 10.8 | 71.0 | 23.1 |
|  | Thermal | 10.7 | 61.6 | 21.7 |
|  | Light | 6.4 | 12.5 | 11.4 |
| N-TiO2/CC | Light | 8.37 | 19.9 | 13.8 |
| TiO2/CC | Light | 9.3 | 18.5 | 26.2 |