Supporting Information for

Violet Arsenic Phosphorus: Switching p-Type into High Performance n-Type Semiconductor by Arsenic Substitution

Rui Zhai1#, Zhuorui Wen1#, Xuewen Zhao2#, Junyi She1, Mengyue Gu1, Fanqi Bu1, Chang Huang3, Guodong Meng1, Yonghong Cheng1, and Jinying Zhang1*

1 State Key Laboratory of Electrical Insulation and Power Equipment, Center of Nanomaterials for Renewable Energy, School of Electrical Engineering, Xi’an Jiaotong University, Xi’an, Shaanxi 710049, P. R. China

2 State Grid Integrated Energy Service Group Co., Ltd., Beijing 100052, P. R. China

3 Instrumental Analysis Center of Xi'an Jiaotong University, Xi'an Jiaotong University, Xi'an 710049, P. R. China

#Rui Zhai, Zhuorui Wen, and Xuewen Zhao are co-first authors and contributed equally to this work.

*Corresponding author. E-mail: jinying.zhang@mail.xjtu.edu.cn (Jinying Zhang)

First-principles Calculations

Density functional theory (DFT) of bulk VP and P20.61As0.39 were implemented in the Vienna Ab Initio Simulation Package (VASP) code. The Perdew-Burke-Ernzerhof (PBE) functional within the generalized gradient approximation (GGA) was adopted to describe electronic exchange-correlation energy. The ionic cores were described with the projector augmented wave (PAW) method. The calculated structures were the periodic boundary conditions. A basis set of plane waves was up to an energy cutoff of 500 eV. For the structure optimization and energy calculations, the K-points were set to be 2 × 2 ×2. All of the calculations were continued until the force and energy have converged to less than 0.01 eV Å-1 and 10-4 eV, respectively. Calculations of violet phosphorene and P20.61As0.39 phosphorene were carried out on the basis of the framework of DFT and the Vienna ab initio simulation package [S1]. The generalzied gradient approximation proposed by Perdew, Burke, and Ernzerhof is selected for the exchange-correlation potential [S2]. The long range van der Waals interaction is described by the DFT-D3 approach [S3]. The cut-off energy for plane wave is set to 550 eV. The energy criterion is set to 10−6 eV in iterative solution of the Kohn-Sham equation. A vacuum layer of 35 Å is added perpendicular to the sheet to avoid artificial interaction between periodic images. The Brillouin zone integration is performed using a 2×2×1 k-mesh. All the structures are relaxed until the residual forces on the atoms have declined to less than 0.01 eV/Å.

Generally, the carrier mobility, μ2D, of the 2D semi-conductor, with a view to studying the properties of migration of electrons and holes, can be obtained as follows [S4]:

μ2D=eℏ3C2DKBTma*mdE12

where e is the electron charge, ℏ is the reduced Planck constant, KB is the Boltzmann constant and T is the temperature (300 K in our calculations). The ma* and md=mx*my* are the effective mass and average effective mass of carriers along the transport direction, respectively. The in-plane stiffness C2D = 2[∂2E/∂(Δl/l0)2]/S0, where the E is total energy and S0 is the area of the xy plane for the supercell, respectively. The E1 = ΔV/(Δl/l0) is the deformation potential constant, the ΔV =ΔEVBM or ΔECBM (strain range from -2% to 2%, calculated using 1% steps), Δl and l0 are the deformation of the lattice constants along the transport direction and the intrinsic lattice constants, correspondingly.

Photocatalytic Hydrogen Evolution Measurements

10 mg VP-As (P83.4As0.6) single crystals were first ground followed by the addition of 50 mL of deionized water, which was then exfoliated to phosphorene nanosheets using a Ultrasonic Cell Crusher (JYD-250L) at 25 W for 2 h. About 1 wt.% chloroplatinic acid solution was added to the reaction suspension as precursors to obtain Pt co-catalyst. 0.2 M of ascorbic acid was then added as sacrificial agents. The photocatalytic H2 evolution reactions were carried out under irradiation of a Xe lamp (CEL-PF300-T8, 300W, 350 nm - 780 nm) in a quartz cell connected to a glass closed gas circulation and evacuation system (Labsolar-6a, PERFECTLIGHT, Beijing) for 4 h. The production of H2 was detected by an online gas chromatography with TCD detector (GC-9790). High pure Argon gas was used as carrier gas.

Supplementary Figures and Tables

Fig. S1 Optical images of (a) the quartz tube after reaction; (b) the as-produced violet arsenic phosphorus wrapped inside molten lead (from red circle of Fig. S1a)

Fig. S2 SEM image of some pieces of bulk violet arsenic phosphorus

Fig. S3 Detail picture for the single-crystal X-ray diffraction measurements of P83.4As0.6

Fig. S4 Tubular substructure with position number and bond lengths of violet phosphorus

Fig. S5 High-resolution XPS spectra of P2p of VP

Fig. S6 Optical images of (a) the quartz tube after reaction; (b) the as-produced violet arsenic phosphorus wrapped inside molten lead (from yellow box of Figure S3a). (c) SEM image of the products from the red box of Figure S3a accompanied by corresponding elemental mapping analysis, SEM image of (d) the product from the red box in Figure S3a and (e) enlarged layered structure; (f)-(g) the product from the red box in Figure S3a. (h) SEM image accompanied by corresponding elemental mapping analysis and (i) EDS spectrum of the As–P–Pb product

Fig. S7 The nucleation mechanism of violet arsenic phosphorus crystals from lead droplets. (a) Different views of PbP7 crystal structure. (b) The nearest-neighbor phosphorus structure of PbP7 crystals, and (c) the corresponding P2[P9]P2[P8] tubular structure of violet phosphorus framework after recombination

Fig. S8 Schematic illustration of the growth mechanism of violet arsenic phosphorus crystals

Fig. S9 (a) Synthesis parameters for chemical vapor transport method to produce violet arsenic phosphorus. Optical images of (b) the quartz tube after reaction and (c, d) the as-produced violet arsenic phosphorus crystals

Fig. S10 (a) Synthesis parameters for direct vapor condensation method to produce violet arsenic phosphorus. Optical images of (b) the quartz tube after reaction and (c) the as-produced violet arsenic phosphorus crystals. (d) SEM image of the as-produced violet arsenic phosphorus

Fig. S11 The corresponding Source–drain current as a function of gate voltage obtained from a FET based on a VP-As (P83.4As0.6) nanosheet (Vds = 5 V) with the individual (a) gold, (b) silver, and (c) copper electrode

Fig. S12 (a) Raman spectra, (b) valence band XPS, (c) diffuse reflectance spectra and (d) deduced band edges of violet arsenic phosphorus with different substitutional rate of arsenic atoms

Fig. S13 (a) Optical image and (b) corresponding source–drain current (Vds = 5 V) according to gate voltage obtained from a VP-As-low nanosheet based FET

Fig. S14 (a) The optical image and (b) corresponding source–drain current (Vds = 5 V) according to gate voltage of a VP-As (P83.4As0.6) nanosheet based FET after exposure in ambient conditions for 5 hours. (c) The optical image and (d) corresponding source–drain current (Vds = 5 V) according to gate voltage of a VP-As (P83.4As0.6) nanosheet based FET after exposure in ambient conditions for 1 day

Fig. S15 (a) Photocatalytic H2 evolution curves and (b) H2 evolution rates of violet arsenic phosphorene nanosheets and violet phosphorene nanosheets

Table S1 Crystal data and structure refinement for a P83.4As0.6 single crystal

| empirical formula | P83.4As0.6 |
| --- | --- |
| Formula weight | 2627.85 |
| temperature /K | 302 |
| crystal system | monoclinic |
| space group | P 2/n |
| a /Å | 9.2075(4) |
| b /Å | 9.1507(4) |
| c /Å | 21.7698(10) |
| α/° | 90 |
| β /° | 94.388(2) |
| γ /° | 90 |
| volume /Å3 | 1828.84(14) |
| Z | 1 |
| calculated density /g cm-3 | 2.386 |
| μ /mm‑1 | 2.139 |
| Crystal size/mm3 | 0.2 × 0.15 × 0.1 |
| Radiation | MoKα (λ = 0.71073) |
| F(000) | 1271 |
| 2Θ range for data collection /° | 3.752 to 52.742 |
| Index ranges | -11 ≤ h ≤ 11, -11 ≤ k ≤ 11, -28 ≤ l ≤ 28 |
| Reflections collected | 4155 |
| Independent reflections | 3702 |
| Data/restraints/parameters | 3702/12/199 |
| Goodness-of-fit on F2 | 1.095 |
| Final R indexes [I>=2σ(I)] | R1 = 0.0725, wR2 = 0.1730 |
| Final R indexes [all data] | R1 = 0.0794, wR2 = 0.1769 |
| Largest diff. peak/hole / e Å-3 | 2.186/-1.179 |

Table S2 Atomic coordinates of P83.4As0.6 crystal unit cell

|  | x | y | z |
| --- | --- | --- | --- |
| P1 | 0.08459 | 0.0732 | 0.68148 |
| P2 | 0.99096 | 0.90461 | 0.61651 |
| P3 | 0.83486 | 0.8191 | 0.67997 |
| P4 | 0.74316 | 0.65214 | 0.61517 |
| P5 | 0.5844 | 0.5518 | 0.67364 |
| P6 | 0.50386 | 0.38688 | 0.60477 |
| P7 | 0.35195 | 0.3222 | 0.67396 |
| P8 | 0.24056 | 0.15201 | 0.61659 |
| P9 | -0.067 | 0.2599 | 0.6722 |
| P10 | -0.27997 | 0.19441 | 0.70065 |
| P11 | 0.64679 | 0.9718 | 0.67338 |
| As1/P12 | 0.391/0.3848 | 0.712/0.7011 | 0.6697/0.6704 |
| P13 | 0.20298 | 0.52139 | 0.67047 |
| P14 | 0.1412 | 0.51267 | 0.56776 |
| P15 | 0.3602 | 0.51717 | 0.53376 |
| P16 | 0.37724 | 0.7447 | 0.56629 |
| P17 | 0.60315 | 0.78161 | 0.54336 |
| P18 | 0.625 | 1.01048 | 0.57304 |
| P19 | -0.14991 | 0.03215 | 0.5441 |
| P20 | -0.12117 | 0.26375 | 0.57244 |
| P21 | 0.10178 | 0.28138 | 0.5438 |

Table S3 The cell parameters and cell volumes of pristine VP, violet arsenic phosphorus and reported violet antimony phosphorus

|  | Single-crystal XRD data | Powder XRD data | a (Å) | b (Å) | c (Å) | β (°) | V (Å3) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| VP | Yes | Yes | 9.210 | 9.128 | 21.893 | 97.7768 | 1823.5(8) |
| VP-As (This work, P83.4As0.6) | Yes | Yes | 9.2075 | 9.1507 | 21.7698 | 94.388 | 1828.84(14) |
| VP-Sb (P20.56Sb0.44) | None | Yes | 9.2345 | 9.1732 | 22.6176 | 106.077 | 1841.01(16) |
| VP-Sb (P76Sb3.27) | Yes | Yes | 9.2146 | 9.1619 | 21.901 | 97.81 | 1831.82 |

Table S4 Comparison of FET performance of VP-As to reported phosphorus semiconducting materials

| Transistor channel material | Type | Mobility (cm² V⁻¹ s⁻¹) | Refs. |
| --- | --- | --- | --- |
| VP | p | 4.07 | This work |
| VP-As (P83.4As0.6) | n | 137.06 | This work |
| BP | p | 35 | [S5] |
| BP/HATCN | p | 69 | [S5] |
| BP/HATNA | p | 97 | [S5] |
| exfoliated ultralarge BP with CH3COOTBA intercalation | p | 76 | [S6] |
| nonoxidative BP flakes with high crystallinity | p | 60 | [S7] |
| BP-NMP | ambipolar | 50 | [S8] |
| amorphous BP ultrathin film | p | 14 | [S9] |
| BP-C | p | 1995 | [S10] |
| BP | ambipolar | 38 (electrons), 172 (holes) | [S11] |
| BP | p | 100 | [S12] |

Table S5 Comparison of FET performance of VP-As to reported n-type 2D semiconducting materials

| Transistor channel material | Mobility (cm² V⁻¹ s⁻¹) | on/off ratio | subthreshold swing (mV/dec) | Refs. |
| --- | --- | --- | --- | --- |
| VP-As (P83.4As0.6) | 137.06 | 664 | 114 | This work |
| multilayer (ML) MoS2 islands | 70 | 108 | 150 | [S13] |
| MoS2 | 30 | Not mentioned | Not mentioned | [S14] |
| MoS2 under tensile strain | 185 | Not mentioned | Not mentioned | [S15] |
| metal-agglomeration-suppressed MoS2 films | 59.8 | 105 | 500 | [S16] |
| MoS2-PPh3 | 60 | Not mentioned | Not mentioned | [S17] |
| MoS2-ReO3 | 46.3 | Not mentioned | Not mentioned | [S18] |
| MoS2-O2 | 100 | 109 | 80 | [S19] |
| MoS2-NMP | 22.2 | 105 | Not mentioned | [S20] |
| MoS2-DMSO | 29.2 | Not mentioned | Not mentioned | [S20] |
| MoS2-DMF | 26.6 | Not mentioned | Not mentioned | [S20] |
| WS2 | 33 | Not mentioned | Not mentioned | [S14] |
| WS2 | 140 | 106 | Not mentioned | [S21] |
| WS2 encapsulated in hexagonal BN | 100 | 105 | Not mentioned | [S22] |
| monolayered triangular WS2 flakes | 50.5 | 107 | Not mentioned | [S23] |
| WS2-Cl | 60 | 4×106 | Not mentioned | [S24] |
| MoSe2 | 59.4 | Not mentioned | Not mentioned | [S25] |
| self-assembled monolayers modified MoSe2 | 166.5 | Not mentioned | Not mentioned | [S25] |
| bilayer MoSe2 | 65 | 105 | Not mentioned | [S26] |
| WSe2 with amorphous BN capping layer | 7.42 | 106 | Not mentioned | [S27] |
| WSe2-DETA | 25 | Not mentioned | Not mentioned | [S28] |
| WSe2-S | 68.2 | Not mentioned | Not mentioned | [S29] |
| MoTe2 | ≈ 43 | 106 | Not mentioned | [S30] |

# Supplementary References

- G. Kresse, D. Joubert, From ultrasoft pseudopotentials to the projector augmented-wave method. Phys. Rev. B 59(3), 1758–1775 (1999). https://doi.org/10.1103/physrevb.59.1758

- J. Perdew, K. Burke, M. Ernzerhof, Generalized gradient approximation made simple. Phys. Rev. Lett. 77(18), 3865–3868 (1996). https://doi.org/10.1103/PhysRevLett.77.3865

- S. Grimme, J. Antony, S. Ehrlich, H. Krieg, A consistent and accurate ab initio parametrization of density functional dispersion correction (DFT-D) for the 94 elements H-Pu. J. Chem. Phys. 132(15), 154104 (2010). https://doi.org/10.1063/1.3382344

- J. Qiao, X. Kong, Z.-X. Hu, F. Yang, W. Ji, High-mobility transport anisotropy and linear dichroism in few-layer black phosphorus. Nat. Commun. 5, 4475 (2014). https://doi.org/10.1038/ncomms5475

- H. Shi, S. Fu, Y. Liu, C. Neumann, M. Wang et al., Molecularly engineered black phosphorus heterostructures with improved ambient stability and enhanced charge carrier mobility. Adv. Mater. 33(48), 2105694 (2021). https://doi.org/10.1002/adma.202105694

- N. Wang, N. Mao, Z. Wang, X. Yang, X. Zhou et al., Electrochemical delamination of ultralarge few-layer black phosphorus with a hydrogen-free intercalation mechanism. Adv. Mater. 33(1), e2005815 (2021). https://doi.org/10.1002/adma.202005815

- J. Li, C. Chen, S. Liu, J. Lu, W.P. Goh et al., Ultrafast electrochemical expansion of black phosphorus toward high-yield synthesis of few-layer phosphorene. Chem. Mater. 30(8), 2742–2749 (2018). https://doi.org/10.1021/acs.chemmater.8b00521

- J. Kang, J.D. Wood, S.A. Wells, J.-H. Lee, X. Liu et al., Solvent exfoliation of electronic-grade, two-dimensional black phosphorus. ACS Nano 9(4), 3596–3604 (2015). https://doi.org/10.1021/acsnano.5b01143

- Z. Yang, J. Hao, S. Yuan, S. Lin, H.M. Yau et al., Field-effect transistors based on amorphous black phosphorus ultrathin films by pulsed laser deposition. Adv. Mater. 27(25), 3748–3754 (2015). https://doi.org/10.1002/adma.201500990

- W.C. Tan, Y. Cai, R.J. Ng, L. Huang, X. Feng et al., Few-layer black phosphorus carbide field-effect transistor via carbon doping. Adv. Mater. 29(24), 1700503 (2017). https://doi.org/10.1002/adma.201700503

- S. Das, M. Demarteau, A. Roelofs, Ambipolar phosphorene field effect transistor. ACS Nano 8(11), 11730–11738 (2014). https://doi.org/10.1021/nn505868h

- A. Kumar, K. Intonti, L. Viscardi, O. Durante, A. Pelella et al., Memory effect and coexistence of negative and positive photoconductivity in black phosphorus field effect transistor for neuromorphic vision sensors. Mater. Horiz. 11(10), 2397–2405 (2024). https://doi.org/10.1039/d4mh00027g

- H. Xu, H. Zhang, Z. Guo, Y. Shan, S. Wu et al., High-performance wafer-scale MoS2 transistors toward practical application. Small 14(48), e1803465 (2018). https://doi.org/10.1002/smll.201803465

- A. Sebastian, R. Pendurthi, T.H. Choudhury, J.M. Redwing, S. Das, Benchmarking monolayer MoS2 and WS(2) field-effect transistors. Nat. Commun. 12(1), 693 (2021). https://doi.org/10.1038/s41467-020-20732-w

- X. Liu, B. Erbas, A. Conde-Rubio, N. Rivano, Z. Wang et al., Deterministic grayscale nanotopography to engineer mobilities in strained MoS2 FETs. Nat. Commun. 15, 6934 (2024). https://doi.org/10.1038/s41467-024-51165-4

- K.H. Jung, S.J. Yun, Y. Choi, J.H. Cho, J.W. Lim et al., Metal-agglomeration-suppressed growth of MoS2 and MoSe2 films with small sulfur and selenium molecules for high mobility field effect transistor applications. Nanoscale 10(32), 15213–15221 (2018). https://doi.org/10.1039/C8NR03778G

- D. Lee, J.J. Lee, Y.S. Kim, Y.H. Kim, J.C. Kim et al., Remote modulation doping in van der Waals heterostructure transistors. Nat. Electron. 4(9), 664–670 (2021). https://doi.org/10.1038/s41928-021-00641-6

- X. Ma, J. Zhang, J. Lai, M. Zhang, J. Zheng et al., Gradient rhenium doping enabled tunable anisotropic valleytronic material based on monolayer molybdenum disulfide. 2D Mater. 8(3), 035031 (2021). https://doi.org/10.1088/2053-1583/abf762

- J. Tang, Z. Wei, Q. Wang, Y. Wang, B. Han et al., In situ oxygen doping of monolayer MoS2 for novel electronics. Small 16(42), 2004276 (2020). https://doi.org/10.1002/smll.202004276

- X.-K. Li, R.-X. Sun, H.-W. Guo, B.-W. Su, D.-K. Li et al., Controllable doping of transition-metal dichalcogenides by organic solvents. Adv. Electron. Mater. 6(3), 1901230 (2020). https://doi.org/10.1002/aelm.201901230

- D. Ovchinnikov, A. Allain, Y.-S. Huang, D. Dumcenco, A. Kis, Electrical transport properties of single-layer WS2. ACS Nano 8(8), 8174–8181 (2014). https://doi.org/10.1021/nn502362b

- Y. Wang, T. Sohier, K. Watanabe, T. Taniguchi, M.J. Verstraete et al., Electron mobility in monolayer WS2 encapsulated in hexagonal boron-nitride. Appl. Phys. Lett. 118(10), 102105 (2021). https://doi.org/10.1063/5.0039766

- Y. Yue, J. Chen, Y. Zhang, S. Ding, F. Zhao et al., Two-dimensional high-quality monolayered triangular WS2 flakes for field-effect transistors. ACS Appl. Mater. Interfaces 10(26), 22435–22444 (2018). https://doi.org/10.1021/acsami.8b05885

- L. Yang, K. Majumdar, H. Liu, Y. Du, H. Wu et al., Chloride molecular doping technique on 2D materials: WS2 and MoS2. Nano Lett. 14(11), 6275–6280 (2014). https://doi.org/10.1021/nl502603d

- K. Zhao, D. He, X. Liu, F. Ren, J. Wang et al., Enhance carrier diffusion of monolayer MoSe2 by interface engineering. ACS Appl. Mater. Interfaces 16(26), 34349–34357 (2024). https://doi.org/10.1021/acsami.4c05143

- Y. Li, K. Zhang, F. Wang, Y. Feng, Y. Li et al., Scalable synthesis of highly crystalline MoSe2 and its ambipolar behavior. ACS Appl. Mater. Interfaces 9(41), 36009–36016 (2017). https://doi.org/10.1021/acsami.7b10693

- Z. Lu, M. Zhu, G. Zhang, W. Liu, S. Han et al., Electrical characteristics of WSe2 transistor with amorphous BN capping layer. Results Phys. 38, 105568 (2022). https://doi.org/10.1016/j.rinp.2022.105568

- H.G. Ji, P. Solís-Fernández, D. Yoshimura, M. Maruyama, T. Endo et al., Chemically tuned p- and n-type WSe2 monolayers with high carrier mobility for advanced electronics. Adv. Mater. 31(42), 1903613 (2019). https://doi.org/10.1002/adma.201903613

- X. Duan, C. Wang, Z. Fan, G. Hao, L. Kou et al., Synthesis of WS2xSe2–2x alloy nanosheets with composition-tunable electronic properties. Nano Lett. 16(1), 264–269 (2016). https://doi.org/10.1021/acs.nanolett.5b03662

- S. Cho, S. Kim, J.H. Kim, J. Zhao, J. Seok et al., DEVICE TECHNOLOGY. Phase patterning for ohmic homojunction contact in MoTe₂. Science 349(6248), 625–628 (2015). https://doi.org/10.1126/science.aab3175