Supporting Information for

Atomically Dispersed Pt-Ru Dual-Atom Catalysts for Efficient Low-Temperature CO Oxidation Reaction

Yanan Qi1, 2, #, Hongqiu Chen3, #, Feng Hong1,2, #, Xiangbin Cai4, #, Zhehan Ying5, Jiangyong Diao1,2, Zhimin Jia1,2, Jiawei Chen1,2, Ning Wang6, Shengling Xiang6, Xiaowen Chen1,2, Guodong Wen1, 2, Bo Sun1, 2, *, Geng Sun3*, Hongyang Liu1, 2, *

1 School of Materials Science and Engineering, University of Science and Technology of China, Shenyang 110016, P. R. China

2 Shenyang National Laboratory for Materials Science, Institute of Metal Research, Chinese Academy of Sciences, Shenyang 110016, P. R. China

3 Chongqing Key Laboratory of Chemical Theory and Mechanism, School of Chemistry and Chemical Engineering, Chongqing University, Chongqing 401331, P. R. China

4 Division of Physics and Applied Physics, School of Physical and Mathematical Sciences, Nanyang Technological University, Singapore 637371, Singapore

5 Materials Characterization and Preparation Facility (GZ), The Hong Kong University of Science and Technology (Guangzhou), Guangzhou, P. R. China

6 Department of Physics and Center for Quantum Materials, Hong Kong University of Science and Technology, Kowloon, Hong Kong SAR 999077, P. R. China

# Yanan Qi, Hongqiu Chen, Feng Hong, and Xiangbin Cai contributed equally to this work.

* Corresponding authors. E-mail: bosun@imr.ac.cn (Bo Sun); sungengemail@cqu.edu.cn  (Geng Sun); liuhy@imr.ac.cn (Hongyang Liu)

Supplementary Figures and Tables

Fig. S1 XRD patterns of Ru1/ND@G, Pt1/ND@G, Pt1Ru1/ND@G, and Pt1Ru1/ND@G-used

Fig. S2 Additional HAADF-STEM images of Ru1/ND@G

Fig. S3 Additional HAADF-STEM images of Pt1/ND@G

Fig. S4 The distribution of the Pt1-Ru1 distances by counting 50 Pt-Ru atom pairs

Fig. S5 Pt 4f XPS spectra of Pt1/ND@G and Pt1Ru1/ND@G

Fig. S6 Ru 3p XPS spectra of Ru1/ND@G and Pt1Ru1/ND@G

Fig. S7 CO conversion of various PtRu/ND@G catalysts with different Ru loading. Reaction conditions: 1% CO, 1% O2 balanced in He, GHSV = 48,000 mL·gcat-1·h-1

Fig. S8 T50, T100 of various PtRu/ND@G catalysts with different Ru loading

Fig. S9 CO catalytic oxidation performance of different PtM/ND@G catalysts

Fig. S10 (a) Catalytic performance and (b) TOF (30°C) of Pt/ND@G, Ru/ND@G, and PtRu/ND@G with the same metal loading (GHSV = 48,000 mL·gcat-1·h-1)

Fig. S11 Catalytic performance of PtRu /ND@G, PtRu /Graphene, and PtRu/ SiO2 (GHSV = 48,000 mL·gcat-1·h-1)

Fig. S12 The experimental Ru (a, b) and Pt (c, d) EXAFS spectra and the fitting curves of Pt1Ru1/ND@G

Fig. S13 The EXAFS fitting curves of Pt1/ND@G at R-space

Fig. S14 The EXAFS fitting curves of Ru1/ND@G at R-space

Fig. S15 Free energy profiles for CO oxidation on the Pt1/ND@G catalyst (x-axis is the reaction coordinate, y-axis is the free energy determined at 50 ℃ and the partial pressure for CO2, O2 and CO is 1000, 2000, 1000 Pa, respectively. Color codes: grey, orange and red balls represent carbon, platinum and oxygen, respectively)

Fig. S16 Free energy profiles for CO oxidation on the Ru1/ND@G catalyst (x-axis is the reaction coordinate, y-axis is the free energy determined at 50 ℃ and the partial pressure for CO2, O2 and CO is 1000, 2000, 1000 Pa, respectively. Color codes: grey, red, and green balls represent carbon, oxygen and ruthenium, respectively)

Fig. S17 (a), (b), and (c) are the top and side views of the optimized structures of O2 adsorbed on the bridge site, Ru site, and Pt site, respectively, along with the adsorption energy of O2. Color codes: grey, red, orange and green balls are carbon, oxygen, platinum and ruthenium, respectively)

Fig. S18 (a) and (b) HAADF-STEM images of Pt1Ru1/ND@G after the stability experiment

Table S1 Comparison of the structure information and catalytic performance over the Pt1Ru1/ND@G and SACs

| Catalyst | Pt loading (wt%) | Ru loading (wt%) | Temp. (°C) | TOF *102 (s-1) |
| --- | --- | --- | --- | --- |
| Ru1/ND@G | 0 | 0.04 | 30 | ~0 |
| Pt1/ND@G | 0.09 | 0 | 30 | 1.5 |
| Pt1Ru1/ND@G | 0.09 | 0.04 | 30 | 17.6 |
| Pt1Ru1/ND@G-used | 0.10 | 0.05 | 30 | \ |

Table S2 The peak positions and shifts of platinum and ruthenium in the XPS spectra of the catalyst

| catalyst | Pt1/ND@G | Ru1/ND@G | Pt1 Ru1/ND@G |
| --- | --- | --- | --- |
| Peak Position of Pt 4f₇/₂ | 71.7 | \ | 71.4 |
| Peak Position of Ru 3p3/2 | \ | 463.8 | 463.2 |
| BE Shift of Pt (eV) | Ref. | \ | - 0.3 |
| BE Shift of Ru (eV) | \ | Ref. | - 0.6 |

Table S3 The kinetic measurement parameters for catalysts in this work

| catalyst | reaction order in CO | reaction orders in O2 | activation energies (kJ/mol) | pre-exponential factors (h-1) | R2 values |
| --- | --- | --- | --- | --- | --- |
| Pt1/ND@G | + 0.71 | + 0.22 | 17.9 ± 0.6 | 221.4 | 0.99 |
| Ru1/ND@G | \ | \ | 23.4 ± 1.2 | 403.4 | 0.99 |
| Pt1Ru1/ND@G | + 0.53 | + 0.12 | 13.2 ± 0.4 | 492.7 | 0.99 |

Table S4 Fit results for the EXAFS spectra of different catalysts

| Sample | Path | R (Å)a | C.N.b | σ2 (Å2)c | ΔE0(eV)d | R-factore |
| --- | --- | --- | --- | --- | --- | --- |
| Ru foil | Ru-Ru | 2.68(1) | 12 | 0.004 | -3.8(17) | 0.008 |
| RuO2 | Ru-C/O | 1.97(1) | 6 | 0.002 | -3.2(22) | 0.018 |
| Ru1/NDG | Ru-C/O | 2.02(2) | 4.5 | 0.008 | -0.3(23) | 0.012 |
| Pt1Ru1/NDG | Ru-C/O | 2.02(4) | 3.9 | 0.009 | 1.3(36) | 0.018 |
|  | Ru-Pt | 2.58(4) | 0.9 | 0.003 |  |  |
| Pt foil | Pt-Pt | 2.76(1) | 12 | 0.005 | 5.2(4) | 0.003 |
| PtO2 | Pt-C/O | 2.01(1) | 6 | 0.003 | 9.3(12) | 0.014 |
| Pt1/NDG | Pt-C/O | 2.01(4) | 2.4 | 0.009 | 9.8(19) | 0.019 |
|  | Pt-Cl | 2.32(3) | 1.5 | 0.009 |  |  |
| Pt1Ru1/NDG | Pt-C/O | 2.02(2) | 1.8 | 0.004 | 9.4(26) | 0.011 |
|  | Pt-Cl | 2.28(3) | 1.2 | 0.004 |  |  |
|  | Pt-Ru | 2.52(3) | 1.1 | 0.007 |  |  |

a: R is the interatomic distance (the bond length between Pt/Ru central atoms and surrounding coordination atoms). b: CN is the coordination number. c: σ2 is the Debye-Waller factor (a measure of thermal and static disorder in absorber scatterer distances). d: ΔE0 is the edge energy shift (the difference between the zero kinetic energy value of the sample and that of the theoretical model). e: R factor is used to value the goodness of the fitting.

Table S5 Catalytic performance over various catalysts reported in literature

| Catalyst | Pt loading (wt%) | Reaction condition | Temp. (°C) | TOF×102 (s-1) | Refs. |
| --- | --- | --- | --- | --- | --- |
| Pt1Ru1/ND@G | 0.1 | 1% CO，1% O2 | 30 | 17.6 | This work |
| 0.75Pt0.2Fe/ND@G | 0.75 | 1% CO，1% O2 | 30 | 15.1 | [S1] |
| 0.5Ptn/ND@G | 0.5 | 1% CO，1% O2 | 30 | 3.5 | [S2] |
| Pt1/FeOx | 0.17 | 1% CO，1% O2 | 27 | 13.6 | [S3] |
| Pt-SA/A-Fe2O3 | 1.2 | 1% CO，1% O2 | 70 | 6.87 | [S4] |
| Pt/Sn0.2Ti0.8O2 | 0.5 | 1% CO，1% O2 | 80 | 17.2 | [S5] |
| 0.3Pt/TiO2 | 0.3 | 1% CO，1% O2 | 40 | 2.15 | [S6] |
| HO-Pt/TiO2 | 1 | 1% CO，1% O2 | 70 | 11 | [S7] |
| Pt-CC/Al2O3 | 5 | 1% CO, 1% O2 | 120 | 2.8 | [S8] |
| Pt-CD/Al2O3 | 2.2 | 1% CO, 1% O2 | 30 | 14.8 | [S8] |
| Pt NP/TiO2 | 1.0 | 0.5% CO, 5% O2 | 115 | 1.01 | [S9] |
| Pt/CNT-600 | 1 | 1.0 % CO, 20.0 % O2 | 100 | 5.55 | [S10] |
| Co3O4/Pt/Al2O3 | 3.85 | 1% CO, 10% O2 | 60 | 2.7 | [S11] |
| 1%wt Pt/TiO2(B) | 1 | 0.9% CO, 24% O2 | 100 | 10.9 | [S12] |
| CeO2-IMP-Pt | 1.2 | 1% CO, 16%O2 | 80 | 1.2 | [S13] |

Table S6 The structures of optimized Pt1Ru1/ND@G, Pt1/ND@G, and Ru1/ND@G

| catalyst | Optimized structures | Bonds | CNa | R(Å) | Bader charge analaysis |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Pt | Ru |
| Pt1/ND@G |  | Pt/C | 3 | 1.93 | +0.22e | \ |  |
| Ru1/ND@G |  | Ru/C | 4 | 2.02 | \ | +0.62e |  |
| Pt1Ru1/ND@G |  | Ru/C | 3 | 1.98 | +0.05e | +0.54e |  |
|  |  | Pt/C | 2 | 1.92 |  |  |  |
|  |  | Ru-Pt | 1 | 2.52 |  |  |  |

aCN is the coordination number.

Table S7 The adsorption energies of CO and O2 on Pt1Ru1/ND@G, Pt1/ND@G, and Ru1/ND@G

| catalyst | Reaction | Eads(eV) |
| --- | --- | --- |
| Pt1Ru1/ND@G | CO(g)->CO* | -1.74 |
|  | CO*+O2(g)->CO*+O2* | -1.91 |
| Pt1/ND@G | CO(g)->CO* | -1.46 |
|  | CO*+O2(g)->CO*+O2* | -0.96 |
| Ru1/ND@G | CO(g)->CO* | -1.52 |
|  | CO*+O2(g)->CO*+O2* | -0.98 |

Supplementary References

- Z. Jia, X. Qin, Y. Chen, X. Cai, Z. Gao et al., Fully-exposed Pt-Fe cluster for efficient preferential oxidation of CO towards hydrogen purification, Nat. Commun. 13, 6798 (2022). https://doi.org/10.1038/s41467-022-34674-y

- Z. Jia, M. Peng, X. Cai, Y. Chen, X. Chen et al., Fully exposed platinum clusters on a nanodiamond/graphene hybrid for efficient low-temperature CO oxidation, ACS Catal. 12, 9602–9610 (2022). https://doi.org/10.1021/acscatal.2c02769

- B. Qiao, A. Wang, X. Yang, L.F. Allard, Z. Jiang et al., Single-atom catalysis of CO oxidation using Pt1/FeOx, Nat. Chem. 3, 634–641 (2011). https://doi.org/10.1038/nchem.1095

- W. Chen, Y. Ma, F. Li, L. Pan, W. Gao et al., Strong electronic interaction of amorphous Fe2O3 nanosheets with single‐atom Pt toward enhanced carbon monoxide oxidation, Adv. Funct. Mater. 29, 1904278 (2019). https://doi.org/10.1002/adfm.201904278

- J. Chen, S. Xiong, H. Liu, J. Shi, J. Mi et al., Reverse oxygen spillover triggered by CO adsorption on Sn-doped Pt/TiO2 for low-temperature CO oxidation, Nat. Commun. 14, 3477 (2023). https://doi.org/10.1038/s41467-023-39226-6

- Z. Zhou, W. Guan, X. Pan, A. Wang, T. Zhang, Synthesis of pyrazines from biomass-derived vicinal diols using ammonia over heterogeneous Pt/CeO2/Al2O3 catalysts, ACS Catal. 15, 5664–5673 (2025). https://doi.org/10.1021/acscatal.5c00372

- L. Zhang, X. Cheng, G. Zhang, W. Qiu, H. He et al., High active platinum clusters on titanium dioxide supports toward carbon monoxide oxidation, Appl. Catal. B Environ. 266, 118629 (2020). https://doi.org/10.1016/j.apcatb.2020.118629

- Y. Chen, Y. Feng, L. Li, J. Liu, X. Pan et al., Identification of active sites on high-performance Pt/Al2O3 catalyst for cryogenic CO oxidation, ACS Catal. 10, 8815–8824 (2020). https://doi.org/10.1021/acscatal.0c02253

- H. Hojo, M. Gondo, S. Yoshizaki, H. Einaga, Atomic and electronic structure of Pt/TiO2 catalysts and their relationship to catalytic activity, Nano Lett. 22, 145–150 (2022). https://doi.org/10.1021/acs.nanolett.1c03485

- W. Chen, J. Cao, J. Yang, Y. Cao, H. Zhang et al., Molecular-level insights into the electronic effects in platinum-catalyzed carbon monoxide oxidation, Nat. Commun. 12, 6888 (2021). https://doi.org/10.1038/s41467-021-27238-z

- X. Liu, Q. Zhu, Y. Lang, K. Cao, S. Chu et al., Oxide‐nanotrap‐anchored platinum nanoparticles with high activity and sintering resistance by area‐selective atomic layer deposition, Angew. Chem. Int. Ed. 56, 1648–1652 (2017). https://doi.org/10.1002/anie.201611559

- J. Liu, T. Ding, H. Zhang, G. Li, J. Ca et al., Engineering surface defects and metal–support interactions on Pt/TiO2(B) nanobelts to boost the catalytic oxidation of CO, Catal. Sci. Technol. 8, 4934–4944 (2018). https://doi.org/10.1039/C8CY01410H

- J. Chen, Y. Wanyan, J. Zeng, H. Fang, Z. Li et al., Surface engineering protocol to obtain an atomically dispersed Pt/CeO2 catalyst with high activity and stability for CO oxidation, ACS Sustain. Chem. Eng. 6, 14054–14062 (2018). https://doi.org/10.1021/acssuschemeng.8b02613