Supporting Information for

Temperature-Dependent Infrared Engineering for Extreme Environments: All-Dielectric Thermal Photonic Metamaterials Stable at 1873 K in Air

Yang Liu1, He Lin1,2,3, Yunxia Zhou1, Liming Yuan1, Yanqin Wang1,2, Xiaoliang Ma1,2, Cheng Huang1,2, Xiangang Luo1,2

1State Key Laboratory of Optical Field Manipulation Science and Technology, Institute of Optics and Electronics, Chinese Academy of Sciences, Chengdu 610209, P. R. China

2College of Materials Sciences and Opto-Electronic Technology, University of Chinese Academy of Sciences, Beijing 100049, P. R. China

3School of Automation Engineering, University of Electronic Science and Technology of China, Chengdu 611731, P. R. China

Yang Liu, He Lin, and Yunxia Zhou contributed equally to this work.

*Corresponding authors. E-mail: maxl@ioe.ac.cn (Xiaoliang Ma); huangc@ioe.ac.cn (Cheng Huang); lxg@ioe.ac.cn (Xiangang Luo)

Supplementary Figures and Tables

Fig. S1 Detailed data for solution S00. a) Predicted values, true values, and RCWA value from the neural network at 1500 K; b) Evolution of FOM and elapsed time; c) Infrared spectrum across 300–1500 K; d) TPM layer architecture and spectral performance

Fig. S2 Detailed data for solution S10. a) Predicted values, true values, and RCWA value from the neural network at 1500 K; b) Evolution of FOM and elapsed time; c) Infrared spectrum across 300–1500 K; d) TPM layer architecture and spectral performance

Fig. S3 Detailed data for solution S20. a) Predicted values, true values, and RCWA value from the neural network at 1500 K; b) Evolution of FOM and elapsed time; c) Infrared spectrum across 300–1500 K; d) TPM layer architecture and spectral performance

Fig. S4 Detailed data for solution S30. a) Predicted values, true values, and RCWA value from the neural network at 1500 K; b) Evolution of FOM and elapsed time; c) Infrared spectrum across 300–1500 K; d) TPM layer architecture and spectral performance

Fig. S5 Detailed data for solution S40. a) Predicted values, true values, and RCWA value from the neural network at 1500 K; b) Evolution of FOM and elapsed time; c) Infrared spectrum across 300–1500 K; d) TPM layer architecture and spectral performance

Fig. S6 Detailed data for solution S50. a) Predicted values, true values, and RCWA value from the neural network at 1500 K; b) Evolution of FOM and elapsed time; c) Infrared spectrum across 300–1500 K; d) TPM layer architecture and spectral performance

Fig. S7 Detailed data for solution S01. a) Predicted values, true values, and RCWA value from the neural network at 1500 K; b) Evolution of FOM and elapsed time; c) Infrared spectrum across 300–1500 K; d) TPM layer architecture and spectral performance

Fig. S8 Detailed data for solution S11. a) Predicted values, true values, and RCWA value from the neural network at 1500 K; b) Evolution of FOM and elapsed time; c) Infrared spectrum across 300–1500 K; d) TPM layer architecture and spectral performance

Fig. S9 Detailed data for solution S21. a) Predicted values, true values, and RCWA value from the neural network at 1500 K; b) Evolution of FOM and elapsed time; c) Infrared spectrum across 300–1500 K; d) TPM layer architecture and spectral performance

Fig. S10 Detailed data for solution S31. a) Predicted values, true values, and RCWA value from the neural network at 1500 K; b) Evolution of FOM and elapsed time; c) Infrared spectrum across 300–1500 K; d) TPM layer architecture and spectral performance

Fig. S11 Detailed data for solution S41. a) Predicted values, true values, and RCWA value from the neural network at 1500 K; b) Evolution of FOM and elapsed time; c) Infrared spectrum across 300–1500 K; d) TPM layer architecture and spectral performance

Fig. S12 Detailed data for solution S02. a) Predicted values, true values, and RCWA value from the neural network at 1500 K; b) Evolution of FOM and elapsed time; c) Infrared spectrum across 300–1500 K; d) TPM layer architecture and spectral performance

Fig. S13 Detailed data for solution S12. a) Predicted values, true values, and RCWA value from the neural network at 1500 K; b) Evolution of FOM and elapsed time; c) Infrared spectrum across 300–1500 K; d) TPM layer architecture and spectral performance

Fig. S14 Detailed data for solution S22. a) Predicted values, true values, and RCWA value from the neural network at 1500 K; b) Evolution of FOM and elapsed time; c) Infrared spectrum across 300–1500 K; d) TPM layer architecture and spectral performance

Fig. S15 Detailed data for solution S32. a) Predicted values, true values, and RCWA value from the neural network at 1500 K; b) Evolution of FOM and elapsed time; c) Infrared spectrum across 300–1500 K; d) TPM layer architecture and spectral performance

Fig. S16 Runtime of the GA‑RCWA, GA‑NN, and multi‑objective algorithms

Fig. S17 Schematic of the atmospheric transmission model

Fig. S18 Atmospheric transmittance and background radiance

Fig. S19 Spectral radiance of sample S32 vs. metal oxide substrates under the mid-latitude summer model

Fig. S20 Spectral radiance of sample S32 vs. metal oxide substrates under the tropical model

Fig. S21 Spectral radiance of sample S32 vs. metal oxide substrates under the sub-arctic winter model

Fig. S22 X-ray diffraction patterns of BeO and TiO2 before and after annealing

Fig. S23 Mechanical properties of 2-μm YSZ. a-c) Nano-indentation testing before annealing; d-f) Nano-scratch testing before annealing; g-i) Nano-indentation after annealing; j-l) Nano-scratch testing after annealing

Fig. S24 Comparative transmittance spectra of air, blank sapphire, and TPMs on sapphire in a) visible and b) microwave bands

Fig. S25 Comparative transmittance spectra of blank sapphire and TPMs on sapphire in microwave bands across 300 to 1000 K

Fig. S26 Temperature-time curve of the thermal shock test

Fig. S27 Radiative cooling performance of the TPMs. a) Measured radiative cooling power (Prad) within the 5-8 μm spectral band at 1014 K. b) Theoretical radiative cooling power (BIR, band-integrated radiance) within the 5-8 μm band across the 300-1500 K temperature range

Fig. S28 Mechanical properties of TPM on superalloy substrate. a-c) Nano-indentation and d-f) Nano-scratch testing after thermal shock testing

Table S1 Material‑property trade‑offs for high‑temperature dielectric layers

| Materials | n (mid‑IR) | Melting point /K | CTE /×10-6· K-1 | Stability | Reflectivity (8-14 μm, 300 K) |
| --- | --- | --- | --- | --- | --- |
| BeO | ~1.7-1.9 | ~2,800 | ~9 | Excellent | ~0.7 |
| TiO2 | ~2.4-2.6 | ~2,130 | ~9 | Excellent | ~0.1 |
| Al2O3 | ~1.7-1.8 | ~2,323 | ~8 | Excellent | ~0.3 |
| MgF2 | ~1.3-1.4 | ~1,536 | ~13-15 | Good | ~0 |
| SrTiO3 | ~2.3-2.5 | ~2,350 | ~10-12 | Good | ~0.2 |

Table S2 RMSE between the GA-NN and RCWA methods

| Solution | 300 K | 600 K | 900 K | 1200 K | 1500 K |
| --- | --- | --- | --- | --- | --- |
| S00 | 0.113 | 0.066 | 0.083 | 0.082 | 0.066 |
| S10 | 0.147 | 0.178 | 0.18 | 0.186 | 0.153 |
| S20 | 0.115 | 0.087 | 0.088 | 0.092 | 0.075 |
| S30 | 0.176 | 0.13 | 0.135 | 0.131 | 0.193 |
| S40 | 0.132 | 0.095 | 0.094 | 0.077 | 0.189 |
| S50 | 0.061 | 0.042 | 0.081 | 0.078 | 0.073 |
| S01 | 0.181 | 0.167 | 0.177 | 0.177 | 0.152 |
| S11 | 0.104 | 0.079 | 0.092 | 0.088 | 0.085 |
| S21 | 0.164 | 0.147 | 0.142 | 0.147 | 0.121 |
| S31 | 0.129 | 0.116 | 0.11 | 0.113 | 0.164 |
| S41 | 0.078 | 0.032 | 0.037 | 0.064 | 0.059 |
| S02 | 0.089 | 0.062 | 0.059 | 0.052 | 0.05 |
| S12 | 0.12 | 0.08 | 0.082 | 0.084 | 0.075 |
| S22 | 0.133 | 0.041 | 0.029 | 0.033 | 0.023 |
| S32 | 0.036 | 0.044 | 0.046 | 0.041 | 0.076 |

Table S3 RMSE between the temperature-dependent infrared engineering model and the baseline model

| Solution | 300 K | 600 K | 900 K | 1200 K | 1500 K |
| --- | --- | --- | --- | --- | --- |
| S00 | 0 | 0.088 | 0.104 | 0.134 | 0.217 |
| S10 | 0 | 0.093 | 0.11 | 0.137 | 0.201 |
| S20 | 0 | 0.081 | 0.105 | 0.135 | 0.212 |
| S30 | 0 | 0.06 | 0.097 | 0.131 | 0.204 |
| S40 | 0 | 0.064 | 0.099 | 0.134 | 0.21 |
| S50 | 0 | 0.066 | 0.097 | 0.13 | 0.187 |
| S01 | 0 | 0.093 | 0.103 | 0.131 | 0.231 |
| S11 | 0 | 0.083 | 0.1 | 0.128 | 0.219 |
| S21 | 0 | 0.087 | 0.11 | 0.139 | 0.214 |
| S31 | 0 | 0.073 | 0.101 | 0.131 | 0.206 |
| S41 | 0 | 0.065 | 0.092 | 0.126 | 0.185 |
| S02 | 0 | 0.098 | 0.116 | 0.145 | 0.239 |
| S12 | 0 | 0.083 | 0.096 | 0.123 | 0.215 |
| S22 | 0 | 0.077 | 0.1 | 0.13 | 0.211 |
| S32 | 0 | 0.074 | 0.097 | 0.129 | 0.187 |

Table S4 The solution set of calculation results

| Solution | FOM1 | FOM2 | FOM3 | FOM |
| --- | --- | --- | --- | --- |
| S00 | 0.726149 | 0.724382 | 0.39985 | 0.726149 |
| S10 | 0.700473 | 0.803136 | 0.472367 | 0.677662 |
| S20 | 0.728331 | 0.792397 | 0.472367 | 0.677138 |
| S30 | 0.65116 | 0.816634 | 0.472367 | 0.597522 |
| S40 | 0.670991 | 0.823468 | 0.513417 | 0.607961 |
| S50 | 0.693503 | 0.881931 | 0.659241 | 0.676372 |
| S01 | 0.670991 | 0.722991 | 0.558035 | 0.676191 |
| S11 | 0.722527 | 0.753752 | 0.472367 | 0.700634 |
| S21 | 0.66631 | 0.792905 | 0.558035 | 0.657315 |
| S31 | 0.647265 | 0.810376 | 0.558035 | 0.636807 |
| S41 | 0.692117 | 0.880237 | 0.659241 | 0.697779 |
| S02 | 0.736387 | 0.722527 | 0.606531 | 0.733615 |
| S12 | 0.703984 | 0.767895 | 0.659241 | 0.712292 |
| S22 | 0.709638 | 0.830359 | 0.716531 | 0.735161 |
| S32 | 0.713195 | 0.875735 | 0.659241 | 0.729517 |

Table S5 Band-integrated radiance of S32 and oxide substrates in 3-5 µm

| T /K BIR /W·m-2 Cases | 300 K | 600 K | 900 K | 1200 K | 1500 K |
| --- | --- | --- | --- | --- | --- |
|  | TPMs/Subs | TPMs/Subs | TPMs/Subs | TPMs/Subs | TPMs/Subs |
| MS-1km | 0.0037/0.013 | 1.35/5.53 | 8.92/44.43 | 24.81/129.82 | 54.43/253.32 |
| MS-8km | 0.29/0.68 | 79.45/259.26 | 504.51/2074.53 | 1375.58/6083.57 | 2923.89/11913.37 |
| MS-15km | 0.57/1.2 | 14.21/41.34 | 888.25/3282.59 | 2402.24/9624.43 | 5034.31/18864.51 |
| Tp-1km | 0.0023/0.010 | 1.02/4.65 | 6.98/37.51 | 19.42/109.65 | 43.31/213.94 |
| Tp-1km | 0.21/0.57 | 63.73/229.40 | 411.51/1844.07 | 1132.49/5407.40 | 2440.97/10582.25 |
| Tp-1km | 0.45/1.01 | 119.66/374.53 | 754.74/2980.03 | 2050.75/8726.08 | 4336.86/17080.21 |
| SW-1km | 0.034/0.049 | 6.71/13.71 | 39.84/104.59 | 104.43/303.84 | 208.78/594.17 |
| SW-8km | 0.83/1.29 | 174.33/411.56 | 1078.50/3290.34 | 2908.18/9765.39 | 5979.95/19322.46 |
| SW-15km | 1.20/1.87 | 253.00/589.33 | 1572.07/4721.80 | 4254.71/14050.00 | 8763.18/27854.49 |

Table S6 Radiation suppression efficiency and radiation attenuation values of S32 and oxide substrates

| Cases | 300 K |  | 600 K |  | 900 K |  | 1200 K |  | 1500 K |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | η /% | IdB /dB | η /% | IdB /dB | η /% | IdB /dB | η /% | IdB /dB | η /% | IdB /dB |
| MS-1km | 72% | -5.5 | 76% | -6.2 | 80% | -7.0 | 81% | -7.2 | 79% | -6.8 |
| MS-8km | 58% | -3.8 | 69% | -5.1 | 76% | -6.2 | 77% | -6.4 | 75% | -6.0 |
| MS-15km | 51% | -3.1 | 64% | -4.7 | 73% | -5.7 | 75% | -6.0 | 73% | -5.7 |
| Tp-1km | 78% | -6.6 | 78% | -6.6 | 81% | -7.2 | 82% | -7.4 | 80% | -7.0 |
| Tp-8km | 64% | -4.4 | 72% | -5.5 | 78% | -6.6 | 79% | -6.8 | 77% | -6.4 |
| Tp-15km | 56% | -3.6 | 68% | -4.9 | 75% | -6.0 | 77% | -6.4 | 77% | -6.0 |
| SW-1km | 30% | -1.5 | 51% | -3.1 | 62% | -4.2 | 66% | -4.7 | 65% | -4.6 |
| SW-8km | 36% | -1.9 | 58% | -3.8 | 67% | -4.8 | 70% | -5.2 | 69% | -5.1 |
| SW-15km | 36% | -1.9 | 57% | -3.7 | 67% | -4.8 | 70% | -5.2 | 69% | -5.1 |