Supporting Information for

Integrated Performance Metrics of Porous Carbon Toward Practical Supercapacitor Devices

Yuting Song1, Sicheng Fan1, Zerui Yan1, Dafu Tang1, Xiang Gao1, Jiawei Guo1, Yunlong Zhao2, Qiulong Wei1,*

1State Key Laboratory of Physical Chemistry of Solid Surface, Fujian Key Laboratory of Surface and Interface Engineering for High Performance Materials, College of Materials, Xiamen University, Xiamen 361005, P. R. China

2Dyson School of Design Engineering, Imperial College London, London SW72BX, UK

*Corresponding author. E-mail: qlwei@xmu.edu.cn (Qiulong Wei)

S1 Calculation of the volume of electrolyte for supercapacitor pouch cells

S1.1 Volume of electrolyte based on the porosity of activated carbon (AC) electrodes

The mass loading of the electrode was 13 mg cm−2 and a thickness of 200 μm (double sides, as measured by the cross-sectional SEM image in Fig. S3, except for the thickness of the Al foil). Thus, the ρelectrode is 0.65 g cm-3 (13 mg cm−2/200 μm).

The electrode area was 24 cm2 for each piece. The total volume of the electrodes: Velectrode=24×200×10-4× (10+11) = 10.08 mL.

The true density (ρAC) of the electrode powder was 1.94 g cm−3.

Porosity of the electrode: Pelectrode = (1-ρelectrodeρAC)×100% = 1-0.651.94×100% = 66.5%.

Hence, the pore volume of the electrode:

VAC+VP = Velectrode×Pelectrode = 10.08×66.5% = 6.7 mL.

The accumulative pore volume of the activated carbon is 0.65 mL g−1. The pore volume of AC material: VAC = 0.65 mL g−1×(6.5 mg cm−2×24 cm2×2×21×95%)/1000 = 4.04 mL.

The stacking pore volume of the electrode is VP = (VAC+VP) −VAC=6.7−4.04 = 2.66 mL.

The porosity of the stacking pore volume corresponds to VP/Velectrode = (2.66/10.08)×100 = 26.4%.

The separator also exhibits electrolyte absorption, which must be accounted for in total volume calculations. The total length of the separator is 103.2 cm. The volume of the separator is VSeparator = 103.2×6×30×10-4 = 1.86 mL, and the pore volume of the separator is

VS = Vseparator×73% = 1.8576×73% = 1.36 mL.

Vpore  = VAC+VP+VS = 6.7+1.36 = 8.06 mL.

S1.2 Volume of electrolyte is based on the Q of the device

The voltage window of the supercapacitor is 0-2.7 V.

The rated capacitance of the supercapacitor is 137 F.

The Q of the device is Qtheo=137 F×2.7 V = 370 C, and related volume of electrolyte (1 M Net4BF4 in ACN) is [(370C)/(96485 C mol−1)]/(1 mol mL−1)≈3.8 mL.

VQ = 3.8 mL.

S2 Prediction of Edevice based on 43 AC samples

The mass loading of the AC electrode is 13 mg cm-2 (double sides, AC: conductive carbon: binder=95:3:2). Furthermore, the area of electrodes in soft-packaged pouch supercapacitors is 24 cm2. Furthermore, the electrolyte is 1 M Net4BF4 in ACN and separator is NKK TF4030 cellulose separators. The porosity of stacking pore in electrode is considered about 26%. The true density of different AC is assumed as 2 g cm−3.

The volume of AC (Vcarbon), Vcarbon = mAC/ρture.

The pore volume of AC (VAC), VAC = mAC*PAC

The volume of electrode, Velectrode = (VAC+Vcarbon)/ (1−26%).

The stacking pore volume (VP), VP = Velectrode*26%.

S3 Calculation of descriptor (η)

Edevice=18CSV2*mAC3.6Mtotal

Mtotal=mAC+melectrolyte+minactive

mincative =mS+mAl+(mconductive crabon+mbinder)+mP

The mass ratio between AC and other components can help simplify this equation. Because the current collector and separator exhibit approximately equal areas to the electrode, the mass ratio can simplify to the ratio of their respective area densities. The density of Al is well-established as ~2.7 g cm−3 with the Al foil thickness of 12 μm, the area density is calculated to be 3.24 mg cm−2. According to Table S1, the area density of separator is 1.263 mg cm−2. Assuming an AC mass loading of ma mg cm−2, the mass ratio between components becomes mAC: mAl: mS= ma: 3.24: 1.263. So, mAl=3.24ma*mAC, mS=1.263ma*mAC. Furthermore, the masses of conductive carbon and binder are determined by their respective ratios in the electrode slurry composition. We defined the electrode containing 95 wt.% AC powder, 3 wt.% conductive carbon, and 2 wt.% binder. Hence (mconductive crabon+mbinder) = 3%+2%95%*mAC = 0.053mAC.

melectrolyte=ρeVelectrolyte=ρe*VAC+VP+VS=ρe*mAC*PAC+26%*mACρtrue+VAC1-26%+PS*mSρS=ρemAC*(1.35PAC+0.35ρtrue+0.125PSma)

Mtotal=mAC+ρemAC*1.35PAC+0.35ρtrue+3PSma+1.263ma*mAC+3.24ma*mAC+0.053mAC+mP=mAC1.053+ρe*1.35PAC+0.35ρtrue+3PSma+4.503ma+mP

Because the density of commercial electrolyte (1 M Net4BF4 in ACN) is 0.8639 g mL−1, PS=73% (Table S1), and ρtrue≈2 g cm−3, so the equation can continue simplify to:

Mtotal=mAC1.166PAC+6.4ma+1.2+mP

The Edevice:

Edevice=18CSV23.6*(1.166PAC+6.4ma+1.2+ζ)

η=CS(1.166PAC+6.4ma+1.2)

where ζ is the correction coefficient from the mass of package (ζ=mPmAC).

S4 Supplementary Figures and Tables

Fig. S1 The design and assemble of supercapacitor pouch cell. This pouch cell is composed of 10 pieces of positive electrode and 11 pieces of negative electrode

Fig. S2 N2 adsorption‒desorption isotherms of the AC materials

Fig. S3 Cross‒sectional SEM images of the AC electrode (double-side coating)

Fig. S4 The true density of the AC materials

Fig. S5 Charging and discharging curves at different current densities of supercapacitor pouch cell with volumes of electrolyte: a VAC, b VAC+VS, c VAC+VP, d Vpore and e 1.15 Vpore

Fig. S6 Rate performance of supercapacitor pouch cells with different volumes of electrolyte

Fig. S7 Charging and discharging curves of the supercapacitor measured by coin cell

Fig. S8 Ragon plots of as-assembled supercapacitor pouch cells with different volumes and commercial 100 F cylindrical supercapacitors

Fig. S9 Charging and discharging curves of supercapacitor pouch cells with different electrolyte concentrations: a 0.25 M, b 0.5 M and c 1.5 M. The added electrolyte volume is consistent in 7.9±0.1 mL

Fig. S10 The ionic conductivities of electrolytes with different concentrations

The ionic conductivities of electrolytes with different concentrations were tested based the formula of σ=L/RS [S1] at room tempreture, where σ is ionic conductivity, R is the impedance, L is the distance between two parallel electrode and S is the area of the electrode. The L and S are constants for the same equipment. Additionally, the 0.01 M KCl (σKCL=1.41 mS cm−1) was as nominal solution, and the ionic conductivities of electrolytes is calculated by following equation, σelectrolyte=RKClRelectrolyte×σKCl. Thus, the ionic conductivities are calculated by the measured impendences of specific electrolyte.

Fig. S11 a Rate performance. b Ragone plots and c Cycling performance of supercapacitor pouch cells with different electrolyte concentrations

Fig. S12 Required volume of electrolyte and Edevice of supercapacitors using AC materials with different true densities

For true density of ACs in between 1.8 and 2.1 g cm−3, the simulated Edevice revealed minimal variation. Therefore, a true density of 2.0 g cm−3 was adopted for the 43 AC materials form literature in the subsequent analyses.

Fig. S13 Mass distributions of the components in supercapacitor and the key parameters of AC materials and electrodes. Commercial supercapacitors were disassembled to analyze their mass distribution and properties of AC materials

Fig. S14 a N2 adsorption‒desorption isotherms of the AC materials of different cylindrical supercapacitors. b Charging and discharging curves of cylindrical supercapacitors

Fig. S15 The plot of Edevicce vs. specific surface area of AC materials

Fig. S16 The influence of correction coefficient (ζ) on Edevice

Using CS = 95 F g−1, PAC = 0.65 mL g−1, and ma = 13 mg cm−2, the influence of the packaging factor ζ on the Edevice is investigated. For a ~140 F supercapacitor cells, the ζ of pouch package and cylindrical package is 0.35 and 0.89, respectively, corresponding to 87% and 73% of normalized Edevice (when ζ = 0). Usually, when larger supercapacitor cell is assembled, the influence of ζ would be decrease.

Fig. S17 a The 3D function relation plots of (a) ma (mg cm−2) and PAC (mL g−1) with respect to η, where CS = 95 F g−1. b ma (mg cm−2) and CS (mL g−1) to η, fixing the PAC = 0.65 mL g−1

Fig. S18 The Edevice of AC (CS = 95 F g−1, PAC = 0.65 mL g−1) across varying mass loadings (ranging from 2 to 40 mg cm⁻², double-side coating)

Table S1 The parameter specification of separators

| NKK TF4030 cellulose separators |  |
| --- | --- |
| thickness | 30μm |
| width | 60 mm |
| density | 0.421 g cm−3 |
| porosity | 73% |
| strength | ≥7.8 N/15mm |
| pH | 5.5-8.0 |

Table S2 Characterization of the AC electrode

| The parameters of commercial activated carbon electrode |  |
| --- | --- |
| mass loading (mg cm−2) | 6.5 |
| mass ratio of electrode (AC: conductive carbon: binder) | 95:3:2 |
| thickness of the electrode (μm) | 100 |
| true density (g cm−3) | 1.94 |
| accumulative pore volume (mL g−1) | 0.65 |
| specific surface area (m2 g−1) | 1051 |
| the volume ratio of stacked pores to the electrode | 26.7% |
| Vpore (mL) | 8.15 |
| VAC (mL) | 4.04 |
| VP (mL) | 2.67 |
| Vs (mL) | 1.36 |

Table S3 The densities and ionic conductivities of electrolytes

| Concentrations | Density (g mL−1) | Ionic conductivity (mS cm−1) |
| --- | --- | --- |
| 0.25 M Net4BF4 in ACN | 0.807 | 24.07 |
| 0.5 M Net4BF4 in ACN | 0.825 | 36.13 |
| 1.0 M Net4BF4 in ACN | 0.864 | 52.9 |
| 1.5 M Net4BF4 in ACN | 0.898 | 58 |

Table S4 The accumulative pore volume, specific capacitance, BET surface area, electrolyte and predicted Edevice for 43 AC materials from literature

| Carbon Sample | Accumulative pore volume (mL g−1) | Specific capacitance (F g−1) | BET surface area (m2 g−1) | Electrolyte | #Edevice (Wh kgdevice-1) | Refs. |
| --- | --- | --- | --- | --- | --- | --- |
| YP-50F YP-80F PW-400 SC-1800 ACS-PC EL-104 EL-106 ACC-10 ACC-15 ACC-20 APC-700-1 APC-700-2 APC-800 APC-950 APC-1000 APC-1050 APC-1100 AEL-1000 AEL-1100 AEL-1200 | 0.70 1.10 0.80 0.80 0.90 0.80 0.90 0.40 0.50 0.80 0.80 0.80 0.90 0.80 0.80 0.80 0.90 0.80 0.70 0.70 | 94.3 95.7 84.3 128 135.3 93.5 93.7 98 105.1 107.5 122.6 124.3 117.1 108.2 105.1 97.1 93.8 91.8 89.8 81.8 | 1694 2264 1724 1821 1796 1721 1907 1094 1436 2004 1708 1700 1815 1555 1569 1496 1761 1701 1685 1602 | 1 M Net4BF4 in ACN | 7.84 6.85 6.73 10.22 10.40 7.47 7.21 9.26 9.50 8.59 9.79 9.93 9.01 8.64 8.40 7.76 7.21 7.33 7.46 6.80 | [S2] |
| PICA A PICA B PICA C | 1.63 1.12 0.71 | 115 100 90 | 2315 2100 1500 | 1.7 M N(C2H5)4CH3SO3 in ACN | 6.95 7.11 7.45 | [S3] |
| CDC-700 | 1.4 | 170 | 2250 | 1 M Net4BF4 in ACN | 11.02 | [S4] |
| ND 1300-AR ND 1300-VAC ND 1700-AR ND 1700-VAC | 1.11 1.11 1.23 1.30 | 22 21 24 20 | 356 314 430 364 | 1 M Net4BF4 in ACN | 1.57 1.50 1.64 1.34 | [S5] |
| Hurd-a-1 Hurd-a-3 Hurd-a-5 Hurd-b-5 Bast-a-5 Bast-b-5 | 0.73 1.16 1.71 1.06 1.76 0.86 | 94 144 167 136 146 103 | 1910 2879 2801 2446 2671 1909 | 1.8 M Net4BF4 in PC | 7.73 10.09 9.87 9.87 8.50 8.03 | [S6] |
| CPr48 CS48 CP48 CPr15 CS15 CP15 CPr15T CSU CPrU | 0.25 0.58 0.29 0.21 0.45 0.25 0.2 0.57 0.28 | 62 115 50 48 93 57 32 94 60 | 850 2000 1300 713 1470 923 630 2200 1000 | 1 M Net4BF4 in ACN | 6.29 10.04 4.98 4.97 8.59 5.78 3.33 8.24 6.00 | [S7] |

Note: #Energy density is simulated via the provided E-tool.

S5 E-tool for supercapacitor

| Input information of materials |  |  |  |
| --- | --- | --- | --- |
| Electrode properties |  | Sepatator |  |
| active material | activated carbon (AC) | NKK TF4030 |  |
| accumulative pore volume of activated carbon (mL/g) | 0.65 | porosity (%) | 73% |
| true density (g/cm3) | 2 | thickness (μm) | 30 |
| porosity of stacking pores | 26% | width (cm) | 6 |
| double-side mass loading (ma, mg/cm2) | 13 | density (g/cm3) | 0.421 |
| content of active material (wt.%) | 95% | Electrolyte |  |
| specific capacitance (F/g) | 95 | 1 M Net4BF4 in ACN |  |
| width (cm) | 4.3 | density (g/mL) | 0.8639 |
| length (cm) | 5.6 | Cuerrent collector |  |
| area of single electrode (cm2) | 24.08 | areal density of 12 μm Al foil (mg/cm2) | 3.24 |
| positive pieces | 10 | Operating voltage of supercapacitor |  |
| negative pieces | 11 | voltage window (V) | 2.7 |
| Supercapacitor device |  |  |  |
| mass of AC (mAC, g) | 6.57 | mass of electrolyte (Vtotal) (g) | 6.91 |
| volume of AC (cm3) | 3.29 | mass of separator (g) | 0.78 |
| VAC (cm3) | 4.06 | mass of current collector (Al foil) (g) | 1.64 |
| total volume of electrode (cm3) | 9.93 | mass of package (g) | 2.17 |
| VP (cm3) | 2.58 | mass of binder and conductive carbon (g) | 0.35 |
| Vpore (cm3) | 6.64 | total mass of device (Mtotal, g) | 18.42 |
| Vs (cm3) | 1.36 | rated capacitance (F) | 141 |
| Output results of supercapacitor cell |  |  |  |
| EAC (Wh/kg) | 22.90 | conversion factor (f) | 0.34 |
| Edevice (Wh/kg) | 7.77 |  |  |
| NOTE: 1VAC is the volume of pore in AC; VP is the volume of stacking pore; Vs is the volume of pore in separator; |  |  |  |
| 2The cacluating equation of energy density : EAC=1/2*C*V2/mAC; Edevice=1/2*C*V2/Mtotal |  |  |  |

Supplementary References

- S. Wang, L. Yu, S. Wang, L. Zhang, L. Chen et al., Strong, tough, ionic conductive, and freezing-tolerant all-natural hydrogel enabled by cellulose-bentonite coordination interactions. Nat. Commun. 13(1), 3408 (2022). https://doi.org/10.1038/s41467-022-30224-8

- X. Liu, D. Lyu, C. Merlet, M.J.A. Leesmith, X. Hua et al., Structural disorder determines capacitance in nanoporous carbons. Science 384(6693), 321-325 (2024). https://doi.org/ 10.1126/science.adn6242

- J. Gamby, P.L. Taberna, P. Simon, J.F. Fauvarque, M. Chesneau, Studies and characterisations of various activated carbons used for carbon/carbon supercapacitors. J. Power Sources 101(1), 109-116 (2001). https://doi.org/10.1016/S0378-7753(01)00707-8

- Y. Korenblit, M. Rose, E. Kockrick, L. Borchardt, A. Kvit et al., High-rate electrochemical capacitors based on ordered mesoporous silicon carbide-derived carbon. ACS Nano 4(3), 1337-1344 (2010). https://doi.org/10.1021/nn901825y

- M. Zeiger, N. Jäckel, D. Weingarth, V. Presser, Vacuum or flowing argon: What is the best synthesis atmosphere for nanodiamond-derived carbon onions for supercapacitor electrodes? Carbon. 94(507-517 (2015). https://doi.org /10.1016/j.carbon.2015.07.028

- W. Sun, S.M. Lipka, C. Swartz, D. Williams, F. Yang, Hemp-derived activated carbons for supercapacitors. Carbon 103, 181-192 (2016). https://doi.org/ 10.1016/j.carbon.2016.02.090

- C. Vix-Guterl, E. Frackowiak, K. Jurewicz, M. Friebe, J. Parmentier et al., Electrochemical energy storage in ordered porous carbon materials. Carbon 43(6), 1293-1302 (2005). https://doi.org/ 10.1016/j.carbon.2004.12.028