Supporting Information for

Modulation of the Spin State of Atomic Fe-N4 Sites with Interlayer-Adjacent Ir-N4 for Superior ORR Activity

Yan Tan1, Aoshuang Li1, Yijie Wang1, Xiucai Jiang1, Yiwen Cheng1, Dongliang Chao2,*, Yuzhong Zhang1,*, Chuanwei Cheng1,*

1School of Physics Science and Engineering, Tongji University, Shanghai 200092, P. R. China

2Laboratory of Advanced Materials, Aqueous Battery Center, Shanghai Key Laboratory of Molecular Catalysis and Innovative Materials, Electron Microscope Center of Fudan University, Faculty of Chemistry and Materials, Fudan University, Shanghai 200433, P. R. China

* Corresponding authors. Email: cwcheng@tongji.edu.cn (Chuanwei Cheng); yzzhang@tongji.edu.cn (Yuzhong Zhang); chaod@fudan.edu.cn (Dongliang Chao)

S1 Electrochemical measurements

A platinum wire electrode in a hydrogen-filled chamber was used to simulate the reversible hydrogen electrode (RHE) as the working electrode, with a graphite rod as the counter electrode and an Hg/HgO electrode as the reference electrode. The open-circuit potential-time curve was measured over 2000 seconds in 0.1 M KOH solution using this three-electrode system, and the average open-circuit potential obtained was used as the potential correction value for Hg/HgO relative to RHE.

The observed potential and Hg/HgO can be transformed into RHE using the following formula: E(RHE) = E(Hg/HgO) + 0.880 V.

The K-L equation was used to determine the number of electron transfers (n) that occurred during ORR：

1j=1jk+1jdl=1nFkCO2+10.62nFCO2DO22/3ν-1/6ω1/2

Where, respectively, j, jk, and jdl represent the measured current density, kinetic current, and diffusion-limiting current density. k (cm s-1) is the heterogeneous rate constant for electron transfer. F stands for the Faraday constant (96485 C mol−1), and ν for the kinetic viscosity of electrolyte (1.0 × 10−2 cm2 s-1). The oxygen concentration in 0.1 M KOH (1.2 × 10−6 mol cm−3) is donated as CO2. The diffusion coefficient of oxygen is donated as DO2 (1.9 × 10−5 cm2 s−1).

In accordance with previous studies [S1], a carbon paper integrated with a gas diffusion layer supported on nickel foam was employed as the substrate for the gas diffusion electrode half-cell tests. To achieve a homogeneous catalyst loading, 5 mg of the as-prepared catalyst was dispersed into a mixed solution of 10 µL of 5 wt% Nafion solution containing 500 µL ethanol, followed by sonication for 0.5 hours. Subsequently, 100 µL of the catalyst ink was uniformly drop-cast onto the gas diffusion electrode. The catalyst-coated electrode was then transferred to a vacuum oven and dried at 40 °C for 30 minutes. After complete drying, the electrode was assembled into an in-situ electrochemical reaction cell for performance evaluation. During the tests, an Ag/AgCl electrode and a Pt wire were used as the reference electrode and counter electrode, respectively. Pure oxygen was continuously purged into the bottom chamber of the cell. Polarization curves of all catalysts were measured in 1.0 M KOH electrolyte until stable cyclic voltammetry profiles were observed. All potentials were converted to the reversible hydrogen electrode scale.

The TOF of catalysts was obtained by following equations:

TOF = I4nF

Where I is the reduction current (A) recorded in GDE measurements, n is the molar number of atomic Fe sites obtained from ICP, and F is the Faraday constant.

S2 Finite element multi-physics field simulation

A three-dimensional electrochemistry module in COMSOL Multiphysics 6.2 was called to simulate the concentration distribution of the electrolyte at the electrolyte/electrode surface. The 3D nanoparticle was determined to be a regular decahedron with a side length of 1.2 μm. The 3DOM nanoparticle was determined to be a regular decahedron with a side length of 1.2 μm and a pore diameter of 0.2 μm. The conductivity of the IrFe-SACs was set to be 3 × 105 S m-1. The ionic conductivity of the electrolyte was determined to be 65 S m–1. The diffusion coefficient of oxygen in electrolyte was set to be 1 × 10-12 m2 s-1. An overpotential of 1.0 V was to excite the oxygen transport process.

S3 DFT calculation details

The models of IrFe-SACs, CoFe-SACs, NiFe-SACs, PtFe-SACs, RuFe-SACs, MnFe-SACs, MnFe-SACs, CuFe-SACs, Ir-SACs and Fe-SACs were built in the hexagonal cell with lattice constants of 14.76 Å, 14.76 Å, and 35.00 Å. The interaction between neighboring crystal cells can be significantly reduced by the vacuum layer of 35.00 Å. The massive carbon nanosheet substrate was simulated using a 6×6 graphene supercell carbon layer, which was partly substituted by M-N4 (M = Co, Fe, Ni, Ru, Cu, Mn, Zn, Pt, Ir) sites.

In our calculations, the cutoff energy of plane wave expansion was employed at 400 eV and 450 eV for structural optimization and derivation of Gibbs free energy, respectively. The Brillouin zone was sampled using a 4×4×1 k mesh by Gamma-centered scheme. The electronic ground-state energy converged to lower than 10-4 eV for structural optimization and 10-5 eV for total energy calculation, and the crystal structure was relaxed to a Hellmann Feynman force of less than 0.01 eV Å−1.

The computational hydrogen electrode (CHE) model was used to determine the Gibbs free energy of each elementary reaction in ORR processes. The four electronic reaction routes listed below can be used to characterize the entire ORR process:

*+O2(g)+H2O(l)+e-→HOO*+OH-HOO*+e-→O*+OH-O*+H2O(l)+e-→HO*+OH-HO*+e-→OH-+*

ORR electrocatalytic properties are commonly described by Gibbs free energy change, which is calculated as:               ΔG=ΔE+ΔZPE-TΔS-neU

where ΔE is characterized as the total energy change of system; n is electron transfer number in a certain state; ΔZPE and ΔS stand for the zero-point energy change and entropy change, respectively, which are based on the calculated vibration frequency of the reactants and products by DS-PAW or the standard table. The Gibbs free energy of O2 was calculated as GO2=2GH2O-2GH2-4.92 eV to prevent improper description of the O2 triplet state in DFT calculations. The theoretical overpotential (ηORR or ηOER) of a reaction was determined as the difference between the voltage needed to convert all free energy steps and the minimal potential (1.23 V) needed for ORR/OER in theory:

ηORR=max(ΔG1-4)+1.23eVe

The calculation formula of total density of states center Ec is as follows:

Ec=-∞+∞EρEdE-∞+∞ρEdE

where ρE is the total density of states, and E is corresponding energy eigenvalue.

Supplementary Figures and Tables

Fig. S1 Partial possible bilayer bimetallic atomic catalyst configurations

Table S1 Ground state energies (E) and diatomic metal spacings (d) for various atomic configurations based on DS-PAW

| Models | d (Å) | E (eV) | Models | d (Å) | E(eV) |
| --- | --- | --- | --- | --- | --- |
| Co(1) | 3.044 | -30201.122 | Co(11) | 5.709 | -30201.327 |
| Co(2) | 2.727 | -30201.663 | Co(12) | 5.860 | -30201.335 |
| Co(3) | 4.018 | -30201.292 | Co(13) | 5.808 | -30201.321 |
| Co(4) | 3.212 | -30201.060 | Co(14) | 6.229 | -30201.261 |
| Co(5) | 3.193 | -30201.337 | Co(15) | 6.275 | -30201.322 |
| Co(6) | 3.812 | -30201.301 | Co(16) | 6.497 | -30201.048 |
| Co(7) | 4.592 | -30200.612 | Co(17) | 6.806 | -30201.344 |
| Co(8) | 4.749 | -30201.032 | Co(18) | 7.580 | -30201.331 |
| Co(9) | 5.213 | -30201.056 | Co(19) | 8.400 | -30201.328 |
| Co(10) | 5.505 | -30201.323 | Co(20) | 9.337 | -30201.312 |
| Co(0) | 2.511 | -30201.963 |  |  |  |

Table S2 The calculated results of various oxygen intermediates for different atomic configurations. "G" refers to the total Gibbs free energy of the whole system (oxygen intermediate + small molecular species) in certain reaction step

| Items |  | Models |  | *(+H2+O2) |  | *OOH |  | *O |  | *OH |  | *(+H2O) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| E/eV |  | CoFe-SACs |  | -1309.0965 |  | -1323.8386 |  | -1314.7630 |  | -1319.3238 |  | -1309.0965 |
| ZPE/eV |  |  |  | 0.0000 |  | 0.4286 |  | 0.0697 |  | 0.3523 |  | 0.0000 |
| TS/eV |  |  |  | 0.0000 |  | 0.1892 |  | 0.0624 |  | 0.0903 |  | 0.0000 |
| G/eV |  |  |  | -1332.6165 |  | -1333.7993 |  | -1335.7757 |  | -1336.6818 |  | -1337.5365 |
| ΔG/eV |  |  |  | 4.9200 |  | 3.7372 |  | 1.7608 |  | 0.8547 |  | 0.0000 |
| U=1.23 V |  |  |  | 0.0000 |  | 0.0472 |  | -0.6992 |  | -0.3753 |  | 0.0000 |
| E/eV |  | NiFe-SACs |  | -1307.4708 |  | -1322.5558 |  | -1313.5079 |  | -1318.0237 |  | -1307.4708 |
| ZPE/eV |  |  |  | 0.0000 |  | 0.4294 |  | 0.0690 |  | 0.3548 |  | 0.0000 |
| TS/eV |  |  |  | 0.0000 |  | 0.1853 |  | 0.0657 |  | 0.0908 |  | 0.0000 |
| G/eV |  |  |  | -1330.9908 |  | -1332.5117 |  | -1334.5246 |  | -1335.3797 |  | -1335.9108 |
| ΔG/eV |  |  |  | 4.9200 |  | 3.3991 |  | 1.3862 |  | 0.5311 |  | 0.0000 |
| U=1.23 V |  |  |  | 0.0000 |  | -0.2909 |  | -1.0738 |  | -0.6989 |  | 0.0000 |
| E/eV |  | MnFe-SACs |  | -1311.0771 |  | -1325.2287 |  | -1316.1794 |  | -1320.7829 |  | -1311.0771 |
| ZPE/eV |  |  |  | 0.0000 |  | 0.4286 |  | 0.0675 |  | 0.3412 |  | 0.0000 |
| TS/eV |  |  |  | 0.0000 |  | 0.1911 |  | 0.0581 |  | 0.1016 |  | 0.0000 |
| G/eV |  |  |  | -1334.5971 |  | -1335.1913 |  | -1337.1901 |  | -1338.1632 |  | -1339.5171 |
| ΔG/eV |  |  |  | 4.9200 |  | 4.3258 |  | 2.3270 |  | 1.3539 |  | 0.0000 |
| U=1.23 V |  |  |  | 0.0000 |  | 0.6358 |  | -0.1330 |  | 0.1239 |  | 0.0000 |
| E/eV |  | CuFe-SACs |  | -1304.4016 |  | -1319.5540 |  | -1310.5284 |  | -1315.0305 |  | -1304.4016 |
| ZPE/eV |  |  |  | 0.0000 |  | 0.4280 |  | 0.0685 |  | 0.3537 |  | 0.0000 |
| TS/eV |  |  |  | 0.0000 |  | 0.1866 |  | 0.0664 |  | 0.0917 |  | 0.0000 |
| G/eV |  |  |  | -1327.9216 |  | -1329.5126 |  | -1331.5464 |  | -1332.3886 |  | -1332.8416 |
| ΔG/eV |  |  |  | 4.9200 |  | 3.3290 |  | 1.2952 |  | 0.4530 |  | 0.0000 |
| U=1.23 V |  |  |  | 0.0000 |  | -0.3610 |  | -1.1648 |  | -0.7770 |  | 0.0000 |
| E/eV |  | RuFe-SACs |  | -1310.1918 |  | -1324.5461 |  | -1314.9766 |  | -1320.0661 |  | -1310.1918 |
| ZPE/eV |  |  |  | 0.0000 |  | 0.4382 |  | 0.0679 |  | 0.3391 |  | 0.0000 |
| TS/eV |  |  |  | 0.0000 |  | 0.1756 |  | 0.0584 |  | 0.1125 |  | 0.0000 |
| G/eV |  |  |  | -1333.7118 |  | -1334.4835 |  | -1335.9871 |  | -1337.4595 |  | -1338.6318 |
| ΔG/eV |  |  |  | 4.9200 |  | 4.1483 |  | 2.6447 |  | 1.1723 |  | 0.0000 |
| U=1.23 V |  |  |  | 0.0000 |  | 0.4583 |  | 0.1847 |  | -0.0577 |  | 0.0000 |
| E/eV |  | PtFe-SACs |  | -1307.8772 |  | -1322.9869 |  | -1313.9419 |  | -1318.4528 |  | -1307.8772 |
| ZPE/eV |  |  |  | 0.0000 |  | 0.4282 |  | 0.0689 |  | 0.3550 |  | 0.0000 |
| TS/eV |  |  |  | 0.0000 |  | 0.1891 |  | 0.0661 |  | 0.0892 |  | 0.0000 |
| G/eV |  |  |  | -1331.3972 |  | -1332.9478 |  | -1334.9591 |  | -1335.8071 |  | -1336.3172 |
| ΔG/eV |  |  |  | 4.9200 |  | 3.3694 |  | 1.3581 |  | 0.5101 |  | 0.0000 |
| U=1.23 V |  |  |  | 0.0000 |  | -0.3206 |  | -1.1019 |  | -0.7199 |  | 0.0000 |
| E/eV |  | IrFe-SACs |  | -1310.2555 |  | -1324.9336 |  | -1315.7519 |  | -1320.4409 |  | -1310.2555 |
| ZPE/eV |  |  |  | 0.0000 |  | 0.4348 |  | 0.0707 |  | 0.3528 |  | 0.0000 |
| TS/eV |  |  |  | 0.0000 |  | 0.1795 |  | 0.0598 |  | 0.0899 |  | 0.0000 |
| G/eV |  |  |  | -1333.7755 |  | -1334.8784 |  | -1336.7611 |  | -1337.7979 |  | -1338.6955 |
| ΔG/eV |  |  |  | 4.9200 |  | 3.8171 |  | 1.9344 |  | 0.8976 |  | 0.0000 |
| U=1.23 V |  |  |  | 0.0000 |  | 0.1271 |  | -0.5256 |  | -0.3324 |  | 0.0000 |
| E/eV |  | ZnFe-SACs |  | -1302.6257 |  | -1317.6007 |  | -1308.5112 |  | -1313.0738 |  | -1302.6257 |
| ZPE/eV |  |  |  | 0.0000 |  | 0.4285 |  | 0.0674 |  | 0.3524 |  | 0.0000 |
| TS/eV |  |  |  | 0.0000 |  | 0.1878 |  | 0.0688 |  | 0.0939 |  | 0.0000 |
| G/eV |  |  |  | -1326.1457 |  | -1327.5599 |  | -1329.5326 |  | -1330.4353 |  | -1331.0657 |
| ΔG/eV |  |  |  | 4.9200 |  | 3.5058 |  | 1.5331 |  | 0.6304 |  | 0.0000 |
| U=1.23 V |  |  |  | 0.0000 |  | -0.1842 |  | -0.9269 |  | -0.5996 |  | 0.0000 |
| Items | Models |  | * |  | *OOH |  | *O |  | *OH |  | * |  |  |
| E/eV | Pt-111 |  | -324.6554 |  | -340.5743 |  | -329.9436 |  | -335.1102 |  | -324.6554 |  |  |
| ZPE/eV |  |  | 0.0000 |  | 0.4050 |  | 0.0562 |  | 0.3332 |  | 0.0000 |  |  |
| TS/eV |  |  | 0.0000 |  | 0.1575 |  | 0.0628 |  | 0.1105 |  | 0.0000 |  |  |
| G/eV |  |  | -348.1754 |  | -350.3693 |  | -350.9074 |  | -352.3970 |  | -353.0954 |  |  |
| ΔG/eV |  |  | 4.9200 |  | 2.7261 |  | 2.1880 |  | 0.6984 |  | 0.0000 |  |  |
| U=1.23 V |  |  | 0.0000 |  | -0.9639 |  | -0.2720 |  | -0.5316 |  | 0.0000 |  |  |
| E/eV | Ir-SACs |  | -1,317.0225 |  | -1,332.6671 |  | -1,323.4089 |  | -1,328.5056 |  | -1,317.0225 |  |  |
| ZPE/eV |  |  | 0.0000 |  | 0.4577 |  | 0.0892 |  | 0.3840 |  | 0.0000 |  |  |
| TS/eV |  |  | 0.0000 |  | 0.1216 |  | 0.0311 |  | 0.0396 |  | 0.0000 |  |  |
| G/eV |  |  | -1,340.5425 |  | -1,342.5310 |  | -1,344.3708 |  | -1,345.7812 |  | -1,345.4625 |  |  |
| ΔG/eV |  |  | 4.9200 |  | 2.9315 |  | 1.0917 |  | -0.3187 |  | 0.0000 |  |  |
| U=1.23 V |  |  | 0.0000 |  | -0.7585 |  | -1.3683 |  | -1.5487 |  | 0.0000 |  |  |
| E/eV | Fe-SACs |  | -1,317.8284 |  | -1,332.3122 |  | -1,323.2953 |  | -1,327.7780 |  | -1,317.8284 |  |  |
| ZPE/eV |  |  | 0.0000 |  | 0.4163 |  | 0.0679 |  | 0.3408 |  | 0.0000 |  |  |
| TS/eV |  |  | 0.0000 |  | 0.1658 |  | 0.0659 |  | 0.1211 |  | 0.0000 |  |  |
| G/eV |  |  | -1,341.3484 |  | -1,342.2617 |  | -1,344.31 |  | -1,345.1783 |  | -1,346.2684 |  |  |
| ΔG/eV |  |  | 4.9200 |  | 4.0067 |  | 1.9552 |  | 1.0901 |  | 0.0000 |  |  |
| U=1.23 V |  |  | 0.0000 |  | 0.3167 |  | -0.5048 |  | -0.1399 |  | 0.0000 |  |  |

Table S3 The calculated results of various oxygen intermediates for different atomic configurations. "G" refers to the total Gibbs free energy of the whole system (oxygen intermediate + small molecular species) in certain reaction step

| Items | Models | *(+H2+O2) | *OOH | *O | *OH | *(+H2O) |
| --- | --- | --- | --- | --- | --- | --- |
| E/eV | FeN4C12 | -776.6109 | -791.0873 | -782.4278 | -786.8327 | -776.6109 |
| ZPE/eV |  | 0.0000 | 0.4194 | 0.0710 | 0.3414 | 0.0000 |
| TS/eV |  | 0.0000 | 0.1650 | 0.0660 | 0.1098 | 0.0000 |
| G/eV |  | -800.1309 | -801.0329 | -803.4427 | -804.2211 | -805.0509 |
| ΔG/eV |  | 4.9200 | 4.0180 | 1.6081 | 0.8298 | 0.0000 |
| U=1.23 V |  | 0.0000 | 0.3280 | -0.8519 | -0.4002 | 0.0000 |
| E/eV | IrFeN6 | -634.3242 | -651.8147 | -641.4821 | -645.2968 | -634.3242 |
| ZPE/eV |  | 0.0000 | 0.4488 | 0.0862 | 0.3801 | 0.0000 |
| TS/eV |  | 0.0000 | 0.1397 | 0.0371 | 0.0638 | 0.0000 |
| G/eV |  | -657.8442 | -661.7056 | -662.4530 | -662.6005 | -662.7642 |
| ΔG/eV |  | 4.9200 | 1.0586 | 0.3112 | 0.1637 | 0.0000 |
| U=1.23 V |  | 0.0000 | -2.6314 | -2.1488 | -1.0663 | 0.0000 |
| E/eV | (Ir)N4 FeN4 | -632.9697 | -647.3669 | -638.0711 | -642.9731 | -632.9697 |
| ZPE/eV |  | 0.0000 | 0.4336 | 0.0596 | 0.3458 | 0.0000 |
| TS/eV |  | 0.0000 | 0.1401 | 0.0809 | 0.1293 | 0.0000 |
| G/eV |  | -656.4897 | -657.2733 | -659.1124 | -660.3767 | -661.4097 |
| ΔG/eV |  | 4.9200 | 4.1363 | 2.2972 | 1.0330 | 0.0000 |
| U=1.23 V |  | 0.0000 | 0.4463 | -0.1628 | -0.1970 | 0.0000 |
| E/eV | IrN4 (Fe)N4 | -632.9697 | -647.9507 | -639.0275 | -643.4613 | -632.9697 |
| ZPE/eV |  | 0.0000 | 0.4320 | 0.0667 | 0.3258 | 0.0000 |
| TS/eV |  | 0.0000 | 0.1776 | 0.0689 | 0.1312 | 0.0000 |
| G/eV |  | -656.4897 | -657.8963 | -660.0497 | -660.8867 | -661.4097 |
| ΔG/eV |  | 4.9200 | 3.5133 | 1.3600 | 0.5229 | 0.0000 |
| U=1.23 V |  | 0.0000 | -0.1767 | -1.1000 | -0.7071 | 0.0000 |
| E/eV | (Ir)Fe-SACs | -1293.4728 | -1308.2833 | -1299.1433 | -1303.8073 | -1293.4728 |
| ZPE/eV |  | 0.0000 | 0.4328 | 0.0718 | 0.3561 | 0.0000 |
| TS/eV |  | 0.0000 | 0.1979 | 0.0584 | 0.0870 | 0.0000 |
| G/eV |  | -1316.9928 | -1318.2484 | -1320.1499 | -1321.1582 | -1321.9128 |
| ΔG/eV |  | 4.9200 | 3.6644 | 1.7629 | 0.7546 | 0.0000 |
| U=1.23 V |  | 0.0000 | -0.0256 | -0.6971 | -0.4754 | 0.0000 |
| E/eV | Ir(Fe)-SACs | -1294.3531 | -1308.9473 | -1299.7478 | -1304.5580 | -1294.3531 |
| ZPE/eV |  | 0.0000 | 0.4383 | 0.0725 | 0.3581 | 0.0000 |
| TS/eV |  | 0.0000 | 0.1813 | 0.0559 | 0.0840 | 0.0000 |
| G/eV |  | -1317.8731 | -1318.8904 | -1320.7512 | -1321.9039 | -1322.7931 |
| ΔG/eV |  | 4.9200 | 3.9027 | 2.0419 | 0.8892 | 0.0000 |
| U=1.23 V |  | 0.0000 | 0.2127 | -0.4181 | -0.3408 | 0.0000 |
| E/eV | (IrFe)-SACs | -1,277.5261 | -1,292.1958 | -1,283.0426 | -1,287.7440 | -1,277.5261 |
| ZPE/eV |  | 0.0000 | 0.4506 | 0.0718 | 0.3596 | 0.0000 |
| TS/eV |  | 0.0000 | 0.1661 | 0.0578 | 0.0840 | 0.0000 |
| G/eV |  | -1,301.0461 | -1,302.1113 | -1,304.0485 | -1,305.0883 | -1,305.9661 |
| ΔG/eV |  | 4.9200 | 3.8548 | 1.9176 | 0.8778 | 0.0000 |
| U=1.23 V |  | 0.0000 | 0.1648 | -0.5424 | -0.3522 | 0.0000 |

Fig. S2 Structural diagrams of FeN4C12, IrFeN6, IrN4FeN4, (Ir)Fe-SACs, Ir(Fe)-SACs and (IrFe)-SACs

Fig. S3 ORR path Gibbs free energy step of FeN4C12, IrFeN6, (Ir)N4FeN4 (The active center is the atomic Ir), IrN4(Fe)N4 (The active center is the atomic Fe), (Ir)Fe-SACs, Ir(Fe)-SACs and (IrFe)-SACs

Table S4 ICOHP for different atomic configurations

| Spin State | Models | O* | HO* | HOO* |
| --- | --- | --- | --- | --- |
| 1 | IrFe-SACs | -1.9102 | -1.4807 | -1.2780 |
| 2 |  | -3.5731 | -1.0821 | -1.6895 |
| 1 | RuFe-SACs | -1.6668 | -0.9573 | -0.9500 |
| 2 |  | -3.0606 | -1.1996 | -1.1152 |
| 1 | PtFe-SACs | -3.0753 | -4.0312 | -1.5122 |
| 2 |  | -3.0802 | -4.0300 | -2.0255 |
| 1 | NiFe-SACs | -2.1302 | -1.2268 | -1.5092 |
| 2 |  | -3.7579 | -1.7413 | -2.0431 |
| 1 | MnFe-SACs | -1.7247 | -0.9932 | -0.6533 |
| 2 |  | -3.1381 | -0.7523 | -0.9395 |
| 1 | CuFe-SACs | -2.0149 | -1.1944 | -1.4718 |
| 2 |  | -3.7351 | -1.7381 | -2.0315 |
| 1 | CoFe-SACs | -1.9923 | -1.5796 | -1.3350 |
| 2 |  | -3.6618 | -1.1384 | -1.9136 |
| 1 | ZnFe-SACs | -2.0331 | -1.1327 | -2.0303 |
| 2 |  | -3.7104 | -1.6999 | -1.4426 |
| 1 | Fe-SACs | -1.95703 | -1.7825 | -2.12297 |
| 2 |  | -3.67461 | -1.21039 | -1.53651 |
| 1 | Ir-SACs | -3.98811 | -5.40549 | -5.00848 |
| 2 |  | -3.9878 | -5.40551 | -5.00845 |

Fig. S4 SEM images of (a) NiFe-SACs, (b) CoFe-SACs, (c) MnFe-SACs, (d) RuFe-SACs and (e) CuFe-SACs

Fig. S5 HAADF-STEM images of IrFe-SACs

Table S5 EDS table of IrFe-SACs

| Z | Element | Family | Atomic Fraction (%) | Mass Fraction (%) |
| --- | --- | --- | --- | --- |
| 6 | C | K | 91.84 | 89.20 |
| 7 | N | K | 4.20 | 4.75 |
| 8 | O | K | 3.76 | 4.87 |
| 26 | Fe | K | 0.17 | 1.79 |
| 77 | Ir | M | 0.02 | 0.39 |

Table S6 ICP results of IrFe-SACs

| Samples | Mass /g | Volume /mL | Element | Readout /mg L-1 | Content /mg kg-1 | wt.% |
| --- | --- | --- | --- | --- | --- | --- |
| IrFe-SACs | 0.0104 | 25 | Fe | 8.5941 | 20658.9 | 2.0659% |
|  | 0.0104 | 25 | Ir | 1.8775 | 4513.2 | 0.4513% |

Fig. S6 XRD pattern of IrFe-SACs

Fig. S7 Surface contact angles measured at IrFe-SACs, Fe-SACs, Ir-SACs and Pt/C-RuO2 electrodes

Fig. S8 Fourier-transformed k3-weighted EXAFS fitting results for IrFe-SACs at k space

Table S7 Parameters obtained for the best EXAFS fitting of IrFe-SACs

| Edges | Paths | N | R(Å) | σ2 (10-3 Å2) | Happiness | R-factor |
| --- | --- | --- | --- | --- | --- | --- |
| Ir L3-edge | Ir-N | 3.61±0.05 | 1.95±0.062 | 0.004 | 90.76 | 0.009 |
|  | Ir-Fe | 0.95±0.14 | 2.48±0.013 | 0.034 |  |  |
| Fe K-edge | Fe-N | 3.76±0.01 | 1.89±0.017 | 0.001 | 95.13 | 0.021 |
|  | Fe-Ir | 1.01±0.05 | 2.48±0.028 | 0.013 |  |  |

Where N is the coordination number; R is the distance between absorber and backscatter atoms; σ2

is the Debye-Waller factor (a measure of thermal and static disorder in absorber-scatterer distances);

R-factor is used to value the goodness of the fitting.

Fig. S9 (a) Normalized XANES spectra, (b) Fourier transforms of EXAFS spectra Fe K-edge of IrFe-SACs and the reference materials at R space. XAFS curves represent fitted data based on (c) Fe K-edge experimental data, with the fitted curves of Fe-SACs at the insets. (d) Wavelet transform of Fe K-edge EXAFS spectra for Fe-SACs

Table S8 Parameters obtained for the best EXAFS fitting of Fe-SACs

| Edges | Paths | N | R(Å) | σ2 (10-3 Å2) | Happiness | R-factor |
| --- | --- | --- | --- | --- | --- | --- |
| Fe K-edge | Fe-N | 4.09±0.03 | 2.02±0.021 | 0.006 | 86.52 | 0.011 |
|  | Fe-C | 0.98±0.02 | 2.58±0.018 | 0.015 |  |  |

Where N is the coordination number; R is the distance between absorber and backscatter atoms; σ2

is the Debye-Waller factor (a measure of thermal and static disorder in absorber-scatterer distances);

R-factor is used to value the goodness of the fitting.

Fig. S10 ORR LSV curves of CuFe-SACs, MnFe-SACs, RuFe-SACs, CoFe-SACs, NiFe-SACs, IrFe-SACs and Pt/C

Fig. S11 ORR LSV curves of 3DOM IrFe-SACs and IrFe-SACs without 3DOM structures

Fig. S12 EIS spectrum of various bimetallic atomic catalysts

Fig. S13 ORR LSV curves of IrFe-SACs with different Ir loadings. Here, the "x" in "IrFe-SACsx" denotes the feeding ratio of iridium acetylacetonate during the sample preparation, relative to that used for IrFe-SACs

Table S9 Comparison the ORR activity of IrFe-SACs with the reported other transition metal atomic electrocatalysts

| Catalysts | Eonset (V vs. RHE) |  | E1/2 (V vs. RHE) |  | References |
| --- | --- | --- | --- | --- | --- |
| IrFe-SACs | 0.961 | 0.928 |  | This work |  |
| Co/CoMn-NC | 0.99 | 0.89 |  | [S2] |  |
| Co-SAs@NC | 0.96 | 0.82 |  | [S3] |  |
| FeSA-N-C | 1.00 | 0.892 |  | [S4] |  |
| Co/Ni-NC | 0.951 | 0.89 |  | [S5] |  |
| FeNi/NC@NG | 0.949 | 0.858 |  | [S6] |  |
| IrNi@Co/N-C | 0.973 | 0.898 |  | [S7] |  |
| FeCo-DACs | 0.915 | 0.89 |  | [S8] |  |
| Fe2DAC | 1.00 | 0.898 |  | [S9] |  |
| FeCo-NCH | 0.995 | 0.889 |  | [S10] |  |

Fig. S14 Tafel curves of CuFe-SACs, MnFe-SACs, RuFe-SACs, CoFe-SACs, NiFe-SACs, IrFe-SACs and Pt/C during ORR tests

Fig. S15 Cyclic voltammograms from 1.05 V to 1.15 V vs. RHE in 0.1 M KOH at scan rates of 20, 40, 60, 80 and 100 mV s-1 for (a) one-step synthesized IrFe-SACs, (b) IrFe-SACs, (c) Ir-SACs and (d) Fe-SACs, respectively

Table S10 ICP results of IrFe-SACs(one-step)

| Samples | Mass /g | Volume /mL | Element | Readout /mg L-1 | Content /mg kg-1 | wt.% |
| --- | --- | --- | --- | --- | --- | --- |
| IrFe-SACs (one-step) | 0.0218 | 20 | Fe | 35.5268 | 32593.4 | 3.2593% |
|  | 0.0218 | 20 | Ir | 7.9954 | 7335.2 | 0.7335% |

Fig. S16 (a) Relations between current density and scanning rate of CV curves between 1.05 and 1.15 V of one-step synthesized IrFe-SACs, IrFe-SACs, Ir-SACs and Fe-SACs. ORR LSV polarization curves in (b) 1.0 M KOH with GDEs and (c) 0.1 M KOH with RDEs, (d) TOF for one-step synthesized IrFe-SACs and IrFe-SACs

Fig. S17 (a) ORR LSV curves and (b) Koutecký-Levich diagrams of IrFe-SACs at different rotation speeds and potentials for ORR tests

Fig. S18 ORR polarization curves of (a) IrFe-SACs and (b) Pt/C before and after 3000 CV cycles

Fig. S19 I-t stability measurements curve of IrFe-SACs

Table S11 ICP results of IrFe-SACs after cycling stability tests

| Samples | Mass /g | Volume /mL | Element | Readout /mg L-1 | Content /mg kg-1 | wt.% |
| --- | --- | --- | --- | --- | --- | --- |
| IrFe-SACs | 0.0263 | 20 | Fe | 29.0271 | 22073.8 | 2.2074% |
|  | 0.0263 | 20 | Ir | 5.5024 | 4184.3 | 0.4184% |

Fig. S20 HAADF-STEM images, element mapping and the intensity profiles of IrFe-SACs after 3000 CV stability tests

Fig. S21 High-resolution scans of (a) C 1s, (b) N 1s and (c) Fe 2p for IrFe-SACs before and after ORR stability tests

Fig. S22 Open circuit voltage curves of liquid ZABs based on IrFe-SACs and Pt/C-RuO2 air cathode

Fig. S23 Galvanostatic charge-discharge cycling curves at 10 mA cm-2 of liquid ZABs based on IrFe-SACs-RuO2 air cathode

Table S12 Performance of liquid ZABs based on recently reported oxygen electrocatalysts (-- not mentioned)

| Catalysts | Power density /(mW cm-2) | Specific capacity | Cycling stability | References |
| --- | --- | --- | --- | --- |
| IrFe-SACs | 314 | 815.1 mAh g-1 @5 mA cm-2 | 20 min/cycle 1650 cycles @5 mA cm-2 | This work |
| Fe3Co7-NC | 133 | 747 mAh g-1 @2 mA cm-2 | 20 min/cycle 600 cycles 5 mA cm-2 | [S11] |
| Fe-N2-Fe | 170 | 776.7 mAh g-1 @2 mA cm-2 | 20 min/cycle 1200 cycles 10 mA cm-2 | [S12] |
| FeCo-N-C-700 | 150 | 518.0 mAh g-1 @10 mA cm-2 | 10 min/cycle 252 cycles 5 mA cm-2 | [S13] |
| SS-Co-SAC | 195 | 714.2 mAh g-1 @5 mA cm-2 | 20 min/cycle 100 cycles 10 mA cm-2 | [S14] |
| Fe, Co, N−C | 198 | 726.0 mAh g-1 @2 mA cm-2 | 4 min/cycle 765 cycles 5 mA cm-2 | [S15] |
| CoFe−N−C | 142 | -- | 60 min/cycle 200 cycles 5 mA cm-2 | [S16] |
| meso/micro-FeCo-Nx-CN-30 | 150 | -- | 20 min/cycle 120 cycles 5 mA cm-2 | [S17] |
| IrCo-N-C | 139 | 818.0 mAh g-1 @50 mA cm-2 | 30 min/cycle 450 cycles 5 mA cm-2 | [S18] |
| Ni,Fe-DSAs/NCs | 217 | 780.1 mAh g-1 @40 mA cm-2 | 240 min/cycle 125 cycles 5 mA cm-2 | [S19] |

Table S13 The calculated partial atomic (Ir, Fe, O, H) mean magnetic moments of various oxygen intermediates for IrFe-SACs and Fe-SACs before and after O/OH adsorption (μB=eℏ2me= 5.7884×10-5 eV T-1)

| Items | Models | IrFe-SACs | Fe-SACs |
| --- | --- | --- | --- |
| mO/μB | O* | -0.603 | 0.574 |
| mIr/μB |  | 0.050 | -- |
| mFe/μB |  | -1.178 | 1.229 |
| mO/μB | HO* | 0.090 | 0.106 |
| mIr/μB |  | -0.047 | -- |
| mFe/μB |  | 0.929 | 1.052 |
| mH/μB |  | 0.000 | 0.001 |
| mIr/μB | * | 0.143 | -- |
| mFe/μB |  | 1.337 | 0.000 |

Table S14 The calculated partial atomic (Ir, Fe, O, H) mean charge of various oxygen intermediates for IrFe-SACs and Fe-SACs before and after O/OH adsorption (e = 1.6022×10-19 C)

| Items | Models | IrFe-SACs | Fe-SACs |
| --- | --- | --- | --- |
| QO/e | O* | 4.873 | 4.872 |
| QIr/e |  | 8.823 | -- |
| QFe/e |  | 7.854 | 7.757 |
| QO/e | HO* | 5.045 | 5.051 |
| QIr/e |  | 8.823 | -- |
| QFe/e |  | 7.604 | 7.628 |
| QH/e |  | 0.736 | 0.740 |
| QIr/e | * | 8.859 | -- |
| QFe/e |  | 7.541 | 7.632 |

Fig. S24 PDOS of Ir-d for Ir-SACs

Fig. S25 Band structure of Ir-SACs

Table S15 The HOO(ΔE1), O (ΔE2) and HO (ΔE3) adsorption energy of Ir-SACs, Fe-SACs and IrFe-SACs

| Models | Ir-SACs | Fe-SACs | IrFe-SACs |
| --- | --- | --- | --- |
| EHOO/eV | -13.0239 | -13.0239 | -13.0239 |
| E*/eV | -1317.0225 | -1317.8284 | -1310.2555 |
| EHOO*/eV | -1332.6671 | -1332.3122 | -1324.9336 |
| E1/eV | -2.6207 | -1.4599 | -1.6542 |
| EO/eV | -1.5739 | -1.5739 | -1.5739 |
| E*/eV | -1317.0225 | -1317.8284 | -1310.2555 |
| EO*/eV | -1323.4089 | -1323.2953 | -1315.7519 |
| E2/eV | -4.8125 | -3.8930 | -3.9225 |
| EHO/eV | -7.5614 | -7.5614 | -7.5614 |
| E*/eV | -1317.0225 | -1317.8284 | -1310.2555 |
| EHO*/eV | -1328.5056 | -1327.7780 | -1320.4409 |
| E3/eV | -3.9217 | -2.3882 | -2.6240 |

Fig. S26 Fe-d and O-p orbital PDOS diagrams of IrFe-SACs-O/OH and Ir-SACs-O/OH

Fig. S27 HOMO molecular orbital diagrams of Fe-SACs-OH and IrFe-SACs-OH

Supplementary References

- P. Zhang, H.-C. Chen, H. Zhu, K. Chen, T. Li et al., Inter-site structural heterogeneity induction of single atom Fe catalysts for robust oxygen reduction. Nat. Commun. 15(1), 2062 (2024). https://doi.org/10.1038/s41467-024-46389-3

- B. Sun, S. Zhang, H. Yang, T. Zhang, Q. Dong et al., Revealing the active sites in atomically dispersed multi-metal–nitrogen–carbon catalysts. Adv. Funct. Mater. 34(29), 2315862 (2024). https://doi.org/10.1002/adfm.202315862

- X. Han, X. Ling, Y. Wang, T. Ma, C. Zhong et al., Generation of nanoparticle, atomic-cluster, and single-atom cobalt catalysts from zeolitic imidazole frameworks by spatial isolation and their use in zinc-air batteries. Angew. Chem. Int. Ed. 58(16), 5359–5364 (2019). https://doi.org/10.1002/anie.201901109

- L. Jiao, G. Wan, R. Zhang, H. Zhou, S.-H. Yu et al., From metal–organic frameworks to single-atom Fe implanted N-doped porous carbons: efficient oxygen reduction in both alkaline and acidic media. Angew. Chem. Int. Ed. 57(28), 8525–8529 (2018). https://doi.org/10.1002/anie.201803262

- Y. Yang, B. Li, Y. Liang, W. Ni, X. Li et al., Hetero-diatomic CoN4‐NiN4 site pairs with long-range coupling as efficient bifunctional catalyst for rechargeable Zn-air batteries. Adv. Sci. 11(22), 2310231 (2024). https://doi.org/10.1002/advs.202310231

- Q. Jing, Z. Mei, X. Sheng, X. Zou, Q. Xu et al., Tuning the bonding behavior of d-p orbitals to enhance oxygen reduction through push–pull electronic effects. Adv. Funct. Mater. 34(3), 2307002 (2024). https://doi.org/10.1002/adfm.202307002

- G. Wang, M. Zhang, G. Zhang, Z. Wang, X. Chen et al., Novel approach of diffusion-controlled sequential reduction to synthesize dual-atomic-site alloy for enhanced bifunctional electrocatalysis in acidic and alkaline media. Adv. Funct. Mater. 34(6), 2308876 (2024). https://doi.org/10.1002/adfm.202308876

- J. Qiao, Y. You, L. Kong, W. Feng, H. Zhang et al., Precisely constructing orbital-coupled Fe─Co dual-atom sites for high-energy-efficiency Zn–air/iodide hybrid batteries. Adv. Mater. 36(32), 2405533 (2024). https://doi.org/10.1002/adma.202405533

- H. Liu, L. Jiang, J. Khan, X. Wang, J. Xiao et al., Decorating single-atomic Mn sites with FeMn clusters to boost oxygen reduction reaction. Angew. Chem. Int. Ed. 62(3), e202214988 (2023). https://doi.org/10.1002/anie.202214988

- Z. Jiang, X. Liu, X.-Z. Liu, S. Huang, Y. Liu et al., Interfacial assembly of binary atomic metal-N(x) sites for high-performance energy devices. Nat. Commun. 14(1), 1822 (2023). https://doi.org/10.1038/s41467-023-37529-2

- T. Gu, D. Zhang, Y. Yang, C. Peng, D. Xue et al., Dual-sites coordination engineering of single atom catalysts for full-temperature adaptive flexible ultralong-life solid-state Zn−Air batteries. Adv. Funct. Mater. 33(8), 2212299 (2023). https://doi.org/10.1002/adfm.202212299

- S. Zhao, M. Liu, Z. Qu, Y. Yan, Z. Zhang et al., Cascade synthesis of Fe- N2-Fe dual-atom catalysts for superior oxygen catalysis. Angew. Chem. Int. Ed. 63(40), e202408914 (2024). https://doi.org/10.1002/anie.202408914

- X. Duan, S. Ren, N. Pan, M. Zhang, H. Zheng, MOF-derived Fe, Co@N–C bifunctional oxygen electrocatalysts for Zn–air batteries. J. Mater. Chem. A 8(18), 9355–9363 (2020). https://doi.org/10.1039/d0ta02825h

- W. Xie, Y. Song, S. Li, J. Li, Y. Yang et al., Single-atomic-co electrocatalysts with self-supported architecture toward oxygen-involved reaction. Adv. Funct. Mater. 29(50), 1906477 (2019). https://doi.org/10.1002/adfm.201906477

- S. Sarkar, A. Biswas, E.E. Siddharthan, R. Thapa, R.S. Dey, Strategic modulation of target-specific isolated Fe, Co single-atom active sites for oxygen electrocatalysis impacting high power Zn-air battery. ACS Nano 16(5), 7890–7903 (2022). https://doi.org/10.1021/acsnano.2c00547

- X. Zhou, J. Gao, Y. Hu, Z. Jin, K. Hu et al., Theoretically revealed and experimentally demonstrated synergistic electronic interaction of CoFe dual-metal sites on N-doped carbon for boosting both oxygen reduction and evolution reactions. Nano Lett. 22(8), 3392–3399 (2022). https://doi.org/10.1021/acs.nanolett.2c00658

- S. Li, C. Cheng, X. Zhao, J. Schmidt, A. Thomas, Active salt/silica-templated 2D mesoporous FeCo-nx-carbon as bifunctional oxygen electrodes for zinc–air batteries. Angew. Chem. Int. Ed. 57(7), 1856–1862 (2018). https://doi.org/10.1002/anie.201710852

- M. Xiao, J. Zhu, S. Li, G. Li, W. Liu et al., 3d-orbital occupancy regulated Ir-co atomic pair toward superior bifunctional oxygen electrocatalysis. ACS Catal. 11(14), 8837–8846 (2021). https://doi.org/10.1021/acscatal.1c02165

- Z. Wang, X. Jin, R. Xu, Z. Yang, S. Ma et al., Cooperation between dual metal atoms and nanoclusters enhances activity and stability for oxygen reduction and evolution. ACS Nano 17(9), 8622–8633 (2023). https://doi.org/10.1021/acsnano.3c01287