Supporting Information for

Polyphenol-Gated Composite Electrolytes with Enhanced Cross-Phase Lithium-Ion Transport for Solid-State Lithium Batteries

Xiaoxiao Li1, Minqiang Jiang1, Kai Chen1, Zhixiang Cai1, Yingxin Zhang1, Jiamei Luo1, Lei Hou2, Yazhou Zhou3, Chao Zhang1, Hui Zhang1*, Feili Lai4,5*, Yue-E Miao1*, Tianxi Liu1,6 and Klaus Müllen3,7

1State Key Laboratory of Advanced Fiber Materials, College of Materials Science and Engineering, Donghua University, 2999 North Renmin Road, Shanghai 201620, P. R. China

2State Key Laboratory of Advanced Fiber Materials, College of Chemistry and Chemical Engineering, Donghua University, 2999 North Renmin Road, Shanghai 201620, P. R. China

3Nanotechnology Centre, Centre for Energy and Environmental Technologies, VŠB–Technical University of Ostrava, 17. listopadu 2172/15, Ostrava-Poruba 70800, Czech Republic

4Department of Chemistry, KU Leuven, Celestijnenlaan 200F, Leuven 3001, Belgium

5State Key Laboratory of Metal Matrix Composites, School of Materials Science and Engineering, Shanghai Jiao Tong University, Shanghai 200240, P. R. China

6Key Laboratory of Synthetic and Biological Colloids, Ministry of Education, School of Chemical and Material Engineering, Jiangnan University, Wuxi, 214122, P. R. China

7Department of Molecular Spectroscopy, Max Planck Institute for Polymer Research, Ackermannweg 10, Mainz 55128, Germany

*Corresponding authors. E-mail: zhanghui@dhu.edu.cn (Hui Zhang); feililai@sjtu.edu.cn (Feili Lai); yuee_miao@dhu.edu.cn (Yue-E Miao)

S1 Supplementary Figures and Tables

Fig. S1 DFT-calculated binding energies between TFSI⁻ anion and the polar groups in a, b PDA, c PTA and d PGA, respectively

Fig. S2 a Optimized geometrical configurations and binding energies between Li+ and TFSI− calculated by DFT. b ESP map of the Li+-TFSI⁻ solvation structure

Fig. S3 Schematic illustration of the preparation process for the PDA@LLTO/GE electrolyte

Fig. S4 SEM images of a, b p-LLTO nanofibers, and c, d LLTO nanofibers. The inset in c shows a digital photograph of the LLTO membrane

Fig. S5 TEM image of LLTO nanofiber

Fig. S6 SEM images of PDAx@LLTO nanofibers with different DA concentrations of a, b 0.5 mg mL⁻1 and c, d 4 mg mL⁻1. The insets in a and c show the corresponding digital photographs

Fig. S7 TEM images of a PDA0.5@LLTO, and b PDA4@LLTO nanofibers

Fig. S8 XRD patterns of LLTO and PDAx@LLTO membranes

Fig. S9 High-resolution La 3d XPS spectra of LLTO and PDA2@LLTO membranes

Fig. S10 TGA curves of LLTO/GE and PDAx@LLTO/GE electrolytes

Fig. S11 DSC curves of LLTO/GE and PDAx@LLTO/GE electrolytes

Fig. S12 a Digital photographs of the PDA2@LLTO/GE electrolyte holding a 50 g weight while adhered to a Li metal foil. b The interfacial adhesion comparison between LLTO/GE and PDA2@LLTO/GE electrolytes

Fig. S13 SEM images of a, b PTA2@LLTO and c, d PGA2@LLTO nanofibers. The insets in a and c show the corresponding digital images

Fig. S14 EIS spectra of a, b LLTO/GE, and c-h PDAx@LLTO/GE electrolytes at different temperature ranging from –10 to 60 ℃

Fig. S15 a EIS spectra of PDAx@LLTO/GE electrolytes at room temperature. b The corresponding ionic conductivities of the electrolytes

Fig. S16 LSV curves of different electrolytes

Fig. S17 Chronoamperometry curves of cells at 60 ℃ using a LLTO/GE, and b-d PDAx@LLTO/GE electrolytes under a step voltage of 10 mV. Insets display the corresponding EIS plots before and after polarization

Fig. S18 EIS plots of different electrolytes at room temperature

Fig. S19 Chronoamperometry curves of cells at 60 ℃ using a PTA2@LLTO/GE, and b PGA2@LLTO/GE under a step voltage of 10 mV. Insets display the corresponding EIS plots before and after polarization

Fig. S20 a Solid-state 7Li NMR spectra of LLTO, GE, LLTO/GE and PDA2@LLTO/GE electrolytes. Partially enlarged diagrams from the solid-state 7Li NMR spectra of b LLTO/GE, and c PDA2@LLTO/GE electrolytes

Fig S21 Temperature-variable FTIR spectra of a PDA2@LLTO/GE, b PTA2@LLTO/GE and c PGA2@LLTO/GE recorded in the range of 1690 - 1590 cm−1 during heating from 30 to 100 °C

Fig. S22 2DCOS a, c synchronous and b, d asynchronous spectra of PTA2@LLTO/GE and PGA2@LLTO/GE electrolyte, respectively. Warm colors (red) represent positive intensities, while cold colors (blue) indicate negative intensities

Fig. S23 Schematic diagrams of the carbonyl-assisted Li+ transport modes at the polyphenol interfaces

Fig. S24 Galvanostatic curves of symmetric cells assembled with LLTO/GE and PDA2@LLTO/GE electrolytes at 0.1 mA cm⁻2 and 60 ℃, (a1–a3) show enlarged view of the voltage–time curves during the periods of 250-270, 850-870 and 1350-1370 h, respectively

Fig. S25 CCD tests of a LLTO/GE and b PDA2@LLTO/GE, respectively

Fig. S26 The enlarged views of the voltage-time curves of LLTO/GE and PDA2@LLTO/GE at different current density of a 0.05 mA cm⁻2 and b 0.1 mA cm⁻2, respectively

Fig. S27 XPS spectra of the lithium surface after 20 cycles with LLTO/GE and PDA2@LLTO/GE electrolytes: a S 2p, b Li 1s

Fig. S28 Depth-profiling XPS spectra of a C 1s, b F 1s and c O 1s at different etching depths for the SEI layer on Li anodes disassembled from Li || Li cell assembled with PDA2@LLTO/GE after 100 cycles at 0.2 mA cm⁻2

Fig. S29 EIS plots of Li | LLTO/GE | Li at different cycles

Fig. S30 Long-term cycling properties of LFP| PDA0.5@LLTO/GE |Li and LFP| PDA4@LLTO/GE |Li full batteries under 1 C at 60 ℃

Fig. S31 a Cycling performance of LFP| LLTO/GE |Li and LFP| PDA2@LLTO/GE |Li full batteries with a high LFP loading of 5 mg cm⁻2 under 1 C at 60 ℃. The corresponding charge-discharge curves of b LLTO/GE and c PDA2@LLTO/GE

Fig. S32 Charge/discharge profiles of the LFP| LLTO/GE |Li cell under the varying current density from 0.5 to 5 C at 60 ℃

Figure S33. Long-term cycling properties of full batteries of a LFP| LLTO/GE |Li and LFP| PDAx@LLTO/GE |Li and b LFP| PTA2@LT/GE |Li and LFP| PGA2@LLTO/GE |Li under 5 C at 60 ℃

Fig. S34 a Cycling performance of the high voltage NCM811 full batteries assembled with LLTO/GE and PDA2@LLTO/GE at 1 C at 60 ℃. The corresponding charge–discharge profiles for b LLTO/GE and c PDA2@LLTO/GE, respectively

Fig. S35 XPS spectra of the CEI layers in the NCM811| PDA2@LLTO/GE |Li and NCM811| LLTO/GE |Li cells: a, d C 1s, b, e F 1s, and c, f O 1s

Table S1 Signs of the main cross-peaks in 2DCOS synchronous and asynchronous spectra. Signs read in synchronous and asynchronous spectra (left: Syn; right: Asyn)

| PDA2@LLTO/GE |  |  |  |
| --- | --- | --- | --- |
| 1629 | +,+ | +,+ | C=O…Li+ |
| 1648 | +,+ | C=O…H-X |  |
| 1668 | C=O…C=O |  |  |
|  | 1668 | 1648 | 1629 |
| PGA2@LLTO/GE |  |  |  |
| 1627 | +,+ | +,+ | C=O…Li+ |
| 1647 | +,+ | C=O…H-X |  |
| 1664 | C=O…C=O |  |  |
|  | 1664 | 1647 | 1627 |
| PTA2@LLTO/GE |  |  |  |
| 1621 | +,+ | +,+ | C=O…Li+ |
| 1646 | +,+ | C=O…H-X |  |
| 1662 | C=O…C=O |  |  |
|  | 1662 | 1646 | 1621 |
| C=O…Li+ > C=O…H-X > C=O…C=O |  |  |  |

Based on Noda’s rule, the responsive order of different wavenumbers is determined to be: 1668 → 1648 → 1629 cm-1, 1664 → 1647 → 1627 cm-1, and 1662 → 1646 → 1621 cm-1 for D@LT/GE, G@LT/GE and T@LT/GE electrolytes, respectively.