Supporting Information for

Textile-Scale Liquid-Metal Fibers with Strain-Invariant Conductivity Enable Absorption-Enhanced EMI Shielding

Ruosong Li1, Ruyi Tao1, Youpeng Huangfu2, Zhongyi Bai3, Liping Wei*, 1, Yuan Yan*, 1, Rui Zhang4, Daidi Fan1, *, Biao Zhao4, 5, *

1 School of Chemical Engineering, Northwest University, Xi’an 710127, P. R. China

2 State Key Laboratory of Electrical Insulation and Power Equipment, School of Electrical Engineering, Xi’an Jiaotong University, Xi’an 710049, P. R. China

3 Henan Key Laboratory of Aeronautical Materials and Application Technology, School of Mechatronics Engineering, Collaborative Innovation Center of Processing and Detecting for Aerospace High Performance Materials, Zhengzhou University of Aeronautics, Zhengzhou 450046, P. R. China

4 Institute of Advanced Ceramics, Henan Academy of Sciences, Zhengzhou 450046, P. R. China

5 School of Microelectronics, Fudan University, Shanghai 200433, P. R. China

* Corresponding authors. E-mail:, weiliping@nwu.edu.cn (Liping Wei); y.yan@nwu.edu.cn (Yuan Yan); fandaidi@nwu.edu.cn (Daidi Fan); zhao_biao@fudan.edu.cn (Biao Zhao)

Note S1 Dispersion protocol for Fe particles in EGaIn

A certain amount of Fe powder (particle size: 500 nm) was weighed and added to EGaIn, followed by continuous mechanical stirring to obtain magnetic liquid metal (MLM). Subsequently, N,N-dimethylformamide (DMF) was added to the beaker containing the MLM, and the mixture was sonicated in an ice bath (~0 °C) at 600 W for 1 h to break the MLM into nanoparticles. No surfactant or surface modification was used. Then, thermoplastic polyurethane (TPU) particles were added together with the MLM nanoparticles, and the mixture was continuously mechanically stirred at 50 °C for 12 h to obtain a uniformly dispersed mixture.

Note S2 Relationships among Ga, In, and Fe oxides

In this coaxial wet-spinning configuration, EGaIn liquid metal droplets interspersed with minor Fe particles are dispersed within the core TPU/DMF flow. Upon extrusion, the nascent fiber encounters the external aqueous coagulation bath, facilitating inward diffusion of dissolved oxygen and water. Thermodynamically, Ga exhibits the highest oxygen affinity, as evidenced by the most negative standard ΔG° change per mole of O2 for the oxidation reaction (4/3 Ga + O2 → 2/3 Ga2O3, ΔG° ≈ -665 kJ mol-1 O2 at 298 K), surpassing that of In (-553 kJ mol-1 O2 for analogous In2O3 formation) and Fe (-495 to -508 kJ mol-1 O2 for Fe2O3 and Fe3O₄, respectively; FeOOH formation is less favorable at -488 kJ mol-1). Consequently, any exposed GaIn droplet rapidly nucleates a continuous, dense nanoscale Ga2O3 skin within milliseconds upon trace O2/H2O ingress. Kinetically and geometrically, this oxide preferentially manifests at the LM-bath interface, interconnecting to curtail local pO2 and H2O fluxes, thereby establishing effective passivation. Concurrently, Fe particles, predominantly enveloped by TPU, exhibit minimal exposure to the exterior; even localized contact yields suppressed oxidation (notably FeOOH formation, requiring elevated water activity and protracted diffusion), further inhibited by the preformed Ga2O3 barrier. Thus, Ga2O3 unequivocally dominates the surface oxide composition on fibers and droplets.

Note S3 Simulation of the electric potential before and after stretching

The conductivity and Poisson’s ratio of MLM-7/TPU are listed in Table S1 and Note S4. The Fe particles are modeled as rigid circles.

Table S1 The conductivity and Poisson’s ratio of MLM-7/TPU

| Materials | Conductivity (S/m) | Poisson’s ratio | Young’s modulus |
| --- | --- | --- | --- |
| TPU | 1.2×10-10 | 0.49 | 750 [kPa] |
| EGaIn | 3.4×106 | 0.49 | 0.624 [Pa] |
| Fe | 1.0×107 | 0.29 | 210 [GPa] |

The assumptions are as follows:

1) Fe particles were assumed as rigid circles. The Young’s modulus of Fe is much higher than that of TPU. During macroscopic stretching, the shape of the Fe particles remains unchanged.

2)	Constant volume of TPU during stretching. Rubber-like elastomers commonly have a Poisson’s ratio close to 0.5, meaning they are approximately incompressible.

Before Stretching

In the simulation, the AB side of the composite is grounded by applying a Dirichlet boundary condition. A constant current density of 125 A/m² is imposed on the CD side. Electrical insulation boundary conditions as (S1) are applied to the BC and AD sides, ensuring that no current passes through them. At the interfaces between different phases, contact impedance boundary conditions as (S2) are introduced to account for interfacial resistance.

|  |  | (S1) |
| --- | --- | --- |
|  |  | (S2) |

After Stretching

The volume of the Fe (liquid) and EGaIn droplets are kept constant during stretching. After stretching, the longitudinal elongation of both the TPU in the model is equal to their transversal compression ratio. The EGaIn droplets are transformed from circular to oval shapes. Because the Young’s modulus of the Fe particles is much higher than that of the TPU matrix, the Fe particles remain spherical before and after stretching. However, their centroid positions are displaced in accordance with the deformation of the TPU matrix.

Note S4 Poisson’s ratio calculations

The Poisson’s ratio of the MLM-7/TPU was experimentally determined to be v = 0.49 at room temperature: following ASTM D638/ISO 527 uniaxial tensile protocols, axial (ε∥) and transverse (ε⊥) strains were recorded within the 0−1% linear-elastic regime and linearly regressed to yield ν = 0.49.

COMSOL boundary conditions: Electrical insulation conditions are applied on the AC and BD boundaries of the MLM-7/TPU. In addition, the AB boundary is set to be the ground potential. Meanwhile, a current density of 125 A/m2 is imposed on the CD boundary. In specific, its direction towards to the left.

Mesh parameters: for the accurate computation, an extremely dense mesh is applied to all regions. Specially, the maximum element size is limited to 2.12 μm.

Note S5 Numerical Calculation of Electromagnetic Response

The EM parameters were measured using a vector network analyzer. These parameters were then integrated with the conductivity data to calculate the electric and magnetic field distributions. The electromagnetic (EM) responses are numerically calculated using the commercial software Computer Simulation Technology Microwave Studio (CST MWS). Firstly, the basic physical quantities of the electric field and magnetic field are investigated through frequency-domain finite element simulation. In this study, a brick structure of the self-defined Fe-doped EGaIn is constructed with dimensions (lx = 5) mm along the x-axis, (ly = 5) mm along the y-axis, and thickness (td = 3) mm along the z-axis. The material parameters obtained from experiments are incorporated into CST MWS. The dispersive behavior of the material is modeled in CST MWS by specifying frequency-dependent permittivity and permeability, which are derived from experimental data characterizing the material’s dispersion properties. A linearly polarized plane wave is applied as the excitation source in the frequency range of 8.2−12.4 GHz. The plane wave propagates along the negative z-direction, with the electric field vector oriented along the positive x-direction. The background material is defined as vacuum, and the boundary conditions for (xmin), (xmax), (ymin), and (ymax) are set to Unit Cell. Essentially, the Unit Cell boundary condition virtually replicates the modeled structure periodically in the x-y plane up to infinity, enabling simulation of the material's periodic nature. In contrast, the Open (add space) boundary condition is applied to the (zmin) and (zmax) directions to simulate wave absorption and minimize reflections, mimicking an infinite or open environment.

The assumptions for this simulation are as follows:

1) Periodic structure in x-y (Unit Cell). In practical EM shielding assessments, the test specimen is typically regarded as having sufficient lateral dimensions to negate edge effects. To emulate this condition, “Unit Cell” boundary conditions were applied. This configuration mathematically replicates the constructed 5×5 mm Fe-EGaIn/TPU micro-model infinitely across the x-y plane, thereby enabling the simulation of the material’s macroscopic periodic EM response through the analysis of a single representative volume element.

2) Plane wave along -z with E-field along +x. The incident wave is a plane wave propagating along the -z direction, and the electric field direction is along the +x axis. This is a standard test scenario to simulate the normal incidence of EM waves onto the surface of a shielding material.

3) Open boundaries in z for wave absorption. Since the wave propagates along the z-axis, we need to ensure that after the wave passes through the material or is reflected by the material, it does not encounter the “walls” of the simulation box and be reflected back again, interfering with the calculation results.

Note S6 DFT calculation method

In this work, first principles calculations were performed using the Cambridge Sequential Total Energy Package (CASTEP) in Materials Studio. The exchange-correlation potential was described by the Perdew-Burke-Ernzerhof (PBE) functional within the generalized gradient approximation (GGA), and spin polarization effects were considered throughout. The plane-wave basis set cutoff energy was set to 550 eV, and the Brillouin zone integration was performed using 3×3×1 gamma k-point sample. In the structure optimization stage, a maximum Hellmann-Feynman force of 0.03 eV/Å was used as the convergence criterion, and both the lattice constants and atomic positions were fully relaxed simultaneously. The self-consistent field iteration was converged when the total energy change was less than 10-6 eV. Given that the Fe element has a localized magnetic moment, its initial magnetic moment was set to 4 μB, and a collinear spin polarization scheme was adopted to ensure an accurate description of the magnetic ground state.

Supplementary Figures and Tables

Fig. S1 SEM image of the Fe-EGaIn core

Fig. S2 SEM images and element mapping of interface between the MLM core and TPU sheath

Fig. S3 Gibbs free energy of surface oxides on MLM droplets

Fig. S4 FTIR spectra of TPU and MLM/TPU

Characteristic polyurethane bands that are shifted relative to pure TPU due to the weakening effect of H-bonding on carbonyl vibration, while other bands remain largely unaffected. Specifically, the N−H stretching vibration (hydrogen-bonded urethane N−H) in neat TPU appears around 3325 cm-1, whereas in the MLM/TPU fiber this band shifts to 3280 cm-1. Similarly, the carbonyl (C=O) stretching band of TPU (around 1728 cm-1 in free TPU) is observed at a lower wavenumber (1663 cm-1) in the composite. Such pronounced red-shifts of the N−H and C=O bands indicate strengthened intermolecular interactions in the composite. Additionally, the spectrum of MLM exhibits a broader absorption in the 3500-3200 cm-1 region, likely due to the overlapping O−H stretching from the oxide layers, further confirming the presence of hydroxyl groups involved in hydrogen bonding. In contrast, the aliphatic C−H stretching vibrations (asymmetric at 2950 cm-1 and symmetric at 2850 cm-1) remain essentially unchanged, indicating that the interactions are selective to the polar urethane groups. In this case, the shifts are attributed to hydrogen bond formation between the TPU chains and the hydroxyl-terminated oxide layers present on the LM/Fe particles. The −OH groups on these oxide surfaces can donate or accept hydrogen bonds with the N−H and C=O groups of TPU, effectively “gluing” the metal droplets to the polymer matrix at a molecular level. These hydrogen bonds improve the interface stability, which is crucial for maintaining good electrical contact under mechanical stress. In fact, the strong interfacial bonding helps preserve the conductive network during fiber stretching, thereby contributing to the observed stability of electrical performance (resistance-strain insensitivity) in the MLM/TPU fibers.

Fig. S5 XPS Full survey of MLM/TPU

The O 1s spectrum displays deconvoluted peaks attributable to metal oxides (529.5−530.5 eV), hydroxide (O−H) groups (531.5 eV), and C−O bonds (532.5 eV, likely from the TPU matrix), with the prominence of the O−H signal supporting the presence of surface −OH groups on Ga2O3/FeOOH, i.e., a hydroxylated surface on the LM and Fe particles. The In 3d spectrum indicates a mix of oxidation states, with contributions from metallic In0 (443.5 eV), intermediate In+ (444.5 eV), and oxidized In3+ (445 eV), suggesting partial oxidation of In despite its relative stability compared to Ga (consistent with XRD showing metallic In phases). The Ga 3d spectrum (Fig. S5c) shows peaks corresponding to elemental Ga0 (18 eV), Ga+ (19 eV), oxidized Ga3+ (20.5 eV), and an overlapping In 4d signal from metallic In (17 eV). Notably, the Ga peaks are slightly shifted to lower binding energies compared to typical references (e.g., metallic Ga 18.5 eV, Ga2O3 20.4 eV). This shift can be attributed to the formation of hydrogen bonds involving GaOOH, where interactions between Ga−O−H groups and TPU functional groups increase electron density around Ga, reducing the binding energy by weakening the core electron-nucleus attraction. For iron, the Fe 2p spectrum (Fig. S5d) reveals a mixed oxidation state with signals for Fe0 (707 eV), Fe2+ (709.5 eV), Fe3+ (711 eV), and satellites (715−719 eV), confirming partial oxidation of introduced Fe0 during fiber fabrication (ultrasonic dispersion and coagulation), aligning with XRD evidence of FeOOH formation. These XPS results substantiate the partial oxidation and hydroxylation of the LM (EGaIn) and Fe components in the composite.

Fig. S6 High-resolution XPS spectra of Fe-doped EGaIn/TPU fibers: a O 1s, b In 3d, c Ga 3d, and d Fe 2p, confirming multiple oxidation states and metallic phases

Fig. S7 Magnetization curves of MLM/TPU fibers (MLM-3, MLM-5, MLM-7, and MLM-9) showing the variation of magnetization with magnetic field strength

VSM measurements on MLM/TPU with varying Fe contents reveal narrow S-shaped hysteresis loops with negligible coercivity (20−50 Oe) and remanence, indicative of soft ferromagnetic behavior. Uniform Fe dispersion within the LM core facilitates efficient magnetic domain alignment under external fields. The magnetization curves demonstrate that the saturation moment increases progressively with higher Fe doping levels in the MLM/TPU fibers, reflecting enhanced magnetic response at greater loadings. The MLM-7/TPU fiber optimally balances a high saturation magnetization (Ms 12 emu/g, corresponding to 0.12 emu in the measured sample) with minimal conductivity loss compared to higher loadings, yielding superior electro-magnetic performance. The soft magnetic behavior, as indicated by the narrow hysteresis loops, low coercivity, and steep rise near zero field in the curves, enables facile magnetization/demagnetization for rapid, reversible field responses. This supports applications such as remote actuation, magnetic switches, and motion/strain sensors in flexible devices.

Fig. S8 TGA curves of MLM-7 and TPU

Fig. S9 SEM images and element mapping of MLM/TPU after freeze-pressure process

Fig. S10 Resistance-strain curves under uniaxial tension

Fig. S11 Stress-strain curves of MLM/TPU fibers

Fig. S12 a Elongation at break, b tensile strength, c Young’s modulus, and d toughness for MLM-3/TPU, MLM-5/TPU, MLM-7/TPU, and MLM-9/TPU

Fig. S13 a Temperature−time profile under stepwise DC voltage application. b Cycling stability of Joule heating under repeated voltage switching between 0 and 0.8 V of Fe-free LM/TPU

Fig. S14 Frequency dependence of the SEA, SER, and SET for a MLM-3/TPU, b MLM-5/TPU, c MLM-7/TPU, and d MLM-9/TPU composites in the X-band (8.2−12.4 GHz)

Fig. S15 SEA/SET of MLM/TPU

Fig. S16 Frequency dependence of the T, R, and A for a MLM-3/TPU, b MLM-5/TPU, c MLM-7/TPU, and d MLM-9/TPU composites in the X-band (8.2−12.4 GHz)

Fig. S17 Impedance (z = Zin/Z0) of MLM/TPU textiles, where Z0 = 30 Ω

Fig. S18 Frequency dependence of the a, c shielding effectiveness and b, d power coefficient for a−b pure TPU and c−d TPU/LM composites

Fig. S19 E-field distribution of MLM/TPU: a MLM-3/TPU, b MLM-5/TPU, c MLM-7/TPU, d MLM-9/TPU

Fig. S20 Frequency dependence of a SE and b power coefficient curves of commercial silver-plated conductive fabric

Fig. S21 Frequency dependence of a, c SE and b, d power coefficients of MLM-7/TPU after a−b 100 loading−unloading cycles at 100% tensile strain and c−d subsequent storage at -20 °C for 24 h

Fig. S22 Images showing the deformation of MLM/TPU textiles when stretched from different directions

Table S2 Summary of electrical properties for representative LM composites/textiles: conductivity and ΔR/R0 at the stated tensile strain

| Materials | Conductivity (S m-1) | ΔR/R0 | Refs. |
| --- | --- | --- | --- |
| Fe3O4/EGaIn/PVA | 95 ± 3 kΩ | / | [S1] |
| Ni/EGaIn/Ecoflex | 2.55×105 | 56% at 250% | [S2] |
| PVA/EGaInSn/Ni | 0.015−0.041 | 25%−45% at 5%−50% | [S3] |
| Fe/EGaIn/PDMS | ~3.04×105 | 99.9% at 25% | [S4] |
| Ni/EGaIn/PDMS | ~1.43×105 | 99.9% at 10% | [S4] |
| Liquid-elastomer | 1.37×103 | <10% at 50% | [S5] |
| Fe-EGaIn/gelatin-alginate | 2×105 | 55% at 100% | [S6] |
| PDMS-EGaIn | 14605.4 | 32.2% at 50% | [S7] |
| TPU/Fe-EGaIn | 1.9×103−4.7×104 | ∆SET/SET0 = 2.59% | [S8] |
| EGaIn/MWCNTs/PDMS | 1.315×10-2 | 110% at 120% | [S9] |
| Aramid nanofiber/EGaIn/Gd2O3 | 1.075×105 | 2% at 120% | [S10] |
| F@Ag-EGaIn | 2145 | 137% at 120% | [S11] |
| Galinstan/PDMS | 1.34×103 | 4.305% at 117% | [S12] |
| Fe3O4-EGaIn/PDMS | 25 | 88.9% at 20% | [S13] |
| MLM/TPU | 2.1×104 | 6% at 100% | This study |

| Table S3. Performance of some recent studies using LMs as heaters Liquid metal; Maximum heating temperature; Heating time; Cooling time; Stability; Refs.. EGaIn; 71.9 ℃ (1.2 V); 6.5s; 6.5s; NA; [S14]. EGaIn; 80 ℃ (5 V); <1 min; <1 min; NA; [S15]. EGaIn; 50 ℃ (1.5 V); <3 min; <3 min; NA; [S16]. Galinstan; 110.6 ℃ (4 V); NA; NA; Maintain 83 ℃ for 4000 s at 3 V; [S17]. EGaIn; 110 °C (5 V); NA; NA; Stable 200 heating and cooling cycles (4.5 V, heating for 30 s, cooling for 30 s); [S18]. Galinstan; 65.2 ℃ (0.6 V); NA; NA; Maintain 44 ℃ 3000 s at 0.4 V; [S19]. EGaIn; 120 ℃ (0.8 V); 18s; 18s; Stable heating and cooling cycle for 200 times; [S20]. EGaIn; 200 ℃ (0.8 V); 10s; 10s; Stable heating and cooling cycle for; [S21]. EGaIn; 70 ℃ (1 A); NA; NA; NA; [S22]. Gallium; 101.1 ℃ (6 V); 10s; 10s; NA; [S23]. Galinstan; 150 ℃ (3 V); NA; NA; ΔT = 0 (0% to 60% strain); [S24]. EGaIn; 65 ℃ (0.6 V); 60s; 60s; Stable heating and cooling cycle for 20 times at 0.4 V; [S25]. EGaIn; 200 ℃ (3.5 V); 60s; 60s; Stable heating and cooling cycle for 20 times at 2.5 V; [S26]. EGaIn; 80 ℃ (0.6 V); NA; NA; Stable heating and cooling cycle for 30 times at 0.4 V; [S27]. EGaIn; 179 ℃ (1.75 V); <10 s; <10 s; NA; [S28]. Galinstan; 102 ℃ (2 V); NA; NA; Stable heating and cooling cycle for 50 times at 2 V; [S29]. EGaIn; 110 ℃ (4 V); NA; NA; Maintain 110 ℃ for 7800 s at 4 V; [S30]. Fe-EGaIn; 75.8 ℃ (1.2 V); 10 s; 10 s; Stable heating and cooling cycle for 12 times at 0.8 V; This study. Table S4 Representative studies on EGaIn-based systems highlighting their EMI SET, mechanical properties, electrical conductivity, and stability. |
| --- |
| EGaIn system | Thickness | SE values (dB) |  | R value | Mechanical properties | Conductivity (S·m-1) | ΔR/R0 | Refs. |
|  |  | SET | SER |  |  |  |  |  |
| EGaIn/TPU fibers | / | 30.0 | 4.8 | 0.669 | tensile strength =1.91 MPa elastic modulus = 2.74 MPa elongation at break = 516% toughness = 6.83 MJ·m-3 | 4.12×104. | 0.0078 at 50% strain | [S31] |
| EGaIn-MXene/EG/PAA | 1.5 mm | 52 | 5 | 0.684 | tensile strength = 7.7 MPa tensile strain = 0.25% | 4.0 × 102 | / | [S32] |
| TPU/EGaIn foam | 1.2 mm | 49.5 | / | 0.88 | tensile strength = 2.5−18.9 MPa elongation-at-break = 313−741 % | 2.6 × 103 | 0.15 at 200% strain | [S33] |
| PAA-NHS/Ag NPs/SEBS | 650 µm | 53.2 | 8.7 | 0.865 | robust adhesion = 2.1 J cm-2 | 3.4 × 104 | / | [S34] |
| PVA/EGaInSn-Ni Hydrogels | 3.0 mm | 65.8 | 3.3 | 0.532 | stretchability >800% | 0.041 |  | [S3] |
| PDMS/EGaIn | 0.4 mm | 35.4 | / | 0.90 | elongation at break >150% | 3.1 × 104 | <0.09 at 0−60% strain | [S24] |
| EGaIn/t-PDMS | 10 mm | 50 | 5 | 0.684 | elongation at break: 110−130% | 4 × 104 | / | [S35] |
| Phosphorylated cellulose nanofibrils/EGaIn | 70 μm | 29.8 | 10 | 0.900 | strength at break = 16.1 MPa strain at break = 5.2% | 1.27 × 104 | / | [S36] |
| PDMS-EGaIn/textiles | 0.35 mm | 72.6 | 10.6 | 0.913 | tensile strength = 10.6 MPa elongation at break > 230% | 14 605.4 | 0.323 at 50% strain | [S7] |
| EGaIn/PDMS foam | 10.2 mm | 45.2 | 7.2 | 0.809 | compression modulus = 50−360 kPa (0−60%) | 800. | / | [S37] |
| Silver-plated conductive fabric | 2.2 mm | 62.0 | 14.4 | 0.96 | elongation at break = 60% | 6.2 × 104 | / |  |
| Fe-EGaIn/TPU | 2.5 mm | 33.82 | 2.84 | 0.480 | elongation at break = 444 % toughness = 4.27 MJ·m-3 | 2.1 × 104 | 0.16 at 200% strain | This study |

Supplementaty References

- S. Merhebi, M. Mayyas, R. Abbasi, M.J. Christoe, J. Han et al., Magnetic and conductive liquid metal gels. ACS Appl. Mater. Interfaces 12(17), 20119-20128 (2020). https://doi.org/10.1021/acsami.0c03166

- T.T. Hoang, P.T. Phan, M.T. Thai, J. Davies, C.C. Nguyen et al., Magnetically engineered conductivity of soft liquid metal composites for robotic, wearable electronic, and medical applications. Adv. Intell. Syst. 4(12), 2200282 (2022). https://doi.org/10.1002/aisy.202200282

- B. Zhao, Z. Bai, H. Lv, Z. Yan, Y. Du et al., Self-healing liquid metal magnetic hydrogels for smart feedback sensors and high-performance electromagnetic shielding. Nano-Micro Lett. 15, 79 (2023). https://doi.org/10.1007/s40820-023-01043-3

- G. Yun, S. Tang, S. Sun, D. Yuan, Q. Zhao et al., Liquid metal-filled magnetorheological elastomer with positive piezoconductivity. Nat. Commun. 10(1), 1300 (2019). https://doi.org/10.1038/s41467-019-09325-4

- E.J. Markvicka, M.D. Bartlett, X. Huang, C. Majidi, An autonomously electrically self-healing liquid metal–elastomer composite for robust soft-matter robotics and electronics. Nat. Mater. 17, 618-624 (2018). https://doi.org/10.1038/s41563-018-0084-7

- X.P. Hao, C.W. Zhang, X.N. Zhang, L.X. Hou, J. Hu et al., Healable, recyclable, and multifunctional soft electronics based on biopolymer hydrogel and patterned liquid metal. Small 18(23), 2201643 (2022). https://doi.org/10.1002/smll.202201643

- L. Jia, X. Jia, W. Sun, Y. Zhang, L. Xu et al., Stretchable liquid metal-based conductive textile for electromagnetic interference shielding. ACS Appl. Mater. Interfaces 12(47), 53230-53238 (2020). https://doi.org/10.1021/acsami.0c14397

- Q. Zhang, Y. Wu, X. Bao, S. Li, X. Zhuang et al., High-performance, strain-stable electromagnetic shielding materials enabled by magnetic elastic fiber networks pinning liquid metal. Adv. Sci. 12(38), e10078 (2025). https://doi.org/10.1002/advs.202510078

- Y. Guan, Y. Liu, Q. Li, Y. Shi, H. Li et al., A novel composite material for flexible wearable devices based on eutectic gallium indium (EGaIn), multi-walled carbon nanotubes (MWCNTs) and polydimethylsiloxane (PDMS). Compos. Struct. 291 115653 (2022). https://doi.org/10.1016/j.compstruct.2022.115653

- X. Zhu, H. Wang, Y. He, X. Feng, Y. Zhao, L. Chen, Aramid nanofiber/liquid metal/Gd2O3 flexible films with magnetic-conductive interfaces for electromagnetic interference shielding and Joule heating. Compos. Commun., 57 102430 (2025). https://doi.org/10.1016/j.coco.2025.102430

- X. Sun, J. Fu, C. Teng, M. Zhang, T. Liu et al., Superhydrophobic E-textile with an Ag-EGaIn conductive layer for motion detection and electromagnetic interference shielding. ACS Appl. Mater. Interfaces 14(29) 33650-33661 (2022). https://doi.org/10.1021/acsami.2c09554

- Z. Yu, J. Shang, X. Niu, Y. Liu, G. Liu et al., A composite elastic conductor with high dynamic stability based on 3D‐Calabash Bunch conductive network structure for wearable devices. Adv. Electron. Mater. 4(9), 1800137 (2018). https://doi.org/10.1002/aelm.201800137

- J. Li, Y. Zhang, X. Li, C. Chen, H. Zou et al., Oriented magnetic liquid metal-filled interlocked bilayer films as multifunctional smart electromagnetic devices. Nano Res. 16, 1764-1772 (2022). https://doi.org/10.1007/s12274-022-4843-z

- L. Zheng, M. Zhu, B. Wu, Z. Li, S. Sun, P. Wu, Conductance-stable liquid metal sheath-core microfibers for stretchy smart fabrics and self-powered sensing. Sci. Adv. 7 eabg4041 (2021). https://doi.org/10.1126/sciadv.abg4041

- D. Wu, S. Wu, P. Narongdej, S. Duan, C. Chen et al., Fast and facile liquid metal printing via projection lithography for highly stretchable electronic circuits. Adv. Mater. 36 e2307632 (2024). https://doi.org/10.1002/adma.202307632

- X. Sun, J. An, Y. Sun, X. Guo, J. Wu et al., Liquid–metal microgrid stretchable electronics based on bionic leaf veins with ultra-stretchability and high conductivity. Rare Met. 43(6), 2747-2757 (2024). https://doi.org/10.1007/s12598-024-02636-6

- P. Yi, H. Zou, Y. Yu, X. Li, Z. Li et al., MXene-reinforced liquid metal/polymer fibers via interface engineering for wearable multifunctional textiles. ACS Nano 16, 14490-14502 (2022). https://doi.org/10.1021/acsnano.2c04863

- D. Shukla, H. Wang, O. Awartani, M.D. Dickey, Y. Zhu, Surface embedded metal nanowire-liquid metal-elastomer hybrid composites for stretchable electronics. ACS Appl. Mater. Interfaces 16(11), 14183-14197 (2024). https://doi.org/10.1021/acsami.4c00318

- L. Qiu, J. Li, Q. Yu, W. Han, L. Zhao et al., Liquid metal based conductive textile via reactive wetting for stretchable electromagnetic shielding and electro-thermal conversion applications. Chem. Eng. J. 481 148504 (2024). https://doi.org/10.1016/j.cej.2023.148504

- X. Qi, L. Yu, Y. Liu, L. Chen, X. Li, Liquid metal powders wrapped with robust shell by bimetallic ions chelation strategy for energy harvesting and flexible electronics. Adv. Funct. Mater. 34(13), 2313960 (2024). https://doi.org/10.1002/adfm.202313960

- J. Dong, Y. Peng, X. Nie, Le Li, C. Zhang et al., Hierarchically designed super‐elastic metafabric for thermal‐wet comfortable and antibacterial epidermal electrode. Adv. Funct. Mater. 32(48), 2209762 (2022). https://doi.org/10.1002/adfm.202209762

- Y. Chen, D. Estevez, Z. Zhu, Y. Wang, Y. Mai, F. Qin, Multifunctional conductive hydrogel composites with nickel nanowires and liquid metal conductive highways. ACS Appl. Mater. Interfaces 16, 29267-29281 (2024). https://doi.org/10.1021/acsami.4c05344

- M. Shen, X. Xu, J. Qi, X. Li, B. Xue et al., PMDI cross-linked rare earth/liquid metal reinforced ANF/MXene membranes for multifunctional electromagnetic interference shielding. Compos. Part A Appl. Sci. Manuf. 182 (2024). https://doi.org/10.1016/j.compositesa.2024.108178

- Z. Xu, J. Chen, G. Wang, Y. Zhao, B. Shen, W. Zheng, Stretchable and translucent liquid-metal composite mesh for multifunctional electromagnetic shielding/sensing and joule heating. Compos. Sci. Technol. 249, 110512 (2024). https://doi.org/10.1016/j.compscitech.2024.110512

- S. Li, H. Zhao, H. Xu, H. Lu, P. Luo, T. Zhou, Ultra-flexible stretchable liquid metal circuits with antimicrobial properties through selective laser activation for health monitoring. Chem. Eng. J. 482, 149173 (2024). https://doi.org/10.1016/j.cej.2024.149173

- J. Xie, G. Zhou, Y. Sun, F. Zhang, F. Kang et al., Multifunctional liquid metal-bridged graphite nanoplatelets/aramid nanofiber film for thermal management. Small 20(18), e2305163 (2024). https://doi.org/10.1002/smll.202305163

- J. Dong, Y. Peng, J. Long, Y. Zhang, Z. Wang et al., An all‐stretchable, ultraviolet protective, and electromagnetic‐interference‐free E‐textile. Adv. Funct. Mater. 33(45), 2308426 (2023). https://doi.org/10.1002/adfm.202308426

- Y. Sun, X. Han, P. Guo, Z. Chai, J. Yue et al., Slippery graphene-bridging liquid metal layered heterostructure nanocomposite for stable high-performance electromagnetic interference shielding. ACS Nano 17(13), 12616-12628 (2023). https://doi.org/10.1021/acsnano.3c02975

- Y. Ding, M. Zeng, L. Fu, Surface chemistry of gallium-based liquid metals. Matter 3, 1477-1506 (2020). https://doi.org/10.1016/j.matt.2020.08.012

- Y. Ge, L. Wang, B. Hu, H. Lu, Y. Shao, Bacterial cellulose-based composite films with liquid metal/graphene synergistic conductive pathways for superior electromagnetic interference shielding and joule heating performance. Compos. Sci. Technol. 251, 110582 (2024). https://doi.org/10.1016/j.compscitech.2024.110582

- Q. Li, L. Liu, M. Lin, X. Guo, L. Guan et al., Highly conductive sheath–core structured liquid metal fibers with invariant resistance under high tensile strength. Appl. Mater. Today 42, 102620 (2025). https://doi.org/10.1016/j.apmt.2025.102620

- J. Cho, J. Kim, Highly thermally conductive and EMI shielding composite fabricated via free‐radical polymerization of poly acrylic acid assisted by expanded graphite with liquid metal‐grafted MXene. Polym. Compos. 45(9), 7709-7718 (2024). https://doi.org/10.1002/pc.28298

- X. Zhang, J. Chen, X. Chen, J. Yao, W. Zheng, B. Shen, Recyclable and leakage-suppressed microcellular liquid–metal composite foams for stretchable electromagnetic shielding. Chem. Eng. J. 493, 152478 (2024). https://doi.org/10.1016/j.cej.2024.152478

- Y. Peng, J. Song, Y. Zhang, H. Liu, J. Dong et al., Permeable, wet‐adhesive, and EMI‐resistant liquid metal electronic skin for high‐fidelity electrophysiological monitoring in sweaty and electromagnetic environments. Adv. Mater., 37(42), e08041 (2025). https://doi.org/10.1002/adma.202508041

- Z. Wang, J. Ren, R. Liu, X. Sun, D. Huang et al., Three dimensional core-shell structured liquid metal/elastomer composite via coaxial direct ink writing for electromagnetic interference shielding. Compos. Part A Appl. Sci. Manuf. 136, 105957 (2020). https://doi.org/10.1016/j.compositesa.2020.105957

- N. Ren, Y. Ai, N. Yue, M. Cui, R. Huang et al., Shear-induced fabrication of cellulose nanofibril/liquid metal nanocomposite films for flexible electromagnetic interference shielding and thermal management. ACS Appl. Mater. Interfaces 16(14), 17904-17917 (2024). https://doi.org/10.1021/acsami.4c01220

- B. Yao, X. Xu, H. Li, Z. Han, J. Hao et al., Soft liquid-metal/elastomer foam with compression-adjustable thermal conductivity and electromagnetic interference shielding. Chem. Eng. J. 410, 128288 (2021). https://doi.org/10.1016/j.cej.2020.128288