Supporting Information for

A Flame-Retardant Hydrogen-Bonded Organic Framework Separator for Selective Sodium-Ion Transport toward a NaF-Rich Interphase in Sodium Metal Batteries

Muhammad Ali1,2, Moazzam Ali1,3, Hamid Hussain1,2, Samia Aman1,2, Ufra Naseer4, Asif Mahmood5, Muhammad Tayyab Ahsan6, Yinzhu Jiang1,2,*, Muhammad Yousaf 1,2,*

1 School of Materials Science and Engineering, Zhejiang University, Hangzhou 310027, P. R. China

2Future Science Research Institute, ZJU Hangzhou Global Scientific and Technological Innovation Centre; Zhejiang University, Hangzhou 311215, P. R. China

3 Department of Chemistry, Zhejiang University, Hangzhou, 310027, P. R. China

4College of Optical Science and Engineering, Zhejiang University (ZJU), Hangzhou, 310058, P. R. China

5Centre for Clean Energy Technology, School of Mathematical and Physical Sciences, Faculty of Science, University of Technology Sydney, City Campus, Broadway, NSW 2007, Australia

6Institute for Sustainable Transformation, School of Chemical Engineering and Light Industry, Guangdong University of Technology, Guangzhou 510006, P. R. China

# *Corresponding authors. E-mail: muhammadyousaf@zju.edu.cn (Muhammad Yousaf ); yzjiang@zju.edu.cn (Yinzhu Jiang)

# S1 Finite Element Analysis (FEA)

The simulation used the physical field interface of the thrice current distribution in the electrochemical module of COMSOL Multiphysics software to simulate the deposition of Na+ considering various separator. The deposition on the substrate surface mainly includes two main processes:

Mass transport described by the Nernst-Planck equation

(S1)

Charge transfer described by Butler–Volmer equation

(S2)

We performed a 60 s transient simulation of the deposition system with or without HOF separator. The diffusion of ion concentration follows the Nernst-Planck equation, and the reaction on the electrode surface follows the Butler-Volmer equation. To reduce the computational complexity, the actual system is simplified, as shown in ( Fig. S15). A model domain with a length of 10 μm and 10 μm is constructed, and a thin film domain with a thickness of 1 μm is constructed at the bottom, and the substrate is Na surface. The top anode region and the boundary on both sides are defined as the un-deformed boundary, and the bottom cathode boundary is set as the deformed electrode surface.The model parameter settings and boundary conditions are shown in Table S1.

# S2 Molecular Dynamics (MD)

Molecular dynamics (MD) simulations were employed to investigate the influence of HOF membrane on Na⁺ ion transport. All simulations were performed using the LAMMPS software package [S1] with a time step of 1 fs. The experimental group was configured in a cubic simulation box with dimensions of 4.6 × 4.6 × 4.6 nm3. It contained 50 HOF molecules, 50 molecules each of EC, DEC, and FEC, along with 50 Na+ and 50 PF6- ions, for a total of 9,050 atoms. For the control system, a cubic simulation box of 4.7 × 4.7 × 4.7 nm3 was used, containing 228 molecules each of EC, DEC, and FEC, plus 50 Na⁺ and 50 PF6- ions, totaling 9,064 atoms. Periodic boundary conditions were applied in all three dimensions (x, y, z) for both systems.

The OPLS-AA force field [S2] was used to model the ions and molecules. Intermolecular interactions were described by the Lennard-Jones (LJ) and Coulomb potentials, with a cutoff radius of 1.2 nm for the LJ potential. Long-range Coulombic forces were calculated using the Particle-Particle Particle-Mesh (PPPM) method.

Initially, the systems underwent a 1 ns equilibration run in the NVT ensemble at 333.15K K, regulated by a Nosé–Hoover thermostat. Following equilibration, a 10 ns production run was conducted under the same NVT conditions to calculate the Radial Distribution Functions (RDFs). Subsequently, electric fields of varying strengths were applied along the z-direction, and separate 10 ns production runs were performed for each field strength to determine the drift velocity of the Na⁺ ions.

# S3 Density functional theory (DFT)

In Density Functional Theory(DFT) calculations, structural optimizations were performed by Vienna Ab-initio Simulation Package(VASP) [S3] with the projector augmented wave (PAW) method [S4]. The exchange-functional was treated using the Perdew-Burke-Ernzerhof (PBE) [S5] functional, in combination with the DFT-D3 correction [S6]. The cut-off energy of the plane-wave basis was set at 450 eV in structural optimizations. For optimization of lattice size of bulk structure of HOF, the Brillouin Zone integration was performed with a Gamma [S7] k-point mesh of 4×2×10. For optimization of geometry of electrolyte, the Brillouin Zone integration was performed with a k-point mesh of 1×1×1.  Since VASP utilizes periodic boundary conditions (PBC) by default, the non-periodic nature of the CEL system was simulated using the fixed cell approach. To minimize spurious interactions between periodic images, the system was placed within a sufficiently large cubic vacuum box. We conducted rigorous convergence tests on the total energy relative to the cell size, evaluating box dimensions of 15, 20, 30, and 35 Å. Our results indicated that the total energy was well-converged and remarkably insensitive to the box volume beyond 15 Å, as shown in Fig Sxxx. Consequently, a cubic box with a side length of 15 Å was selected for all subsequent calculations to balance computational efficiency with physical accuracy. To accurately capture long-range dispersion interactions, which are critical for the geometry of complex molecular systems, the Grimme’s DFT-D3 semi-empirical correction was applied [S8].

The self-consistent calculations applied a convergence energy threshold of 10-5 eV. The equilibrium geometries and lattice constants were optimized with maximum stress on each atom within 0.02 eV Å-1. Use method climbing image nudged elastic band [S9] to search for the transition state to describe the migration path of sodium ions.

# S4 Ionic conductivity

Ionic conductivity was determined using electrochemical impedance spectroscopy (EIS) on a CHI760E electrochemical workstation, recorded over a frequency range of 105 Hz to 1 mHz with an AC amplitude of 5 mV. For measurements, 60 μL of electrolyte was applied to the separator, which was then sandwiched between stainless steel (SS) blocking electrodes in a CR2025-type coin cell. Ionic conductivity (σ, S cm-1) was calculated using Equation (S3):

σ=LRA				(S3)

where R is the bulk resistance obtained from the high-frequency intercept of the Nyquist plot (Ω), L is the separator thickness (cm), and A is the electrode area (cm2).

# S5 Porosity

The porosity of the separators was determined by liquid uptake using n-butanol as the wetting solvent. The porosity (%) was calculated according to Equation (S4):

Porosity %= W2-W1V × ρ×100%		(S4)

where W1 is the weight of the dry separator, W2 is the weight after immersion in n-butanol for 3 h, with surface solvent removed using filter paper, V is the geometric volume of the separator, and ρ is the density of n-butanol.

# S6 Electrolyte uptake

Electrolyte uptake of the separators was determined gravimetrically by recording the weight of the dry separator (W1) and the weight after soaking in electrolyte for 2 h (W2). The electrolyte uptake (%) was calculated according to Equation (S5):

Electrolyte uptake %= W2-W1W×100%		(S5)

# S7 Sodium transference number (tNa+)

Na||Na symmetric cells were assembled with different separators, and the Na+ transference number (tNa+) at 60oC was determined using Equation (S6):

tNa+=Is(∆V-IoRo)Io(∆V-IsRs)				(S6)

where ΔV is the applied polarization potential (5 mV), I0 and Is are the initial and steady-state currents, respectively, and R0 and Rs are the corresponding resistances obtained from AC impedance spectroscopy. EIS was recorded using a high-precision electrochemical workstation (Autolab PGSTAT302N) over the frequency range of 105 Hz to 1 mHz to extract resistance values.

# S8 Activation energy

The activation energy (Ea) for Na+ transport was determined from temperature-dependent EIS measurements of Na||Na symmetric cells after 10 cycles at 1 mA cm-2 and 1 mAh cm-2. Impedance spectra were recorded at 293, 303, 313, 323, and 333 K. The activation energy was calculated using the Arrhenius relation (Equation 5):

TRct=Ae-EaRT				(S7)

# S9 Columbic Efficiency

The average columbic efficiency was calculated by the given equations. Where n is number of cycles, Qc cycling capacity, Qt  first plating capacity, and Qs final stripping capacity.

CEavg=nQc+ QsnQc+ QT			(S8)

Supplementary Figures and Tables

Fig. S0 PXRD pattern and TEM/HRTEM images of the HOF

Fig. S1 Fabrication process of the HOF-based separator sheet

Fig. S2 N2 adsorption–desorption isotherms and pore size distribution

Fig. S3 Electrolyte uptake and porosity comparison of separators

Fig. S4 Contact angle images

Fig. S5 SEM image of HOF powder

Fig. S6 Cross-sectional SEM images of HOF separators with different thicknesses

Fig. S7 Ionic conductivity of PP and HOF separators

Fig. S8 Na⁺ transference number of HOF and PP separators

Fig. S9  Tensile stress–strain curves of the HOF separator and commercial PP separator

Fig. S10  Linear sweep voltammetry curves

Fig. S11 Digital photographs of the HOF separator under folding tests

A dry, free-standing HOF separator disk 19mm (diameter) 30um (thickness) was manually folded to 180° and unfolded back to flat for 10 consecutive cycles at room temperature, and photographs were taken after representative folds.  No visible cracking, tearing, or delamination was observed after 10 cycles, confirming the mechanical flexibility of the membrane.

Fig. S12 Time-sequenced combustion images of  PP separator soaked in electrolyte

Fig. S13 Thermogravimetric analysis (TGA) of HOF and PP separators

Fig. S14 Differential scanning calorimetry of HOF and PP separator

Fig. S15 Model for COMSOL simulation

Fig. S16 Na+ concentration field at the electrode interface in cells assembled with HOF and PP

Fig. S17 FEM simulation of the electrolyte current density distribution in a cell model with HOF and PP

Fig. S18 DFT-calculated binding energies between HOF functional groups (N–H, C=O) and ions (Na⁺, PF₆⁻)

Fig. S19 (a) optimized electrolyte configurations in cubic vacuum boxes of 15, 20, 30, and 35 Å; (b) total energy as a function of box size showing negligible energy variation at larger boxes (Γ-point).

Fig. S20 CV profiles of Na||Cu cell with different separators at 0.1mA s-1

Fig. S21 Long-term cycling of symmetric Na||Na cells at 60 °C at 1mA cm-2 and 1mAh cm-2 with different separator thickness

Fig. S22 Long-term cycling of symmetric Na||Na cells at 25 °C at 1mA cm-2 and 1mAh cm-2

Fig. S23 (a) Na||Na symmetrical cell performance with HOF separator at 1 mAh cm-2 and 1 mAh cm-2 (b) Digital photo graph of cycled HOF separator

Fig. S24 Nyquist plot of Na||Na cell with HOF at different temperatures

Fig. S25 Nyquist plot of Na||Na cell with PP at different temperatures

Fig. S26 XPS spectra of SEI on metal anode cycled with PP separator

Fig. S27 XPS spectra of SEI on metal anode cycled with PP separator

Fig. S28  XPS spectra of SEI on metal anode cycled with HOF separator

Fig. S29 (a) Nyquist plots obtained from IS-GEIS results of cell cycled (discharge) with HOF seprator at 0.1C with and eequidistance voltage 0.2V (b) corresponding DRT trasnformation of IS-GEIS

Fig. S30 (a) Nyquist plots obtained from IS-GEIS results of cell cycled (discharge) with PP seprator at 0.1C with and eequidistance voltage 0.2V (b) corresponding DRT trasnformation of IS-GEIS

Fig. S31 Cyclic Voltametery of Na||NVP with HOF and PP separators at 0.5 mV s-1

Fig. S32 Charge-discharge curve of Na||NVP with HOF seprator cycled at 60oC at 5C (1C = 120 mAh g-1)

Fig. S33 Charge-discharge curve of Na||NVP with PP seprator cycled at 60oC at 5C (1C = 120 mAh g-1)

Fig. S34 Long-term cycling stability at 25 °C and 5 C

Fig. S35 Charge-discharge curve of Na||NVP with HOF seprator cycled at 25 oC at 5C (1C = 120 mAh g-1)

Fig. S36 Charge-discharge curve of Na||NVP with HOF seprator cycled at 25 oC at 5C (1C = 120 mAh g-1)

Table S1: Comparison of different parameters for reported separators

| Separator | Ionic Conductivity (mS cm-1) | tNa+ | Na + Contribution | Refs |
| --- | --- | --- | --- | --- |
| HOF | 1.47 | 0.92 | 1.35 | This work |
| COF@PP | 1.13 | 0.82 | 0.93 | [S10] |
| Co-NWS | 1.39 | 0.83 | 1.16 | [S11] |
| Zr-O complex coating layer | 1.05 | 0.78 | 0.82 | [S12] |
| Bis[S(3-methyldimethoxysilyl)propyl]- polypropylene oxide (BSPPO) coating on commercial substrates | 1.33 | 0.69 | 0.92 | [S13] |

Table S2 Comparison of Na∥Na symmetric-cell performance with prior separator reports

| Strategies | Current density (mA cm-2 ) | Areal capacity (mAh cm-2 ) | Cycle life (h) | Electrolytes | Refs |
| --- | --- | --- | --- | --- | --- |
| OHTAPQ@Na | 2 | 2 | 1500 | 1 M NaPF6/DEGDME | [S14] |
| Co-NWS | 0.5 | 0.5 | 500 | 1.0 m NaPF6 in PC:EC = 1:1 v/v, with 10 wt% FEC | [S11] |
| UFS2@GF | 1 | 2 | 500 | 1.0 M NaFSI in PC:EC = 1:1 v/v, with 5 wt% FEC | [S15] |
| Nylon 6-cellulose acetate | 0.5 | 0.5 | 1000 | 1 m NaPF6 EC/DEC wt 5 wt.% FEC | [S16] |
| S-3500 separators | 1 | 0.5 | 1000 | 1 M NaClO4 in EC/DMC | [S17] |
| HOF separator | 2 | 2 | 2000 | 1 m NaPF6 EC/DEC wt 10 wt.% FEC | This work |

Table S3 model parameter settings and boundary conditions

| Cinit | 1 M | Initial concentration |
| --- | --- | --- |
| T0 | 298 K | System temperature |
| I | 2.5 mA cm-2 | Average current density |
| phis_cathode | -0.1 V | Cathode potential |
| alpha_c | 0.5 [S1] | Symmetry factor |
| alpha_a | 0.5 [S1] | Symmetry factor |
| MNa | 22.9898 g mol-1 | Molar mass of Na |
| rhoNa | 0.968 g cm-3 | Density of Na |
| D_Na_pp | 2.19e-12 cm2s-1 | Diffusivity |
| D_Na_HOF | 4.08e-12 cm2s-1 | Diffusivity |
| k_Na_pp | 1.08 mS cm-1 | Ionic conductivity |
| k_Na_HOF | 1.57 mS cm-1 | Ionic conductivity |

# Supplementary References

- A.P. Thompson, H.M. Aktulga, R. Berger, D.S. Bolintineanu, W.M. Brown et al., LAMMPS - a flexible simulation tool for particle-based materials modeling at the atomic, meso, and continuum scales. Comput. Phys. Commun. 271, 108171 (2022). https://doi.org/10.1016/j.cpc.2021.108171

- G.A. Kaminski, R.A. Friesner, J. Tirado-Rives, W.L. Jorgensen, Evaluation and reparametrization of the OPLS-AA force field for proteins via comparison with accurate quantum chemical calculations on peptides. J. Phys. Chem. B 105(28), 6474–6487 (2001). https://doi.org/10.1021/jp003919d

- J. Hafner, Ab-initio simulations of materials using VASP: Density-functional theory and beyond. J. Comput. Chem. 29(13), 2044–2078 (2008). https://doi.org/10.1002/jcc.21057

- P.E. Blöchl, Projector augmented-wave method. Phys. Rev. B 50(24), 17953–17979 (1994). https://doi.org/10.1103/physrevb.50.17953

- J.P. Perdew, K. Burke, M. Ernzerhof, Generalized gradient approximation made simple. Phys. Rev. Lett. 77(18), 3865–3868 (1996). https://doi.org/10.1103/physrevlett.77.3865

- S. Grimme, Semiempirical GGA-type density functional constructed with a long-range dispersion correction. J. Comput. Chem. 27(15), 1787–1799 (2006). https://doi.org/10.1002/jcc.20495

- H.J. Monkhorst, J.D. Pack, Special points for Brillouin-zone integrations. Phys. Rev. B 13(12), 5188–5192 (1976). https://doi.org/10.1103/physrevb.13.5188

- S. Grimme, J. Antony, S. Ehrlich, H. Krieg, A consistent and accurate ab initio parametrization of density functional dispersion correction (DFT-D) for the 94 elements H-Pu. J. Chem. Phys. 132(15), 154104 (2010). https://doi.org/10.1063/1.3382344

- G. Henkelman, B.P. Uberuaga, H. Jónsson, A climbing image nudged elastic band method for finding saddle points and minimum energy paths. J. Chem. Phys. 113(22), 9901–9904 (2000). https://doi.org/10.1063/1.1329672

- M. Ali, H. Hussain, M. Ali, S. Aman, W. Yang et al., Regulating a NaF-rich SEI layer for dendrite-free sodium metal batteries using trifunctional halogenated covalent organic framework separators. Adv. Sci. 12(37), e03693 (2025). https://doi.org/10.1002/advs.202503693

- H. Liu, X. Zheng, Y. Du, M.C. Borrás, K. Wu et al., Multifunctional separator enables high-performance sodium metal batteries in carbonate-based electrolytes. Adv. Mater. 36(5), e2307645 (2024). https://doi.org/10.1002/adma.202307645

- Y. Zhang, S. Yang, S. Liu, Z. Yuan, J. Deng et al., Enabling anion-anchoring and anti-degradation cellulose separators for sodium metal batteries. Energy Storage Mater. 81, 104463 (2025). https://doi.org/10.1016/j.ensm.2025.104463

- Z. Hou, W. Zhang, X. Kong, Q. Ren, Z. Wang et al., Polypropylene oxide-modified cellulose separators for high-rate Na+ transport via a dual-pathway mechanism in sodium-ion batteries. Chem. Eng. J. 513, 162839 (2025). https://doi.org/10.1016/j.cej.2025.162839

- Z. Shen, Z. Bo, R. Shi, L. Liu, H. Li et al., Functional p-π conjugated organic layer empowers stable sodium metal batteries. Adv. Funct. Mater. 35(19), 2420573 (2025). https://doi.org/10.1002/adfm.202420573

- J. Lv, Z. Tang, Q. Zhang, H. Sun, M. OuYang et al., Synergistic dual-polar-functionalized metal–organic framework-modified separator for stable and high-performance sodium metal batteries. ACS Nano 19(16), 16133–16146 (2025). https://doi.org/10.1021/acsnano.5c04051

- S. Guo, W. Li, X. Wu, X. Guo, Z. Gong et al., Functional separator induced interface potential uniform reformation enabling dendrite-free metal batteries. Adv. Funct. Mater. 35(37), 2504599 (2025). https://doi.org/10.1002/adfm.202504599

- J. Wang, Z. Xu, Q. Zhang, X. Song, X. Lu et al., Stable sodium-metal batteries in carbonate electrolytes achieved by bifunctional, sustainable separators with tailored alignment. Adv. Mater. 34(49), e2206367 (2022). https://doi.org/10.1002/adma.202206367