Supporting Information for

Modulating Lattice Oxygen and Transport Kinetics of Li-Rich Cathodes in All-Solid-State Batteries through Multifunctional Li3ScF6 Protective Layer

Peng Lei1, Gang Wu1, Xiang Qi1, Yang Li1, Meng Wu1, Wanqing Ren1, Huan Li1, Lei Gao1, Dan Zhou1*, Li-Zhen Fan1*

1Institute of Advanced Materials and Technology, University of Science and Technology Beijing, Beijing 100083, P. R. China

*Corresponding authors. E-mail: fanlizhen@ustb.edu.cn (Li-Zhen Fan); zhoudan@ustb.edu.cn (Dan Zhou)

Supplementary Figures and Tables

Fig. S1 a) Rate performance comparison of ASSLBs with different thermal temperature-treated LRMO. b) Cycling performance comparison of ASSLBs with different LSF coating amounts. c) Radar chart for comprehensive performance comparison of ASSLBs with different LSF coating amounts

Fig. S2 Raman spectra of B-LRMO and C-LRMO

Fig. S3 SEM images of B-LRMO particles

Fig. S4 SEM image of C-LRMO particles and corresponding EDS mappings of Ni, Co, Mn, O, Sc, and F elements

Fig. S5 HRTEM image of C-LRMO powder

Fig. S6 XPS spectra of a) Sc 2p and b) F 1s for C-LRMO

Fig. S7 XPS spectra of a) Sc 2p and b) F 1s for B-LRMO

Fig. S8 O 1s XPS spectra of a) B-LRMO and b) C-LRMO

Fig. S9 The Ni 2p XPS spectra of a) B-LRMO and b) C-LRMO, Co 2p XPS spectra of c) B-LRMO and d) C-LRMO, Mn 2p XPS spectra of e) B-LRMO and f) C-LRMO

Fig. S10 TOF-SIMS images of a) MnO− and b) ScO− species in the C-LRMO cathode

Fig. S11 The schematic illustration of the ASSLBs

Fig. S12 Nyquist plots of a) LITC and b) LPSCB at 30 ℃

Fig. S13 a) Nyquist plots and b) DC polarization curves of B-LRMO and C-LRMO composite cathode, and c) corresponding ionic or electronic conductivity

Fig. S14 First-cycle charge/discharge voltage profiles of a) B-LRMO and b) C-LRMO at 0.1 C. A voltage of ~4.47 V was selected to distinguish TM oxidation and O oxidation

Fig. S15 CV curves of B-LRMO and C-LRMO

Fig. S16 The cycling voltage decay of B-LRMO and C-LRMO at 0.3 C

Fig. S17 Long-term cycling stability of C-LRMO at 1 C with cathode mass loading of 7.64 mg cm−2

Fig. S18 Discharge voltage curves of a) B-LRMO and b) C-LRMO electrodes at different current densities

Fig. S19 a) Initial discharging voltage profile of the B-LRMO ASSLBs between 2.2 and 4.7 V versus Li+/Li. b) Interfacial impedance evolution of the B-LRMO ASSLBs and c) corresponding DRT profile transformation derived from in situ EIS. d) Initial discharging voltage profile of the C-LRMO ASSLBs between 2.2 and 4.7 V versus Li⁺/Li. e) Interfacial impedance evolution of the C-LRMO ASSLBs and f) corresponding DRT profile transformation derived from in situ EIS

Fig. S20 a) Nyquist plots of B-LRMO and C-LRMO cells after 500 cycles at 0.3 C and b) the comparison of DRT profiles transformation of EIS

Fig. S21 XPS spectra of a) In 3d and b) Cl 2p in the composite cathodes before and after 500 cycles at 0.3 C

Fig. S22 O K-edge XANES spectra of a) B-LRMO and b) C-LRMO at different voltage states

Fig. S23 Sc K-edge spectra of C-LRMO at different voltage states: a) XANES spectra and b) EXAFS spectra

Fig. S24 The XRD patterns of a) the overall and b) the enlarged patterns of the (003) peak for the cycled and pristine cathodes of B-LRMO and C-LRMO

Fig. S25 Relaxed crystal structures of B-LRMO. The color code for atoms: red, O; green, Li; gray, Ni; blue, Co; purple, Mn

Fig. S26 Charge density difference of the C-LRMO. The color code for atoms: red, O; green, Li; gray, Ni; blue, Co; purple, Mn; orchid purple, Sc; periwinkle blue, F

Fig. S27 Calculated mutual reaction energies of different interfaces

Fig. S28 The calculated thermodynamic electrochemical stability windows of LITC and LSF

Table S1 Lattice parameters of B-LRMO and C-LRMO derived from Rietveld refinement of XRD patterns

| Sample | Space group | Lattice parameters |  |  |  |  |  | Vol (Å3) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | a(Å) | b(Å) | c(Å) | α(˚) | β(˚) | γ(˚) |  |
| B-LRMO | R3m | 2.85443 | 2.85443 | 14.26466 | 90.0000 | 90.0000 | 120.0000 | 100.654 |
| B-LRMO | C2/m | 4.92549 | 8.55097 | 5.02809 | 90.0000 | 109.2358 | 90.0000 | 199.948 |
| C-LRMO | R3m | 2.85166 | 2.85166 | 14.21446 | 90.0000 | 90.0000 | 120.0000 | 100.105 |
| C-LRMO | C2/m | 4.92893 | 8.55104 | 5.02811 | 90.0000 | 109.2472 | 90.0000 | 200.077 |

Table S2 Comparison of the electrochemical performance for the LRMO-based ASSLBs

| Cathode materials | Solide electrolyte in cathode | Areal Capacity (mAh cm−2) | Cycle number | Capacity retention (%) | Temperature (℃) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| LLO-Ru@S | Li6PS5Cl | 0.65 | 1.0 C 2022 cycles | 72.0 | 55 | [S1] |
| SC-LRMO | Li6PS5Cl | 1.2 | 1.0 C 300 cycles | 86.0 | 60 | [S2] |
| LRCo10@5LN | BM-Li6PS5Cl | 1.9 | 0.5 C 300 cycles | 85.0 | 25 | [S3] |
| Li1.14Ni0.29Mn0.57O2 | LiAlOCl | 2.0 | 0.3 C 190 cycles | 92.7 | 25 | [S4] |
| S-LRMO | Li3InCl4.8F1.2 | 2.9 | 0.2 C 60 cycles | 80.3 | 25 | [S5] |
| SCM LLO | Li3InCl6 | 2.9 | 0.5 C 431 cycles | 60.0 | 25 | [S6] |
| 5W&LRMO | Li3InCl6 | 3.15 | 0.2 C 100 cycles | 84.1 | 25 | [S7] |
| LBO-LRMO | Li3InCl6 | 0.97 | 1.0 C 2000 cycles | 80.4 | 25 | [S8] |
| LMRO-0.6Li2MnO3/0.05LiNiO2 | Li3InCl6 | 1.96 | 0.2 C 1000 cycles | 87.0 | 25 | [S9] |
| C-LRMO | Li2.6In0.8Ta0.2Cl6 | 1.85 | 1 C 1000 cycles | 84.7 | 30 | This work |
|  |  | 4.17 | 0.1 C 300 cycles | 81.1 | 60 |  |

Supplementary References

- Y. Wang, D. Wu, P. Chen, P. Lu, X. Wang et al., Dual-function modifications for high-stability Li-rich cathode toward sulfide all-solid-state batteries. Adv. Funct. Mater. 34(4), 2309822 (2024). https://doi.org/10.1002/adfm.202309822

- Y. Wu, C. Li, X. Zheng, W. Zhao, H. Wang et al., High energy sulfide-based all-solid-state lithium batteries enabled by single-crystal Li-rich cathodes. ACS Energy Lett. 9(10), 5156–5165 (2024). https://doi.org/10.1021/acsenergylett.4c01764

- W. Du, Q. Shao, Y. Wei, C. Yan, P. Gao et al., High-energy and long-cycling all-solid-state lithium-ion batteries with Li- and Mn-rich layered oxide cathodes and sulfide electrolytes. ACS Energy Lett. 7(9), 3006–3014 (2022). https://doi.org/10.1021/acsenergylett.2c01637

- G. Wang, S. Zhang, H. Wu, M. Zheng, C. Zhao et al., Oxychloride polyanion clustered solid-state electrolytes via hydrate-assisted synthesis for all-solid-state batteries. Adv. Mater. 37(4), 2410402 (2025). https://doi.org/10.1002/adma.202410402

- S. Sun, C.-Z. Zhao, H. Yuan, Z.-H. Fu, X. Chen et al., Eliminating interfacial O-involving degradation in Li-rich Mn-based cathodes for all-solid-state lithium batteries. Sci. Adv. 8(47), eadd5189 (2022). https://doi.org/10.1126/sciadv.add5189

- R. Yu, C. Wang, H. Duan, M. Jiang, A. Zhang et al., Manipulating charge-transfer kinetics of lithium-rich layered oxide cathodes in halide all-solid-state batteries. Adv. Mater. 35(5), e2207234 (2023). https://doi.org/10.1002/adma.202207234

- W.-J. Kong, C.-Z. Zhao, L. Shen, S. Sun, X.-Y. Huang et al., Bulk/interfacial structure design of Li-rich Mn-based cathodes for all-solid-state lithium batteries. J. Am. Chem. Soc. 146(41), 28190–28200 (2024). https://doi.org/10.1021/jacs.4c08115

- S. Sun, C.-Z. Zhao, G.-Y. Liu, S.-C. Wang, Z.-H. Fu et al., Boosting anionic redox reactions of Li-rich cathodes through lattice oxygen and Li-ion kinetics modulation in working all-solid-state batteries. Adv. Mater. 37(6), 2414195 (2025). https://doi.org/10.1002/adma.202414195

- Z. Wu, Q. Shao, Y. Wei, C. Yan, P. Gao et al., Multi-strategies interface and structure design of Li- and Mn-rich layered oxide for all-solid-state lithium batteries. Nano Energy 122, 109281 (2024). https://doi.org/10.1016/j.nanoen.2024.109281