Supporting Information for

Electronic Delocalization of Fe Atom-Cluster for Long-Term Stable Electromagnetic Wave Absorption in Marine Environments

Shaocong Zhong1, Xinyu Wang1, Rurong Zou1, 2, Chang Long2, Pianpian Zhang1, *, Xueting Zhang1, Zihao Zhao1, Ying Liu1, Can Cui1, Yanan Yang1, * and Long Xia1, *

1 College of Materials Science and Engineering, Harbin Institute of Technology (Weihai), Weihai 264209, P. R. China

2 Aerospace Science and Industry Wuhan Magnetism-Electron Co., Ltd, Wuhan 430074, P. R. China

* Corresponding authors. E-mail: zhangpianpian1993@126.com (Pianpian Zhang); yangyanan310@163.com (Yanan Yang); xialonghit@gmail.com (Long Xia)

S1 Supplementary Text

S1.1 Materials

Acrylamide (C3H5NO, AR), 2-Hydroxy-2-methylpropiophenone (C10H12O2, 97%), Polyethylene glycol diacrylate (PEGDA, C5H10O4, Mr~1000), and Carboxymethyl cellulose were both purchased from Shanghai Aladdin Biochemical Technology Co., Ltd (Shanghai, China). Soda-lime glass and PET sheet were purchased from Zhuhai Kaiwei Optoelectronic Technology Co., Ltd (Guangdong, China).

S1.2 Preparations of the NC-FeAC2 film

10 g of acrylamide monomer was mixed with a 5 mg of crosslinker (polyethylene glycol diacrylate), and 8mg of photoinitiator (2-hydroxy-2-methylpropiophenone). The mixture was heated and stirred in a water bath at 80 °C until a clear solution was obtained. Square soda-lime glass plates (0.5 cm thick) and PET sheets (0.2 cm thick) were rinsed three times with deionized water and ethanol, respectively, and then dried for use as the bottom substrate and the top cover for ion-gel fabrication. The precursor solution was drop-cast onto the glass substrate, and glass spacers (2.0 mm thick) were used to define the gap before covering with the PET sheet. A UV lamp (365 nm) was positioned 2 cm above the precursor, followed by UV curing for 1 min. Finally, the top plate was removed and the gel film was peeled off.

S1.3 Preparations of the NC-FeAC2 aerogel film

0.5 g of NC-FeAC2 was added to 10 mL of deionized water and ultrasonicated for 30 min to obtain a homogeneous suspension (Solution A). Separately, 4.0 g of carboxymethyl cellulose was dissolved in 15 mL of deionized water and stirred continuously at 60 °C for 1 h to form a uniform solution (Solution B). Solution A was then slowly dropwise added to Solution B under continuous stirring, and the mixture was further stirred for 30 min to ensure uniform blending. The resulting mixture was transferred into a mold, rapidly frozen with liquid nitrogen, and subsequently freeze-dried at ‒60 °C under 0.1 Pa for 3 days to obtain the aerogel film.

S1.4 Measurement of electromagnetic parameters

The reflection loss of absorbers with various matching thicknesses in the 2−18 GHz range was calculated by complex permittivity (εr) and complex permeability (μr) based on transmission line theory. where Zin is the input impedance of absorber, Z0 is the impedance of free space, f is the frequency of electromagnetic wave, d is the thickness of absorber, and c is the speed of light, respectively.

(S1)

(S2)

(S3)

(S4)

Based on Debye dipole relaxation theory, the model between ε′ and ε″ can be expressed by equation S5, and the complex permittivity imaginary part (ε″) can be separated into polarization loss (εp″) and conduction loss (εc″). where εs is static permittivity, ε∞ is relative permittivity, ω is angular frequency, τ is polarization relaxation time and σ is electrical conductivity, respectively.

(S5)

(S6)

The attenuation constant (α) and impedance matching (Z) can be calculated by the following equations.

(S7)

(S8)

The contribution of the dielectric loss and magnetic loss can be calculated by the following equations.

(S9)

(S10)

S1.5 Density functional theory (DFT) calculations

All the DFT calculations were conducted based on the Vienna Ab initio Simulation Package (VASP). The exchange-correlation potential was described by the Perdew-Burke-Ernzerhof (PBE) generalized gradient approach (GGA). The electron-ion interactions were accounted by the projector augmented wave (PAW). All DFT calculations were performed with a cut-off energy of 400 eV, and the 3×3×1 Monkhorst-Pack grid k-points were selected to sample the Brillouin zone integration. The energy and force convergence criteria of the self-consistent iteration were set to 10‒4 eV and ‒0.02 eV Å‒1, respectively. DFT-D3 method is adopted to describe the van der Waals interaction.

S2 Supporting Figures

Fig. S1 Characteristic of NC-FeACX precursor structure: a, b) SEM image, c) Magnetic property images of NC-FeAC2 and NC-FeNP

Fig. S2 Characteristic of NC structure: a, b) SEM image, c) TEM image and d) EDX elements mapping image for C, O and N

Fig. S3 Characteristic of NC-FeAC1 structure: a-c) SEM image, d-f) TEM image and j) EDX elements mapping image for C, O, N and Fe

Fig. S4 Characteristic of NC-FeAC2 structure: a-c) SEM image, d-f) TEM image and j) EDX elements mapping image for C, O, N and Fe

Fig. S5 Characteristic of NC-FeAC3 structure: a-c) SEM image, d-f) TEM image and j) EDX elements mapping image for C, O, N and Fe

Fig. S6 Characteristic of NC-FeNP structure: a-c) SEM image, d-f) TEM image and j) EDX elements mapping image for C, O, N and Fe

Fig. S7 AC-HAADF-STEM image of a) NC-FeAC1, b) NC-FeAC2, and c) NC-FeAC3 (The red squares are of the same size and yellow circle represents FeAC)

Fig. S8 XPS survey spectra of NC, NC-FeACX, and NC-FeNP

Fig. S9 High-resolution XPS spectrum of C 1s spectra for a) NC, b) NC-FeAC1, c) NC-FeAC2, d) NC-FeAC3, and e) NC-FeNP

Fig. S10 High-resolution XPS spectrum of O 1s spectra for a) NC, b) NC-FeAC1, c) NC-FeAC2, d) NC-FeAC3, and e) NC-FeNP

Fig. S11 The FT-IR spectra of NC-FeACX, and NC-FeNP

Fig. S12 The ID/IG value of NC, NC-FeACX, and NC-FeNP

Fig. S13 Real and imaginary parts of permeability for a) NC, b) NC-FeAC1, c) NC-FeAC2, d) NC-FeAC3, and e) NC-FeNP. f) Angular tangent of permeability curves of NC, NC-FeACx, and NC-FeNP

Fig. S14 Real and imaginary parts of permittivity for a) NC, b) NC-FeAC1, c) NC-FeAC2, d) NC-FeAC3, and e) NC-FeNP

Fig. S15 The contribution of conduction loss in a) NC, b) NC-FeAC1, c) NC-FeAC2, d) NC-FeAC3, and e) NC-FeNP. f) Comparison of conduction loss among samples

Fig. S16 The contribution of polarization loss in a) NC, b) NC-FeAC1, c) NC-FeAC2, d) NC-FeAC3, and e) NC-FeNP. f) Comparison of polarization loss among samples

Fig. S17 The relationship between the conduction and polarization loss with frequency of a) NC, b) NC-FeAC1, c) NC-FeAC2, d) NC-FeAC3, and e) NC-FeNP

Fig. S18 The Cole-Cole plot of a) NC, b) NC-FeAC1, c) NC-FeAC2, d) NC-FeAC3, and e) NC-FeNP. f) Comparison of Cole-Cole plot among samples

Fig. S19 3D reflection loss of a) NC, b) NC-FeAC1, c) NC-FeAC2, d) NC-FeAC3, and e) NC-FeNP

Fig. S20 2D reflection loss projection of a) NC, c) NC-FeAC1, e) NC-FeAC2, g) NC-FeAC3, and i) NC-FeNP. 2D reflection loss curves at different thickness of b) NC, d) NC-FeAC1, f) NC-FeAC2, h) NC-FeAC3, and j) NC-FeNP

Fig. S21 The electromagnetic wave absorption performance image of multiple measurements.

Average electromagnetic wave absorption performance obtained from five repeated measurements of NC, NC-FeACX, and NC-FeNP (6 wt.%)

Fig. S22 The σ value of NC, NC-FeACX, and NC-FeNP measured by four-probe method at 2 MPa

The electrical conductivity of the samples was measured using a ST2742B four-probe powder resistivity tester under a compressive pressure of 2 MPa. This experimentally observed trend agrees well with the conduction-related contribution inferred from our permittivity-based fitting of electromagnetic wave loss.

Fig. S23 3D impedance matching of a) NC, c) NC-FeAC1, e) NC-FeAC2, g) NC-FeAC3, and i) NC-FeNP. 2D impedance matching projection of b) NC, d) NC-FeAC1, f) NC-FeAC2, h) NC-FeAC3, and j) NC-FeNP

Fig. S24 The Correspondence between 2D reflection loss and impedance matching curves at different thickness of a) NC, b) NC-FeAC1, c) NC-FeAC2, d) NC-FeAC3, and e) NC-FeNP

Fig. S25 3D radar wave scattering single of a) NC-FeAC1, d) NC-FeAC3, and g) NC-FeNP. RCS simulation curves of b, c) NC-FeAC1, e, f) NC-FeAC3, and h, i) NC-FeNP

Fig. S26 a) XPS survey spectra. b) C 1s, c) N 1s, d) Fe 2p, and e) Cl 2p high-resolution XPS spectra of NC-FeAC2 after one-month corrosion

The XPS survey spectrum clearly reveals the presence of Cl element (Fig. S26a), the high-resolution Cl 2p spectrum (Fig.S26e) shows a Cl 2p3/2 component at ~199.5 eV, which can be assigned to metal-chloride (M-Cl) species, indicating that Fe clusters preferentially adsorb/bind Cl‒. Meanwhile, the C 1s spectrum (Fig. S26b) can be deconvoluted into contributions from C-C, C-O-C, C=O, and O-C=O bonds, and the N 1s spectrum (Fig.S26c) consists of pyridinic N, pyrrolic N, graphitic N, and N-O species; both spectra exhibit no pronounced changes compared with those before corrosion, suggesting that the carbon framework and N-coordination environment remain largely intact. Notably, the Fe 2p peaks (Fig.S26d) show a slight shift toward higher binding energies, implying an increased average oxidation state of Fe, which is consistent with electron withdrawal induced by chloride coordination predominantly on Fe cluster domains.

Fig. S27 a) The range of real and imaginary permittivity of samples after NaCl treatment. Real and imaginary parts of permittivity for b) NC-FeAC1, c) NC-FeAC2, d) NC-FeAC3, and e) NC-FeNP after NaCl treatment. f) Angular tangent of permittivity curves of NC, NC-FeACx, and NC-FeNP after NaCl treatment. g) The attenuation constant of samples after NaCl treatment

Fig. S28 a) The range of real and imaginary permeability of samples after NaCl treatment. Real and imaginary parts of permeability for b) NC-FeAC1, c) NC-FeAC2, d) NC-FeAC3, and e) NC-FeNP after NaCl treatment. f) Angular tangent of permeability curves of NC, NC-FeACx, and NC-FeNP after NaCl treatment. g) The C0 value of samples after NaCl treatment

Fig. S29 The contribution of conduction loss in a) NC, b) NC-FeAC1, c) NC-FeAC2, d) NC-FeAC3, and e) NC-FeNP after NaCl treatment. f) Comparison of conduction loss among samples after NaCl treatment

Fig. S30 The contribution of polarization loss in a) NC, b) NC-FeAC1, c) NC-FeAC2, d) NC-FeAC3, and e) NC-FeNP after NaCl treatment. f) Comparison of polarization loss among samples after NaCl treatment

Fig. S31 The Cole-Cole plot of a) NC-FeAC1, b) NC-FeAC2, c) NC-FeAC3, and d) NC-FeNP after NaCl treatment. e) Comparison of Cole-Cole plot among samples after NaCl treatment

Fig. S32 The relationship between the conduction and polarization loss with frequency of a) NC-FeAC1, b) NC-FeAC2, c) NC-FeAC3, and d) NC-FeNP after NaCl treatment

Fig. S33 3D reflection loss of a) NC-FeAC1, b) NC-FeAC2, c) NC-FeAC3, and d) NC-FeNP after NaCl treatment

Fig. S34 2D reflection loss projection of a) NC-FeAC1, c) NC-FeAC2, e) NC-FeAC3, and g) NC-FeNP after NaCl treatment. 2D reflection loss curves at different thickness of b) NC-FeAC1, d) NC-FeAC2, f) NC-FeAC3, and h) NC-FeNP after NaCl treatment

Fig. S35 3D impedance matching of a) NC-FeAC1, c) NC-FeAC2, e) NC-FeAC3, and g) NC-FeNP after NaCl treatment. 2D impedance matching projection of b) NC-FeAC1, d) NC-FeAC2, f) NC-FeAC3, and h) NC-FeNP after NaCl treatment

Fig. S36 The Correspondence between 2D reflection loss and impedance matching curves at different thickness of a) NC, b) NC-FeAC1, c) NC-FeAC2, d) NC-FeAC3, and e) NC-FeNP after NaCl treatment

Fig. S37 a) 3D RCS simulation curves of NC-FeACX, and NC-FeNP. 2D RCS simulation curves of b) NC-FeAC1, c) NC-FeAC2, d) NC-FeAC3 and e) NC-FeNP

Fig. S38 EMW performance of a) matrix and stretched NC-FeAC2 film and b) matrix and unstretched NC-FeAC2 film measured by bow-method

Fig. S39 Surface temperature variation of the samples with the increasing heating time

Fig. S40 Comparison of EMW absorption performance under marine environments [S1-S12]

Supplementary References

- Q. Ban, Y. Song, L. Li, H. Zhang, X. Wu et al., Confined diffusion engineering of FeCoNi-embedded hollow carbon microcage toward controllable electromagnetic wave absorption and anticorrosive polyvinylidene fluoride composite in marine environment. Small 21(41), e08008 (2025). https://doi.org/10.1002/smll.202508008

- B. Li, L. Ma, S. Li, J. Cui, X. Liang et al., Electromagnetic wave absorption and corrosion resistance performance of carbon nanoclusters/Ce–Mn codoped barium ferrite composite materials. Int. J. Miner. Metall. Mater. 32(3), 699–709 (2025). https://doi.org/10.1007/s12613-024-2997-2

- J. Yao, J. Zhou, L. Lu, F. Yang, Z. Yao et al., Rare earth lanthanum pinning effect for corrosion resistance ultraefficient microwave absorption FeCo@rGO composites. J. Mater. Sci. Technol. 177, 181–190 (2024). https://doi.org/10.1016/j.jmst.2023.07.075

- M. Zhao, S. Ran, X. Guo, Z. Wang, Q. Hou et al., Magnetic-dielectric synergy in Fe3O4/MoS2@polyaniline composites for high-efficiency electromagnetic wave absorption and corrosion resistance. J. Alloys Compd. 1048, 185300 (2025). https://doi.org/10.1016/j.jallcom.2025.185300

- W. Wang, F. Qu, Y. Zhang, Z. Liu, H. Chang et al., Enhanced corrosion resistance of flaky carbonyl iron through dual silane surface modification for the application of electromagnetic wave absorption coatings. J. Mater. Sci. 59(4), 1721–1735 (2024). https://doi.org/10.1007/s10853-023-09301-w

- X. Zhao, H. Li, W. Chen, W. Li, Z. Han et al., Carbon-based composites from Ti-Ni MOFs with enhanced electromagnetic wave absorption and corrosion resistance. Colloids Surf. A Physicochem. Eng. Aspects 727, 138369 (2025). https://doi.org/10.1016/j.colsurfa.2025.138369

- H. Wang, H. Ren, C. Jing, J. Li, Q. Zhou et al., Two birds with one stone: Graphene oxide@sulfonated polyaniline nanocomposites towards high-performance electromagnetic wave absorption and corrosion protection. Compos. Sci. Technol. 204, 108630 (2021). https://doi.org/10.1016/j.compscitech.2020.108630

- L. Duan, J. Zhou, J. Tao, Y. Liu, Y. Yan et al., Genome engineering of materials based on Ce doping, high-performance electromagnetic wave absorber for marine environment. Compos. Part B Eng. 287, 111882 (2024). https://doi.org/10.1016/j.compositesb.2024.111882

- J. Ge, Y. Cui, L. Liu, F. Meng, F. Wang, The fabrication of FeMnO/RGO as anticorrosive microwave absorbent toward marine environment. Synth. Met. 282, 116933 (2021). https://doi.org/10.1016/j.synthmet.2021.116933

- H. Liu, W. Xu, H. Ren, D. Li, J. He et al., Integrated comprehensive protection coating achieved by ligand engineering modulated MXene@LDH heterojunction with anti-corrosion, electromagnetic wave absorption and fire safety. Chem. Eng. J. 486, 150444 (2024). https://doi.org/10.1016/j.cej.2024.150444

- P. Liu, Z. He, X. Li, L. Ding, S. Liu et al., Multifunctional hollow carbon microspheres enable superior electromagnetic wave response and corrosion barrier. Adv. Mater. 37(35), 2500646 (2025). https://doi.org/10.1002/adma.202500646

- Y. Wang, S. Zhu, H. Guan, Q. Man, Silica coated MOFs-derived composites with excellent electromagnetic wave absorption and corrosion resistance. Colloids Surf. A Physicochem. Eng. Aspects 694, 134043 (2024). https://doi.org/10.1016/j.colsurfa.2024.134043