Supporting Information for

Breaking the Limitations of Sulfur Redox Kinetics by Accelerated Li+-Desolvation in Lithium–Sulfur Batteries

Tan Wang1, Zhenhua Wang1, *, Xiaotian Gao1, Zhe Bai1, Wanning Liu1, Yu Bai1, David Rooney2, *, Kening Sun1, *

1Beijing Key Laboratory of Green Hydrogen and Fuel Cells, School of Chemistry and Chemical Engineering, Beijing Institute of Technology, Beijing 100081, P. R. China

2School of Chemistry and Chemical Engineering, Queen's University Belfast, Belfast, Northern Ireland, BT9 5AG, UK

*Corresponding authors. E-mail: wangzh@bit.edu.cn (Zhenhua Wang); d.rooney@qub.ac.uk (David Rooney); sunkn@bit.edu.cn (Kening Sun)

S1 Materials characterizations

XRD was performed to determine the composition of the samples (Ultima IV-185, Cu Kα radiation). The Raman spectra were measured with a 532 nm laser (HORIBA, HR Evolution). The morphology was obtained by SEM (Hitachi S-8230), TEM, and HR-TEM (JEM-2100F). The XPS spectra were measured to test the surface element characteristics (Kratos Axis Supra). X-ray absorption data were collected at the Aichi Synchrotron Radiation Center. ICP-OES was used to test the content of Ce and P. HAADF-STEM was collected using Theims Z field emission electron microscope (FEI, Netherlands).

S2 Electrochemical measurements

We prepared the cathode slurry through mixing CNT/S (CNT and sulfur powders were mixed in a 7:3 ratio and then heated at 155°C for 12 h), super P, and PVDF in a mass ratio of 7:2:1. With a mass ratio of 3:6:1, the modified interlayer slurry was prepared from P/Ce-NC (or PNC or P/Ce@NC), CNT, and PVDF. The cathode slurry and modified interlayer slurry were all stirred for 12 h and then loaded onto the aluminum foil and Celgard 2500 separator. Under excessive-electrolyte conditions (electrolyte-to-sulfur (E/S) ratio is 30 μL/mg(S)), the sulfur mass loading was 1.0-1.3 mg cm−2. While under lean-electrolyte conditions (E/S ratio is 8 μL/mg(S)), the sulfur mass loading was set at 5.31 mg cm−2. Then kept at 60℃ overnight. LSBs used Li metal as the anode (φ14 mm), CNT/S as the cathode (φ12 mm), and P/Ce-NC or P/Ce@NC or PNC as the separator (φ19 mm), 1 M dilithium (trifluoromethane sulfonylimide) imide (LiTFSI) in DOL/DME (1:1 volume ratio) with 1 wt% % LiNO3 as the electrolyte (Canrd Technology Co. Ltd). The Li–S pouch cell was assembled using a sulfur cathode (45 mg sulfur loading) and a lithium foil anode (100 μm thick), with dimensions of 3×4 cm2 and 4×5 cm2, respectively. The E/S ratio was kept at 3.75 μL/mg(S). Galvanostatic charge/discharge cycling between 1.7 and 2.8 V was tested by a Neware battery testing system. The pouch cells need to be tested using battery clamps (Changgao New Materials Co., Ltd). The in-situ Raman measurements were conducted on custom-assembled LSBs using a sample chamber with quartz optical windows. Raman spectra were acquired simultaneously with the discharge process from the open-circuit voltage to 1.7 V at a rate of 0.15 C. The CHI660e (Shanghai Chenhua) electrochemical workstation was used for CV, symmetric CV, and EIS. Assembly of Li2S6 symmetrical cell: The working electrodes were fabricated by creating a homogeneous dispersion of 20 mg catalyst (P/Ce-NC or PNC) in 2 mL ethanol. This solution was uniformly applied onto a carbon paper substrate until an areal loading of 0.5 mg cm−2 was obtained. Symmetrical cells were constructed containing 40 μL of Li2S6 solution sandwiched between two identical electrodes and a Celgard 2500 separator. Symmetric CV tests were conducted on the Li2S6 symmetric cell within the voltage range of -1.0 V to 1.0 V. In addition, CV tests were conducted on Li–S batteries within the voltage range of 1.6-2.8V.

S3 Li2S nucleation test

The cell was assembled with a carbon paper-based working electrode (loaded with P/Ce-NC or PNC), a lithium foil counter electrode, a Celgard 2500 separator, and the electrolyte of Li2S8 solution of 2.0 mol L-1 and a blank electrolyte, respectively. We subjected the batteries to galvanostatic discharge to 2.1 V (0.112 mA) and then potentiostatic discharge at 2.09 V until the current fell below 10 μA.

S4 Theoretical calculations

We employed the Vienna Ab initio Simulation Package (VASP) to carry out spin-polarized density functional theory (DFT) calculations [S1]. The exchange-correlation energy was treated with the Perdew-Burke-Ernzerhof (PBE) functional [S2]. The cut-off energy was set to 520 eV, and a vacuum layer was set at least 15 Å. In addition, the spin polarization was considered in the DFT calculations. The electronic energy convergence was set at 10⁻4 eV [S3]. The adsorption energy (Eads) was defined as:

Ebinding=Etotal-Eslab-Eads                                (S1)

Etotal, Eslab and Eads are the energy of total, the energy of optimized structure, and the energy of LiPSs. The Gibbs free energy was calculated using the following formula.

G=Gcorrection+EDFT=EZPE+∆U-TS+EDFT=U-TS+EDFT=GT+EDFT	(S2)

Where Gcorrection is the corrected Gibbs free energy by zero-point energy, EDFT denotes the energy obtained by DFT calculation, U, S and T represent the internal energy, the entropy, and the absolute temperature, respectively. EZPE represents the zero-point energy. GT can be calculated by the VASPKIT code after the frequency calculation of adsorbed LiPS.

S5 Supplementary Figures and Tables

Fig. S1 XRD patterns of P/Ce-ZIF8 and P-ZIF8.

Fig. S2 XRD patterns of P/Ce-NC and PNC.

Fig. S3 SEM images of (a, b) P/Ce-NC and (c, d) PNC.

Fig. S4 TEM and HRTEM of (a, b) P/Ce-NC and (c, d) PNC.

Fig. S5 HAADF image of the P/Ce-NC.

Fig. S6 BET test of P/Ce-NC.

Fig. S7 XPS spectra of N 1s in the P/Ce-NC.

Fig. S8 PDOS of the Ce 4f orbitals in Ce-NC.

Fig. S9 PDOS of the Ce 3d orbitals in (a) P/Ce-NC and (b) Ce-NC.

Fig. S10 The snapshots of commercial electrolyte (a) without and (b) with P/Ce-NC via MD simulation.

Fig. S11 In-situ Raman spectra with (a) P/Ce-NC and (b) PNC catalyst layer.

Fig. S12 SEM images of (a) P/Ce-NC and (b) PNC catalyst layer.

Fig. S13 The amperometric i-t and EIS curves of the battery with (a) P/Ce-NC and (b) PNC interlayer. (c) Ionic conductivity. (d) Li+ transference number and the ionic conductivity of P/Ce-NC and PNC.

Fig. S14 PDOS of P/Ce-NC-Li2S2 and Ce-NC-Li2S2.

Fig. S15 Geometric configurations of (a) S8, (b) Li2S8, (c) Li2S6, (d) Li2S4, (e) Li2S2, and (f) Li2S on P/Ce-NC.

Fig. S16 Geometric configurations of (a) S8, (b) Li2S8, (c) Li2S6, (d) Li2S4, (e) Li2S2, and (f) Li2S on PNC.

Fig. S17 Li2S nucleation test for the battery with (a) P/Ce-NC and (b) PNC catalyst layer.

Fig. S18 CV curves of symmetric cells with Li2S6.

Fig. S19 In-situ Raman spectra of (a, b) P/Ce-NC and (c, d) PNC system.

Fig. S20 Optical images of the Li anode after cycling in an in situ Raman sample chamber.

Fig. S21 F 1s XPS spectra of the lithium anode after 50 cycles of the battery with P/Ce-NC catalyst layer.

Fig. S22 Tafel plots based on the peak C1.

Fig. S23 The peak current versus the square root of scan rate at peak C2.

Fig. S24 EIS measurements of P/Ce-NC-based battery, (a) fresh cell, (b) discharge to 2.30 V, (c) discharge to 2.10 V, (d) discharge to 2.03 V, and (e) discharge to 1.70 V.

Fig. S25 EIS measurements of PNC-based battery, (a) fresh cell, (b) discharge to 2.30 V, (c) discharge to 2.10 V, (d) discharge to 2.02 V, and (e) discharge to 1.70 V.

Fig. S26 DRT profiles of PNC-based battery at different voltages (a) fresh, (b) discharge to 2.30 V, (c) discharge to 2.10 V, (d) discharge to 2.02 V, and (e) discharge to 1.70 V.

Fig. S27 Polarization resistance of D1-8 for P/Ce-NC-based battery at different voltages.

Fig. S28 The charge-discharge profiles of the PNC-based battery from 0.1 C to 6 C.

Fig. S29 The corresponding voltage gap value of Li−S batteries using different catalyst layers.

Fig. S30 EIS performance of battery with P/Ce-NC catalyst layer (a) before and (b) after 50 cycles.

Discussion: The P/Ce-NC battery exhibits significantly lower resistance than the PNC battery, both before and after cycling. This indicates that the P/Ce-NC catalyst layer could promote the conversion kinetics of LiPSs during long cycles.

Fig. S31 SEM images of the lithium anode after cycling of (a) PNC and (b) P/Ce-NC-based battery.

Discussion: The anode after cycling was tested by SEM, and it is evident that the PNC battery exhibits severe corrosion. In stark contrast, the lithium anode of the P/Ce-NC battery exhibits a uniform surface. This finding further validates that the P/Ce-NC can effectively suppress the shuttle effect and promote uniform deposition of the lithium anode.

Fig. S32 SEM images of the P/Ce-NC catalyst layer after 1000 cycles of the P/Ce-NC-based battery.

Discussion: As shown in Fig. S32, after 1000 cycles, the morphology of the P/Ce-NC catalyst remained highly intact, and no structural collapse was observed. This observation further confirms the excellent structural stability of the P/Ce-NC catalyst.

Fig. S33 XRD patterns of (a) P/Ce@NC and (b) P/Ce@ZIF8.

Discussion: The reference sample of P/Ce@NC was synthesized by an identical method with a high loading of Ce. The XRD pattern showed identical diffraction patterns, and in addition, the diffraction peak corresponding to CeP appears.

Fig. S34 (a, b) TEM and (c) HRTEM image of P/Ce@NC.

Discussion: The TEM image clearly shows the shape of a rhombic dodecahedron and a large number of loosely arranged nanoparticles on its surface (Fig. S34b). The HRTEM image of P/Ce@NC exhibits clear lattice fringes (0.34 nm), corresponding to a single-layer CeP about (111) lattice plane.

Fig. S35 (a) The rate performance and (b) cycling performance at 1 C of the battery with P/Ce@NC interlayer.

Discussion: Galvanostatic charge/discharge test was performed at different current densities, the discharge capacity is 1200.66, 934.36, 812.47, 721.78, 646.06, 591.94, 541.60, 486.23, 382.47 mAh g-1 of 0.1, 0.2, 0.5, 1, 2, 3, 4, 5, 6 C, respectively. The cyclic tests show the stability of P/Ce@NC-based battery under 1 C (Fig. S35b), which shows a reversible specific capacity of 937.75 mAh g-1 and a low average capacity fading of 0.058% per cycle.

Table S1 Content of Ce elements in different catalysts

| sample | Mass (g) | Constant volume V0（mL) | Test element | Test the concentration of liquid elements Co (mg L–1) | Dilution factor f | Concentration of the original solution C1 (mg L–1) | Element content Cx (mg kg–1) | Element content W (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ce-129.0 | 0.0517 | 25 | Ce | 0.671 | 1 | 0.671 | 324.4 | 0.03% |
| Ce-322.5 | 0.0531 | 25 | Ce | 0.567 | 1 | 0.567 | 266.8 | 0.03% |
| Ce-645.0 | 0.0490 | 25 | Ce | 0.746 | 1 | 0.746 | 380.8 | 0.04% |

Discussion: As shown in Table S1, even when we significantly increased the amount of the Ce(NO3)3·6H2O precursor from 64.5 mg up to 129.0, 322.5, and even 645.0 mg (denoted as Ce-129.0, Ce-322.5, and Ce-645.0), no Ce species could be detected in the final products.

Table S2 ICP-OES analysis result of the P/Ce-NC and P/Ce@NC

| Sample | Ce (wt.%) |  | P (wt.%) | Zn (wt.%) |
| --- | --- | --- | --- | --- |
| P/Ce-NC | 5.30 | 2.80 |  | 0.30% |
| P/Ce@NC | 10.53 | 3.12 |  |  |

Discussion: As shown in Table S2, residual Zn content in P/Ce-NC is quantified to be as low as 0.30 wt. %, which would exert negligible influence on catalytic performance [S4, S5].

Table S3 EXAFS fitting parameters at the Ce L3-edge for various samples

| Sample | Shell | CNa | R(Å)b | σ2(Å2)c | ΔE0(eV)d | R factor |
| --- | --- | --- | --- | --- | --- | --- |
| CeO2 | Ce-O | 2* | 2.138±0.001 | 0.0010±0.0001 | 5.9±0.4 | 0.0124 |
|  | Ce-O | 6* | 2.341±0.001 |  |  |  |
|  | Ce-O | 2* | 3.126±0.001 |  |  |  |
|  | Ce-Ce | 7* | 3.809±0.001 | 0.0005±0.0001 | 3.2±0.6 |  |
| P/Ce-NC | Ce-N | 3.9±0.6 | 2.505±0.001 | 0.0088±0.0001 | 1.8±0.9 | 0.0049 |
|  | Ce-O | 3.7±0.8 | 2.622±0.001 | 0.0160±0.0001 | 4.5±0.1 |  |

aCN, coordination number; bR, the distance to the neighboring atom; cσ2, the Mean Square Relative Displacement (MSRD); dΔE0, inner potential correction; R factor indicates the goodness of the fit. S02 was fixed to 0.730, according to the experimental EXAFS fit of CeO2 by fixing CN as the known crystallographic value. This value was fixed during EXAFS fitting, based on the known structure of CeO2. Fitting range: 3.0 ≤ k (/Å) ≤ 9.5 and 1.5 ≤ R (Å) ≤ 3.9 (CeO2); 2.0 ≤ k (/Å) ≤ 9.5 and 1.5 ≤ R (Å) ≤ 2.6 (P/Ce-NC). A reasonable range of EXAFS fitting parameters: 0.700 < Ѕ02 < 1.000; CN > 0; σ2 > 0 Å2; |ΔE0| < 15 eV; R factor < 0.02.

Table S4 The IpCOHP values of various samples

| Sample | Li−O1# in DME | Li−O2# in DME |  |  | Li−O in DOL |
| --- | --- | --- | --- | --- | --- |
| P/Ce-NC | 0.02 |  | 0.12 | 0.06 |  |
| DME | 0.13 |  | 0.14 | 0.13 |  |

Table S5 The DLi+ values for various electrochemical reaction processes

| Sample | Peak A | Peak C1 | Peak C2 |
| --- | --- | --- | --- |
| P/Ce-NC | 1.25×10-7 | 2.81×10-8 | 7.85×10-8 |
| PNC | 2.64×10-8 | 3.51×10-9 | 1.19×10-8 |

Table S6 The resistance of the battery with P/Ce-NC layer at different voltages

| voltage | Fresh | 2.30 V | 2.10 V | 2.03 V | 1.70 V |
| --- | --- | --- | --- | --- | --- |
| D1/Ω | 0.72 | 0.09 | 0.11 | 0.81 | 2.01 |
| D2/Ω | 0 | 0 |  | 0.76 | 0.33 |
| D3/Ω | 6.45 | 7.93 | 4.50 | 1.88 | 2.91 |
| D4/Ω | 0.22 | 0 | 3.02 | 3.71 | 3.89 |
| D5/Ω | 0.10 | 1.25 | 0.95 | 1.69 | 1.72 |
| D6/Ω | 0 | 0.96 | 0.53 | 1.38 | 2.05 |
| D7/Ω | 0 | 1.08 | 0.88 | 8.77 | 0 |
| D8/Ω | 219.10 | 6.14 | 5.10 | 22.72 | 175.90 |

Table S7 The resistance of the battery with PNC layer at different voltages

| voltage | Fresh | 2.30 V | 2.10 V | 2.03 V | 1.70 V |
| --- | --- | --- | --- | --- | --- |
| D1/Ω | 0.50 | 0.69 | 0.62 | 1.15 | 1.84 |
| D2/Ω | 0 | 0 | 0 | 0.17 | 0.52 |
| D3/Ω | 7.80 | 6.79 | 5.45 | 6.67 | 4.32 |
| D4/Ω | 5.01 | 2.72 | 2.26 | 3.15 | 2.67 |
| D5/Ω | 0.73 | 4.85 | 5.18 | 11.39 | 15.71 |
| D6/Ω | 0 | 1.23 | 0.69 | 3.26 | 3.68 |
| D7/Ω | 0 | 0.72 | 0.85 | 9.25 | 23.11 |
| D8/Ω | 303.17 | 6.48 | 7.99 | 40.70 | 100.04 |

Table S8 Comparison of the cycling performance of P/Ce-NC and different reported LSBs based on single-atom catalysts and desolvation aspects

| Materials | Rate | Cycle Number | capacity decay/ per cycle | Reference |
| --- | --- | --- | --- | --- |
| S/CoNC@ZnNC DSNCs | 1 C | 500 | 0.0.63% | Adv Mater 2024, 36, e2310547[S6] |
| CoPNC | 1 C | 600 | 0.056% | Adv. Funct. Mater. 2024, 2412279.[S7] |
| Ni-NSC SAC | 1 C | 1200 | 0.070% | Angew Chem Int Ed Engl 2024, e202418749.[S8] |
| w-PBDT | 0.5 C | 500 | 0.088% | Adv. Mater. 2024, 36, 2401473[S9] |
| TBAl3 | 0.3 C | 700 | 0.07% | Adv. Funct. Mater. 2025, 2500077[S10] |
| P/Ce-NC | 1 C | 1700 | 0.036% | This Work |

Supplementary References

- V. Wang, N. Xu, J.-C. Liu, G. Tang, W.-T. Geng, VASPKIT: a user-friendly interface facilitating high-throughput computing and analysis using VASP code. Comput. Phys. Commun. 267, 108033 (2021). https://doi.org/10.1016/j.cpc.2021.108033

- M. Chakraborty, P. Pal, B.R. Sekhar, Half metallicity in Pr0.75Sr0.25MnO3: a first principle study. Solid State Commun. 145(4), 197–200 (2008). https://doi.org/10.1016/j.ssc.2007.10.025

- C. Li, S. Qi, L. Zhu, Y. Zhao, R. Huang et al., Regulating polysulfide intermediates by ultrathin Co-Bi nanosheet electrocatalyst in lithium–sulfur batteries. Nano Today 40, 101246 (2021). https://doi.org/10.1016/j.nantod.2021.101246

- H. Shang, X. Zhou, J. Dong, A. Li, X. Zhao et al., Engineering unsymmetrically coordinated Cu-S(1)N(3) single atom sites with enhanced oxygen reduction activity. Nat. Commun. 11(1), 3049 (2020). https://doi.org/10.1038/s41467-020-16848-8

- Y. Xiong, J. Dong, Z.-Q. Huang, P. Xin, W. Chen et al., Single-atom Rh/N-doped carbon electrocatalyst for formic acid oxidation. Nat. Nanotechnol. 15(5), 390–397 (2020). https://doi.org/10.1038/s41565-020-0665-x

- L. Ren, K. Sun, Y. Wang, A. Kumar, J. Liu et al., Tandem catalysis inside double-shelled nanocages with separated and tunable atomic catalyst sites for high performance lithium-sulfur batteries. Adv. Mater. 36(14), 2310547 (2024). https://doi.org/10.1002/adma.202310547

- Y. Li, Z. Chen, X.-Y. Zhong, T. Mei, Z. Li et al., Modulating the coordination environment of co single-atom catalysts: impact on lithium-sulfur battery performance. Adv. Funct. Mater. 35(2), 2412279 (2025). https://doi.org/10.1002/adfm.202412279

- F. Zhang, Z. Tang, T. Zhang, H. Xiao, H. Zhuang et al., Electronic modulation and symmetry-breaking engineering of single-atom catalysts driving long-cycling Li−S battery. Angew. Chem. Int. Ed. 64(6), e202418749 (2025). https://doi.org/10.1002/anie.202418749

- X. Miao, C. Song, W. Hu, Y. Ren, Y. Shen et al., Achieving high-performance lithium–sulfur batteries by modulating Li+ desolvation barrier with liquid crystal polymers. Adv. Mater. 36(29), 2401473 (2024). https://doi.org/10.1002/adma.202401473

- Y. Jiang, Y. Liao, J. Yu, X. Li, T. Jin et al., Multi-effect ionic liquid additives achieve high cycle stability lithium-sulfur batteries by constructing an electrostatic shielding layer and eliminating ‘dead sulfur’. Adv. Funct. Mater. 35(32), 2500077 (2025). https://doi.org/10.1002/adfm.202500077