Supporting Information for

Ultra-Sodiophilic Mixed Conductor Interphase Enabling Uniform Top Deposition for Quasi-Solid-State Sodium Metal Batteries

Chunching Lu1, #, Guangxiang Zhang1, #, Yuxiang Niu2, Yupeng Zhu2, Siyuan Li2, Hua Huo1, Yulin Ma1, *, Pengjian Zuo1, Geping Yin1, Yunzhi Gao1, Liguang Wang3, *, Chuankai Fu1, *, and Wei Chen2, *

1State Key Laboratory of Space Power-Sources, School of Chemistry and Chemical Engineering, Harbin Institute of Technology, Harbin 150001, P. R. China

2Department of Chemistry, National University of Singapore, 3 Science Drive 3, 117543, Singapore

3College of Chemical and Biological Engineering, Zhejiang University, Hangzhou 310058, P. R. China

#Chunching Lu and Guangxiang Zhang contributed equally to this work.

*Corresponding authors.  E-mail: phycw@nus.edu.sg (Wei Chen); chuankaifu@hit.edu.cn (Chuankai Fu); mayulin@hit.edu.cn (Yulin Ma); wanglg@zju.edu.cn (Liguang Wang)

Supplementary Figures and Tables

Fig. S1 Optical photos of the Na anode surface after treatment with different concentrations of SbF3 in DME.

Optical photos indicate that the protective layer on the Na metal surface is most compact when the concentration of SbF3 is 100 mM.

Fig. S2 Cycling performance of Na||Na symmetric cells with Na anode after chemical treatment in different SbF3 concentrations at 0.1 mA cm−2.

The cycling stability of Na metal treated with 100 mM SbF3 solution is optimal.

Fig. S3 Optical photos of a 0.1 M and b 0.2 M SbF3 in DME.

The solution of 0.2 M SbF3 in DME shows a turbid state, indicating that SbF3 cannot be completely dissolved.

Fig. S4 The SEM images of the SFC-Na anode after treatment by SbF3/DME solutions with different CMC concentrations.

When the CMC content in SbF3/DME solution is 1 wt.%, the MCI layer is the densest and uniform.

Fig. S5 a Schematic diagram of adhesion experiment, b adhesion experiment of MCI layer without or with 1 wt.% CMC.

Adhesion tests show that the addition of 1 wt.% CMC effectively promotes the adhesion between the MCI layer and the Na-metal substrate.

Fig. S6 XPS spectra of C 1s on the SFC-Na surface.

C=O-OR, C-O, and other organic components generated by DME solvent can improve the flexibility of the MCI layer.

Fig. S7 XPS spectra of a F 1s and b O 1s on the F-Na surface.

Organic components and NaF are also detected on the surface of F-Na.

Fig. S8 XRD spectra of a F-Na and b SCF-Na.

XRD analysis further verifies the phase composition, with distinct diffraction peaks corresponding to NaF (PDF#70-2508) and Na₃Sb alloy (PDF#74-1162) in the surfaces of F-Na and SFC-Na anodes.

Fig. S9 The air stability of P-Na, F-Na, and SCF-Na.

Owing to the high compactness and excellent chemical stability of MCI, the SFC-Na anode can remain stable for 30 min in the air, which is superior to that of F-Na (3 min) and P-Na (5 min).

Fig. S10 Surface energies (eV/Å2) of NaF on the surface of SFC-Na.

The evolution mechanism of Na deposition on the MCI is elucidated by DFT, employing modeled NaF (001) surfaces with the lowest surface energies.

Fig. S11 Surface energies (eV/Å2) of Na3Sb on the surface of SFC-Na.

The evolution mechanism of Na deposition on the MCI is elucidated by DFT, employing modeled Na3Sb (110) surfaces with the lowest surface energies.

Fig. S12 DFT simulations of Na+ diffusion in NaF a and Na atom diffusion in Na3Sb b.

The Na+ diffusion energy barrier in NaF is much higher than Na atom diffusion energy barrier in Na3Sb, demonstrating the significant role of Na3Sb in promoting electrochemical kinetics.

Fig. S13 The band gap of a NaF and b Na3Sb.

NaF in MCL exhibits high electron blocking ability, which can effectively prevent electron tunneling, while Na3Sb phase can improve electron conductivity, achieve rapid electron transfer, and avoid charge accumulation.

Fig. S14 Ring-opening polymerization mechanism of DOL.

The polymerization mechanism involves a Lewis acid PF5– species derived from NaPF6, which reacts with trace water to generate protons that initiate the ring-opening polymerization of DOL.

Fig. S15 a 13C NMR and b 1H NMR spectra before and after DOL polymerization. c GPC spectrum of DGPE.

DOL was polymerized successfully, achieving a polymerization degree of 89.7% and number-average and weight-average molecular weight of 5,149 g mol-1 and 27,616 g mol-1, respectively.

Fig. S16 The impedance of Na||Na symmetric cells under different storage times before cycling.

After long-term storage, the impedance of Na||Na symmetric cells remain almost unchanged, proving the good compatibility between DGPE and SFC-Na.

Fig. S17 Nyquist plots of a P-Na, b F-Na, and c SFC-Na in the Na||Na symmetric cells at different temperatures after 5 cycles.

The impedances of Na+ transport across the SEI (RSEI) layer and charge-transfer (Rct) at different temperatures are further measured by EIS to reflect the superiority of the MCI in inducing the construction of the stable and robust SEI layer and interfacial Na+ migration.

Fig. S18 Equivalent circuit of impedance fitting.

The EIS values are fitted by the corresponding equivalent circuit.

Fig. S19 Impedance values of a RSEI and b Rct.

The RSEI and Rct of quasi-solid-state symmetrical cells with SFC-Na anodes are markedly lower than those of cells with P-Na or F-Na anodes, demonstrating clear superiority.

Fig. S20 Galvanostatic long-term discharging performance of Na||Na symmetric cells with P-Na, F-Na, and SFC-Na anodes.

The cells with P-Na and SF-Na stabilized for only 2 h and 8 h, respectively, before short circuit, whereas the SFC-Na cell maintained a stable voltage plateau at 80 mV for 22 h, demonstrating effective suppression of Na dendrite growth.

Fig. S21 Cycling performance of Na||Na symmetric cells with SFC-Na anode with different CMC contents at 0.5 mA cm−2.

The Na||Na symmetric cells with an SFC-Na anode consisting of 1wt.% CMC exhibits the best cycling stability.

Fig. S22 Cycling performance of Na||Na symmetric cells with SFC-Na anode at 2.0 mA cm−2.

Even at a higher current density of 2 mA cm⁻2, the SFC-Na cells can stably cycle for 180 h without short circuit.

Fig. S23 Correlation between Z-real and ω-1/2 for P-Na, F-Na and SFC-Na anodes.

The construction of the MCI enhances the Na⁺ diffusion coefficient, thereby mitigating the concentration gradient across the corresponding SEI layer and promoting a more uniform distribution of Na⁺ during migration and stripping.

Fig. S24 The images of a P-Na, b F-Na, and c SFC-Na show the 2D distribution of the local electric field at t = 10 s.

The corresponding two-dimensional distributions of Na⁺ concentration and the local electric field reveal Na+ accumulation near the protrusion tip, where an intensified local electric field further accelerates dendritic growth.

Fig. S25 Cross-sectional SEM images of SFC-Na anode: a initial state and b after 200 cycles.

After long-term cycling, the MCI layer remains firmly adhered to the Na metal surface.

Fig. S26 The SME images of the deposited Na on the P-Na, F-Na, and SFC-Na surfaces at 0.5 mA cm-2 for 5 h and 10 h.

Driven by the strong Na+ affinity of SFC-Na, the Na metal deposited on its surface exhibits a smoother morphology.

Fig. S27 Comparison of the morphology of Na3V2(PO4)3 (NVP) cathode before a and after gelation e, with corresponding surface EDX mappings shown in b-d, f-h, respectively.

SEM images and elemental mappings of the pristine NVP cathode reveal a granular morphology with uniformly distributed F and V elements, indicating a homogeneous distribution of the active material and electrolyte.

Fig. S28 Optical photo a and cycling performance b of SFC-Na||NVP pouch cell with a capacity of ~200 mAh.

The 200 mAh pouch cell based on SFC-Na anode and NVP cathode delivers stable capacity retention and high Coulombic efficiency over 40 cycles at 1C.

Table S1 Surface energy (eV Å-2) of different crystal surfaces of NaF and Na3Sb

| NaF |  | Na3Sb |  |
| --- | --- | --- | --- |
| Surface | Surface energy (eV) | Surface | Surface energy (eV) |
| (001) | 0.016 | (001) | 0.052 |
| (001) | 0.037 | (110) | 0.021 |
| (111) top-F | 0.186 | (010) | 0.033 |
| (111) top-Na | 0.186 |  |  |

Table S2 Comparison of the lifespan of the SFC-Na anode with the reported works

| Artificial interphase | Electrolyte | Test conditions | Cycle life (hours) | Refs. |
| --- | --- | --- | --- | --- |
| Al2O3-Na | 1 M NaClO4-EC/DEC | 0.5 mA cm-2/1 mAh cm-2 | 120 | [9] |
| Multilayer-MoS2-Na | 1 M NaClO4-EC/DEC | 0.5 mA cm-2/0.25 mAh cm-2 | 100 | [33] |
| NaBr-Na | 1 M NaPF6-EC/PC | 1 mA cm-2/1 mAh cm-2 | 250 | [34] |
| NaxSny-Na | 1 M NaPF6-EC/PC | 0.5 mA cm-2/0.25 mAh cm-2 | 1000 | [35] |
| Na3PS4-Na | 1M NaPF6-EC/PC | 1 mA cm-2/ 1 mAh cm-2 | 275 | [36] |
| NaxSny-Na | 1 M NaPF6-EC/DMC | 0.25 mA cm-2/0.125 mAh cm-2 | 600 | [37] |
| NaCl-Na | 1 M NaClO4-EC/DMC | 0.3 mA cm-2/ 0.3 mAh cm-2 | 1000 | [38] |
| ZMOF-NSC@Na | 1M NaFSI-EC/PC | 0.5 mA cm-2/ 0.5 mAh cm-2 | 900 | [39] |
| Na3P-Na | 1 M NaClO4- EC/DEC/FEC | 1 mA cm-2/1 mAh cm-2 | 500 | [40] |
| SFC-Na | 1M NaPF6- DOL/DME/FEC | 0.5 mA cm-2/0.5 mAh cm-2 | 1000 | This work |

Table S3 Surface energy (eV Å-2) of different crystal surfaces of NaF and Na3Sb

| Components of electrolytes | Test conditions | Cycle life | Capacity retention | Refs. |
| --- | --- | --- | --- | --- |
| DOL/Al(OTf)3/NaTFSI/FEC | NVP loading: 1.12 mg cm-2 Rate: 0.5C | 600 | 96.7% | [1] |
| TMPTA/NaPF6/EC/DEC /FEC | NVP loading: 13.01 mg cm-2 Rate: 1C | 1000 | ~80% | [3] |
| PEGMA/TEP/NaTFSI/FEC/ AIBN | NVP loading: - mg cm-2 Rate: 0.2C | 400 | 91% | [5] |
| PEGMA/TEP/NaTFSI/ PVDF-HFP/FEC | NVP loading: 1.2 mg cm-2 Rate: 1C | 500 | 91.7% | [46] |
| BA/NaPF6/DEC/EC/AIBN | NVP loading: 1.5 mg cm-2 Rate: 1C | 300 | 83% | [47] |
| HMPP/ETPTA/NaClO4/ PC/FEC | NVP loading: 1 mg cm-2 Rate: 5C | 1000 | 97% | [48] |
| EA/EDA/NaPF6/SN/ PPO/FEC | NVP loading: 3 mg cm-2 Rate: 3C | 700 | 83.3% | [49] |
| PAN | NVP loading: 2.1mg cm-2 Rate: 1C | 1600 | 96.03% | [50] |
| PEGDA/PVDF-HFP/ NaTFSI/NaBOB/PC/EC | NVP loading: 1.8 mg cm-2 Rate: 2C | 500 | / | [51] |
| TMPTMA/HDDA/NaTFSI/ ABVN/FEC/DMC/PC | NVP loading: 0.891 mg cm-2 Rate: 2C/5C | 700/1000 | 95.58/95.31% | [52] |
| DOL/DME/NaPF6/FEC | NVP loading: 2 mg cm-2 Rate: 2C/5C | 2000/1100 | 93.7%/94.3% | This work |

Table S4 Electrochemical performance of full cells with various alloy anodes and SFC-Na

| Cathode | Anode | Cycle life | Rate | Capacity retention | Anode reaction mechanism | Refs. |
| --- | --- | --- | --- | --- | --- | --- |
| NaxFe[Fe(CN)6] | Na-Au alloy | 300 cycles | 1C | 85.7% | Alloying | [53] |
| Na4Fe3(PO4)2 | Na-K/C alloy | 200 cycles | 1C | 94.6% | Alloying | [54] |
| Na3V2(PO4)3 | Na-Bi alloy | 1000 cycles | 5C | 90% | Alloying | [55] |
| Na3V2O2(PO4)2F | Na-In/C alloy | 800 cycles | 1C | 87.6% | Alloying | [56] |
| Na3V2(PO4)3 | Sb/GO | 50 | 1.5C | 81.3% | Alloying | [57] |
| Na3V2(PO4)3 | Sb@HCF | 1000 | 1C | 84.1 | Alloying | [58] |
| Na3V2(PO4)3 | SFC-Na | 3000 cycles | 2C | 92.2% | Surface-induced “top” Na deposition | This work |
|  |  | 1100 cycles | 5C | 94.3% |  |  |