Supporting Information for

Multifunctional Conductive and Elastic Matrices–Engineered Si Nanocomposite Anodes for Liquid and Solid-State Lithium Batteries

Young-Han Lee1,2, Je-Hyeon Han1,2, Deok-Gyu Kim1,2, Jung-Woon Yoo1,2, Yoon-Cheol Ha3,4*, Jae-Hun Kim5*, and Cheol-Min Park1,2*

1 Department of Advanced Materials Science and Engineering, Kumoh National Institute of Technology, Gumi, Gyeongbuk 39177, Republic of Korea

2 Department of Energy Engineering Convergence, Kumoh National Institute of Technology, Gumi, Gyeongbuk 39177, Republic of Korea

3 Battery Research Division, Korea Electrotechnology Research Institute (KERI), Changwon, Gyeongnam 51543, Republic of Korea

4 Electric Energy Materials Engineering, KERI School, University of Science and Technology (UST), Daejeon 34113, Republic of Korea

5 School of Materials Science and Engineering, Kookmin University, Seoul 02707, Republic of Korea

*Corresponding authors. E-mail: cmpark@kumoh.ac.kr (Cheol-Min Park)； jaehunkim@kookmin.ac.kr (Jae-Hun Kim)；ycha@keri.re.kr (Yoon-Cheol Ha)

Supplementary Figures and Tables

Fig. S1 Schematic illustration of the ASSLB cell configuration used for electrochemical testing

Fig. S2 Structural and electrochemical comparison of Si/M (M = Al, Zn, Sn) composites prepared under identical high-power MM conditions with 10 wt% metal incorporation. XRD patterns of a Si/Al-10, b Si/Zn-10, and c Si/Sn-10 composites. Voltage profiles of d Si/Al-10, e Si/Zn-10, and f Si/Sn-10 composites during the first cycle

Fig. S3 Average size of Si crystallites in Si/Sn-10 composites calculated using the Scherrer equation

Fig. S4 Schematic illustration of the nanoindentation test setup

Fig. S5 Morphological characteristics of the Si/a-Sn/TMS composites. PSA results for a Si/a-Sn/FeSi2, c Si/a-Sn/CoSi2, and e Si/a-Sn/NiSi2. SEM images of b Si/a-Sn/FeSi2, d Si/a-Sn/CoSi2, and f Si/a-Sn/NiSi2

Fig. S6 XRD pattern of the Si/CoSi2 composite synthesized via high-power MM

Fig. S7 Electrochemical performance results for the Si/CoSi2 composite. a Galvanostatic voltage profiles of the Si/CoSi2 composite anode. b Long-term cycling performance of the Si/CoSi2 composite anode (current density: 300 mA g–1)

Fig. S8 Microstructural characteristics of the Si/a-Sn/FeSi2 composite: a BFTEM image, b HRTEM image with SAED pattern, c FFT patterns for selected regions, and d STEM image with EDX elemental mappings

Fig. S9 Microstructural characteristics of the Si/a-Sn/NiSi2 composite: a BFTEM image, b HRTEM image with SAED pattern, c FFT patterns for selected regions, and d STEM image with EDX elemental mappings

Fig. S10 Average sizes of Si crystallites in Si/a-Sn/TMS composites calculated using the Scherrer equation: a Si/a-Sn/FeSi2, b Si/a-Sn/CoSi2, and c Si/a-Sn/NiSi2

Fig. S11 Structural characteristics of the high-power MM-derived TMS phases. XRD patterns of high-power MM-derived a FeSi2, b CoSi2, and c NiSi2

Fig. S12 Electronic conductivity measurements of high-power MM-derived TMS phases (FeSi2, CoSi2, and NiSi2). a Schematic illustration of the SUS|TMS pellet|SUS symmetric cell configuration used to measure electronic conductivity. b I–V profiles of the TMS phases measured in the symmetric cell. c Electronic conductivities calculated from the slopes of the I–V curves

Fig. S13 Load–displacement profiles obtained from nanoindentation tests on the high-power MM-derived TMS particles: a FeSi2, b CoSi2, and c NiSi2

Fig. S14 Voltage profiles of TMS anodes measured at a current density of 100 mA g–1. a FeSi2, b CoSi2, and c NiSi2

Fig. S15 Morphological characteristics of the Si/a-Sn/CoSi2/G composite: a PSA result and b SEM image

Fig. S16 Load–displacement profile obtained from a nanoindentation test on an MCMB graphite particle

Fig. S17 TGA curve of PVC under an N2 atmosphere

Fig. S18 Electrochemical performance results for the PVC-pyrolyzed carbon anode: a voltage profiles and b cycling performance of the PVC-pyrolyzed carbon anode tested at 100 mA g–1

Fig. S19 I–V profile of the PVC-pyrolyzed C and the corresponding calculated electronic conductivity

Fig. S20 Morphological characteristics of the Si/a-Sn/CoSi2/G/C nanocomposite: a PSA result and b SEM image

Fig. S21 XRD pattern of the PVC-pyrolyzed carbon obtained by thermal pyrolysis at 700 °C under an Ar atmosphere

Fig. S22 Raman spectra of the pristine Si and Si/a-Sn/CoSi2/G/C nanocomposite in the range of 400–600 cm–1

Fig. S23 Voltage profiles of the commercial graphite anode tested at 100 mA g–1

Fig. S24 CV profiles of Si, Sn, graphite, PVC-pyrolyzed amorphous carbon, and the Si/a-Sn/CoSi2/G/C nanocomposite anode measured at a scan rate of 3 mV s–1 over a voltage range of 0.01–2.0 V (vs. Li+/Li)

Fig. S25 Ex situ XRD patterns of the Si/a-Sn/CoSi2/G/C anode at the pristine state, fully lithiated state (0.01 V), and delithiated state (2.0 V)

Fig. S26 Phase evolution of the Sn reference anode at the pristine state, fully lithiated state (0.01 V), and delithiated state (2.0 V). a Ex situ XRD patterns and b ex situ Sn K-edge EXAFS spectra

Fig. S27 Ex situ Sn K-edge EXAFS spectra of the Si/a-Sn/CoSi2/G/C anode at the pristine state, fully lithiated state (0.01 V), and delithiated state (2.0 V)

Fig. S28 Ex situ EIS analysis of the Si/a-Sn/CoSi2/G/C anode after 10, 50, and 100 cycles. a Experimental Nyquist plots. b Equivalent circuit fitting of the impedance spectra using an Rs–(Rint||CPEint)–(Rct||CPEct)–W model. c Evolution of Rint and Rct extracted from the fitting

Fig. S29 N2 adsorption–desorption isotherms of a pristine Si, b Si/Sn-10, c Si/a-Sn/CoSi2, d Si/a-Sn/CoSi2/G, and e Si/a-Sn/CoSi2/G/C composites

Fig. S30 OM images and photographs showing changes in the thicknesses of pristine Si, Si/Sn, Si/a-Sn/CoSi2, Si/a-Sn/CoSi2/G, and Si/a-Sn/CoSi2/G/C anodes in the fully discharged (0 V vs. Li+/Li) and fully charged (2 V vs. Li+/Li) states

Fig. S31 Voltage profiles of the graphite|NCM811 full cell measured at various current densities from 0.1 to 5 C with a cathode loading of 15.5 mg cm–2

Fig. S32 Voltage profiles of the Si/a-Sn/CoSi2/G/C|NCM811 full cells during the initial activation cycle at 0.1 C with cathode loadings of a 15.3 mg cm–2 and b 12.7 mg cm–2

Fig. S33 Comparison of the electrochemical performance of the Si/a-Sn/CoSi2/G/C|NCM811 full cell with those of previously reported Si-based full cells

Fig. S34 Photograph of three commercial green LED bulbs (3 V) powered by the Si/a-Sn/CoSi2/G/C|NCM811 full cell

Fig. S35 Structural characteristics and ionic conductivity of argyrodite LPSC SE: a XRD pattern and b ionic conductivity measured by DC polarization in an electron-blocking symmetric cell (DC bias: 50 mV)

Fig. S36 Structural characterization of the Si/a-Sn/CoSi2/G/C nanocomposite after pressing under 375 MPa for ASSLB assembly. a BFTEM image, b HRTEM image with the corresponding SAED pattern (inset), and c STEM image with the corresponding EDX elemental mappings of Si/a-Sn/CoSi2/G/C

Fig. S37 Schematic illustration of the ASSLB half-cell configuration

Fig. S38 Electrochemical comparison of Si/a-Sn/CoSi2 and Si/a-Sn/CoSi2/G/C anodes in sulfide-based ASSLB half cells. Voltage profiles of a Si/a-Sn/CoSi2 and b Si/a-Sn/CoSi2/G/C anodes. c Cycling performance of Si/a-Sn/CoSi2 and Si/a-Sn/CoSi2/G/C anodes at a current density of 300 mA g–1

Fig. S39 Electrochemical performances of the Si|LPSC|NCM811 and Si/a-Sn/CoSi2/G/C|LPSC|NCM811 full cells: a voltage profiles of the Si/a-Sn/CoSi2/G/C|LPSC|NCM811 and b Si|LPSC|NCM811 full cells at a current density of 0.3 C (cathode loading: 14.7 mg cm–2, temperature: 60 °C)

Fig. S40 EDX elemental mapping of the Si/a-Sn/CoSi2/G/C anode before cycling in an ASSLB

Fig. S41 EDX elemental mapping of the Si/a-Sn/CoSi2/G/C anode after 100 cycles in an ASSLB

Table S1 Electrochemical performance of pristine Si and Si/Sn composite anodes with varying Sn contents

| Materials | Initial discharge capacity (mAh g–1) | Initial charge capacity (mAh g–1) | Initial Coulombic efficiency (%) | Capacity retention after 30 cycles (%) |
| --- | --- | --- | --- | --- |
| Pristine Si | 3916.2 | 3275.4 | 83.6 | 3.9 |
| Si/Sn-5 | 3582.4 | 3167.9 | 88.4 | 25.0 |
| Si/Sn-10 | 3384.3 | 3129.2 | 92.5 | 33.2 |
| Si/Sn-15 | 3332.6 | 3049.8 | 91.5 | 33.8 |
| Si/Sn-20 | 3262.1 | 2955.7 | 90.6 | 34.0 |

Table S2 Electrochemical performance of Si/a-Sn/TMS composite anodes

| Materials | Initial discharge capacity (mAh g–1) | Initial charge capacity (mAh g–1) | Initial Coulombic efficiency (%) | Capacity retention after 30 cycles (%) |
| --- | --- | --- | --- | --- |
| Si/a-Sn/FeSi2 | 2024.0 | 1763.1 | 87.1 | 74.6 |
| Si/a-Sn/CoSi2 | 1961.7 | 1771.5 | 90.3 | 83.2 |
| Si/a-Sn/NiSi2 | 2051.6 | 1756.9 | 85.6 | 74.9 |

Table S3 Plastic and elastic deformation energies of Si and high-power MM-derived TMS particles derived from the load-displacement profiles

| Materials | Plastic deformation energy (10–10 J) | Elastic deformation energy (10–10 J) | Total deformation energy (10–10 J) |
| --- | --- | --- | --- |
| Si | 30.372 | - | 30.372 |
| FeSi2 | 118.099 | 41.378 | 159.477 |
| CoSi2 | 121.098 | 56.869 | 177.967 |
| NiSi2 | 97.710 | 41.246 | 138.956 |

Table S4 Comparison of the electrochemical performance of the Si/a-Sn/CoSi2/G/C anode with previously reported Si/TMS-based anodes for LIBs

| Materials | ICE (%) | Current density (mA g-1) | Reversible capacity after Xth cycle (mAh g-1) | Capacity retention (%) | Electrolyte | Refs. |
| --- | --- | --- | --- | --- | --- | --- |
| Si/TiSi2 heterostructure | 59.4 | 1300 | 937 (X=100) | 79.3 | 1.0 M LiPF6 (EC/DEC) | [18] |
| Si@TiSi2@NC | 83 | 200 | 1553.3 (X=100) | 71.5 | 1.0 M LiPF6 (EC/DEC+5wt%FEC) | [19] |
| Porous Si@TiSi2 | 74.5 | 400 | 1180 (X=50) | 66.3 | 1.5 M LiPF6 (EC/DEC+25vol%FEC) | [20] |
| Si/FeSi2/CrSi2 | 86 | 1000 | 841 (X=100) | 87.9 | 1.0 M LiPF6 (EC/DEC+25vol%FEC) | [21] |
| Si-FeSi2-G-C | 87.0 | 100 | 925 (X=80) | 88.5 | 1 M LiPF6 (EC/DEC+10wt%FEC) | [22] |
| Si/FeSi2@C NPs | 87.6 | 200 | 1375 (X=100) | 56.1 | 1.0 M LiPF6 (EC/DEC/EMC+FEC) | [23] |
| Si/Co-CoSi2/rGO | 77.9 | 100 | 921.8 (X=80) | 98.6 | 1.3 M LiPF6 (EC/DMC) | [24] |
| Si@CoSi2/Co-NPC@CNT | 76.1 | 200 | 1258 (X=100) | 74.6 | 1.0 M LiPF6 (EC/DEC+5wt%FEC) | [25] |
| Si-NiSi2-Al2O3@C | 74.3 | 200 | 680 (X=100) | 94.4 | 1 M LiPF6 (EC/DEC+30vol%FEC) | [26] |
| Si/NiSi2/C | 76.9 | 200 | 1827.7 (X=50) | 87.6 | 1 M LiPF6 (EC/DMC+2wt%FEC) | [27] |
| Si/NiSi2/C | 78 | 1000 | 1500 (X=100) | 79.8 | 1 M LiPF6 (EC/DMC+2wt%FEC) | [27] |
| Cu-Si alloy nanotube | 42 | 840 | 1670 (X=100) | 77.6 | 1.0 M LiPF6 (EC/DEC) | [35] |
| Cu-Si alloy nanotube | 37 | 1600 | 1380 (X=100) | 77.1 | 1.0 M LiPF6 (EC/DEC) | [35] |
| Cu-Si alloy nanotube | 33 | 3200 | 1210 (X=100) | 76.2 | 1.0 M LiPF6 (EC/DEC) | [35] |
| Cu3Si/Si | 88.9 | 200 | 1675.4 (X=100) | 66.2 | 1.0 M LiPF6 (EC/DMC/EMC+5vol%FEC) | [36] |
| Si/Cu3Si/Al2O3 | 76 | 200 | 750 (X=100) | 89.2 | 1 M LiPF6 (EC/DMC+5vol%FEC) | [37] |
| Si-Cu3Si-CNT/G-C | 82.8 | 200 | 1084 (X=100) | 87.6 | 1.0 M LiPF6 (EC/DEC+10wt%FEC) | [38] |
| Cu9Si/Si NWs | 52.4 | 200 | 655.5 (X=100) | 55.6 | 1.0 M LiPF6 (EC/DMC/EMC+5vol%FEC) | [39] |
| Si/TiFeSi2 | 80 | 200 | 930 (X=100) | 93 | 1.3 M LiPF6 (EC/DEC+2%FEC) | [40] |
| Si/a-Sn/CoSi2/G/C | 80.7 | 300 | 1147.4 (X=100) | 91.4 | 1.3 M LiPF6 (EC/DEC+10 wt%FEC) | This work |

Table S5 Comparison of the energy densities of graphite|NCM811 and Si/a-Sn/CoSi2/G/C|NCM811 full cells at various current densities

| Anode material | Mass of anode (mg) | Mass of AAM (mg) | Mass of separator (mg) | Mass of cathode (mg) | Mass of NCM811 (mg) | Current density (mA g–1) | Specific capacity (mAh g–1) | Average voltage (V) | Energy (Wh) | Energy density (Wh kg–1) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Graphite | 8.61 | 6.89 | 1.76 | 15.23 | 12.18 | 18 | 179.0 | 3.63 | 0.00791 | 309.1 |
|  |  |  |  |  |  | 90 | 152.5 | 3.56 | 0.00661 | 258.3 |
|  |  |  |  |  |  | 180 | 140.2 | 3.54 | 0.00605 | 236.1 |
|  |  |  |  |  |  | 360 | 124.8 | 3.52 | 0.00535 | 209.0 |
|  |  |  |  |  |  | 540 | 112.2 | 3.50 | 0.00478 | 186.8 |
|  |  |  |  |  |  | 900 | 88.1 | 3.46 | 0.00371 | 145.0 |
| Si/a-Sn /CoSi2/G/C | 2.87 | 2.01 | 1.76 | 15.23 | 12.18 | 18 | 187.4 | 3.78 | 0.00863 | 434.4 |
|  |  |  |  |  |  | 90 | 175.5 | 3.62 | 0.00774 | 389.6 |
|  |  |  |  |  |  | 180 | 174.2 | 3.54 | 0.00751 | 378.2 |
|  |  |  |  |  |  | 360 | 163.6 | 3.45 | 0.00687 | 346.2 |
|  |  |  |  |  |  | 540 | 151.9 | 3.37 | 0.00623 | 313.9 |
|  |  |  |  |  |  | 900 | 139.7 | 3.31 | 0.00563 | 283.6 |

Table S6 Comparison of the electrochemical performance of the Si/a-Sn/CoSi2/G/C|NCM811 full cell with previously reported Si-based full cells

| Anode | Cathode | Discharge capacity after Xth cycles (mAh g–1) | Current density (mA g–1) | Capacity retention (%) | Refs |
| --- | --- | --- | --- | --- | --- |
| carbon-coated Si nanosheets | LCO | 111.3 (X=50) | 70 | 80 | [17] |
| Si@TiSi2@NC | NCM622 | 143.9 (X=50) | 80 | 80.2 | [19] |
| Si-Cu3Si-Al2O3 | LMO | 70 (X=50) | 60 | 77.2 | [37] |
| Amorphous Columnar Si | NCM622 | 125 (X=50) | 36 | 70 | [41] |
| Amorphous Columnar Si | NCM811 | 142 (X=50) | 42 | 67 | [41] |
| Si@N-ECGB | NCM811 | 140 (X=100) | 140 | 84 | [42] |
| Si submicroncube@C | LFP | 122 (X=100) | 85 | 85.3 | [43] |
| Si-graphite | NCM523 | 119.3 (X=100) | 60 | 71 | [44] |
| Si/SiO2 | LCO | 149 (X=50) | 150 | 90 | [45] |
| Ag/ZnO-Si@C-PCNF | NCM513 | 135 (X=50) | 30 | 100 | [46] |
| Fe14Si86/C | NCM111 | 79 (X=150) | 75 | 54.1 | [47] |
| Fe25Si75 | NCM111 | 109 (X=150) | 75 | 77 | [47] |
| Si p-NS@TNS | LFP | 138 (X=80) | 100 | 95.2 | [48] |
| Si@graphene cage | LCO | 88 (X=30) | 135 | 87 | [49] |
| Si@CMR | NCM622 | 151.3 (X=100) | 90 | 90 | [50] |
| Si@CMR | NCM622 | 110.2 (X=100) | 180 | 85 | [50] |
| Si@C@MoS2 | LCO | 136.1 (X=60) | 150 | 91.7 | [51] |
| Si/a-Sn/CoSi2/G/C | NCM811 | 137.1 (X=100) | 180 | 81.2 | This work |
| Si/a-Sn/CoSi2/G/C | NCM811 | 130.9 (X=100) | 540 | 89.2 | This work |

Table S7 Energy density calculation of the Si/a-Sn/CoSi2/G/C|LPSC|NCM811 ASSLB full cell

| Mass of anode (mg) | 2.83 |
| --- | --- |
| Mass of Si/a-Sn/CoSi2/G/C (mg) | 1.98 |
| Mass of 30 µm-thick LPSC SE (mg) | 4 |
| Mass of cathode (mg) | 15.60 |
| Mass of NCM811 (mg) | 12.01 |
| Current density (mA g–1) | 18 |
| Specific capacity (mAh g–1) | 162.1 |
| Average voltage (V) | 3.47 |
| Energy (Wh) | 0.00676 |
| Energy density (Wh kg–1) | 301.2 |

Table S8 Comparison of the electrochemical performance of the Si/a-Sn/CoSi2/G/C|LPSC|NCM811 ASSLB full cell with previously reported Si-based ASSLB full cells

| Anode | Cathode | Solid electrolyte | Cathode loading (mg cm–2) | Stack pressure (MPa) | Operating temp. (°C) | Current density (mA cm–2) | Areal capacity (mAh cm–2) | Refs. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| μm-Si | NCM111 | Li3PS4 | 18.3 | 75 | 30 | 0.15 | 2.20 | [53] |
|  |  |  |  |  |  | 0.3 | 1.83 |  |
|  |  |  |  |  |  | 0.75 | 1.28 |  |
|  |  |  |  |  |  | 1.5 | 0.64 |  |
|  |  |  |  |  |  | 3.0 | 0.27 |  |
|  |  |  |  |  |  | 4.5 | 0.15 |  |
|  |  |  |  |  |  | 6.0 | 0.07 |  |
| Li6PS5Cl-infiltrated Si | LCO | Li6PS5Cl | 10.0 | 140 | 30 | 0.14 | 1.04 | [54] |
|  |  |  |  |  |  | 0.28 | 0.90 |  |
| Si-SE-CB | NCM811 | Li6PS5Cl | 7.93 | 50 | 25 | 0.08 | 1.49 | [55] |
|  |  |  |  |  |  | 0.16 | 1.41 |  |
|  |  |  |  |  |  | 0.32 | 1.28 |  |
|  |  |  |  |  |  | 0.79 | 1.13 |  |
|  |  |  |  |  |  | 1.58 | 1.03 |  |
| Si-SE-C | NCM811 | Li5.4PS4.4Cl1.6 | 14.88 | 150 | 25 | 0.15 | 1.99 | [56] |
|  |  |  |  |  |  | 0.30 | 1.74 |  |
|  |  |  |  |  |  | 0.60 | 1.46 |  |
|  |  |  |  |  |  | 1.49 | 1.01 |  |
|  |  |  |  |  |  | 2.98 | 0.67 |  |
| Si | NCM811 | Li3PS4 | 13.6 | 75 | 30 | 0.15 | 1.77 | [57] |
|  |  |  |  |  |  | 0.30 | 1.49 |  |
|  |  |  |  |  |  | 0.75 | 1.16 |  |
|  |  |  |  |  |  | 1.5 | 0.84 |  |
|  |  |  |  |  |  | 3.0 | 0.48 |  |
|  |  |  |  |  |  | 4.5 | 0.27 |  |
|  |  |  |  |  |  | 6.0 | 0.14 |  |
| Col-Si | N90C5M5 | Li6PS5Cl | 12.9 | 3 N·m | 25 | 0.07 | 1.95 | [58] |
|  |  |  |  |  |  | 0.45 | 1.72 |  |
|  |  |  |  |  |  | 0.75 | 1.63 |  |
|  |  |  |  |  |  | 1.5 | 1.54 |  |
| Si@MOF | LFP | PVDF/PEO/ garnet | 15.4 | N/A | 60 | 0.1 | 2.20 | [59] |
|  |  |  |  |  |  | 0.2 | 1.40 |  |
|  |  |  |  |  |  | 0.5 | 0.80 |  |
|  |  |  | 20.2 | N/A | 60 | 0.1 | 2.60 |  |
|  |  |  |  |  |  | 0.2 | 1.80 |  |
|  |  |  |  |  |  | 0.5 | 1.10 |  |
| C-Li1Si-60 | NCM811 | Li6PS5Cl | 10.2 | 60 | 30 | 0.10 | 2.00 | [60] |
|  |  |  |  |  |  | 0.20 | 1.80 |  |
|  |  |  |  |  |  | 0.61 | 1.60 |  |
|  |  |  |  |  |  | 1.02 | 1.40 |  |
|  |  |  |  |  |  | 2.04 | 1.20 |  |
|  |  |  |  |  |  | 6.12 | 0.75 |  |
| In-Si | NCM90 | Li5.5PS4.5Cl1.5 | 8.75 | 50 | 55 | 1.23 | 1.08 | [61] |
|  |  |  |  |  |  | 4.92 | 0.94 |  |
|  |  |  |  |  |  | 7.38 | 0.86 |  |
| Li21Si5/ Si-Li21Si5 | LCO | Li3InCl6/ Li6PS5Cl | 23.4 | 0 | 45 | 0.6 | 2.32 | [62] |
|  |  |  |  |  |  | 1.3 | 1.85 |  |
|  |  |  |  |  |  | 2.5 | 1.46 |  |
|  |  |  |  |  |  | 3.8 | 1.23 |  |
|  |  |  |  |  |  | 5.0 | 1.01 |  |
|  |  |  |  |  |  | 6.3 | 0.79 |  |
|  |  |  |  |  |  | 7.6 | 0.57 |  |
| Si/a-Sn /CoSi2/G/C | NCM811 | Li6PS5Cl | 15.3 | 40 | 60 | 0.28 | 2.48 | This work |
|  |  |  |  |  |  | 0.55 | 2.32 |  |
|  |  |  |  |  |  | 1.38 | 2.02 |  |
|  |  |  |  |  |  | 1.93 | 1.82 |  |
|  |  |  |  |  |  | 2.75 | 1.63 |  |
|  |  |  |  |  |  | 5.50 | 1.38 |  |
|  |  |  |  |  |  | 8.25 | 1.13 |  |