Supplementary information 1

Supplementary Table 1. A summary of the XCT scanning parameters
	Part identifier
	Voxel size (µm3) 
	Voltage (kV)
	Current (µA)
	Integration time (ms)
	Number of projections
	Number of images averaged/projection

	B1
	24.986
	100
	90
	1000
	1000
	3

	B2
	30.06
	100
	90
	1000
	1000
	3

	T1+B3
	30.87
	100
	90
	1000
	1000
	3

	T2+B4
	30.06
	100
	90
	1000
	1000
	3

	T3+B5
	30.06
	100
	90
	1000
	1000
	3

	T4+b6
	30.06
	100
	90
	1000
	1000
	3
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Supplementary Figure S1. Virtual machining analysis for section B5+T3 and B6+T4 (sections stitched) along the length. Scale bar corresponds to 5 mm.
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