Supplementary Material

The application of tannic acid-coated magnetite nanoparticles for recovery of microplastics from the water system

Amoudjata Sacko*a, Jemal Fito Nurea, Hlengilizwe Nyonib, Bhekie Mambaa, Thabo Nkambulea, Titus A.M. Msagatia*

aInstitute of Nanotechnology and Water Sustainability Research Unit, College of Science, Engineering, and Technology, University of South Africa, Florida Campus, 1709, Johannesburg, South Africa

bInstitute for Energy and Environmental, Pennsylvania State University, University Park, PA 16802, United States

*Corresponding authors Emails: 58563237@mylife.unisa.ac.za, +27 71 13 69 6 91 (Amoudjata Sacko) and msagatam@unisa.ac.za, +27 72 31 10 693  (Titus A.M. Msagati)

Figure S1. The schematic representation of PS and PET microplastics

Figure S2. Images of nano adsorbents (a) magnetite and (b) tannic acid-coated magnetite

Figure S3. Measurement of the zetasizer nano range size adsorbents distribution of tannic acid-coated magnetite

Table S1. Concentrations of interfering species

| Ions |  | Concentration (mg/L) |
| --- | --- | --- |
| Chloride (Cl-) | 292 |
| Sulfate (SO42-) | 710 |
| Carbonate (CO32-) | 530 |
| Phosphate (PO43-) | 710 |
| Nitrate (NO3-) | 425 |
| Humic acid (DOM) | 20 |

Kinetic and isotherm studies

lnqe-qt=lnqe-k1t                                                     (S1)

tqt=1k2qe  2+ tqe                                                                        (S2)

Where k1 and k2 represent the rate constants of the pseudo-first-order and pseudo-second-order kinetic models respectively, t is the reaction time (min), and qe (mg/mg) and qt are the MPs adsorption quantity adsorbed at equilibrium and at the time t respectively.

Langmuir:   Ceqe=1qmCe+ 1qmkl                                 (S3)

Freundlich:   lnqe=lnkF+ 1nlnCe                         (S4)

Where Ce (mg) and qe (mg/mg) represent the mass of MPs at equilibrium and the adsorption capacity at equilibrium respectively, qm (mg/mg) is the maximum adsorption capacity of the adsorbent, kL is the Langmuir constant, kF is the Freundlich constant and n represents the adsorption strength constant.