# Supplementary Information

Dual-mode Colorimetric and Fluorescent Detection of Tumor Cells Based on Gold Nanoparticles-Loaded Phosphine Covalent Organic Frameworks

Bilian Li1 · Min Zhou1 · Chun Zhao2 · Lin Xiao1 · Tianle Qi1 · Hanbin Xu1 · Linjiang Guo1 · Guobao Ning1 · Xiaokang Lu1 · Keming Zhu3 · Hui Zhao4 · Can-Peng Li1

1School of Chemical Science and Technology, Yunnan University, 2 North Cuihu Road, Kunming 650091, People’s Republic of China

2Affiliated Hospital of Yunnan University, Yunnan University, 176 Qingnian Road, Kunming 650021, People’s Republic of China

3School of Life Science Yunnan University, 2 North Cuihu Road, Kunming 650091, People’s Republic of China

4Laboratory for Conservation and Utilization of Bioresource, Yunnan University, 2 North Cuihu Road, Kunming 650091, People’s Republic of China

Bilian Li, Min Zhou, and Chun Zhao contributed equally to this work.

Corresponding Authors：Keming Zhu · Hui Zhao · Can-Peng Li

E-mail: lcppp1974@sina.com (C.-P. Li); 1731226017@qq.com (K. Zhu); zhaohui@ynu.edu.cn (H. Zhao)

# Supplementary Methods

Evaluation of the hydrogen peroxid

According to previous literatures [1-2], we verified the production of hydrogen peroxide by ultraviolet-visible spectrum. As depicted in Fig. S5, the production of H2O2 was confirmed using horseradish peroxidase (HRP) and 3,3', 5,5'-tetramethylbenzidine (TMB). In the presence of glucose, the characteristic absorption peak of oxidized TMB at 650 nm, Au@COFs catalyzed glucose to produce hydrogen peroxide, and hydrogen peroxide produced hydroxyl radicals catalyzed by horseradish peroxidase, which changed TMB from colorless to blue, indicating that H2O2 was produced by Au@COFs catalysis.

# Supplementary Figures and Tables

Fig. S1 XRD spectra of AuNPs.

Fig. S2 HRTEM images of COFs (A), Au@COFs (B), AuNPs(C); EDS elemental mapping picture of Au@COFs (D).

Fig. S3 Steady-state kinetics of COFs, 4-NP, glucose concentration rate relationship curve (A, C); Lineweaver Burk linear fitting (B, D).

Fig. S4 Fluorescence spectrum of MIL-53(Al) (A); XPS of MIL-53(Al) (B); FTIR spectrum of MIL-53(Al) (C); XRD patterns of MIL-53(Al) (D).

Fig. S5 TEM images of MIL-53(Al) (A-D).

Fig. S6 The catalytic efficiency of different substrate concentrations over time.

Fig. S7 UV-vis absorption spectra of Au@COFs incubated with glucose, TMB and HRP to prove the H2O2 production.

Table S1 Cancer cell determination using the proposed method.

| Sample | Added (cells mL−1) | Found (cells mL−1) | RSD (%) | Recovery (%) |
| --- | --- | --- | --- | --- |
| 1 | 100 | 95±12 | 8.2 | 95.0 |
| 2 | 200 | 205±20 | 9.7 | 102.5 |
| 3 | 500 | 522±19 | 3.6 | 104.4 |
| 4 | 1000 | 981±30 | 3.1 | 98.1 |
| 5 | 5000 | 4978±321 | 6.4 | 99.6 |
| 6 | 10000 | 9950±528 | 5.3 | 99.5 |

# References

1. Pezhhan H, Akhond M, Shamsipur M. Histidine capped-gold nanoclusters mediated fluorescence detection of glucose and hydrogen peroxide based on glucose oxidase-mimicking property of gold nanoparticles via an inner filter effect mechanism. J Lumin. 2020;228:117604.

2. Lu M, Su L, Luo Y, Ma X, Duan Z, Zhu D, Xiong Y. Gold nanoparticle etching induced by an enzymatic-like reaction for the colorimetric detection of hydrogen peroxide and glucose. Anal Methods. 2019:11(37):4829-34.