(Supplementary data)

(b)

(a)

Fig 1S: PXRD spectra of (a) TS350 (b) TS750

Fig. 2S: Fluorescence intensity of TS550 NP’s at different excitation wavelengths

Figure 3S: FT-IR spectra of Imidacloprid

Table 1S: Structures of different pesticides selected in present work.

| Sr. No. | Name of Pesticide | Structure of Pesticide |
| --- | --- | --- |
| 1 | Imidacloprid (neonicotinoid) |  |
| 2 | Thiamethoxam (neonicotinoid) |  |
| 3 | Quinalphos (organothiophosphate) |  |
| 4 | Triazophos (organothiophosphate) |  |
| 5 | Dichlorvos (organophosphate) |  |
| 6 | Cypermethrin (pyrethroid) |  |
| 7 | Chlorantaranilipore (ryanoid) |  |
| 8 | Lambda cyhalothrin (pyrethroid) |  |
| 9 | Cartap hydrochloride (carbamate) |  |

Table 2S: Physico-chemical properties of soil selected

| Soil |  | Bathinda |
| --- | --- | --- |
| Texture |  | Loamy Sand |
| pH |  | 8.3 |
| Electrical conductivity (mmho/cm) |  | 0.59 |
| Organic Matter (%) |  | 0.285 |
| Mineral content | Potassium (ppm) | 180 |
|  | Zinc (ppm) | 1.992 |
|  | Manganese (ppm) | 11.11 |
|  | Iron (ppm) | 7.9 |
|  | Copper (ppm) | 1.196 |

Table 3S: Parameters obtained from XRD spectra of NP’s

| Nanoparticle | Crystallite size (nm) | Lattice strain | d-spacing (Å) |
| --- | --- | --- | --- |
| TS550 | 14nm | 11.28 × 10-3 | 3.5053 |
| TS750 | 121.68 nm | 1.2 × 10-3 | 3.24625 |
| TS550 on interaction with IMP | 13.76nm | 11.47 × 10-3 | 3.5080 |