Supporting file

Energy and Pollution Mitigation: The Role of Coconut Sugar in Microbial Fuel Cell

Table S1: Physicochemical properties of local USM pond wastewater and M-phenolic-wastewater.

| Physicochemical variables | Local USM pond wastewater | M-phenolic wastewater |
| --- | --- | --- |
| Color | Light yellow | Light yellow |
| Temperature | 27.0 ± 3.0˚C | 27.0 ± 3.0˚C |
| Electrical conductivity | 67 ± 5 μS/cm | 101 ± 4.5 μS/cm |
| pH | 7.39 ± 0.2 | 6.91 ± 0.05 |
| Odor | Unpleasant odor | Unpleasant odor |
| Phenol | 0 ppm | 500 ppm |
| Pb2+ | 0 ppm | 50 ppm |
| Cd2+ | 0 ppm | 50 ppm |
| Cr3+ | 0 ppm | 50 ppm |

2.4. Analytical measurements

To calculate the force density (PD), and the current density (CD) the following equations were used .

V = IR   ------------------------(1)

PD =  VRA2 ------------------(2)

CD = IA   ------------------------(3)

where, V= voltage output, I = current, R = external resistance, A = cross-sectional area.

Cp=  A2mk(V2-V1)     ---------------(4)

where, A = CV curves area, m = loaded mass quantity in CV instrument, k = scan rate of CV in mV/s,  V2-V1 = potential range of CV (total voltage range).

Table S2: Research evaluating the relative energy efficiency of several organic substrates for MFC.

| Organic substrate | Current density (mA/cm2) | Power density (mW/m2) | References |
| --- | --- | --- | --- |
| Chocolate industry wastewater | 0.302 | - | (Patil et al. 2009) |
| Macroalgae, Ulva lactuca | 0.025 | 0.98 | (Velasquez‐Orta et al. 2009) |
| Oil palm trunks sap | 59.21 | 1.84 | (Akil 2024) |
| Food waste | 28.94 | 0.69 | (Alshammari 2023) |
| Food waste | 38.15 | 1.05 | (Alshammari 2023) |
| Local bakery waste | 69.73 | 3.51 | (Ghada et al. 2023) |
| Commercial sugar | - | 0.108 | (Omenesa Idris et al. 2023) |
| Dragon fruit waste | 19.375 | 1.98 | (Yaqoob et al. 2024) |
| Pineapple waste | 24.6 | 1.92 | (Dao et al. 2024) |
| Coconut sugar | 105.13 | 72.77 | Present work |

References

Akil A (2024): An innovative step to fabricate biomass-derived reduced graphene oxide electrodes to boost energy efficiency with metal removal using an electrochemical approach. Biomass Conversion and Biorefinery, 1-16

Alshammari MB (2023): Impact of self-fabricated graphene–metal oxide composite anodes on metal degradation and energy generation via a microbial fuel cell. Processes 11, 163

Dao WY, Ahmad A, Alshammari MB (2024): Energy production with removal of lead and chromium from wastewater through microbial fuel cells energized by organic waste substrate. Biomass Conversion and Biorefinery, 1-13

Ghada MA, Alshammari AS, Alomari AD (2023): Biomass and domestic waste: a potential resource combination for bioenergy generation and water treatment via benthic microbial fuel cell. Environmental Science and Pollution Research, 1-14

Omenesa Idris M, Al-Zaqri N, Warad I, Hossain A-MA, Masud N, Ali M (2023): Impact of Commercial Sugar as a Substrate in Single‐Chamber Microbial Fuel Cells to Improve the Energy Production with Bioremediation of Metals. International Journal of Chemical Engineering 2023, 9741246

Patil SA, Surakasi VP, Koul S, Ijmulwar S, Vivek A, Shouche Y, Kapadnis B (2009): Electricity generation using chocolate industry wastewater and its treatment in activated sludge based microbial fuel cell and analysis of developed microbial community in the anode chamber. Bioresource technology 100, 5132-5139

Velasquez‐Orta SB, Curtis TP, Logan BE (2009): Energy from algae using microbial fuel cells. Biotechnology and bioengineering 103, 1068-1076

Yaqoob A, Daud N, Hussin M, Ibrahim M, Al-Sadoon M, Abdulrahman R (2024): Role of dragon fruit waste (DFW) in microbial fuel cell to treat metal-polluted wastewater with electricity generation. International Journal of Environmental Science and Technology, 1-12