Supporting Information

Self-healing and polymer welding of soft and stiff epoxy thermosets via silanolates

Amelia A. Putnam-Neeb1,2, Jordan M. Kaiser1,3, Amber M. Hubbard1,2, Dayton P. Street1,2, Matthew B. Dickerson1, Dhriti Nepal1, and Luke A. Baldwin1*

1Materials and Manufacturing Directorate, Air Force Research Laboratory, Wright Patterson Air Force Base, Ohio, 45433, United States.

2National Research Council Research Associate, Air Force Research Laboratory, Wright Patterson Air Force Base, Ohio, 45433, United States.

3UES, Inc. Dayton, Ohio, 45432, United States.

Figure S1: MALDI-TOF MS spectra of different flow conditions compared to the batch synthesis for the oligomerization of AMS to make PAMS. The continuous flow parameters of 160 °C and a 60 min retention time (top spectrum) yielded a product similar to that of the batch reaction conditions (bottom spectrum). The PAMS synthesized by flow gave a molecular weight of 1500 – 2000 g mol-1, or about 11-19 repeating siloxane units.

Figure S2: Nuclear magnetic resonance (NMR) spectra of PAMS (top) and KPAMS (bottom). 1H NMR was recorded using a Bruker Avance 400 MHz spectrometer with DMSO-d6 solvent.

Figure S3: Thermogravimetric analysis (TGA) of all KPAMS-BDDE formulations. The end weight after decomposition is highest with less BDDE as a result of the residual potassium content from increasing concentration of KPAMS.

Figure S4: Thermogravimetric analysis (TGA) of all KPAMS-DGEBA formulations.

Figure S5: Cyclic TGA of each formulation of a) KPAMS-BDDE and b) KPAMS-DGEBA. For each experiment, TGA was performed twice using the same sample, heating to 200 °C both times to determine if water was removed. In each plot, the first cycle is denoted by a solid line, and the second cycle is shown as a dashed line. Final mass loss for each cycle is tabulated in Table S1.

Table S1: Final mass loss for cyclic TGA experiments for all adaptable network formulations.

| Adaptable network composition | Final Mass Loss |  |
| --- | --- | --- |
|  | 1st Cycle | 2nd Cycle |
| 40 wt% BDDE | 4.449% | 1.521% |
| 60 wt% BDDE | 2.958% | 1.247% |
| 80 wt% BDDE | 1.945% | 0.2788% |
| 40 wt% DGEBA | 3.680% | 0.7308% |
| 60 wt% DGEBA | 2.376% | 1.031% |
| 80 wt% DGEBA | 1.807% | 0.4767% |

Figure S6: Drawing of the 3-piece aluminum mold used for self-healing and welding of adaptable network dogbone specimens (top). The mold consisted of a single female piece and two male pieces to fit on each end. Fractured dogbones were placed in the wells of the mold, which was then placed in a hot press (bottom) to weld under 5 MPa of pressure at 110 °C for 45 min.

Figure S7: Primary exchange mechanism of silanolate adaptable networks.

Table S2: Thermal properties of KPAMS-BDDE networks. Thermal characterization from DSC and DMA was repeated in triplicate, and error is reported as one standard deviation.

| BDDE content | Td (5%) | Gel Fraction | Tg (DSC) | Tg (Eʹ) | Tg (tan δ) |
| --- | --- | --- | --- | --- | --- |
| 40 wt% | 222 °C | 0.63 | -7 ± 1 °C | 10 ± 5 °C | 20 ± 6 °C |
| 60 wt% | 253 °C | 0.88 | 11.1 ± 0.9 °C | 24 ± 2 °C | 34 ± 3 °C |
| 80 wt% | 343 °C | 0.94 | -7 ± 1 °C | 12 ± 1 °C | 23 ± 1 °C |

Table S3: Stoichiometric ratios of amine to epoxide groups within each formulation used for KPAMS-BDDE networks. A formulation with 59.73 wt% BDDE would give an exact 2:1 epoxide:amine ratio.

| BDDE content | Epoxide | Amine |
| --- | --- | --- |
| 40 wt% | 1.00 | 1.11 |
| 60 wt% | 2.02 | 1.00 |
| 80 wt% | 5.39 | 1.00 |

b)

a)

Figure S8: In situ FT-IR of a) KPAMS-BDDE and b) KPAMS-DGEBA synthesis with 60 wt% diepoxide crosslinker. The epoxide groups (914 cm-1) of the DGEBA were reacted away over the 180 min cure time. For BDDE, epoxide groups were mostly exhausted within the first ~10 min. An additional FT-IR spectrum of KPAMS-BDDE was included from before the reaction was heated to 80 °C to show the reaction of epoxy groups.

Table S4: Thermal properties of KPAMS-DGEBA formulations. Thermal characterization from DSC and DMA was repeated in triplicate, and error is reported as one standard deviation.

| DGEBA content | Td (5%) | Gel Fraction | Tg (DSC) | Tg (Eʹ) | Tg (tan δ) |
| --- | --- | --- | --- | --- | --- |
| 40 wt% | 138 °C | 0.62 | 6 ± 1 °C | 19 ± 4 °C 81 ± 4 °C | 29 ± 4 °C 85 ± 4 °C |
| 60 wt% | 218 °C | 0.97 | 4 ± 1 °C 103 ± 2 °C | 7 ± 1 °C 92 ± 1 °C | 15 ± 5 °C 111 ± 1 °C |
| 80 wt% | 289 °C | 1.02 | 91.7 ± 0.8 °C | 97 ± 3 °C | 110 ± 3 °C |

Table S5: Stoichiometric ratios of amine to epoxide groups within each formulation used for KPAMS-DGEBA networks. A formulation with 68.41 wt% DGEBA would give an exact 2:1 epoxide:amine ratio.

| DGEBA content | Epoxide | Amine |
| --- | --- | --- |
| 40 wt% | 1.00 | 1.62 |
| 60 wt% | 1.39 | 1.00 |
| 80 wt% | 3.69 | 1.00 |

Figure S9: Representative a) DSC and b) DMA results of 60 wt% DGEBA with 40 wt% KPAMS (green) or PAMS (black) as a control without dynamic bonding. The single Tg shown in the PAMS-DGEBA network (74.64 ± 0.06 °C from DSC) suggests a more uniform distribution of the polysiloxane. The silanolate-containing KPAMS-DGEBA has two Tg values present, indicating poor mixing between the starting materials.

Figure S10: Pristine samples of a) 60 wt% BDDE and b) 60 wt% DGEBA. The dogbone specimens were then healed and retested, and a representative sample (black trace) is shown in Fig. 6 with multiple healing iterations.

Figure S11: DSC curves of a 60 wt% BDDE sample before and after a self-healing/welding cycle (110 °C, 5 MPa, 45 min). The similar Tg in both experiments indicates that the self-healing properties were not a result of additional curing within the material.