Supplementary information

Nickel nanoparticle decorated reduced graphene oxide via one-step microwave-assisted synthesis and its lightweight and flexible composite with Polystyrene-block-poly(ethylene-ran-butylene)-block-polystyrene polymer for electromagnetic wave shielding application

David Skoda 1*, Jarmila Vilcakova 1,2, Raghvendra Singh Yadav 1, Barbora Hanulikova 1, Tereza Capkova 1, Marek Jurca 1, Michal Urbanek 1, Petr Machac 3, Lucie Simonikova 3, Jan Antos 1, Ivo Kuritka 1

1 Tomas Bata University in Zlin, Centre of Polymer Systems, Tr. Tomase Bati 5678, Zlin, CZ-76001, Czech Republic

2 Tomas Bata University in Zlin, Faculty of Technology, Department of Physics and Materials Engineering, Vavreckova 5669, 76001 Zlín, Czech Republic

3 Department of Chemistry, Faculty of Science, Masaryk University, Kotlarska 2, Brno, CZ-61137, Czech Republic

*Correspondence: dskoda@utb.cz

Figures

Fig. S1. MW-reaction record for NiG sample.

Fig. S2. XPS survey spectra of NiG and NiG-800 sample.

Fig. S3. High-resolution XPS spectra of O 1s for NiG sample.

Fig. S4. High-resolution XPS spectra of N 1s for NiG sample.

Fig. S5. High-resolution XPS spectra of O 1s for NiG-800 sample.

Fig. S6. High-resolution XPS spectra of N 1s for NiG-800 sample.

Fig. S7. TG curves of NiG (black) and NiG-800(70)-SEBS (blue) samples were recorded in the air. TG curve of NiG sample recorded in nitrogen.

Fig. S8. Dependence RTA (%) of NiG-800(50)-SEBS and NiG-800(70)-SEBS on frequency.

Fig. S8 provides another view of the shielding efficiency of NiG-800 filled SEBS polymer samples. The relationship between reflected (R), absorbed (A), and transmitted (T) portions of electromagnetic wave intensity follows:

R2 + A2 + T2 = 1

Using this equation, the direct determination of R and T from measured values of S11 and S21 enables one to extract the absorbed part (A) of electromagnetic wave intensity. Visualizing the proportion between the three components in “RAT analysis” (analysis of each sample's reflection, absorption, and transmission capability) indicates a higher absorption percentage of samples with a higher concentration of nanoparticles. The high absorption ability of structured NiG-800 is very important from the application point of view as the absorption of electromagnetic radiation from highly filled composites usually leads to protecting portable electronic products from unwanted secondary emissions of EMI.

Tables

Table S1. NiG sample characterization and precursor amounts.

| sample | GO | Ni(acac)2 [g] | Ni [mmol] | DDA [g] | C [wt%] 800 °C EDX | Ni [wt%] 800°C EDX | NiG-800 Ni ICP [wt%] |
| --- | --- | --- | --- | --- | --- | --- | --- |
| NiG | 0.510 | 0.499 | 1.94 | 1.01 | 70.12 | 29.6 | 25.0 |

Table S2. NiG800-SEBS nanocomposite composition.

| Composite sample | NiG800 | SEBS |
| --- | --- | --- |
|  | [mg] | [mg] |
| NiG800(70)-SEBS | 202.6 | 86.9 |
| NiG800(50)-SEBS | 115.7 | 113.3 |