MECHANISMS OF MERCURY REMOVAL FROM WATER WITH HIGHLY EFFICINT MXENE AND SILVER CRYOGEL COMPOSITE FILTERS

Chingis Daulbayev1,2, Armanbek Nursharip1, Zhandos Tauanov3,4, Rosa Busquets5, Alzhan Baimenov1,3*

1National Laboratory Astana, Nazarbayev University, Nur-Sultan, Kazakhstan

2Institute of Nuclear Physics, Almaty, Kazakhstan

3Al Farabi Kazakh National University, Almaty, Kazakhstan

4Satbayev University, Almaty, Kazakhstan

5School of Life Sciences, Pharmacy and Chemistry, Kingston University, Penrhyn road, KT1 2EE, Kingston upon Thames, Greater London, UK

*Corresponding author: alzhan.baimenov@nu.edu.kz

Figure S1. EDX mapping of MXene/Ag/PEI

Figure S2. EDX mapping of MXene/Ag

Figure S3. High-resolution XPS spectra of MXene

Figure S4. Zeta potential vs. pH values for PEI, PEI/MXene and PEI/MXene@Ag samples

| Element | Line | Mass% | Atom% |
| --- | --- | --- | --- |
| C | K | 77.02±0.03 | 85.39±0.04 |
| O | K | 13.69±0.04 | 11.39±0.03 |
| Na | K | 0.40±0.01 | 0.23±0.00 |
| Mg | K | 1.00±0.01 | 0.55±0.00 |
| Al | K | 0.23±0.00 | 0.12±0.00 |
| Si | K | 0.20±0.00 | 0.10±0.00 |
| S | K | 0.62±0.01 | 0.26±0.00 |
| Ca | K | 4.13±0.02 | 1.37±0.01 |
| Fe | K | 1.21±0.02 | 0.29±0.00 |
| Cu | K | 1.50±0.03 | 0.31±0.01 |
| Total |  | 100.00 | 100.00 |
| Map_001_wholespectrum |  | Fitting ratio 0.0135 |  |

Figure S5. SEM/EDS mapping images and elemental composition of commercial activated carbon

| Element | Line | Mass% | Atom% |
| --- | --- | --- | --- |
| C | K | 68.00±0.04 | 75.38±0.05 |
| O | K | 27.13±0.06 | 22.58±0.05 |
| Al | K | 0.21±0.00 | 0.11±0.00 |
| S | K | 4.65±0.02 | 1.93±0.01 |
| Total |  | 100.00 | 100.00 |
| Map_003_wholespectrum |  | Fitting ratio 0.0331 |  |

Figure S6. SEM/EDS mapping images and elemental composition of commercial ion-exchange resin

| Element | Line | Mass% | Atom% |
| --- | --- | --- | --- |
| C | K | 57.83±0.04 | 67.05±0.04 |
| O | K | 32.17±0.05 | 28.01±0.05 |
| Na | K | 0.46±0.01 | 0.28±0.00 |
| Al | K | 1.65±0.01 | 0.85±0.00 |
| Si | K | 7.16±0.02 | 3.55±0.01 |
| K | K | 0.45±0.01 | 0.16±0.00 |
| Ca | K | 0.29±0.01 | 0.10±0.00 |
| Total |  | 100.00 | 100.00 |
| Map_004_wholespectrum |  | Fitting ratio 0.0203 |  |

Figure S7. SEM/EDS mapping images and elemental composition of commercial zeolite Y

A

B

C

Figure 8. XPS spectra of PEI/MXene@Ag  for  Ag3d a) before and b) after mercury adsorption; c) Hg 4f after the adsorption